## Slide 2: Introduction to the activities of WP4.5 at CERN Quench detection, protection and diagnostic methods for HFM
18.04.2023
Mariusz Wozniak

## Slide 3: Scope of the WP4.5
1) Quench Detection Technology Development
2) Conductors for Protection
3) Protection Limits Development
4) Protection Technology Development
5) Models and Simulation Tools Development
2 images from:
L. Rossi et al. Instruments 2021, 5(1), 8. and J Ferradas Troitino et al. Supercond. Sci. Technol. 34 (2021) 084003 (17pp)

## Slide 4: Complete list of defined activities
Note: some activities are not resourced or scheduled for later
selected activities
The following slides will cover the most recent results on
If you are interested in not covered activity please contact me for discussion or ask questions at the end.

## Slide 5: Impedance Measurement for Continuous Condition Monitoring (including quench detection)
Current Status:
Built hardware required to inject and measure the response of stimuli signals, like:
  DAC (inject) & ADC (measure) cards
  FPGA to supervise the cards and relay the collected samples
Quantified performance when measuring LTS magnets in non-powered state
Upcoming Tasks:
Quantify the performance when measuring HTS magnet (non-powered)
Quantify the performance when powering magnets for LTS and HTS
Evaluate the systems operational impact on auxiliary systems.
FPGA
WP4.5-T1-D5
Courtesy of Magnus Christensen and SM18 colleagues
Conceptual illustration of how future quench detection may be implemented.
SC circuit
Stimuli inject.
Impedance of warm D2 magnet, all coils in series.
Orange – ELQA team with ‘commercial hardware’,
Blue - Newly Developed hardware, tot. aquisition time 1.2s
Notes: Concept advantages:
-Allows for enhanced noise rejection compared to contemporary methods.
-Can provide insight into magnet’s instantaneous impedance – this could aid in quench detection.
To minimize the operational impact on auxiliary equipment, such as power converters and existing quench detection systems, the injection hardware is designed to inject low amplitude signals (1-100mV).

## Slide 6: E-CLIQ: External Coil Coupled Loss Induced Quench
WP4.5-T4-D2
WP4.5-T5-D5
Courtesy of Tim Mulder
A set of very compact copper coils strategically positioned close to the primary coils, similar to resistive quench heaters, see Mulder et al. 2023
Thanks to I. Santillana and A. Terricabras (EN/MME) for effort during the mechanical tests
PCB E-CLIQ in development for integration with an SMC
  Optimized for use with low-current amplifier
  Able to generate local dB/dt of > 100 T/s
  Compact envelope, width of a Nb3Sn cable
The design is experimentally verified to withstand mechanical loads of over 200 MPa ✓
Modeling tools further matured

## Slide 7: Dynamic effects in composite superconductors
Developed a 3 D thermo-electromagnetic FEM (Comsol) model to simulate dynamic effects in twisted composite superconductors
  Presently built for high-Jc Nb3Sn wires composed by up to 108 sub-elements, the model can be adapted to other superconductors
Next Steps:
  Validation vs simple cases having an analytical solution and vs existing representative experimental results
  Simulate relevant cases to estimate losses and time constants during magnet quenches
  Derive, from the numerical solutions, semi-analytical formulas that can be implemented in other STEAM codes to estimate the losses in superconducting magnets
Magnetization current distribution in 0.85 mm high Jc wire composed by 37 sub-elements during a quench starting at 11 T and 1.9 K
Courtesy of Bernardo Bordini
WP4.5-T5-D4

## Slide 8: HFM Protection Studies 12T robust dipole - initial concepts
WP4.5-T5-D1
Work request from HFM WP3.1. Collaboration with: Diego Perini, Lucio Fiscarelli. With thanks to Emmanuele Ravaioli.
LEDET
Results from:
https://gitlab.cern.ch/steam/analyses/m12t_r
Tag: 2024.4.0
Case 3 for QH+CLIQ for magnet: modelData_robust_12T_50_mm_MQXF_cable_5_blocks_V2

## Slide 9: HTS Quench tools development Selected Finite Difference results
WP4.5-T5-D6
Courtesy of Tim Mulder
NICQS : No-Insulation HTS Coil Quench Simulator
Modeling tools are in development to describe the thermo-electromagnetic behavior of NI/Controlled-Resistance HTS coils
New: persistent currents within the tapes.
  Required for mechanical evaluation.
  Magnetization and its loss during operation.
New: Eddy currents in structural elements.
  Important for quench protection studies.
  AC-loss generated during operation.
Fast, example: 40 T cooling solenoid: 42 pancake coils, 600 turns each -> simulation time of a few minutes to an hour*.
* Depending on the scenario and solver settings.
NICQS

## Slide 10: HTS Quench tools development Selected FE results
WP4.5-T5-D6
Courtesy of S. Atalay and E. Schnaubelt
Thermal sol. for multiple pancakes
FiQuS : Finite Element Quench Simulator
Dedicated tools for Quench Sim.: A. Vitrano et al.
Numerical approaches for more efficient or faster solutions:
- Thermal Thin Shell Approx. E. Schnaubelt et al.
- EM (H – ϕ) Thin Shell Approx. E. Schnaubelt et al.
- Automated geometry, mesh and solution stages
- Concurrent in time and/or space solving (HPC) (w.i.p.)
Corse and fine solutions for parareal algorithm
Mesh of 3D HTS stack of double pancakes

## Slide 11: Coupled structural and quench tools
WP4.5-T5-D8
Two-way coupling successfully implemented between ANSYS-LEDET models:
ANSYS APDL provides the element centroids to LEDET.
LEDET solves the transient and transfers back to ANSYS the temperature and e.m. forces across the magnet.
ANSYS solves the transient mechanics problem as a series of static steps (quasi-static approximation).
* Largest discrepancy (5 MPa) due to the different pole temperature. Small mismatch in the coil windings due to a larger temperature from LEDET (more accurate coupling losses).
Resulting azimuthal stress in the coils. (t = 1 s)
Results comparison (IL path) between this new approach and a full ANSYS model*.
[J. Ferradas, “Mechanical behavior of a Nb3Sn accelerator magnet during a quench”, PhD Thesis)
Temperature distribution during a Quench Integral test (OL Heater discharge, t = 1 s)
Winding pole is assumed to stay at 1.9 K
LEDET
Slide courtesy of J. Ferradas Troitino & E. Ravaioli

## Slide 12: Parametrized quench tools
WP4.5-T5-D10
https://espace.cern.ch/steam
https://indico.cern.ch/event/1161448/
FRAMEWORK
Need to consider multiple design constraints in the analysis (specifications, tolerances, failure cases,…)
Capabilities (WIP):
  Uncertainty Quantification
  Design of Experiment
  Optimization
Slide courtesy of E. Ravaioli & M. Wozniak

## Slide 13: CCT magnet quench tools
WP4.5-T5-D13
Work to simulate quench in 3D in CCT magnets
Coupling between FiQuS (FE) and LEDET (FD)
Exchange of temperatures due to eddy currents (WIP)
Slide courtesy of E. Ravaioli & M. Wozniak
Collaboration with and support of the Fusillo team at CERN
LEDET
Concept of Fast Quench Propagation Conductors for CCT magnets, M. Wozniak et al.
Initial simulation of eddy currents in the formers and outer shell of Fusillo magnet (w.i.p.)

## Slide 14: Conclusions
Activities scope and structure are defined
Many interesting R&D topics are identified
Very good progress on resourced tasks
Many tasks are not initiated due to a lack of manpower for WP4.5 or collaborating WPs.
Further refinements and adjustments of activities are expected and required
Clarification of budget and priorities is required
Clarification of collaboration in and outside CERN