## Slide 1
Controlling refractive index and reducing the GWP of Cerenkov gas radiators: challenge in an era of diminishing fluorocarbon availability
“From the Speed of Sound to the Speed of Light: and beyond!”
G. Hallewell
Aix Marseille Université, CNRS/IN2P3, CPPM, Marseille, France
1
.
ECFA Detector R&D Roadmap,
Photodetectors & Particle ID (ECFA TF-4)
Meeting @ CERN May16-17th 2023
With thanks to Christoph Frei, Christian Joram and Antonello di Mauro (CERN),
Helen McNamee and Andy Penman (F2 Chemicals, UK)
Notes: 1

## Slide 2: Abstract (from meeting web pages)
COMPASS and LHCb use C4F10 and CF4 Cherenkov gas radiators.
These Saturated FuoroCarbons (CnF(2n+2)) have high GWPs, however
(5000-9000*CO2) so there is impetus to reduce their consumption.
Sound velocity monitoring was used for controlling real-time blending C5F12 with N2 in the SLD CRID. The technique could be valuable in the future operation to meet optical & low GWP constraints of future blended Cherenkov gas radiators.
Oxygenated fluorocarbons (CnF2nO) for example 3M NOVEC ® types can offer similar optical performance, with GWPs equivalent to CO2.
Closed molecular rings with oxygen atom link have GWPs as high as SFCs:
to be avoided.
Legislation & market forces will limit FC availability, maybe leaving “holes” in the CnFx “spectrum”, unfilled by CnF2nO equivalents.
Blending low molar concentrations of heritage-stock higher-order SFCs
or 3M NOVEC®5110: C5F10O (GWPzero) with light gases, N2, Ar, CO2… would
reproduce C4F10 and CF4 radiator optics but with reduced GWP “load”.
Examples are explored.
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 3: Historical - fluorocarbons: military and industrial (heat transfer) uses (3)
3
Vapour phase (non-contact) soldering of components on PCBs
(particularly surface mount) in high T fluorocarbon atmosphere !!!
The demand for vapour phase soldering is hardly going to “evaporate”.
New, lower GWP, transfer vapours will be needed (e.g. NOVEC)
G. Hallewell ECFA TF-4 Meeting May16-17th 2023

## Slide 4
4
https://e-publishing.cern.ch/index.php/CERN_Environment_Report/issue/view/102;
G. Hallewell ECFA TF-4 Meeting May16-17th 2023
Disappearing
Fluorocarbons?

## Slide 5
Which NOVEC®? What molecular structure: C6F12O (GWP = 0)?
Extremely unfair and deceptive to group NOVEC
on the same line as SF6 (GWP = 23000)
CF4 LHCb RICH2: GWP = ¬ 4880_CO2* [16]
C2F6 ATLAS evap cooling (potential use): GWP = ¬ 11000_CO2*
C3F8 F2 Chemicals , Astor, ATLAS evap cooling: GWP = ¬ 8900_CO2*
C4F10 LHCb RICH1, COMPASS RICH: GWP = ¬ 8500_CO2*
C5F12 PP50: GWP = ¬ 8500_CO2*
C6F14 PP1, F2 Chemicals: Liquid cooling, many expts: GWP = ¬ 8000_CO2*
For some perspective: SF6 GWP = ¬ 23000_CO2*
See references: 100 yr (average of 2nd, 4th & 5th assessment reports; AR2,4,5)
https://www.ghgprotocol.org/sites/default/files/ghgp/Global-Warming-Potential-Values%20%28Feb%2016%202016%29_1.pdf
R1234ze
GWP=7
5
G. Hallewell ECFA TF-4 Meeting May16-17th 2023
https://e-publishing.cern.ch/index.php/CERN_Environment_Report/issue/view/102;

## Slide 6: Alternatives to the saturated (CnF(2n+2)) molecules (“Fluoro-oygenates”: CnF2nO) ?
Could the solution be as “simple” as substituting an oxygen atom for 2 fluorines in the molecule?
3M NOVEC® 649 (C6F12O) & 5110 (C5F10O) GWP < 1 !!!
Can CFO’s be made over a wide Cn order range (n=16)?
CF2O, C2F4O, C3F6O, C4F8O, C5F10O, C6F12O…
Would the electronics industry be the commercial market driver for such alternatives (we are a small consumer…)?
G. Hallewell: RICH 2022, Edinburgh : Sept 12-16, 2022
6

## Slide 7: Molecular shapes and GWP (1)
Upper: molecular shapes of SFCs, including common gaseous Cherenkov radiators Lower: shapes of some non-cyclic CnF2nO analogues
(20-year GWPs noted where known – refs at end)
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 8
Shape examples of cyclic, non-cyclic
& non-cyclic double carbon-bonded C4F8O isomers
refs at end.­
Molecular shapes and GWP (2)
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
!!
?


## Slide 9
9
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
CERN has tested NOVEC 649
Equivalent radiation stability
to C6F14 used as a liquid coolant
in all LHC experiments;
(C6F12O) needs dessicants, but standard molecular sieves, activated-C OK: chosen SiPM coolant; LHCb Sci-Fi tracker

## Slide 10: Q: But What gives NOVEC 649/1230 (a spurred-Oxygen fluoro-ketone) its low GWP?
A: Structure!: a double-bonded oxygen atom on a peripheral spur of the molecule
This fluoro-ketone configuration is:
CF3CF2C(O)CF(CF3)2
10
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 11: Q: What gives NOVEC 649/1230 its low GWP?
Scission by UV photons of l around 300 nm
In the atmosphere (low pressure, high UV): the fragments do not reassociate* into saturated fluorocarbons of the type CnF(2n+2) (which would have high GWP)
*The Environmental Impact of CFC Replacements HFCs and HCFCs
T. WALLINGTON et al Environ.Sci.Technol.1994(28)7 320A https://doi.org/10.1021/es00056a714
https://www.nist.gov/system/files/documents/el/fire_research/R0301570.pdf
11
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
[15]

## Slide 12
Positive and Negative exeriences with C4F8O as a substitute for C4F10
Cherenkov radiator gas
(BTeV and ALICE VHMPID)
12
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 13
13
BTeV study: optics good – GWP not
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 14: Shapes of CnF2nO molecules and GWP:
c-octafluorooxolane (C4F8O),
MW = 216: GWP = 12000 BTEV stuff?
3M Specialty Gas PFG-3480 is a high-performance chamber cleaning gas that has environmental advantages and can help reduce operating costs. PFG-3480 reduces emissions of global warming compounds by 90 percent when compared to the traditional plasma enhanced chemical vapor deposition(PECVD) cleaning gas, C2F6. The replacement does not require changes to existing processes
Perfluortetrahydrofuran – The BTeV choice
From June 2000 3M datasheet
https://repository.library.noaa.gov/
044ed5ad-93ae-40e3-9420-d78
a4729ff0f
14
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 15: Shapes of CnF2nO molecules and GWP:
Octafluortetrahydrofuran – the probable ALICE VHMPID config
C4F8O acquired from Synquest (FL,USA) : reported by A. di Mauro:
15
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 16: Another exciting example: Novec 5110: C5F10O MW = 282: GWP <1
Mixing potential here with currently-available
low GWP « Fluoro-oxygenate » (CnF2nO) :
Blend with N2 to match C4F10 - or even CF4 - refractivity?
16
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 17
Refractive index & GWP ’load’ in a Cherenkov Gas Radiator
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
3 large RICH detectors currently in operation at CERN:
using saturated fluorocarbon gas volumes ˜ 50-100 m3:
C4F10 (COMPASS, LHCb RICH 1): GWP20 = 4880,
CF4 (LHCb RICH 2): GWP20 = 6870
A Cherenkov radiator vessel of volume V(m3) filled with
a blend of gases of densities ri (kgm-3),
fractional concentrations wi and individual GWPi (tonnes CO2 eq.)
has a GWP environmental “load” (& release potential) L given by:
) (tonnes CO2 eq.)
The corresponding radiator gas mixture refractivity is given by :
)
(2)
Can blend small concentration of high refractivity (heavier) SFC or NOVEC vapour with light transparent gas
(or gases) for similar optical properties to a lighter SFC at high concentration, but with a lower overall
GWP load. In this context the replacement of a lighter SFC by a (GWP = 1) “NOVEC” fluoro-ketone alternative would be ideal, but the
absence of convenient NOVEC fluids blends of legacy stock heavier SFCs could be considered. Taking the case of a binary mixture of a
heavy fluoro-ketone or SFC vapour x of refractivity (n-1)x a light transparent partner y of refractivity (n-1)y, the molar concentration, wx, necessary
to replicate the refractivity of a light SFC z with refractivity (n-1)z can be expressed as:
wx=((n-1)z-n-1y)(n-1x-n-1y) (3
Can blend small concentration wx of (heavier) SFC or NOVEC® vapour of high
refractivity (n-1)x with wy of light transparent gas to substitute the refractivity (n-1)z
to a lighter SFC at high concentration – to achieve a lower overall GWP load.
wx =
V,r

## Slide 18
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (100m3: t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (100m3: t.CO2)
CF4 | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | - |  | n/a | n/a
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
GWP loads of SFCs & 3M NOVEC ® 5110 blended with N2
((n-1) = 310.10-6) to match refractivity of CF4 and C4F10.
Positions of presently unavailable-in-bulk CnF2nO fluids in red
*Made in research quantities by Synquest Inc. as isomers Heptafluorobutyryl fluoride PN: 2116-2-07 CAS: 335-42-2
Octafluoro-2-butanone PN: 2117-2-10 CAS: 337-20-2 & Heptafluoroisobutyryl fluoride PN: 2116-2-0A CAS: 677-84-9
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 19
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (100m3: t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (100m3: t.CO2)
CF4 | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | - |  | n/a | n/a
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
GWP loads of SFCs & 3M NOVEC ® 5110 blended with N2
((n-1) = 310.10-6) to match refractivity of CF4 and C4F10.
Positions of presently unavailable-in-bulk CnF2nO fluids in red
!!
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 20
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (100m3: t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (100m3: t.CO2)
CF4 | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | - |  | n/a | n/a
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
GWP loads of SFCs & 3M NOVEC ® 5110 blended with N2
((n-1) = 310.10-6) to match refractivity of CF4 and C4F10.
Positions of presently unavailable-in-bulk CnF2nO fluids in red

## Slide 21
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (100m3: t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (100m3: t.CO2)
CF4 | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | - |  | n/a | n/a
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
GWP loads of SFCs & 3M NOVEC ® 5110 blended with N2
((n-1) = 310.10-6) to match refractivity of CF4 and C4F10.
Positions of presently unavailable-in-bulk CnF2nO fluids in red
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 22
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (100m3: t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (100m3: t.CO2)
CF4 | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | - | 0 |  | 0
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
GWP loads of SFCs & 3M NOVEC ® 5110 blended with N2
((n-1) = 310.10-6) to match refractivity of CF4 and C4F10.
And should fantasy become reality?
WOULDN’T THIS BE WONDERFUL?
AND THIS?
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 23
The ideal new radiator fluids would be the non-cyclic CnF2nO molecules with the same carbon order as CF4, C4F10 if these become available.
We should NOT be considering flammable gases or high pressure (large PV stored energy) gas radiators for underground areas (this is an even bigger “fantasy”).
However in their absence we can blend NOVEC 5100
or even legacy high-order fluorocarbons
to reduce gas radiator GWP:
23
But how to blend?
(see aslo annex)
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 24
Use speed of sound measured in real-time
(traditionally also called “c” by acousticians to confuse things)
to get the molar concentrations of the gas components wi
Then use standard refractivity formula to get from calculated w1,2
to refractive index of the radiator gas in real-time along with standard relativistic expressions to get from n to Cherenkov g thresholds for different particle species and b = 1 angle
Real-time measurement of speed of sound c takes us via the relative concentrations of the components to the speed of light b in the radiator gas (see annex for algorithms used)
24
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
)

## Slide 25
Chart: C5F12-N2 40 ⁰C
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
SLD-CRID: Cherenkov threshold in C5F12/N2 mixtures vs. measured speed of sound in radiator gas mixture (1)
Typical mix 87%C5F12,13%N2
C5F12 concentration (%)
25
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 26
Chart: C5F12-N2 40 ⁰C: N2-NOVEC5110 (C5F10O) might be very similar
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
Thresh/c | 0.99969 | 0.99954 | 0.9994 | 0.99926 | 0.99911 | 0.99897 | 0.99883 | 0.99868 | 0.99854 | 0.9984 | 0.99825
SLD-CRID: Cherenkov threshold in C5F12/N2 mixtures
vs. measured speed of sound in radiator gas mixture (2)
Cherenkov Threshold (GeV/c)
b = 1/n
Measured Sound Velocity (m/s)
So.. from c to b…
26
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 27
Chart: 
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
C5F12 concentration (%)
LHCb RICH 2 with C5F10O/N2
GWP load = (0.12 molar*1*V.r)
LHCb RICH 2: CF4 thresholds
GWP load = (0.95 molar*4880*V.r)
Cherenkov threshold in C5F12/N2 mixtures and GWP load comparison with LHCb RICH2 (new vol.?)
N2-NOVEC5110 (C5F10O) might be very similar (MW 282 vs 288)
Novec 5110 gives a huge GWP load reduction of 4636 V.r units
Even substituting 0.9 molar CF4 with 0.12 molar C5F12 reduces GWP load by 3784 V.r units
27
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 28
Chart: e.g.: COMPASS, LHCb RICH 1: C4F10-N2 @ 25 ⁰C: animation for N2 depassivation
| 352.80554329709202 | 263.393983949394 | 217.54894792942801 | 188.28848822732601 | 167.42098121844799 | 151.49471355246499 | 138.76788802501201 | 128.253185480963 | 119.34320896725301 | 111.640770856572 | 104.873532673703
e thresh | 0.20021 | 0.1704 | 0.15087 | 0.13682 | 0.12609 | 0.11754 | 0.11053 | 0.10464 | 0.099602 | 0.095231 | 0.09139
mu thresh | 4.2043 | 3.5783 | 3.1683 | 2.8733 | 2.6478 | 2.4683 | 2.3211 | 2.1974 | 2.0916 | 1.9998 | 1.9192
pi thresh | 5.4857 | 4.6688 | 4.1339 | 3.7489 | 3.4548 | 3.2206 | 3.0284 | 2.8671 | 2.7291 | 2.6093 | 2.5041
kthresh | 19.9006 | 16.9373 | 14.9967 | 13.6001 | 12.533 | 11.6835 | 10.9864 | 10.401 | 9.9004 | 9.4659 | 9.0841
pthresh | 37.4788 | 31.898 | 28.2434 | 25.613 | 23.6034 | 22.0035 | 20.6907 | 19.5883 | 18.6455 | 17.8272 | 17.1082
% C4F10 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Situation for RICH radiators using C4F10 with N2 passivant
Cherenkov Threshold (GeV/c)
C4F10 concentration in radiator gas (%)
Measured Sound Velocity (m/s)
28
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
Can make the same C5F10O comparison
as for a CF4 radiator (see preceeding table)
But low GWP non-cyclic C4F8O
would be easier to circulate, if available.

## Slide 29
Chart: 
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
C5F12 concentration (%)
LHCb RICH 1: C4F10 thresholds
GWP load = (6870*V.r)
Cherenkov threshold in C5F12/N2 mixtures and GWP load comparison with LHCb RICH1 (new vol.?)
N2-NOVEC5110 (C5F10O) might be very similar (MW 282 vs 288)
85% Novec 5110 gives a huge GWP load reduction of 6870 V.r units
29
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 30
The uncertain ECHA path to prohibition
[33] ECHA/NR/23/04;
https://echa.europa.eu/-/echa-publishes-pfas-restriction-proposal]
[34] ECHA Candidate List of substances of very high concern for Authorisation;
https://echa.europa.eu/candidate-list-table
[35] Annex to the Annex XV restriction report proposal for restriction:
Per- & polyfluoroalkyl substances (PFASs);ECHA; 22/03/2023 https://echa.europa.eu/documents/10162/d2f7fce1-b089-c4fd-1101-2601f53a07d1
[36] Per- and polyfluoroalkyl substances (PFAS); ECHA
https://echa.europa.eu/hot-topics/perfluoroalkyl-chemicals-pfas
We need to clarify the 3M attitude to future NOVEC production
Electronics industry is the driver!
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 31: Conclusion
Saturated (CnF(2n+2)) fluorocarbons under attack for their high GWP
Reduce wastage, purification loss in present installations;
Mix smaller molar concentrations of heavy SFCs
or better CnF2nO with light N2 etc. carriers for desired ref. index;
SLAC SLD CRID sonar (1990s): Cherenkov angle/b measurement
& dynamic C5F12/N2 blend control: ultrasonic feedback to flow controllers
Refractive index can be continuously monitored by utrasound even in dynamically-varying trimixes, if 3rd component conc. known from another sensor ;
New (non-cyclic) CnF2nO molecules very promising (particuarly
C5F10O (3M NOVEC ® 5110)): blend studies starting (Antonello Di Mauro)
(need optical studies)  potentially huge GWP savings
 CF2O & lin. C4F8O would be ideal…
We are a small-scale users who will always ride on the
coat-tails for the semiconductor manufacturing industry.
We should nonetheless enter discussions with manufacturers!
31
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 32: Other resources: References, Annexes & supporting information
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 33: Historical: fluorocarbons: military (mainly radar) and industrial uses (1)
33
Radar magnetron Direct immersion
G. Hallewell ECFA TF-4 Meeting May16-17th 2023

## Slide 34
34
Saturated Liquid FC immersion for destroying
(accelerated burn-in) and preserving (cooling) electronics
Historical: fluorocarbons - military and industrial (heat transfer) uses (2)
G. Hallewell ECFA TF-4 Meeting May16-17th 2023

## Slide 35
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 36
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 37
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 38
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 39: References; (numbering from earlier slides) mainly on fluorocarbon fluids and GWP
39
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 40
References
[1] CERN Environment Report 2017–2018 https://doi.org/10.25325/CERN-Environment-2020-001
[2] Eco-gas mixtures and mitigation procedures for Green-house Gases (GHGs);
B. Mandelli ECFA Detector R&D Road-map Symposium: T.F. 1 Gaseous Detectors, 29/4/2021
https://indico.cern.ch/event/999799/contributions/4204191
/attachments/2236047/3789965/BMandelli_ECFA.pdf,
[3] R&D for the optimization of the use of greenhouse gases in particle detector systems; B. Mandelli;
Mini workshop on gas transport parameters for present and future generation of experiments:
CERN April 22, 2021
https://indico.cern.ch/event/1022051/contributions/4325947/
[4] Studies to reduce greenhouse gas emissions from detectors at the LHC;
G. Rigoletti; EP-DT Seminar May 4, 2022.pdf (cern.ch)
[5] Long term experience with C4F10 in COMPASS RICH-1;
S. Dalla Torre et al; Presentation 11th Intl. Workshop on Ring Imaging Cherenkov detectors,
Edinburgh, Scotland, Sept 12-16 2022.
https://indico.cern.ch/event/1094055/contributions/4932286/attachments/2508724/4311387/
RICH2022_C4F10_dallatorre.pdf
[6] 3M PFG-3480: c-octofluorotetrahydrofuran (C4F8O).
Note: fluid out of production : product reference now used for a non-fluidic product.
For historic product data sheet mentioning its high GWP see (for example):
http://static6.arrow.com/aropdfconversion/a7116f41dfdd5b79d2eb7b40afd687f8af23d8ef/
mediawebserver(563).pdf
[7] M. Artuso et al; Nucl. Instr & Meth. A Volume 558, (2006), 373-387
[8] Product #2H07-2-08 Synonyms: 2,2,3,3,4,4,5,5-octafluorotetrahydrofuran,
Perfluorotetrahydrofuran; CAS No: 773-14-8, MDL No. MFCD00465561:
SynQuest Labs Inc., 13201 Rachael Boulevard, Alachua, FL 32615, USA
https://www.synquestlabs.com/Home/ProductDetail?SearchText=Octafluorotetrahydrofuran
[9] T. Acconcia et al ; Nucl. Instr & Meth A 767 (2014) 50–60
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 41
References (cont. 1)
[10] Abundances, emissions, and loss processes of the long-lived and potent greenhouse gas
octafluorooxolane (octafluorotetrahydrofuran, c-C4F8O) in the atmosphere;
M. Vollmer et al ; Atmos. Chem. Phys., 19, 3481–3492, 2019
[11] 3M Novec® range of fluorinated fluids; https://www.3m.com/3M/en_US/p/c/b/novec/?Ntt=novec
[12] 3M Novec 649/1230 fluid (C6F12O);
https://multimedia.3m.com/mws/media/569865O/3m-novec-engineered-fluid-649.pdf,
https://multimedia.3m.com/mws/media/124688O/3m-novec-1230-fire-protection-fluid.pdf]
[13] 3M Novec 5110 fluid (C5F10O);
https://multimedia.3m.com/mws/media/1132123O/3m-novec-5110-insulating-gas.pdf
[14] CERN report EN-CV 22/12/2017, EDMS 1751219 2017-334 rev 1.0: T
echnical Note NOVEC Fluids Qualification Report: Report on the study executed for the qualification
of the NOVEC Fluid for Detector Cooling applications.
[15] Understanding the stability and environmental characteristics of a sustainable Halon alternative.
J. Owens, 3M Performance Materials 3M Center, St. Paul, MN 55144
[16] CERN Mini-workshop on gas transport parameters for present and future generation of
experiments 20/04/2021;S. Easo; LHCb-RICH detectors and their gas radiators
https://indico.cern.ch/event/1022051/contributions/4333562/attachments/2231064/3780374/
LHCb-RICH-Current-GasRadiators-April-2021.pdf,
Options for alternate radiators in LHCb-RICH system (including calculations by O. Ullaland); S. Easo,
https://indico.cern.ch/event/1022051/contributions/4319538/attachments/2231436/3781060/
LHCb-RICH-Future-Radiators.pdf
[17] S.Easo; Nucl.Inst.& Meth. A 876 (2017) 168-173
[18] E. Lemmon, M. Huber, & M. McLinden; REFPROP Standard reference database 23, version 9.0 (2010)
U.S. National Institute of Standards & Technology.
[19] E. Nappi & J. Seguinot Rivista del Nuovo Cimento Vol. 28, N. 8-9 2005 DOI 10.1393/ncr/i2006-10004-6
[20] K. Abe et al. ; IEEE Trans. Nucl. Sci. 45 (1998) 648 SLAC-PUB-7705 DOI: 10.1109/23.6826 [21] G. Hallewell et al; Nucl. Instr. & Meth A264 (1988) 219-234
[22] G. Hallewell; Nucl. Instr & Meth A 876, (2017) 50-53
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 42
References (cont. 2)
[23] G. Hallewell et al; MDPI Instruments (2021) 5(1), 6;
[24] P. Stassi et al; Ultrasonic Gas mixture analysis system in the Forward RICH of DELPHI,
DELPHI Internal Note 95-124 RICH73, 25 July 1995
[25] M.Sannino; Nucl. Instr. and Methods in Physics Research A 595 (2008) 208–211
[26] Monitoring, Alignment and Control of the RICH Detectors; C. D'Ambrosio et al; LHCb-Memo-2000-80 RICH 6 September 2000.
[27] P. Fauland, PhD thesis; (COMPASS experiment) University of Bielefeld March 2004.
[28] Now marketed as SensComp model 600 transducer, http://www.senscomp.com/ultrasonic-sensors/
[29] T. Blake et al; Nucl. Instr. Meth A791 (2015) 27-31
[30] A. Papanestis; Nucl. Instr. Meth. A766 (2014) 14–18
[31] R. Calabrese et al; 2022 JINST 17 P07013
[32] R. Bates et al; 2013 JINST 8 P02006
[33] ECHA/NR/23/04; https://echa.europa.eu/-/echa-publishes-pfas-restriction-proposal]
[34] ECHA Candidate List of substances of very high concern for Authorisation;
https://echa.europa.eu/candidate-list-table
[35] Annex to the Annex XV restriction report proposal for restriction:
Per- & polyfluoroalkyl substances (PFASs);
ECHA; 22/03/2023 https://echa.europa.eu/documents/10162/d2f7fce1-b089-c4fd-1101-2601f53a07d1
[36] Per- and polyfluoroalkyl substances (PFAS); ECHA
https://echa.europa.eu/hot-topics/perfluoroalkyl-chemicals-pfas
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 43: Ultrasonic gas analysis in a process environment with multiple background gases
43
https://www.mdpi.com/2410-390X/5/1/6
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 44: The ultrasonic algorithm to find wi=1,2… for radiator gas components
44
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 45
(1) Calculate data base of individual CVi..n CPi..n
over expected T, P. range:
Example here: C3F8: (mol. wt.) = 188 in N2 (mol. wt. = 28)
45
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 46
(2) Calculate c‘theo’ as a function of concentration from component
Cp, Cv’s over the expected sonar temperature, pressure range to
make database of c‘theo’ vs. conc. fit equations
(example here 0- 1% C3F8 (m.w.= 188 in N2 (m.w.= 28): only one pressure shown here for clarity)
46
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 47
(3) CAN UTILITY: Store these c‘theo’ vs. molar conc. polyfit coeffs covering expected temperature & pressure range in “cans” at P,T grid intersections
T 
P 
Tmin
Tmax
Pmax
Pmin
Tstep
Pstep
Tmeas
Pmeas
(4) Calculate component concentrations wi from measured sound velocity cmeas & stored fit coeffs. interpolated to correspond to the measured T, P
!! This grid can become 3-D or higher-D with known contaminant gas(es) 
47
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 48: Aah…but what if there are 3 gases present? Acoustic Ambiguity ? (2 combinations  same c… so find w3 from a different source…) Examples: CO2 from infra-red, O2 from EC cell… etc
48
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 49
49
LHCb RICH 2 change in refractivity with varying CO2 radiator addition
(From RICH2013)
Stable N2
content
Substitution of CF4 by CO2 under consideraton:
but we earlier saw a possible NOVEC5110
C5F10O/N2 (or C5F10O/CO2) GWP advantage…
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 50: Example: Look-up tables of SoS. vs. composition for C3F8/N2 (+ CO2) (ATLAS silicon tracker cooling leak analysis)
50
CAN UTILITY DB expanded
from 2-D to 3-D:
C3F8/N2 fit coeffs
stored @{T, P, CO2} grid
Extra interpolation step,
starting from grid cub(oid) of uncertainty
to Tmeas, Pmeas,CO2 meas
Calculate sound vel vs. conc. eqns from
C3F8 & N2 AND KNOWN CONTAMINANT GAS
Cp & Cv over expected T,P, %CO2 range.
Demonstration:
1st acoustic measurement of concentrations of binary gas pair
of interest (C3F8/N2)
in known varying conc. of 3rd gas (CO2) :
(4 envelopes cycling every 4 hours)
Algorithm: industrial & anaesthesia applications
https://www.mdpi.com/2410-390X/5/1/6
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 51
T
P
CO2
P
T
P
P
P
P
P
P
T
T
T
T
T
T
CO2
CO2
CO2
CO2
CO2
CO2
H2O
Example with a second known contaminant gas: here H2O but could be another measurable gas : 4-D {T,P, CO2, H2O} Process dataspace example ‘Cans’ of c vs. conc1,2 fit coefficients now at corners of tesseract. (Here in Coxeter B4 projection)
8 cube faces:
2 x {T,P,CO2} exc. H2O
2 x {T,P, H2O} exc. CO2
2 x {T, CO2, H2O} exc. P
2 x {P, CO2, H2O} exc. T
Opposite cubic faces explored in the following slides
H2O
H2O
H2O
H2O
H2O
H2O
H2O
51
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 52
Tessar-Action
Extractio-reduction
https://www.mdpi.com/2410-390X/5/1/6
52
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 53
CAN FILLING: Of course, CP & CV for all gases (primary & background)
must be calculated for all T, P points on the n-D grid;
CAN UTILITY: Calculate & fit c in gas pair of primary interest from CP & CV over their conc. range AND @T, P, known background gas conc. Grid points.
Database size (3-D example)
DB size = No. primary fit coeffs * **…
RoI_n = range of interest_n: d_n = stepsize_n  Database explosion ?!?
Increasing stepsize ( longer interpolation distance) can reduce No. of cans (“cubes” become “cuboids”)…
Some dimensions can be suppressed altogether using physical law (rather than empirical changes):
example for temperature dimension:
Database growth control
(important in instruments using embedded m-controllers)
53
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 54
The uncertain ECHA path to prohibition
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 55
The SLD CRID ultrasonic gas radiator control system at SLAC
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 56
Chart: C5F12-N2 40 ⁰C
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
SLD-CRID: Cherenkov threshold in C5F12/N2 mixtures vs. measured speed of sound in radiator gas mixture (1)
Typical mix 87%C5F12,13%N2
C5F12 concentration (%)
LHCb RICH 2 with C5F10O/N2
GWP load = (0.12 molar*1*V.r)
LHCb RICH 2: CF4 thresholds
GWP load = (0.9 molar*7000*V.r)
SLD-CRID: Cherenkov threshold in C5F12/N2 mixtures and GWP load comparison with LHCb RICH2
N2-NOVEC5110 (C5F10O) might be very similar (MW 266 vs 288)
Novec 5110 gives a HUGE GWP load reduction of 6300 (V.r/1000) tonnes
Even substituting 0.9 molar CF4 with 0.12 molar C5F12 reduces GWP load by 5300 (V.r/1000) tonnes
56
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 57
The SLD CRID experience: barrel CRID gas radiators (1990s)
87% C5F12/13%N2
gas radiator
Sonar transducer
6 transducer pairs
@ 3 different heights
(hydrostatics)
57
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 58
Improvements in maintaining C5F12/N2 refractive index
through sonar-based active mixture control
● Sonar
□ Inclusive Angles
● Sonar
□ Inclusive Angles
b = 1 Cherenkov Angle (mrad)
30400 30600 30800 31000 31200
33500 34000 34500 35000 35500
Run Number
With active mixture control: dr/r ~ 0.2%
b = 1 Cherenkov angle comparison (1995-6 runs) between reconstructed ring data (□) in the SLD barrel CRID and angles from sonar-deduced refractive index corrected for atmospheric pressure (●)
Using the flowmeter
analyzer in supply line
to modify the blend by
hardwired 4-20mA link to mass flow controllers
0,3 mrad rms
Before use of flowmeter
analyzer in supply line
Note: before and after
blend stabilization sonar
interpreted b=1 radius
agreed well with
reconstructed radii!!
58
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 59
Polaroid Capacitative transducer components
Capacitative 350V activation/ bias  rapid response
37mm diameter determines 50 kHz dominant frequency: can operate over wide pressure range (50mbar >35 bar…)
59
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 60
Low temperature (-80°C)
N2 gas-induced condensation (B):
of C5F12 fromC5F12/N2 radiator gas (flow~1m3/hr, negligible C5F12 loss)
followed by (C) electric re-evaporation
(1-1.5m below condenser liq. level)
Cold N2 gas (‘conditioned’ by
counter-flow with boil-off LN2
from liquid argon calorimeter: (A))
Ultrasonic (speed of sound) – aided
“on-the fly” mixing of typical
17%N2 /83%C5F12 (molar) radiator gas mixture (D)
SLD Barrel CRID C5F12/N2 gas radiator: continuous thermodynamic recirculation
A
B
C
D
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 61: Shapes of CnF2nO molecules and GWP:
Octafluortetrahydrofuran – the probable ALICE VHMPID config
C4F8O acquired from Synquest (FL,USA) : reported by A. di Mauro:
61
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 62: SynQuest Labs Inc., 13201 Rachael Boulevard Rt 2054, Alachua, FL 32615, USA
62
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 63: SynQuest Labs, Inc. Can manufacture different C4F8O configurations
The cyclic molecule seems to be cheaper for SynQuest to manufacture:
whereas 3M make NOVEC 649, 5110 which are non-cyclic
63
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023

## Slide 64: Another linear all single-bonded geometry C4F10O..? TO BEWARE??? Bis(pentafluoroethyl)ether / Perfluoroethyl ether
GWP = ??
Unfriendly (not nice to mice) & lachrygene
https://pubchem.ncbi.nlm.nih.gov/compound/Bis_pentafluoroethyl_-ether
https://www.govinfo.gov/content/pkg/CFR-2017-title40-
vol23/xml/CFR-2017-title40-vol23-part98-subpartA-appA.xml
64
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023