## Slide 1
LHCb optical system status
Overview of system
Running experience
On behalf of all the LHCb sub-systems

## Slide 2
LHCb sub-systems
VELO 5000
Cu links
Silicon Tracker
2016
optical links
Outer Tracker
432
optical links
RICH
484
optical links
Calo
82 x 12-way optical links
Muon
152 + 152 x 12-way optical links

## Slide 3
Standardised optical link
Agilent HFBR-7XX
GOL
VCSEL-SMA
Fibre
Breakout
12-way MTP/MPO
~ 100m
Cassette
XILINX FPGA
Agilent HFBR-7XX
TLK 2501
System summary | Radiation environment (10 years)
1.6 Gbit/s serial data, 8b/10b | 
3084 single-channel VCSELs | 24krad 3.4 x 1012 neq 3.1 x 1011 hadrons >20MeV
234 12-channel TXs | 2.2krad 3.4 x 1011 neq 1.9 x 1010 hadrons >20MeV
850nm, multi-mode 50/125 | 

## Slide 4
VCSEL problems
All 3084 from same vendor
Oxide-confined, 850nm, 6mW, 1mA threshold
Packaging (2 steps): TO-46
SMA
Burn-in after TO-46 packaging (48h at 100degC, 15mA)
Vendor promises:
good handling (ESD) procedures (but LHCb can’t!)
good hermetic sealing
wafer position tracing (all from one wafer)
Bias currents 1.5 – 3 mA, modulation current = 10mA (fixed)
They are ALWAYS biased above threshold

## Slide 5
Chart: VCSEL Failures in LHCb ST
| 39831 | 40118 | 40133 | 40211 | 40271 | 40313 | 40328 | 40357 | 40361 | 40367 | 40369 | 40374 | 40378 | 40387 | 40391 | 40402 | 40408 | 40447 | 40451 | 40452 | 40520 | 40575
VCSEL Failures in LHCb | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 22 | 23
Timeline
Before spring 2010:
RICH2 early deaths (2007-2008)
RICH1 (3): 2009(2), 2010(1)
All of Muon deaths
Rate is slow (or zero) except Silicon Tracker (biggest user)
Since spring 2010:
All deaths in OT
Most in ST
RICH2 (2)
Lots of downtime

## Slide 6
Statistics
Chart: 
| OT | ST | RICH | Muon | TOTAL
Total VCSELS dead | 5 | 22 | 9 | 9 | 45
Chart: 
| OT | ST | RICH | Muon | TOTAL
Percentage of sub-detector | 1.1574 | 1.0913 | 1.8595 | 5.9211 | 1.4591

## Slide 7
Optical Spectrum Analysis
Higher bias
Dead VCSEL

## Slide 8
Results inconclusive:
Two dead VCSELs had normal spectrum before death
One with clear shift: will send for analysis
Optical Spectrum Analysis
Chart: RICH2: Column C1

## Slide 9
Vendor admits failure rate is much higher than normal
Observations:
LIV curves: downward shift in diode-turn-on voltage
Only light output from spontaneous emission
-> electro-luminescence images
Failure analysis by vendor

## Slide 10
Current aperture?
New devices from same wafer with very small bias current
Dead VCSEL
Failure analysis by vendor

## Slide 11
Vendor sent samples to contractor for TEM imaging
Images shows cracks:
Recognised failure mode of oxide-confined VCSELs: manufacturing defect
Defect on edge plus mechanical stress between layers create cracks
Failure analysis by vendor

## Slide 12
Short-term:
Replaced failed devices during winter shutdown
Additional spares purchased (Same device, but from different wafer)
Extended burn-in of samples already in progress
Longer term:
Manufacturer proposes new device
- design modifications to mitigate this effect
Radiation resistance unknown…… to be checked by LHCb
Make decision in 2011
- possible replacement in long shutdown
Mitigation Plans