## Slide 1: ATLAS optical system status, VCSEL failures, analysis and mitigation
T. Flick, University of Wuppertal
Opto Working Group mini-workshop
CERN, March 8, 2011

## Slide 2: Overview
Pixel statistics
SCT statistics
Larg statistics
Failure investigations
  Humidity investigation
  Usage of different VCSEL types
Getting new plugins
  Spares
  Old-style
  New desing

## Slide 3: The SCT / Pixel Off-detector Optical Device
Jig used for precision placement of array wrt guide pins  purely passive alignment
Epoxy Epo-Tek 353ND over active surface of VCSEL
SCT uses 12 channels,
Pixel uses 8 channels

## Slide 4: VCSEL failures SCT
Laser failures still going on
Replacement of devices for which redundant channel cannot be used
Need more plugins to keep detector (replacement) going
^
01/2010
07/2010
01/2011
Date

## Slide 5: SCT Weekly
Faillure rate per week after shutdown same order as before shutdown.
~20/week

## Slide 6: Pixel Statistics
Normally, single channel failures per plugin
Plugins have been replaced a.s.a.p. after failure to keep the detector going
  No redundancy
Started to replace with plugins which have been extracted in 2009 at global replacement.

## Slide 7: Pixel Weekly
2010
2011

## Slide 8: LAr optical links
~ 400 mm
OTX
G-link TX
SMUX
FEB
present
Single channels devices serving
128 detector channels each
Not pluggable  soldering needed

## Slide 9: VCSEL failures in LArg
OTx failures in LArg detector was first observed failure (2008)
Devices are single channel TO cans
Green: OTx replaced in 2009
Red: OTx replaced in last shutdown

## Slide 10: Optical Spectra (Larg OTx)
Optical spectra have been measured several times and are rather stable
Clear separation in the distribution
VCSEL failing devices show narrow spectrum
  Failures with normal spectrum developed short circuit, not due to VCSEL
Optical spectrum width as indicator!?

## Slide 11: Pixel on-detector fear
Pixel has the same optical package on-detector as it is off-detector
Did a „what would be if“ calculation
Ingredients:
  Expected bright time before failure
  Luminosity profile
  Occupancy with this
  Hübner factor
  ...
No failures in the detector package still
Will differences in the off- and on-detector
operation help to survive?

## Slide 12: Post-Mortem Studies
Use range of techniques
  Electroluminescence
    Dark areas sensitive to damage.
  EBIC
    Electron Beam Induced Current
    Beam energy gives depth.
    2D scan of beam and measure induced currents  sensitive to defects
    Select where to cut device with FIB
  STEM
    See defects in active region and DBR mirror.

## Slide 13: EBIC comparison
All taken with same SEM settings: 10KV spot 5 (roughly same mag 4700X and 5000x)
Original Image LUTs stretched to accentuate EBIC changes across VCSELs
Only Ch 10 shows distinct EBIC minima (dark spots) within the emission region
Ch 06 & 08 show some inhomogeneity but no distinct minima
Small dark speckles are surface topography
Ch 06
Ch 08
Ch 10

## Slide 14: STEM Failed Channel after FIB cut
DBR
MQW
Oxide

## Slide 15: STEM Unused Channel

## Slide 16: Used Working Channel Plan View SEM
Dislocations starting to form on edge of aperture
Further investigations needed as well as discussion with experts about what is to be seen here.

## Slide 17: Understanding the Reason
Investigation about the failure reason is ongoing
Found a correlation between the humidity in the different crates and the failure rates
SCT very clear indication
Pixel also the same correlation, but not as strong

## Slide 18: Humidity
Damp heat tests:
  85°C/85%RH
TEM picture for failed device
  Dislocation network covers full active region.
  This failure mode not seen in p implant VCSELs
    dislocation growth related to the oxide.
  Corrosive reaction between moisture and oxide during operation (electrolytic process)
    point defects

## Slide 19: Humidity
All oxide VCSELs use steam to grow the oxide layer.
  If this created defects would be seen in poor reliability in dry operation.
    Verified by damp storage + dry heat tests.
  Accumulation of point defects  dislocation networks which grow through “climb“ (absorption of interstitial point-defects).

## Slide 20: Humidity (3)
Oxide VCSELs vulnerable to stress during damp heat.
Can lead to semiconductor cracking
Moisture builds up stress in porous oxide layer.
Moisture absorption the oxide
Cracks in the aperture
Dislocation growth leads to device failure.

## Slide 21: Aging Factors
Accelerated aging model
From data at 85/85, 85/60, and 85/30 ARH=0.058 (with RH in %).

## Slide 22: Tests for our Optopackages
U-L-M photonics is doing a industrial standard 85°C/85% rel. humidity test (damp heat)
SCT has a setup at SR1 to compare plugin in dry(N2) and humid (air) environment
Testing Truelight VCSEL as well as AOC lasers to check for a more reliable laser device
  First plugins have been assembled with AOC lasers
  Light coupling to the fibres still to be inproved but ok for the first go

## Slide 23: U-L-M photonics testing
U-L-M photonics got several VCSEL arrays
Bonded onto test card
Card is kept in a climate chamber being able to operate the device and do regular measurements

## Slide 24: VCSELs without Epoxy
Around 30 channels have been under test
Some with and some without epoxy
VCSELs without epoxy start to dye after 120 hours already
All dead after 460h
Test was to run up to 1000 h in the first go.
Standard aim would be 4000h

## Slide 25: VCSELs with Epoxy
VCSELs being potted with epoxy (same as used in the detector)
Dying (8 channels) in between 300 and 400h of operation
Epoxy helps to prevent from humidity.... At least a bit...

## Slide 26: U-L-M photonics Plans
2 soaked TrueLight arrays (22 channels active) and 3 virgin TrueLight arrays as reference under operation
  with 10mA driving current
  85°C / 0% R.H. conditions for initial 1000 h
  both samples without epoxy
  L-I-V measurements will be taken ones a week
3 virgin TrueLight arrays
  covered with optical epoxy
  to be inserted in 85C - 85% R.H. environmental chamber for 1000 h for STORAGE (no operation)  will epoxy trap the humidity?
Will test with AOC devices too
testing if humidity only
causes the failure
testing if epoxy traps
Humidity

## Slide 27: CERN: Optical Spectra of TXs in Air and N2
Running 8 TXs (92 VCSELs) in SR1: 4 In Nitrogen and 4 in air (1% and 50% RH at 20oC).
4 new units were added around day 62 (2 N2 + 2 Air) and these were virgin units from Minglee (each new TX has 1 dead channel)
Max. operational time is now 115 days, newer samples 50 days, one unit added at day 21 (94 days operation)
To date there are no VCSEL failures (would not expect any for another 2-3 months).
Key to plots shown below (old = red, new = blue)

## Slide 30: An example ST432 running in Air

## Slide 31: T224 running in air after 91 days

## Slide 32: N2 vs. Air testing
Changes are occurring in the samples operating in air and we continue to monitor at regular (but less frequent) intervals.
We may increase the frequency again as we get closer to what we believe will be the onset of failures. It is even possible that we will automate the process and take much more frequent measurements.

## Slide 33: Pixel Crate relative Humidity
Normally 40-50% rel. humidity in the USA15 racks. We did a good sealing
and flowing dry air though it.
Preventing the danger of oil or dirt in the air by appropriate filtering

## Slide 34: Pixel Crates Temperature

## Slide 35: How to get out?
New plugins to replace the existing ones are needed urgently
  Taiwan is doing more plugins old style (AOC instead of Truelight VCSELs)
  BPM chips are reworked from plugins failing in the pit
  New BPM chips have been produced (old process redone)
  BGA housing
  New plugin layout needed
  New producers for plugins are under evaluation.
  XLOOM will do prototype now (to be delivered mid of April to start damp heat test)
    They will use a better epoxy to optimise the humidity resistance.
    Semi hermetic package
    Will use ULM VCSELs which are optimised to survive the damp heat tests.
    Interest in iFlame has also been expressed for Pixel on-detector and LAr

## Slide 36
XLOOM

## Slide 37
XLOOM

## Slide 38: Integration of iFlame
Aim: find mounting arrangement for iFlame which is backward compatible with ATLAS.
  Electrical connector Samtec QTE 40 way.
  Location screw holes on BOC.
  Ensure that MT guide pins are in correct position for Infineon SMCs.
Tx Plugin has to be modified to integrate iFlame package
PCB will hold BPM driver chip and passive components
Connection to iFlame by wirebonds

## Slide 39: iFlame Integration into a Plugin
iFlame OSA
Plastic support with screw holes for location
Samtec QTE
TX PCB

## Slide 40: Summary
ATLAS subdetector still suffering from dying lasers
A very good candidate as cause of failure is humidity
Detailed studies on this going on (in the labs and in industry)
Old style spares and replacement plugins as well as a new design of the plugin is under production to keep the detectors alife for data taking

## Slide 41: Backup

## Slide 42: Laser Reliability
Semiconductor lasers have very high minority carrier concentrations  high recombination rates.  dislocations can grow at relatively low T and low I.
GaAs-based lasers vulnerable to climb dislocations DLD.
  Electrical and optical recombination from dangling bonds
InGaAsP are not vulnerable to the growth of climb dislocations.
Dislocations can start from ESD or mechanical stress.
Very slow growth until within 1 diffusion length of active region, followed by “rapid” growth ~ 1 mm/minute
Deliberate damage of stripe laser with scribe at edge

## Slide 43: Sandia: Electroluminescence
Low Level Emission Image
Overlay: Optical and Emission
Possible scratch on surface
Speckled emission pattern

## Slide 44: Destructive insight
Laser Bulk investigations show defects inside the bulk and the aperture opening  kind of short?
There is clearly a defect in the bulk in the region of the aperture, growing from there?
Further investigations needed as well as discussion with experts about what is to be seen here.