## Slide 1: Voltage transient simulations of the LHC main dipoles Marvin Janitschke, TE-MPE-PE, DOCT
Gentner scholarship
Acknowledgements: Special thanks to: E. Ravaioli, C. Wiesner, M. Wozniak, M. Bednarek, R.G. Saederup and all colleagues involved in the LHC FPA snapshot tests

## Slide 2: Main dipole LHC circuit
Each octant
Each circuit consists of: - 154 MB dipoles
- 13 kA power converter (PC)
- Bus-bars between magnets - Current leads, sensing devices and earth fault systems
Protection
Protection by-pass diodes
Protective parallel resistors
4x Quench heater per magnet aperture
2x Energy extraction systems for protection (EE)
1
1
2
2
3
3
4
4
4
4
5
5
6
6
7
7
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
EE1
EE2

## Slide 3
Parameter | Value | Unit
Length | 14.3 | m
Operating temperature | 1.9 | K
Nominal field | 8.33 | T
Current at nominal field | 11850 | A
Inductance at nominal field | 98.7 | mH
Stored energy at nominal field | 1.3 | GJ
Inner coil diameter | 56 | mm
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
LHC main dipole magnet
Beam-screen
Beam-screen and quench heaters not to scale

## Slide 4: Quench detection systems
- Quenches in the main dipoles are detected in 2 ways:
Via voltage taps at extremes and middle point:
Problem: Symmetric quench!
Comparing voltages across 4 adjacent magnets:
If voltage across a full magnet differs from its reference:  Quench detected
1
2
iQPS
nQPS
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 5: Usual transient in main dipole circuit
Initial quench
Subsequent quenches
Event | Name | Time
1. | Quench detection | ~ -10 ms
2. | Fast Power Abort | ~ 0 s
3. | Opening of the first energy extraction (middle of chain) | ~ 100 ms
4. | Opening of the second energy extraction (end of chain) | ~ 600 ms
5. | End of discharge | ~ 350-400 s
Subsequent quenches due to:
- Gaseous helium propagation - Spurious triggering of quench protection
- …
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 6: Usual transient in Main dipole circuit
Developed resistance in magnet leads to diode opening
After each switch opening (PC, EE1, EE2) we observe voltage waves travelling through the magnet
 Exponentially decaying wave seeing a different phase shift at each magnet
+ Further phenomena like superposition/ reflection etc.
Wave progagates from the middle towards the ends
From the beginning towards the center
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 7: Typical examples of the signal
Normal signal in a transient
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
Flat signal with only very little bumps
Expected, as magnet apertures are supposingly identical
Other recorded signals
QDS threshold
QDS threshold
Significant bumps, which can occur at PC, EE1 or EE2 Bumps sometimes even shortly cross QDS thresholds  potential spurious triggering Indicate impedance differences between the apertures
Unbalanced dipole impedance
More examples can be found: MP3 day 2022, 01.12.2022, E. Ravaioli & M. Janitschke: FPA tests: Results and plans for the future
Peak-to-Peak amplitude

## Slide 8: Unexplained behavior: Unbalanced dipole impedance
BUT:
Expected voltage signals from simulations
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 9: Unexplained behavior: Unbalanced dipole impedance
BUT:
Measured voltage signals
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 10: Modelling of the magnets – so far
- In case of no quench, the circuit behavior can be captured relatively precisely by a pure electrical model, utilizing ideal inductors  Simulation in SPICE
- In order to account for the unbalanced impedance, the magnet model got replaced  Instead of pure inductors, each aperture is split up into two inductors, one bridged by a resistor
- Values were found empirically
E. Ravaioli, K. Dahlerup-Petersen, F. Formenti, J. Steckert, H. Thiesen, A. Verweij, "Modeling of the Voltage Waves in the LHC Main Dipole Circuits", IEEE Trans. Appl. SC, Vol 22, June 2012 , DOI: 10.1109/TASC.2011.2176306.
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
Aperture 1
Aperture 2

## Slide 11: Modelling of the magnets – so far
E. Ravaioli, K. Dahlerup-Petersen, F. Formenti, J. Steckert, H. Thiesen, A. Verweij, "Modeling of the Voltage Waves in the LHC Main Dipole Circuits", IEEE Trans. Appl. SC, Vol 22, June 2012 , DOI: 10.1109/TASC.2011.2176306.
Fitting works pretty good at low current  At high currents this breaks down
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 12: The beam-screen and its effects
Included in the magnet to protect the coils from particle and radiation impact
1 mm of steel and ~75 µm of co-laminated copper
R.G. Saederup, "Local Transfer Function Measurement (TFM) Data Analysis", edms 2675917
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
Previous investigations showed:
Strong correlation between the unbalanced impedance and beam screen
surface resistance

## Slide 13: The beam-screen and its layers
1 production series
1
1
2
3
3
2
Pure copper Polluted copper Steel layer
1
2
3
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 14
Inner layer with higher purity
Outer layer with lower purity
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 15: Main dipole – the new model
The eddy current effect is taken into account with coupling loops consisting of and are mutually coupled with to the magnets main inductances
Derivation only requires measured values
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
Simplified schematic, only showing 1/3 beam-screen layer

## Slide 16: Main dipole – the new model: Results
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
of an FPA @ 2 kA w/ 10A/s ramp
Low current

## Slide 17: Main dipole – the new model: Results
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
of an FPA @ 11 kA w/ 10A/s ramp
High current

## Slide 18: Main dipole – the new model: Results
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
of an FPA @ 11 kA w/ 10A/s ramp
High current
Fitting not perfect yet  Investigation of other parameters ongoing

## Slide 19: Main dipole – the new model: Results
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
The beam-screen effect can also be seen and reproduced in the frequency domain Transfer Function Measurements with the beamscreen at:
    20 K
    30 K
    40 K
The introduced impedance differences
can be accurately reproduced
Modelling of the main dipole in the frequency domain is work in progress

## Slide 20: Conclusion
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
2011 equivalent model | 2022 equivalent model
Good accuracy | Good accuracy
Empirical (not physics-driven) | Physics-driven
Predictive only for FPA | Predictive for various events
 | Able to predict new magnet’s behavior (?)
 | Possible to add a short circuit to the model
Not easily scaled | Scaled with current
Not easily expandable | Expandable with other effects
 | Expandable to frequency behaviour
Practical | Difficult to develop
Courtesy to E. Ravaioli
Further analysis of the beam-screen surface resistances showed a significant spread in purity and thickness of the different copper layers of the beam-screen  Novel electrical network model of the main dipole

## Slide 21: Thanks a lot for your attention! 
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 22: Appendix
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 23: LHC main dipole magnet (MB)
We will come back to these components
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 24
Parameter | Value | Unit
Length | 14.3 | m
Operating temperature | 1.9 | K
Nominal field | 8.33 | T
Current at nominal field | 11850 | A
Inductance at nominal field | 98.7 | mH
Stored energy at nominal field | 1.3 | GJ
Inner coil diameter | 56 | mm
Parameter | Value | Unit
Number of turns | 320 | -
Number of strands per turn | 28/36 | -
Number of filaments per strand | 8900/6500 | -
Critical current @ 10 T, 1.9 K | 13.75 | kA
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
LHC main dipole magnet
Beam-screen

## Slide 25: Data from Butting (2003/2004) – Random example
Series | Specimen Tube No. | Charge-No. (Bohler) | Coil No. | RRR Cu | U @293 K [V] | U @77 K [V] | U @4.2 K [V] | Length [m] | Width [m] | Thickness (total) | Thickness I (OFE-Cu) | Thickness (P506) | @ 4.2 K
10 | P. 5358 | 391324/1 | 96/1 | 145.820 | 0.00699600 | 0.00112400 | 0.00006300 | 0.07586000 | 0.00200000 | 0.00107800 | 0.00008360 | 0.00099440 | 1.66
10 | P. 5399 | 387025/2 | 95/1 | 81.218 | 0.00695900 | 0.00116000 | 0.00011200 | 0.07586000 | 0.00200000 | 0.00107500 | 0.00008280 | 0.00099220 | 2.95
Series | Specimen Tube No. | Charge-No. (Bohler) | Coil No. | RRR Cu | U @293 K [V] | U @77 K [V] | U @4.2 K [V] | Length [m] | Width [m] | Thickness (total) | Thickness I (OFE-Cu) | Thickness (P506) | 
10 | P. 5358 | 391324/1 | 96/1 | 145.820 | 0.00699600 | 0.00112400 | 0.00006300 | 0.07586000 | 0.00200000 | 0.00107800 | 0.00008360 | 0.00099440 | 1.66
10 | P. 5399 | 387025/2 | 95/1 | 81.218 | 0.00695900 | 0.00116000 | 0.00011200 | 0.07586000 | 0.00200000 | 0.00107500 | 0.00008280 | 0.00099220 | 2.95
CERN acceptance criteria
, I = 1 A
Now inserting all values from above (Butting) yields:
Material | (T= 293 K) ] | (T= 77 K) ] | (T= 4.2 K) []
Copper (RRR = 146) | 1.7e-8 | 2.0e-9 | 1.06e-10
Copper (RRR = 81) | 1.7e-8 | 2.1e-9 | 1.92e-10
Steel | 6.8e-7 | 5.3e-7 | 5.0e-7
Material |  |  | 
Copper (RRR = 146) | 1.7e-8 | 2.0e-9 | 1.06e-10
Copper (RRR = 81) | 1.7e-8 | 2.1e-9 | 1.92e-10
Steel | 6.8e-7 | 5.3e-7 | 5.0e-7
Specimen | U @293 K [V] | U @77 K [V] | U @4.2 K [V]
P. 5358 | 0.0059 | 0.00086 | 0.0000482
P. 5399 | 0.0060 | 0.00092 | 0.0000872
Calculated voltages based on provided ,
Correction for Stainless-Steel at 293 K:
15%
23%
23%
13%
20%
22%
Error to Butting voltages
RRR and were not included (?)
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 26: New approach – multi-layered copper
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 27
Inner layer with higher purity
Outer layer with lower purity
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 28: Main dipole – the new model: Results
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
of an FPA @ 11 kA w/ 10A/s ramp
High current
Modelling results from 2011

## Slide 29: Modelling result - Examples
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 30: Voltages across the magnet
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 31: Conclusion
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles
Previous modelling approaches of the main dipole were not able to reproduce the unbalanced dipole behavior at all current level
Past investigations showed a strong correlation of beam-screen surface resistances and unbalancedness
Further analysis of the surface resistances shows a significant spread in purity and thickness of the different copper layers of the beam-screen
These measured parameters were utilized in a novel model, which couples the magnet‘s main inductance to the induced eddy currents loops in the beam-screen
The results indicate to agree with measurements on low- as well as on high current levels
Still work in progress to continue analyzing other parameters in the process in order to improve the fit
The results and the model can also be used in the frequency domain, to reproduce Transfer Functions measured of the magnet  to be shown soon

## Slide 32: The outliers
What is going on here? Can we model this? And if so, what could it be?
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 33: The outliers
What is going on here? Can we model this? And if so, what could it be?
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles

## Slide 34: The outliers
Inter-turn short found shortly after
R.G. Saederup, "Local Transfer Function Measurement (TFM) Data Analysis", edms 2675917
Marvin Janitschke | Voltage transient simulations of the LHC main dipoles