## Slide 1: Coating the Wide-Open Waveguide Crab Cavity - set-up, planning and implementation
Fabian Manke, Alban Sublet, Thibaut Richard, Mauro Taborelli, Lucie Baudin, Ana Teresa Perez Fontenla, Stephan Pfeiffer
30/03/2022
FCC RnD Meeting

## Slide 2: Outline
Principal coating set-up
Coating recipe and test bench results
Simulations and process planning
Current state: Going full-scale
Perspectives for the year

## Slide 3: Outline
Principal coating set-up
Coating recipe and test bench results
Simulations and process planning
Current state: Going full-scale
Perspectives for the year

## Slide 4: 1. Multi-cathode coating set-up
Challenging internal geometry
Assembly of six independent, alignable cathode cylinders
Air-cooled movable magnets
Bipolar HiPIMS technique in Ar
Nb cylinders
Stainless
steel tube
FWHM
≈2cm
F. Avino et al, TTC, 05.02.2020, Geneva
Moving
magnet
Air flow
Nb sputtering flux
“Mushroom” ridge
140 cm, 290 kg
25 cm

## Slide 5: Outline
Principal coating set-up
Coating recipe and test bench results
Simulations and process planning
Current state: Going full-scale
Perspectives for the year

## Slide 6: 2. Coating testbench
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 7: 2. Coating testbench
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 8: 2. Coating testbench
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
STEP1
STEP2
5cm
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 9: 2. Coating testbench
1
CAT
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
STEP1
STEP2
5cm
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 10: 2. Coating testbench
1
2
CAT
CAT
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
STEP1
STEP2
5cm
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 11: 2. Coating testbench
1
2
3
CAT
CAT
CAT
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
STEP1
STEP2
5cm
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 12: 2. Coating testbench
Validate recipe, power, magnets for desired film uniformity and morphology
Three cathode coating testbench
The six-way cross
Nb cylinders
Stainless
steel tube
Moving
magnet
Air flow
Nb flux
STEP1
STEP2
5cm
Side view
Bottom view
Before coating
After coating
Longitudinal cathode view

## Slide 13: 2. Thin film densification : RF hot spot
1
2
3
STRONG tilt along cathode axis and curve in plane
Film entirely porous and delaminated in DCMS
Still voids near substrate at 500W sequential Bipolar HiPIMS
DCMS, parallel, 3x1kW
Delaminated
3 µm
2 μm
BP, HiPIMS sequential, 500W
F. Manke et al, HiPIMS Today, 22/03/2023

## Slide 14: 2. Thin film densification : RF hot spot
1
2
3
STRONG tilt along cathode axis and curve in plane
Film entirely porous and delaminated in DCMS
Dense films achieved for 1kW Bipolar HiPIMS
 Preparing publication of 3D sample results
BP HiPIMS, parallel, 3x1kW
DCMS, parallel, 3x1kW
Delaminated
3 µm
BP HiPIMS, sequential, 1kW
1 µm
1 µm
Reduced coating time by 30% to 15min
More recycling w. adjacent plasmas + fields ?
F. Manke et al, HiPIMS Today, 22/03/2023

## Slide 15: Outline
Principal coating set-up
Coating recipe and test bench results
Simulations and process planning
Current state: Going full-scale
Perspectives for the year

## Slide 16: 3. Simulations: mock-up geometry
Confirms importance of individual powering + insulation
Breakdown voltage of -270V at 15W power matches experiment within 10%
ne [m-3]
5W individual power
15W common power
A. Pflug, DSMC/PIC-MC Code Documentation, Fraunhofer IST, Braunschweig, Germany,, https://simulation.ist.fraunhofer.de/doku.php?id=start
Simulation: T. Richard

## Slide 17: 3. Benchmarking of XRF thickness measurements
Obtain Nb deposition profile from subsequent MC transport simulation
Compare to experimental thickness measurements with XRF
Use synthetic diagnostic for post-processing in MATLAB
Overall strong agreement (within ≈ 20%), pending local MC counting errors and slight shift of source
Yxrf
0
Lxrf
F. Manke et al, PLATHINIUM, 09/2021

## Slide 18: 3. Full WOWCC simulations as starting point
PICMC / DSMC simulations to establish cross-sectional Nb deposition profiles
“Mushroom” ridge
Argon plasma density from Fraunhofer PIC-MC
4µs
Simulation: T. Richard
F. Manke et al, 18th PSE, Erfurt 2022

## Slide 19: 3. Full WOWCC simulations
PICMC / DSMC simulations to establish cross-sectional Nb deposition profiles
“Mushroom” ridge
Argon plasma density from Fraunhofer PIC-MC
5µs
Simulation: T. Richard
F. Manke et al, 18th PSE, Erfurt 2022

## Slide 20: 3. Full WOWCC simulations
PICMC / DSMC simulations to establish cross-sectional Nb deposition profiles
“Mushroom” ridge
Simulation: T. Richard
Argon plasma density from Fraunhofer PIC-MC
6µs
F. Manke et al, 18th PSE, Erfurt 2022

## Slide 21: 3. Synergies: transport comparison
 | Fraunhofer DSMC | SIMTRA | Molflow
Erosion profile | PIC-MC, single step | From PIC-MC / fitted | From PIC-MC / fitted
Propagation | MC particle tracker | MC particle tracker | MC ray tracer
Collisions | From customizable cross-section database | Select neutral metal + gas and potential type (Moliere) | None
Geometry | Triangulated by GMSH | Geometric primitives | Re-meshed from .stl
Resources | HPC, 1 to 10 days  Reactions + geometry | Desktop PC, ½ to 2 days  Extent of sources | Desktop PC, ¼ to 2 days  Nr. of “facets” in mesh
WOWCC imported |  |  | 
F. Manke et al, 18th PSE, Erfurt 2022

## Slide 22: 3. Synergies: Code development
PICMC / DSMC simulations to establish cross-sectional Nb deposition profiles
Spin-off: Transport code benchmarking and extension to Molflow: gas collisions
“Mushroom” ridge
L = 0
Niobium flux profile from Molflow (collisionless)
 Local discrepancies since flux from distant cathodes did not scatter off argon gas
F. Manke et al, 18th PSE, Erfurt 2022

## Slide 23: 3. Synergies: The SWELL cavity
PICMC / DSMC simulations to establish cross-sectional Nb deposition profiles
Spin-off: Transport code benchmarking and extension to Molflow: gas collisions
Transport simulations for SWELL coating
D

## Slide 24: 3 Synergies: Fundamental dynamics
Bipolar High Power Impulse Magnetron Sputtering
[2] F. Avino et al, Plasma Sources Sci. Technol. 28, 01LT03, 2019
[3] F. Avino et al,Thin Solid Films 706,138058, 2020
[4] F. Avino, F. Manke, A. Sublet, T. Richard:
Plasma Sources Sci. Technol. 30, 115015, 2021
Comprehensive measurements and deeper fundamental understanding of plasma potential dynamics in bipolar magnetron discharges
  Documented Potential Drop-n-Rise in various settings
  Elucidated electron funneling in balanced configurations
  Established conditions for a secondary “reverse” discharge

## Slide 25: 3. Process planning: Magnet step size
Across region of strongest variations  within 2 cm from nearest cathode
Chose 25 mm steps to
avoid bottle-necking by
local deposition minima
F. Manke et al, 18th PSE, Erfurt 2022

## Slide 26: 3. Heat load simulations
Molflow / Synrad heat deposition profile
ANSYS simulations of ¼ WOWCC
Process steps:
  3×5min coating with 200s breaks each, 2.5cm steps along the cavity
1
2
3
“cut-off”
“cut-off”
cavity center
1500 W
F. Manke et al, PLATHINIUM, 09/2021
ANSYS simulations by L. Baudin

## Slide 27: 3. Cooling requirements
Molflow / Synrad heat deposition profile
ANSYS simulations of ¼ WOWCC
Process steps:
  3×5min coating with 200s breaks each, 2.5cm steps along the cavity
1
2
3
“cut-off”
“cut-off”
cavity center
1500 W
Chart: Time [s]
Air stationary
F. Manke et al, PLATHINIUM, 09/2021
ANSYS simulations by L. Baudin

## Slide 28: 3. Cooling requirements
Molflow / Synrad heat deposition profile
ANSYS simulations of ¼ WOWCC
Process steps:
  3×5min coating with 200s breaks each, 2.5cm steps along the cavity
1
2
3
“cut-off”
“cut-off”
cavity center
1500 W
Chart: Time [s]
Air stationary
Forced air convection
F. Manke et al, PLATHINIUM, 09/2021
ANSYS simulations by L. Baudin

## Slide 29: 3. Cathode power limits
Molflow / Synrad heat deposition profile
ANSYS simulations of ¼ WOWCC
Process steps:
  3×5min coating with 200s breaks each,
  2.5cm steps along the cavity
Forced air cooling required
Corner cathodes at 75% power in cut-offs
1
2
3
“cut-off”
“cut-off”
cavity center
1500 W
1
100% corners 75% corners
bake-out limit
F. Manke et al, PLATHINIUM, 09/2021
ANSYS simulations by L. Baudin

## Slide 30: Outline
Principal coating set-up
Coating recipe and test bench results
Simulations and process planning
Current state: Going full-scale
Perspectives for the year

## Slide 31: 4. Infrastructure upgrade
Electrical works underway  verify pumping + bake-out control
Compressed air + breakout box for cathodes requested
 STILL waiting: 6x HiPIMS power supplies  lab test in April (?)
WOWCC bake-out jacket set (PTFE coated)
Chemistry lifting tool + slings
Control PC for pumps, bake-out,
Later: motion, cathodes

## Slide 32: 4. Coating Assembly
Design with
“Mock-up” cavity
Surface Preparation
Fabrication
Courtesy: T. Mikkola, G. Villiger, P. Naisson and the AP team
bottom + top bell
Nb tubes
port
aligners
vacuum
breaks
Mock-up parts
 Procured fasteners, ports, ceramics
Reception of main components from AP
Cathode tubes after vacuum firing
Bells + bolts after vacuum firing
Plastics after degreasing
Aligners in ultrasonic bath
Clean room testing
F. Manke et al, 6th CERN SRF Workshop, 02/2023

## Slide 33: 4. Cathode Assembly and Storage
Cathode assembly needs support and storage
Chariot Design
Implementation
Courtesy G. Villiger
F. Manke et al, 6th CERN SRF Workshop, 02/2023

## Slide 34: 4. Full scale magnet motion
Single Cathode Concept
Bottom spacer
(ceramic)
Niobium
cylinders
Stainless
steel tube
Moving
magnet
Bottom stopper, wire return option
Motorized wire coil modules
Magnetmotion wire
Static cooling
cane
Six Cathode Design
Implementation
Stepper motors, gear heads
Magnets with weights
Bottom stops,
ceramics
Insulated canes, anchors
Top-bell “crown”,
coil frames
MASSIVE courtesy: P. Garritty
F. Manke et al, 6th CERN SRF Workshop, 02/2023

## Slide 35: 4. In-situ XRF diagnostic
XRF benchmark on samples
In-situ Diagnostic Design
Implementation
Yxrf
0
Lxrf
3D movable system
WOWCC
Rotary stage
Vertical aligner
XRF probe casing
Cable guide
Stepper driver
and XRF trigger
F. Manke et al, 6th CERN SRF Workshop, 02/2023

## Slide 36: Outline
Principal coating set-up
Coating recipe and test bench results
Simulations and process planning
Current state: Going full-scale
Perspectives for the year

## Slide 37: 5. Timeline: State and Planning
2020
2021
2022
2023
2024
2019
Cathode choice
Process steps, multi-code benchmark
Milestones
Cavity
systems
Simulations
Diagnostics
Coating Equipment
Cathode systems
Horiz. Trolley + tooling
vert. trolley
bake-out jackets
cavity support
full motion system
magnet motion prototype
fabrication
guiding, align, updates, release
Insulation, integration
Main assembly design
SEM + XRF: 3D samples, geometric corrections
cabling, design
In-situ XRF concept
Test-bench
Focus on cylind. magnetron
Triple cathode cyl. magnetron
HiPIMS coating recipies
Magnet / power / process params.
1st full cavity coating
Void-free 3D coating
Production start
Final assembly concept
Tests, measurements, publish
Implement.
Assembly + Testing
development + publishing
LP Rinsing
SUBU tooling
Lifting tool design
storage trolley
fabrication
HiPIMS power supply fabrication + testing
Improvements
Testing, usage
Heat management + feedback to MME
2nd Run
HP Rinsing , optical inspections
Procedure optimization
Branching to other projects
Control optim.
Advanced interface (?)
Coating shields(?)
Infrastructure (pump, air, PC)
Final prototype + publication
Now
New fellow?
fixes
TEST

## Slide 39: Bipolar HiPIMS coating recipe
High Power Impulse Magnetron Sputtering
  Vc during Main Pulses (MP), at 1kHz with with 30 μs duration (3% duty cycle)
  Same time-average power P as DC Magnetron Sputtering
   Denser plasmas (x10) with higher fraction of Nb+
   Accelerate Nb+ by Positive Pulses (PP) for denser, less columnar films
MP
PP
Average Power : 500 W
 Pulse Power : 16.6 kW

## Slide 40: XRF diagnostic implementation
In-situ diagnostic
3D movable system
Stepper power + XRF trigger
rotary stage
aligner
XRF probe casing
(in fabrication + cabling)
XRF probe / electronics from lead-paint diagnostic
Quantifying coating thickness uniformity : Transport simulation vs. Measurement
F. Manke et al, 6th CERN SRF Workshop, 02/2023
Movable system currently under testing
Update batch script control (win cmd)
XRF probe head wiring by cabling team
XRF probe casing to be produced on CNC
Final acquisition + electronics tests by supplier M. Dupayrat thereafter
Safety sign-off by RP on final diagnostic