## Slide 1
Dust charging and dust-surface interaction in the laboratory
Workshop on Dust Charging and Beam-Dust Interaction in Particle Accelerators, CERN (13-15 June 2023)
Cécile Arnas
Laboratory of Physics of Ions-Molecules Interaction (PIIM)
CNRS, Aix-Marseille university, 13013 Marseille, France
CENTRE NATIONAL
DE LA RECHERCHE
SCIENTIFIQUE

## Slide 2
2
Discharge chambers for dust-
nanoparticle production
Base vacuum: from 10-5 Pa to 10-4 Pa
Plasmas (gas): 10 - 100 Pa
40 cm

## Slide 3
Discharges between electrodes in reactive gases
Ar plasma with sputtered atoms
98% Ar plasmas mixed with 2% methane
carbonaceous
nanoparticles
≃ 200 nm
W nanoparticles
≃ 25 nm

## Slide 4
Outline
    Size evolution, density, internal structure (indication on growth mechanisms)
    Modification of the discharge parameters during negative charging
    Modeling of charging mechanisms
    Transport inside the plasma
Nanoparticles produced from cathode sputtering in DC discharges

## Slide 5
Molecular (ion, neutral) precursors
Nucleation
(nuclei of 1-4 nm)
Agglomeration
Molecular sticking
t
    Nanoparticles
Specific collisions/reactions
(complex plasma chemistry)
t
Standard model of formation

## Slide 6
sputtering threshold (Ar/C) ~ 70 eV
sputtering threshold (Ar/W) ~ 34 eV
Cathode sputtering with energetic Ar+
    Nanoparticle growth in sputtering DC discharges
Cathode
Dust substrates
Ar (30-60 Pa)
Ar+ accelerated in the
cathode sheath
10 s
100 s
50 s
25 s
Substrate holder
0 100 200 300 400 500 E (eV)
100
10-2
10-4
W
C
Sputtering Yield

## Slide 7
Carbon nanoparticles
Tungsten nanoparticles
45 s
60 s
200 nm
200 nm
Size increase vs plasma duration
Agglomeration
Molecular sticking
200 nm
Flux of sputtered atoms:
GC ~ GW ~ 1018 m-2s-1
SEM images
Plasma duration (s)

## Slide 8
60 s
Growth by agglomeration and deposition
Tungsten nanoparticle ~ 28 nm
Tungsten crystallites
(nuclei) of 2-3 nm
TEM-HR image
Carbon nanoparticle ~ 25 nm
Nuclei of ~ 3 nm
Carbon sticking around

## Slide 9
Nanoparticle density
Extinction coeficient: Cext = Cabs+ Cscat and x = 2πa/l0 < 0.3
m = complex refractive index of carbon nanoparticle
m = 1.3 + i 0.08
I0
I
Spectrometer
PM
Laser
0.53 mm
Plasma duration (min)
I/I0
nNP ~ 2 108 cm-3
Beer-Lambert law:
2a ~ 55 nm
t = 600 s
Carbon nanoparticles:
L

## Slide 10
Charging of carbon nanoparticles
to the detriment of discharge/plasma
No sputtering: PAr , Id , Vd are cte
With sputtering and NPs production:
Compensation of the electron loss by the increase of Vd
decrease of Vd due to the loss of a part of NPs on the anode
Increase again due to the appearance of a new NP generation
Nanoparticle-plasma coupling
Three discharges parameters : PAr = 60 Pa, Id = 70 mA,
Vd : self-regulated parameter (control the ionization)
Plasma duration (s)

## Slide 11
Charge of an isolated spherical dust particle
Dust charge
Looking for 𝜑, the floating potential :
= Ze
= 0
i
e
a
Maxwellian e- and ions: Te < 5 eV and Te >> Ti ~ Tg
(
(
exp(
Ion current :
higher mobility of e- :
Electron current :
Orbital Motion Limited model (OML):
From Boltzman law:
exp(
)

## Slide 12
OML cannot explain agglomeration (Coulomb repulsion)
Consider charge fluctuations --> nuclei can be briefly neutrals,
positively charged
Charge distribution (T. Matsoukas et al, J. Appl. Phys.,1995)
Charge during the agglomeration phase
Transformed to a partial differentiel equation:
= -
nq : fraction of nanoparticles carrying the charge q
=
a ~ 2-3 nm: Z ~ 6e- - 9e-
a = 14 nm: Z ~ 42 e-
For Te = 2 eV , Ti 0.04 eV
OML --> = - 4.3 eV

## Slide 13
Gaussian charge distribution: n(q) =
Charge
0.2
0.6
1.0
when ni / ne = 1
when ni / ne = 10
Explains the nanoparticle growth by agglomeration of nuclei at the condition of ne depletion
 charging to the detriment of plasma electrons
T. Matsoukas et al , J. Appl. Phys. 77, 1995
Average charge: = k
Ln
Charge during the agglomeration phase

## Slide 14
size
q3
q4
q2
q1
sticking
nucleation
agglomeration
1D sectional model: size distribution divided into bins
or sections along the plasma
In each section: sizes 1-100 nm
100 continuity eq for the total volume density
+ 100 eq for the average chargeTapez une équation ici.
Nucleation
Transport
Growth by sticking
Growth by agglomeration
NP volume balance in each section
Averaged NP charge of each section:
Gaussian charge distribution : smallest NPs can be neutral or > 0
3 coupled numerical modules*: argon DC discharge – molecular ions formation – NP evolution
*A. Michau, K. Hassouni et al, Plasma Chem. Plasma Process. 32 (2012); J. Appl. Phys. 121 (2017)
Modelling of the growth and charge evolution
Carbon NPs
Cathode
Anode

## Slide 15
At x ~ 2 cm from the cathode
(position of electric field reversal)
0 20 40 60 80 100
Sizes (nm)
NP density cm-3
Size evolution during the charging mechanism
Agglomeration can only occur between
nuclei (neutral, positively charged)
and big nanoparticles (negatively charged)
0 2 4 6 8 10 12 13
x (cm)
ne (cm3)
Red curve:
ne calculated self-consistenly through
the coupling of the 3 numerical modules:
coupling of negative molecular ions,
negatively charged nanoparticles and ne

## Slide 16
Outline
    Size evolution, internal structure (indications on formation), density
    Modification of the discharge parameters at large density
    Modeling of charging mechanisms (agglomeration)
    Transport inside the plasma
Nanoparticles produced from cathode sputtering in DC discharges

## Slide 17
Applied forces on an isolated spherical nanoparticle
Electric force : Fe = ZeE (E = - ∇Vp where Vp: plasma potential)
Ion drag force : Fi = 2/3pa2n0marviui(1 - )
r0 = Coulomb radius
: Coulomb logarithm
Thermophoretic force : Fth
Gravity: FG = 4/3pa3rg (negligible)
Fe
Fi
Fth
FG

## Slide 18
Sputtering DC magnetron discharges
Tungstène cathode (sputtering)
Par = 30 Pa, Id = 0.3 A (Vd ~ 200 V)

## Slide 19
W nanoparticles produced in magnetron discharges
Tungstène cathode (sputtering)
Par = 30 Pa, Id = 0.3 A (Vd ~ 200 V)
(10 successive plasmas of 200s)
Guard ring
a ~ 15 nm
NP substrate
a ~ 5 nm

## Slide 20
2D plasma parameters measurements
ne : maximum inside magnetic arches
Te : inverse variation of ne
VP : increase inside magnetic arches
max after the last magnetic arch
Tar : Ar heating due to collisions
with sputtered atoms of <E> ~ 12 eV
ne, Te, VP : Langmuir probe measurements
Tar: measurement byLIF
OML model; a = 5 nm

## Slide 21
Force balance
Guard ring
a ~ 5 nm
Upper part:
Fe and Fth : same range of values
nanoparticles under the guard ring
are pushed to the the guard ring
near the axis: pushed outside magnetic arches and downwards
Lower part:
Fth is dominant: pushed down
Fe + Fth + Fi =0
negligible

## Slide 22
Force balance
Guard ring
a ~ 5 nm
Upper part:
Fe and Fth : same range of values
nanoparticles under the guard ring
are pushed to the the guard ring
near the axis: pushed outside magnetic arches and downwards
Lower part:
Fth is dominant: pushed down
When NPs are transported down they have
more “space, time” to grow than NPs near
the guard ring
Fe + Fth + Fi =0
negligible

## Slide 23
Summary
    Size evolution, density, internal structure (growth by agglomeration, sticking)
    Modification of the discharge parameters due to their negative charge
    Various modeling of charging mechanisms (+ fluctuations) and growth
    Applied forces for their transport in the plasma
Nanoparticles produced from cathode sputtering in DC discharges

## Slide 24
Additional slides
NP density reaches ~ 108 cm-3
also found experimentally
0 50 100 150 200 250 // 600
t (s)
NP density (cm3)

## Slide 25
25
N
S
S
z
r
NP substrate
Guard ring
Cathode
Cylindrical Langmuir probe
rLP << rlarmor for z > 2 cm and probe ⊥ B
(also) vde/vthe  0.32
Classical analyses of probe characteristics
Laser Induced Fluorescence (tunable laser diode)
v = c ; transition frequency of an
atom at rest, the laser frequency
Doppler shift: kbT =

## Slide 26
Laser scattering on the dust cloud during the transport of W nanoparticles towards the anode (classical DC discharges)
- V ~ 0.004 cm/s = 14.5 cm/h
-2nd generation appears in the space freed by the 1st generation

## Slide 28
28
New materials, technologies: superior properties to those of bulk materials
    Analogue of dust particles of ISM, planet satellites
High surface area to volume ratio
Photo-emission wavelength decrease with the size decreases size
Lower melting temperature
Stronger materials
Applications:
Optics: thinner displays, photophores, UV filters
Electronics: nanodevice, single electron emission quantum dots
Energy: hydrogen storage, improvement of solar cell efficiency
Chemical: molecular sensor; catalyst
Medicine: drug carriers, in-vitro imaging, cancer treatment