## Slide 1: Wrap-up from Session 1
Ray Veness

## Slide 2: 2D materials (screens) (Stephane Burger)
CERN has a very broad use of these screens and materials at a very wide range of energies and intensities
  ‘Large’ sheets with excellent thermal properties, low beam interaction and specific optical properties
  Already very much limited in applications due to material damage
Some significant steps already taken for novel materials and tested in HiRadMat
  Glassy carbon
  BNNT screens
  CNT foil screens
Real experience both for performance as a screen and for practical issues
Looking forward:
  Already potential materials in our hands for improving performance
  We should procure and test some of the materials shown in the afternoon session
  We should procure and test graphene sheets
  Develop methods for attaching screens without deformation – work with/learn from industry?
Discussion
  We should consider alternative test facilities to HiRadMat: Use of operating machines, lasers…

## Slide 3: Electro-static applications (Louise Jorat)
CERN interest in reducing activation in electro-static septa
  Replacement for existing Tungsten-Rhenium wires
Full large-scale tests made with 100um CNT ropes
  ‘Nodes’ in ropes difficult to remove during production
  Damage during winding leaving ‘hairs’ in finished assembly
Strong evidence of field emission
  This material is not suited to this application
Discussion
  There are methods for ‘healing’ these kinds of defects
  CNTs are used as electron emitters, so this is perhaps fundamentally a challenging application for these materials

## Slide 4: 1D wires (Alex Mariet)
Replacement for carbon filaments and metallic wires in beam intercepting instruments
  Already limiting applications in higher energy machines (SPS, LHC)
  Minimum interactions with beam (low density, low Z)
  High strength to allow long wires (20cm) and small diameters
Material procurement and testing well developed
  3 different material suppliers, range of diameters
  Tests in HiRadMat and in SPS machine
  Strength, density purity still issues
Discussion, future directions
  Purification methods to remove heavy contaminants exist and should be used
  Not clear that many materials producers are looking to significantly improve CNT length and mechanical properties. How can we ‘stimulate’ this?
  Can we make ropes from longer (eg, 14cm) fibres
  Cross-linking between individual CNTs – Will this improve strength? Is it possible?
  Wire manipulation – in liquid to avoid static electricity issues?
  Consider materials other than carbon nano-tubes