## Slide 1: From Jean-Emmanuel’s presentation
Presented the general concept of MC simulations , focusing on FLUKA, he mentioned GEANT4, PHITS (JAEA) and MCNP6 (LANL)
Two main points were outlined
  Importance of properly choosing the FLUKA input parameters including beam shape (pencil or Gaussian), physics models/cards etc… Fro example Single Scattering managed by analog tracking is adequate for thin materials, whereas for thick material condensed tracking and multiple coulomb scattering is ok
  Properly chose the geometry mesh
Then COMSOL was used to estimate wire heating. Nice example simulations of carbon fibres with different impurities and different density

## Slide 2: From Manon’s presentation
Wire scanners are used to measure beam profile using thin wire of tungsten, molybdenum, or carbon fiber.
Low-density materials, such as carbon nanotube, can offer advantages.
The PyTT simulation code can model the thermal behavior of thin targets and is used to compare the thermal behavior of carbon fiber and carbon nanotube wires.
The program allows for the computation of the wire signal and the study of secondary and thermionic electron emission.
Results include the complete suppression of the thermionic emission current for PSI beams and the discrepancy between simulation and measurements for high thermionic current, which could be due to space charge from generated electrons.
The simulations show high sensitivity to material parameters such as temperature dependence of work function and emissivity.
Open points to improve include sensitivity to parameters, uncertainty in emissivity, and work function due to the surface of the material.

## Slide 3: Wrap up - discussion
Very good starting point for further studies and collaborations
Key points to be addressed could be
  Benchmarking of FLUKA, GEANT4 etc…
  Compare COMSOL and PyTT
  Identify main uncertainties: emissivity, thermionic current at high temperature etc..
  Laboratory setups to heat wires, measure emissivity, thermionic current etc…