## Slide 1
Istituto SPIN-CNR
Universita’ di Napoli Federico II
Dipartimento di Fisica “Ettore Pancini”
Ruggero Vaglio
Surface impedance of superconductors
in high magnetic fields, including nonlinear effects
CERN May 23, 2023

## Slide 2
The concept of Surface Impedance for a conducting material
d
d
(harmonic signal = plane wave)
̃

## Slide 3
Assuming :
«we get easily»:
considering and using Maxwell Equations,
(local, complex, constitutive relation)
The Surface Impedance in the local limit
For a thin film of thickness t it is :
For t 0

## Slide 4
Surface Impedance of normal metals in the local limit
(the conductivity and the resistivity are real numbers)
i.e.
In this case we have:
( is called the penetration depth)
For a thin film of thickness t << δ it is:

## Slide 5
Surface Impedance of normal metals in the «anomalous» limit
In a normal metal the local limit fails if the mean
free path l exceeds the penetration depth δ (l > δ)
In this case the electrons traveling with direction normal to the external surface «see»
the electric field only for a small fraction of their motion between two relaxation events.
The rigrous, complete solution of the problems needs the solution of the full kinetic
equation for the electron motion. However an approximate solution, in the limit l >> δ,
can be found using the «ineffectiveness concept» :
δ
l
Again, with this approximation, «we get easily»:
Rn
ρn1/2
anomalous
skin effect
normal
skin effect
(independent of ρn )

## Slide 6
n
s
Surface Impedance of superconductors in the local limit
(two-fluid model)
( )

## Slide 7
(frequency independent)

## Slide 8
Separating the real and imaginary parts, we get ( ) :
from :
and:
Surface Impedance of superconductors in the local limit
(two-fluid model)
If :
In this case it is also:

## Slide 9
BCS (Matthis-Bardeen theory)
The local limit always applies well superconducting compounds and alloys (l small compared to λ , «local dirthy limit)) and HTS (ξ small compared to λ , «local clean limit»), but not for high purity bulk Nb :
local limit validity zone
(l < ξo , RRR<20)
Full non-local
calculation

(Δ= Δ(T) is the «energy gap»)

## Slide 10
Rs (a.u.)
BCS
Two-fluid
Chart: 
| 0 | 2.0000000000000052E-2 | 4.0000000000000112E-2 | 6.0000000000000338E-2 | 8.0000000000000224E-2 | 0.1 | 0.12000000000000002 | 0.14000000000000001 | 0.16000000000000075 | 0.18000000000000024 | 0.20000000000000004 | 0.22000000000000075 | 0.24000000000000021 | 0.26 | 0.28000000000000008 | 0.30000000000000032 | 0.32000000000000173 | 0.34000000000000186 | 0.36000000000000032 | 0.38000000000000184 | 0.40000000000000008 | 0.42000000000000032 | 0.4400000000000015 | 0.4600000000000003 | 0.48000000000000032 | 0.50000000000000011
 | 0 | 0.00040005 | 0.0016008 | 0.0036039 | 0.0064123 | 0.01003 | 0.014463 | 0.019717 | 0.0258 | 0.032722 | 0.040493 | 0.049126 | 0.058634 | 0.069034 | 0.080344 | 0.092583 | 0.10577 | 0.11994 | 0.13511 | 0.15132 | 0.16859 | 0.18698 | 0.20651 | 0.22724 | 0.24923 | 0.27253
HTS
Two fluid:
HTS:
BCS:

## Slide 11
Nb3Sn, T=4.2K
Rs BCS(Ω)
Nb, T=4.2K
Cu 77K
Superconductors :
Normal metals :
BCS
two fluid and HTS
Rs frequency dependence
10-3
10-1
10-2
10-6
10-5
10-4
0.1
10
1
100
YBCO measured values at 77K
YBCO polycrystalline, measured values at 77k
f (GHz)

## Slide 12
A.Andreone, A.Cassinese, A. Di Chiara, M.Salluzzo , R. Vaglio, JAP 78,1862 (1995)
Single frequency (here 3.5GHz) high Q resonator technique
(Rs is measured from the Q value ΔXs from the frequency shift Δf/f )
Ro
V3Si
Measurements of the surface impedance temperature dependence
Rs(μΩ)
T(K)
T(K)
BCS theory, local limit
BCS theory, local limit
Xs(T)/Xs(0)

## Slide 13
x
fluxon viscosity per unit lenght
m : fluxon mass per unit lenght 0
:
«depinning frequency»
̴
Gittleman and Rosenblum,
Phys Rev. Lett. 16, 734 (1966)
Superconductors in a magnetic field
y
y
z
x

## Slide 14
Surface impedance of a superconductor in a magnetic field:
(rf current perpendicular to the field)
Surface reactance
Surface resistance
S. Calatroni, R.Vaglio : IEEE Trans. Superconductivity 2017
assuming
For a thin film :

## Slide 15
For small fields, i.e. for a small number of trapped vortices
with

## Slide 16
For high fields, i.e. for a large trapped flux ( vortex array)

## Slide 17
T = 50K , ν= 8.05GHz
Copper
CC providers 1 – 5
Rsf (mΩ)
νo~ 25GHz
νo~ 40GHz
In the frame of the FCC-HTS beam screen coating project it was proved that this approach describes very well the experimental rf HTS results on YBCO tapes at T< 50K and B> 5T

## Slide 18
How can high field nonlinearities come out:
a) The potential well for fluxons is non-parabolic
b) The viscous term can be not linearly dependent on fluxons velocity
A recent new issue: superconductors are known to present nonlinear effects .
How this would be in high magnetic fields ?
n=1: Calatroni & R.Vaglio, Physical Review Accelerators and Beams, 22, 022001, 2019
n=2: Calatroni & Vaglio IEEE Trans. Appl. Supercond. 31, 3500208, 2021
a)
b) /

## Slide 19
,
,
,
is the depinning frequency
,
is the «nonlinearity parameter» (that can be dependent on the d.c. magnetic field Bo )
It is useful to introduce the following adimensional parameters:
This nonlinear equation can be solved numerically.
Analitically solutions can be also obtained by simple perturbation methods possible
to obtaining a closed analytical expression for the nonlinear surface impedance Z(Irf )
,
n=2
( , )

## Slide 20
Chart: 
Chart: 
The red line represents the time dependence of the first order perturbation analitical solution
The full numerical solution (that we also calculated) would not be distinguishable on this scale.
n=2
The nonlinearity produces a third harmonic (3ω) signal

## Slide 21
Chart: 
The surface impedance (both Rs and Xs) depend on the rf current
n=2

## Slide 22
The nonlinear effects can be measured experimentally to determine characteristics
and «size» of nonlinear effects (i.e. evaluate n, a and its possible Bo dependence)
8GHz, 50K
Preliminary measurements were already performed (Patrick Krkotic) on YBCO HTS samples
n=1 ?

## Slide 23
Chart: 
The black line represents the time dependence of the numerical solution for the fluxons velocity
(proportional to the electrical field)
Problems related to the nonlinear response of superconductors in high magnetic fields (and high rf currents) can possibly occurr for the FCC beam screen coating with HTS

## Slide 24
for copper :
Chart: 
Problems related to the nonlinear response of superconductors in high magnetic fields (and high rf currents) can possibly occurr for the FCC beam screen coating with HTS
The black line represents the time dependence of the numerical solution for the fluxons velocity
(proportional to the electrical field)

## Slide 25
Conclusions
- For any rf application of superconductors in high magnetic field (and sufficiently high rf currents) it is important to take into account nonlinear effects
- The surface impedance (resistance and reactance) is the main parameter characterizing the response of a metallic surface exposed to an rf electromagnetic field
- Superconductors are characterized by a low (but non-zero) surface resistance, and a much larger surface reactance (though still lower than normal metals)