## Slide 1: Polyurethane Pastilles analysis by CERN chemistry lab
Chemistry laboratory TE/VSC/SCC
10/R-015
08/05/2023

## Slide 2: Outline
Samples received
FTIR analysis
TGA analysis
DSC analysis
Other tests
Conclusions
Questions

## Slide 3: Samples: 3 Polyurethane pastilles
1 - Pastille 70 ShA
Non utilisée
2 - Pastille usagée
Point 5 / LHC
3 - 2R Q2C 71 ShA
Degraded PU pastilles seem to be mainly at the
Q2C position?

## Slide 4: Historique des commandes et reference chez A&P

## Slide 5
FTIR analysis

## Slide 6: Instrument: Fourier-Transform Infrared spectroscopy (FTIR)
e.g.: Silicone oil
Exemple: Polymers Identification
Lab. Spectrometer : Bruker Vertex 70
ZnS Window
Polychromatic IR light

## Slide 7: FTIR analysis : Identification of the polyurethane type
ATR FTIR bonds of a polyurethane ester
1 – New pastille
2 – Used pastille
3 – Degraded pastille
          3 samples are the same polyurethane type: POLYURETHANE ESTER
          This information doesn’t answer:
            Is it the same producer?
            Is it the same material (fillers, compounding..)?

## Slide 8: FTIR analysis : Spectral observation
1 – New pastille
2 – Used pastille
3 – Degraded pastille
          Fact: Polyurethane ester are susceptible to hydrolysis
          Observation: absence of the OH band at 3600 -3300 cm-1 
No evidence for hydrolysis

## Slide 9: FTIR analysis : Spectral differences
Bond 1703 cm-1 disappeared: Hydrogen bonded Carbonyl group (C=O)
Bond 1730 cm-1 increased: Free carbonyl group (C=O)
Bond 3333 cm-1 decreased: Hydrogen bonded N-H group
1 – New pastille
3 – Degraded pastille

## Slide 10: FTIR analysis : Hydrogen bonds
Bond 1703 cm-1 disappeared: Hydrogen bonded Carbonyl group (C=O)
Bond 1730 cm-1 increased: Free carbonyl group (C=O)
Bond 3333 cm-1 decreased: Hydrogen bonded N-H group

## Slide 11: Presence of Molykote grease
https://edms.cern.ch/document/909627/1
Molykote BR 2
standard magasin
SCEM 57.75.10.250.9
?
New pastille
Degraded pastille
Molykote grease
MSDS Molykote BR2

## Slide 12
XRF analysis

## Slide 13
XRF spectroscopy
Niton XL3t GOLDD+

## Slide 14
XRF analysis
New Pastille
Molykote Grease BR2
Degraded pastille
The elements S, Zn and P detected in the degraded pastille must originate from the Molykote BR2 Grease

## Slide 15
TGA analysis

## Slide 16
Sample
(20-100 ug)
Oven (1600°C max)
Microbalance
Gas (Ar, Air, etc.)
TGA analysis
(Setaram Labsys Evo)

## Slide 17: Exemple of degradation : PTFE grease after irradiations

## Slide 18: TGA of PU samples (New et chewing gum)
Signal instability due to sample boiling
The TGA analyzes do not show any significant difference between the New sample and and chewing gum which could explain the observable mechanical degradation

## Slide 19
DSC analysis

## Slide 20: DSC technique
DSC measurement cell
thermocouples
In DSC the difference in heat flow between a sample and a reference is measured as a function of time as both the sample and reference are subjected to a controlled temperature profile.
Example of DSC thermogram

## Slide 21: DSC example: Tg(soft segments) and Tg(hard segments)
Polyurethane elastomers (PUR) based on polypropylene glycol and 4,40-diphenylmethane diisocyanate were prepared with various monoethylene glycol (mEG) contents  chain extender
Tg hard segments:
can be undetectable for some formulations of PU
Tg soft segments

## Slide 22: DSC results for PU pastilles
Date | DSC code | Sample name | mass, mg | method | Tg1, °С
2023-03-15 | r0619 | PU sample new | 35.6 | Tg LN | -29.4
2023-03-16 | r0620 | PU sample 62 | 12.9 | Tg LN | -30.0
2023-03-16 | r0621 | PU sample slime-like | 23.1 | Tg LN | -33.6
∆Tg = 4°C
Tg soft segments

## Slide 23
Other tests

## Slide 24: Compression test with Molykote
sample coated and not with Molykote grease under
  5 tons of pressure at 150°C, 1 day
  5 tons of pressure at 80°C, 1 day
 No PU “gel” formation

## Slide 25: Conclusions
Polyurethane type Ester (FTIR)
No hydrolysis (FTIR)
No major chain rupture (TGA)
No big changes in the soft segments (DSC)
Damage of the hydrogen bonding seems to affect strongly the mechanical properties of polyurethanes (FTIR)
Presence of the Molykote grease (FTIR, XRF)
The cause of degradation remains unknown
The main hypothesis for the degradation is the conjunction of pressure, the Molykote grease and time  difficult to reproduce in the laboratory

## Slide 26: Questions
Why do degraded PU pastilles seem to be mainly at the Q2C position?
What is the peculiarity of the central jack at the Q2C position?
Traceability of the pastilles suppliers (company, PU composition, production process)
Traceability of the pastilles in the tunnel (batch, position)
Data on the strength applied as a function of the degradation observed

## Slide 27
Backup-draft slides

## Slide 28: General info about degradation of PURs
During degradation, PURs undergo both chain scissions and cross-linking
PUR esters are more sensitive to hydrolysis
PUR ethers are more sensitive to oxidation
https://doi.org/10.1016/j.polymdegradstab.2013.12.018

## Slide 29: Starting materials for PURs
Polyols
Isocyanates
Chain extenders (amines, ..)
Vulcanizing agents (sulphur, peroxides)
prepolymers

## Slide 30: Polyols
Our case: flexible elastomer  a high molecular weight polyol
Info from the book:
https://books.google.ch/books?hl=en&lr=&id=g93wwhc0gr0C&oi=fnd&pg=PA1&ots=zz5w-g6dDk&sig=plvVWzCiCFtUBpRV5j6UFZSlAxM&redir_esc=y#v=onepage&q&f=false

## Slide 31: Polyols

## Slide 32: Polyols
NB! The ester or ether nature of a PUR originates from its polyol

## Slide 33: Polyols (polyethers)
Structural formula

## Slide 34: Polyols (polyethers)
Structural formula

## Slide 35: Polyols (polyesters)

## Slide 36: Diisocyanates
TDI
MDI

## Slide 37: Chemical reactions of PU synthesis

## Slide 38: Prepolymers

## Slide 39: Prepolymers: free isocyanate contents

## Slide 40: Chain extenders reactions

## Slide 41: Soft and hard
“Polyurethanes (PUs) are a class of segmented copolymers composed of soft and hard segments. The soft segment is usually a polyether or polyester polyol while the hard segment is composed of a diisocyanate and chain extender. The soft segment provides elasticity, whereas the hard segment contributes strength and rigidity through physical cross-linking points.”
https://royalsocietypublishing.org/doi/10.1098/rsos.180536

## Slide 42: Paths of depolymerizaiton of PUR
From the book

## Slide 43: Paths of depolymerizaiton of PUR

## Slide 44: Hydrolysis of PURs
carbamic acid
carbamic acid
ester
urea
urethane

## Slide 45: Hydrolysis of PU
Change in the bond between
carbonyl carbon --- ester oxygen
↓
carbonyl carbon --- hydroxyl oxygen
Esters have a memorable pattern of three intense peaks at ~1700, ~1200, and ~1100 from the C=O and two C-O stretches, and hence follow what I call the “Rule of Three”
In general, for saturated esters, this peak falls from 1210 to 1160, whereas for aromatic esters, it falls from 1310 to 1250.
↓ ester [1210-1160] or [1310-1250]
↓ urethane [1540-1520]
↑ [OH]

## Slide 46: Additives to polyester PURs for better hydrolysis resistivity

## Slide 47: Depolymerisation of PURs:
Chem. nature of the reactants influences hydrolytic stability:
Polycaprolactone glycol (PTMEG is the best)
Isocyanate (MDI > TDI)

## Slide 48: FTIR: PURs wavenumbers
In our new sample, we have two C=O peaks!!!
Which became one C=O peak in the “chewing gum” sample
Apparently, there is some change in the neighbouring of the urethane carbonyl

## Slide 49: FTIR: hydrogen bonds  amino group

## Slide 50: FTIR: hydrogen bonds  amino group
the groups involved in hydrogen bonding have much lower frequencies, ranging from 3300 to as low as 3200 cm-1.
Generally speaking, the N—H groups free from hydrogen bonding have a stretching vibration at 3450 cm-1

## Slide 51: FTIR: hydrogen bonds  C=O

## Slide 52: FTIR: hydrogen bonds  C=O
The 1732-cm-1 component is assignable to the carbonyls free of hydrogen bonding, and the lower frequency component, at approximately 1703 cm-1, is associated with hydrogen-bonded carbonyls.

## Slide 54: Primary, secondary and tertiary…
Primary urethane: if one carbon and two hydrogen atoms are attached to the nitrogen atom
Secondary urethane: if two carbon atoms and one hydrogen atom are attached to the nitrogen atom
Tertiary urethane: if three carbon atoms are attached to the nitrogen atom

## Slide 55: FTIR of isocyanates
Diisocyanates: peak is at unusual region ~2277 cm-1
Do PUs depolymerise to diisocyanates?
Do (and can) we observe a peak at 2277 cm-1?

## Slide 56: PURs resistance
The Vanderbilt Rubber Handbook: Robert O. Babbit

## Slide 57: Paths of depolymerizaiton of PUR
From the article
Recycling of Polyurethane Foams. DOI: https://doi.org/10.1016/B978-0-323-51133-9.00006-1

## Slide 58: Phosphorolysis

## Slide 59
Degradation Hypothesis: Phosphorolysis
          Can the combined action of molykote grease and compression degrade PURs?
* http://wrap.warwick.ac.uk/112512/1/WRAP-degradation-stabilization-polyurethane-elastomers-Xie-2019.pdf

## Slide 60: Phosphorolysis: the article Troev et al.
CAS 68457-79-4
Zinc bis(O,O-diisobutyl) bis(dithiophosphate)
The exchange reactions proceeding between the ester groups during the synthesis of polyesters[10,11] and the exchange reaction between ester groups of phosphonic acid diesters [12,13] gave grounds for us to assume that the esters of phosphonic (I) and phosphoric (II) acids could also participate in the exchange reactions with ester {-OC(O)-} and urethane {-HN-C(O)-O-} groups.
https://doi.org/10.1016/S0141-3910(99)00105-6
The results achieved allow us to suggest that: (i) -- other diesters (alkyl and aryl) of phosphonic acid [(RO)2P(O)H, (ArO)2P(O)H], esters of alkyl(aryl)phosphonic acid [(RO)2 P(O)R, (RO)2 P(O)Ph] as well as alkyl (aryl) ester of phosphoric acid [(RO)3 P(O), (ArO)3 P(O)] may also participate in above mentioned reactions; (ii) – all of the above mentioned esters may also degrade polyesters [-C(O)-O-], polycarbonates [O-C(O)-O-] and phosphorylated polyamides [-C(O)-NH-].
We plan to investigate this assumption experimentally.

## Slide 61: Phosphorolysis
New functional groups formed
with ion bonds
What is the FTIR signal for
[NR4]+ group??
(originally a neutral amine
group -NR3- )

## Slide 62: Phosphorolysis
new functional groups in the polymer
with covalent bonding
What is the FTIR signal for
P(O)H(OR)2 group??
originally no P=O bonds in the polymer…

## Slide 63: Alcoholysis/glycolysis of PURs

## Slide 64: Alcoholysis/glycolysis of PURs
urethane linkages
Polymer  oligomers
(keeping the urethane linkages  no many changes to FTIR)

## Slide 65: Devulcanisation and Reclamation

## Slide 66: Devulcanisation and Reclamation

## Slide 67: Devulcanisation and Reclamation
“Vulcanized rubbers are infusible and insoluble materials with a 3D crosslinked structure (100% gel content), which are difficult to process and reprocess for further compound production. Therefore, these rubbers need to be partially soluble with lower crosslink density, which can be achieved by partially destroying the initial crosslinked structure, giving more chain mobility (molecular freedom). The soluble fraction can interact and bond with the polymer matrix chains. Thermomechanical, thermochemical, ultrasonic, and microwave are common techniques for partial breakup of the crosslinked structure of vulcanized rubbers. Regardless of the method used, there are two concepts related to the process of destroying the crosslinked structure of rubber including devulcanisation and reclamation. Reclamation is based on the scission of C–C bonds in the rubber backbone to reduce the MW and obtain some plasticity. On the other hand, devulcanisation is the specific cleavage of S–S and C–S bonds, partially destroying the 3D network to produce plasticity.
In an ideal devulcanisation process, the rubber backbone should not be damaged. However, selective breakup of the crosslinked structure inside vulcanized rubber is not possible without damaging some C–C bonds in the backbone. Table 3 reports the energy required for breaking the different bonds of crosslinked rubbers. In general, reclamation and devulcanisation might occur at the same time, making their differentiation difficult in a specific process (Figure 14) [1].“
Materials 2020, 13, 782; doi:10.3390/ma13030782
“Produce plasticity” !!! Our PUR sample also became more plastic!!

## Slide 68: Thermolysis of PU

## Slide 69: FTIR: hydrolysis
Fact: hydrolysis = OH buildup
C=O constant
Idea: should we also use the ratio C=O/OH?