## Slide 1: Meeting
Pascal Studer
Laboratory for Soft Materials
Research – MagRES project
June 2023
Notes: Small update over chemistry work on epoxies

## Slide 2: Toughness – SiO2 nanofiller system
Base system

## Slide 3: Toughness results – SiO2 nanofiller
Chart: Fracture toughness @ LN2
| 0 | 1.5 | 2.5 | 5 | 7.5 | 10
Base System (DGEBA + MPD) | 2.06 | 2.42
Butylamine (f=3, R=9:8) | 4.42 | 5.11 | 5.35 | 5.84 | 2.34
2-Heptylamine (f=3, R=9:8) | 4.49 | 2.78 | 3.6 | 3.84
Mix1 (5% Butylamine, 95% 2-HA, f=3, R=9:8) | 4.45 | 5.03 | 4.57 | 3.17 | 1.37
Benzylamine (f=3, R=9:8) | 0.65

## Slide 4: TEM imaging – SiO2 nanofiller
60 nm cut thickness
~20 nm particles
7.5 vol. % particles (butylamine system)

## Slide 5: Project INSITU
Polyol synthesis of Gd2O3 NP
Crosslinking of polyol without purification
Final Epoxy resin
Dispersion & mechanical breakup of particle agglomerates is obsolete (particles pre-dispersed)
Gadolinium Oxide nanoparticles
  MRI imaging (High magnetic moment)
  Magnetic refrigerant (Magnetocaloric effect ~2-20K)
  Fluorescent phosphor (Doping with other RE’s)

## Slide 6: Classical Polyol method recap
Classical polyol method
  Polyalcohol solvent + NaOH + Gd-Salt
  Dissolution of precursor, heating 100-200°C
  Gives nanoparticles + NaCl
  Low conversion efficiency
  Not easy to separate particles
Fig.1 : Initial classical polyol syntheses, SEM of product after
Solvent exchange & drying
Particles
NaOH / NaCl /…

## Slide 7: Thermal decomposition paper
Basis research paper
  Thermal decomposition of Gd(CH3COO)3 hydrate at 260°C
  Solvent: PEG-1000
  Particle sizes: ~200 nm
  Crystallite sizes: ~4 nm
  Gd2O3 confirmed
  PEG-1000 partially decomposes & acts as surface capping agent
Research paper on which based new approach
Replace PEG-1K by EG (ethylene glycol)

## Slide 8: Basic experiments
Blank | Gd-ac, PEG-1K | 
S1 | 0.1g Gd-ac, 0.12g PEG-1K, 2.38g EG | Complete Dissolution at 150C Instantaneous formation of particles at 250°C
S2 | 0.1g Gd-ac, 0.12g PEG-1K, 2.38g Glycerol | Complete dissolution of pellets at 150°C No particle formation when heated to 250°C+
 | 0.1g Gd-ac, 0.12g PEG-1K, 2.38g 1,4-BDO | Dissolution of pellets from 160-170°C Sudden nanoparticle formation at 170-180°C
S4 | 0.1g Gd-ac, 2.5 1,4-BDO | Dissolution of pellets at 165°C "Particle formation" when cooled, but just precipitation of precursor probably Particle formation when heated to 200-250 with heatgun
S5 | 0.1g Gd-ac, 0.12g PEG-1K, 2.38g EG | Dissolution of pellets at 150°C No particles are formed when heated upto 200°C for 5 minutes in oil bath (Compare with sample3!)
S3-2 | sample 3 heated to 260°C | No visible change
S6 | 0.1g Gd-ac, 2.5g 1,3-BDO | Pellets dissolve at 165-170°C Sudden particle formation at 180-190°C
Ethylene glycol works, butanediol too, glycerol doesn’t
Ethylene glycol particles formed at 250°C (boiling point: 190°C)
Some PEG-1K stabilizes particles

## Slide 9: Scanning electron micrographs
Particles synthesized in ethylene glycol, without PEG-1K
Hydrothermal reactor @ 250°C
Particles synthesized in ethylene glycol, with 5 wt. % PEG-1K
Hydrothermal reactor @ 250°C
Less prone to sedimentation

## Slide 10: Scanning electron micrographs
Particles synthesized in 1,4-butanediol, with 5 wt. % PEG-1K
250°C
Particles synthesized in 1,3-butanediol, with 5 wt. % PEG-1K
250°C

## Slide 11: TGA of commercial VS synthesized powders

## Slide 12: Wide-angle XRD Setup (Xeuss 3.0, G-floor, XRD platform)
Source
CuKa
1.54 A
Sample
Slits
Detector
Moving axis
High Flux beam profile
45 mm detector-sample distance
3 Detector positions
3 * 30 min irradiation time
Sample: 0.5 mm washer with kapton foil

## Slide 13: Wide-angle XRD before/after annealing at 800°C for 2 hours – Commercial powder
Main peaks of cubic Gd2O3 present after annealing
Before annealing not
45 mm detector-sample distance, 3*30 min irradiation, Hi-Flux beam profile
(222)
(400)
(440)
(622)
After annealing
Before annealing
Before annealing

## Slide 14: Wide-angle XRD before/after annealing at 800°C for 2 hours
Main peaks of cubic Gd2O3 present after annealing
Beam transmission: Factor 1000 lower (?!) Denser packing?
Less prominent than for the commercial particles
(222)
(400)
(440)
(622)
After annealing
Before annealing

## Slide 15: Resins
+Accelerator
Custom weak acidic resin
 CryoSet III
Commercial resin (CTD-101K)
DGEBA, Pyrogallol, PPG-DGE
Weakly acidic (aromatic –OH)
Extremely long pot-life
PPG-DGE adjusts toughness & Tg
Industry standard resin
CryoSet II Resin
DGEBA, MPD, 2HA
Long pot-life
High toughness
Alkaline
Functionalized vs non-functionalized samples
Commercial vs synthesized
Two (or three) resins
 2*2*2 = 8 samples
USAXS / SEM(TEM) / Mechanical properties / Drop-test

## Slide 16: Particle functionalization
+
Alkaline surface funcitionalization  Isoelectric point > 7
 Better stabilization in acidic media
-NH2 crosslinkable to
  Epoxides
  Isocyanates
EtOH
24h

## Slide 17: Gd2O3 nanoparticles Characterization
XRD: Crystal structure & Material ✔
USAXS: Dispersion quality of composite June/July
SEM/TEM: Dispersion quality of composite June/July
SEM: Particle shape & size ✔
Isoelectric point of Gd2O3: 7.5-9.5
  At this pH, no net charge on particle surface  agglomeration most probable
  Move pH away from IEP  increase acidity of surrounding medium