## Slide 1: Parametric analysis for 14+ T magnet based on block coils
Ezio Todesco
Technology Department
European Organization for Nuclear Research (CERN)
Acknowledgements to J. C. Perez and S. Izquierdo Bermudez
D. Perini for feedback and discussions

## Slide 2: CONTENTS
Previous dipoles based on block coils (see Appendix)
Two features of block coils and main parameters
Sensitivity analysis

## Slide 3: PREVIOUS DIPOLES ON BLOCK COILS
HD2
      13.74 T reached at 4.5 K, never tested at 1.9 K
      35 mm aperture (diameter)
      45 mm equivalent coil width
      480 A/mm2 overall current density at 15 T

## Slide 4: PREVIOUS DIPOLES ON BLOCK COILS
FRESCA2
      14.6 T reached at 1.9 K
      100 mm aperture
      80 mm equivalent coil width
      220 A/mm2 overall current density at 13 T

## Slide 5: CONTENTS
Previous dipoles based on block coils
Two features of block coils and main parameters
Sensitivity analysis

## Slide 6: TWO FEATURES OF BLOCK COILS AND MAIN PARAMETERS
Two features of block coils
  The ratio between peak field and bore field
  Coil efficiency
Parameters of magnetic design
  Iron contribution
  How much to share the 14 T between coil width and current density
  The two in one effect

## Slide 7: PEAK TO BORE FIELD RATIO
For large coils width/bore width, the ratio l=peak field/bore field goes to 1 (it is 1.03 in LHC MB)
  Block coils in general have a less favorable peak/bore field ratio if there is no iron pole
  We should aim a peak field 2% more than bore field, but we will probably get more (4-6%) if there is no iron pole
Message: keep an eye on lambda, and check if iron pole is viable for FQ
14+ T
HD2: 1.052
(no iron pole)
As given in
G. Sabbi, IEEE TAS 15
Fresca2,
with iron pole
Fresca2: 1.015 with iron pole
As given in
A. Milanese, IEEE TAS 22

## Slide 8: ESTIMATE OF COIL EFFICIENCY
For a solenoid of thickesss w
  m0 is the coil efficiency: ratio between overall current density and coil width
  In practical units (w in mm, j in A/mm2), efficiency is
  4p10-4 T/(A/mm) = 0.00126 T/(A/mm)
For a cosq dipole
  B=m0jw/2
  Efficiency is 0.000628 T/(A/mm)
  For a 60 degrees coil 0.000693 T/(A/mm)
  For a sector coil with wedges and field quality efficiency is 0.00066 T/(A/mm)
Question: what can we expect for blocks?

## Slide 9: EQUIVALENT COIL WIDTH DEFINITION
Equivalent coil width is defined as the width of the sector coil that has the same quantity of conductor of the actual coil – needed to account for wedges and non sector coils
  LHC dipole: 27 mm
  FalconD and 12 T: 37-40 mm
  D20 and HD2: 45-46 mm
  FrescaII: 80 mm
LHC MB
FalconD
HD2

## Slide 10: COIL EFFICIENCY
Coil efficiency gc is defined as the the field divided by overall current density (over insulated coil) and equivalent coil width
  For naked sector coils: gc=0.00066 T/(A/mm)
  Tevatron: 0.00069 (removing iron)
  LHC MB and MBPCT1: 0.00066 (removing iron and grading)
For block coils the efficiency is about 10% lower, we can expect 0.00060 from previous designs
  gc=0.00059 T/(A/mm) for HD2 (removing iron)
  gc=0.00061 T/(A/mm) for FrescaII (removing iron)
Message: keep an eye on the efficiency, it will be probably lower than in a sector coil …
  (see my Covid-19 Lecture notes chapter 4, for the whole discussion on coil efficiency, in particular section 4.4 and 4.5) https://indico.cern.ch/event/1274005/

## Slide 11: IRON CONTRIBUTION
Iron contribution for sector coil
with
  r aperture radius
  w coil width
  RI iron radius
Can be as large as 30%, but there is saturation – I would rather consider 15%
  15% more than 0.00060 is 0.00070
  To be checked with FEM, and to be seen the influence of iron pole
  Now we have all the pieces to estimate the width and current density for a 14 T magnet (we will estimate two in one later, it is small)

## Slide 12: COIL WIDTH SELECTION
Since one has
To get 14 T:
With 50 mm coil width, you need 400 A/mm2
With 55 mm coil width, you need 360 A/mm2
With 60 mm coil width, you need 320 A/mm2
  Note: MQXF has 460 A/mm2, 11 T has 530 A/mm2
Message: current density is 10-20% than in MQXF

## Slide 13: SOMETHING MORE ABOUT COIL EFFICIENCY
25 mm aperture and 55 mm coil width: cross-sectional surface of
  If the cable width is 25 mm, one get two layers of about 60 mm
  Having a longer block in the midplane gives more field
  Message: do we really have to align the two decks as in HD2, Fresca2, RMM ?
(cosq)/r=0.89/84=0.0106
25
80
25
50
27°
(cosq)/r=0.99/82.5=0.0120
8.6°

## Slide 14: TWO IN ONE
Two in one brings an additional, positive contribution to coil efficiency (as iron)
A very rough estimate is
  Where d is the inter-beam distance and r is the baricenter of the coils
  (see next slide and chapter 9.7 of notes in https://indico.cern.ch/event/1274005/
  the estimate is rather optimistic (i.e. it overestimate the real contribution since the sector is collapsed in the plane)

## Slide 15: TWO IN ONE
Estimate of the total current in the coil
Estimate of the baricenter
Increase due to two-in-one is 6%
  For a given current density, and on the short sample we will see in the next section
Message: two-in-one allows decreasing current density by ≈5% (lower stress, easier protection …)

## Slide 16: LOADLINE FRACTION AND SHORT SAMPLE
LHC dipole: 86% at 8.3 T and 7 TeV
  But they work today at 83.5%, 6.8 TeV
MQXF: 77% (7 TeV)
  These fractions computed on specified cable critical current, the production is better
I would place the magnet at 80% of short sample
  14/0.8=17.5 T short sample
  Note for FCC the target was 16 at 86%, i.e. 18.6 T (1 more tesla, D. Tommasini, et al., IEEE TAS 28)
  RMM reached 16.7 T peak field (E. Gautheron, et. al IEEE TAS 23)

## Slide 17: LOADLINE FRACTION AND SHORT SAMPLE
To operate at 14 T, short models should reach systematically more … how much ?
  For LHC and HL LHC magnets, an ultimate was defined (7% more; corresponding to 7.5 TeV operation)
  For MQXF, with 11.3 T peak field, this means 12.1 T – it went systematically up to 13 T and above (6 out of 7 models)
  For 14 T, we should have the possibility of testing at least up to 15 T – this has implications on current (is it possible to go above 20 kA?) and on protection and mechanics
  The structure should be designed to go up to short sample

## Slide 18: CONTENTS
Previous dipoles based on block coils
Main parameters
Sensitivity analysis

## Slide 19: CONTENTS
The Factor X: ratio between critical surface slope and loadline slope
  This quantity is important since it rules the parametric dependence
  In the plot, factor X is 1 – this is the case of magnet with thin coils as MCBXF
Loadline
Critical surface
X=1

## Slide 20: CONTENTS
The Factor X: ratio between critical surface slope and loadline slope
  This quantity is important since it rules the parametric dependence
  Typically high field magnets have X>1
  Property of the design but also of the superconductor
Loadline
Critical surface
X=2

## Slide 21: CONTENTS
The Factor X: ratio between critical surface slope and loadline slope
  If you add cable width, so to lower the loadline, you gain much less in short sample …
  You can compute how much exactly for a linear case
  See seminar in July my Covid-19 Lecture notes chapter 8 and 9, for the whole discussion on coil efficiency) https://indico.cern.ch/event/1274005/
Loadline
Critical surface
X=2

## Slide 22: FACTOR X
The factor X is an analytical tool to estimate the sensitivity of short sample on magnet parameters
  Geometrically, is defined as the slope of the critical surface divided by the slope of the loadline
  It is an adimensional parameter
  k: fraction of sc in the insulated coil
  s: slope of the sc critical surface
  weq: equivalent coil width
  gc: coil efficiency, see previous slides
  DI: iron contribution
Factor X is 1-1.5 for magnets with 10-mm-coil widths like RHIC or MCBXF
Factor X is around 3.7 for LHC dipoles (28 mm coil width)

## Slide 23: FACTOR X
The larger is X, the less you gain in short sample field improving the design by
  Adding conductor (more coil width weq)
  Adding superconductor (increasing the sc fraction in the strand k)
  Improving the critical surface (increasing the slope s)
  (see notes chapters 8 and 9)
  For LHC dipole, increasing the cable width or the critical current, or the sc content, by 20%, you gain in short sample only 20%/(1+3.7), i.e. 4%
  How much is the factor X for 14+ T dipole?

## Slide 24: FACTOR X
Slope at 17.5 T: 250 (A/mm2)/T
  Every additional tesla you lose 250 A/mm2
  This is half of the slope of Nb-Ti
Filling factor: fraction of sc in the insulated cable
  With 0.9 Cu fraction, 1.1 mm diameter and 0.15 mm insulation: 0.36
  With 0.9 Cu fraction, 1.0 mm diameter and 0.15 mm insulation: 0.34
  With 1.2 Cu fraction, 0.85 mm diameter and 0.15 mm insulation: 0.29
Coil width: let us take 55 mm
Iron contribution: 15%
Factor X is around 3.2

## Slide 25: SENSITIVITY ANALYSIS
Dependence on strand critical current
  A gain of 10% in critical current gives 10%/4.2=2.4% more short sample field (0.4 T)
Dependence on coil width
  Increasing 9% coil width from 55 to 60 mm you gain 2.2% in short sample (0.4 T) – that is you have 2% more margin on the loadline
  Decreasing 10% coil width from 55 to 50 mm you lose 2.4% in short sample (0.4 T) – that is you have 2% less margin on the loadline
Dependence on copper ratio of the strand
  Going from the 1.0 mm strand with 0.9 copper ratio to MQXF strand (0.85 mm with 1.2 copper):
  Filling factor lowers from 0.34 to 0.29 (-15%)
  You lose in short sample 15%/4.2=3.5%, i.e. 0.6 T, i.e. 3% on margin on the loadline

## Slide 26: SENSITIVITY ANALYSIS
Dependence on l: quite different
  Nearly whatever you gain in l you get in short sample
  In our case, if we manage to reduce the ratio peak field/bore field of 2%, we gain 1.6% of margin on the loadline!
Message: try to reduce the ratio peak field/bore field as much as possible

## Slide 27: QUENCH PROTECTION
Time margin definition: time needed to quench all superconductor from the beginning of quench not to exceed Tmax
  I0: nominal current
  Gq= quench integral of the magnet fully quenched
  G(Tmax)= MIITs of the cable (depending on specific heats, resistivity, and copper quantity)

## Slide 28: QUENCH PROTECTION
Limits on time margin
  LHC dipoles have a time margin of 100-200 ms (outer/inner layer)
  HL-LHC Nb3Sn magnets (MQXF and 11 T) have 40 ms
  40 ms for Tmax=350 K was set as target for protection for FCC T. Salmi, et al., IEEE TAS 2019
Estimate of time margin
  n: copper to SC ratio
  j0: nominal overall current density
  Ud: energy density in the insulated coil
  Cpave: average specific heat of insulated coil (over material and temperature)
  r: average resistivity of copper (over temperature)

## Slide 29: QUENCH PROTECTION
14+T versus MQXF
  n from 1.2 to 0.9 (-25%)
  j0 from 480 to 360 (55 mm case) :
If the energy density is lower than in MQXF, 0.9 copper ratio could work
  From preliminary studies: 14+T is around 0.08 J/mm3, versus 0.10 J/mm3 of MQXF

## Slide 30: APPENDIX
Previous dipoles based on block coils and flared ends (see Appendix)

## Slide 31: LNBL HD2
Scope: R&D Nb3Sn magnet based on block coils
  Name: HD2
  Reference field: 15 T*
  Design: LBNL
  Production: LBNL
  Period: 2005-2010
  Units: one short model HD2
    a-b-c tests, plus d-e without cold bore,
    i.e. with 43 mm aperture
  Length: 1 m
  Material: Nb3Sn
  Op. temperature: tested only at 4.5 K
  Aperture diameter: 35 mm
    Including the inner structure
  Outer diameter: 600 mm
    Note: reference field not defined, papers establish a target of 15.0 T bore field
    13.74 T reached at 4.5 K
    A second iteration on the design was done, named HD3 (2010-2014)

## Slide 32: LNBL HD2
Main features
  A dipole with accelerator features based on blocks
  No wedges needed in the coil
  Two layer coil, limiting the free aperture at 35 mm
  Saddle ends to give space to the aperture
    A similar paradigm adopted for FrescaII, but with four layers (no wedges, saddle ends

## Slide 33: LNBL HD2
Strand diameter | (mm) | 0.800
Filament size | (mm) | 
N strands |  | 51
Cu/No_cu |  | 0.95
Critical current density | (A/mm2) | 1250 (16 T, 4.22 K)
Cable width | (mm) | 22
Eq. coil width | (mm) | 45.9
Cable mid thickness | (mm) | 1.400
Keystone angle | (°) | 0.000
N. turns |  | 54
N. blocks |  | 2
Insul. thickness (az/radial) | (mm) | 0.11/0.11

## Slide 34: LNBL HD2
Main parameters
  Current: 17400 A
  Loadline fraction: 0.96 (4.5 K)
  0.88 (1.9 K)*
  Temperature margin: --
  Equivalent coil width: 44.1 mm
  Inductance: 5.6 mH
  Stored energy: 0.75 MJ
  Grading: no
  Distance coil to iron: few mm
  Iron contribution to field: 15%
  Saturation: 10%
  Overall current density: 483 A/mm2
  *never tested at 1.9 K

## Slide 35: LNBL HD2
Mechanical structure
  Bladder and keys and Al shell
  Iron is very close to the coil (few mm)
  Radial (horizontal) stress: 107/154 MPa (lower/upper deck)
    This estimated via the Fx value given in the literature divided by the cable width
Protection
  Energy extraction and quench heaters

## Slide 36: FRESCA2
Scope: dipole for cable test station at CERN
  Name: FRESCA2
  Reference field: 13 T, with 15 T as ultimate
  Design: CERN
  Production: CERN and CEA
  Period: 2012-2019
  Units: one
    Coil replacement
  Length: 1.2 m
  Material: Nb3Sn
  Op. temperature: 1.9 K
  Aperture diameter: 100 mm
  Outer diameter: 1030 mm
    14.6 T reached

## Slide 37: FRESCA2
Main features
  Unprecedented coil width (80 mm equivalent)
  Very low overall current density to achieve the 13 T target (220 A/mm2)
  A large aperture dipole with accelerator features based on blocks
  No wedges needed in the coil
  Four layers coil, required by the large aperture of 50 mm
  Saddle ends to give space to the aperture
    Same paradigm adopted for HD2

## Slide 38: FRESCA2
Strand diameter | (mm) | 1.000
Filament size | (mm) | 48
N strands |  | 40
Cu/No_cu |  | 1.3
Critical current density | (A/mm2) | 1400 (15 T, 4.22 K)
Cable width | (mm) | 21.32
Eq. coil width | (mm) | 81.6
Cable mid thickness | (mm) | 1.890
Keystone angle | (°) | 0.000
N. turns |  | 156
N. blocks |  | 4
Insulation thickness (az/radial) | (mm) | 0.200/0.200

## Slide 39: FRESCA2
Main parameters
  Current: 10900 A
  Loadline fraction: 0.72
  Temperature margin: 5.8
  Inductance: 50 mH
  Stored energy: 4.6 MJ
  Distance coil to iron: 20 mm
  Iron contribution to field: 15%
  Overall current density: 220 A/mm2

## Slide 40: FRESCA2
Mechanical structure
  Bladder and keys and Al shell
  Radial (horizontal) stress: 80/100 MPa (lower/upper deck)
    This estimated via the Fx value given in the literature divided by the cable width
Protection
  Energy density on the insulated coil: 0.122 J/mm3
  Energy extraction and heaters