## Slide 1: First Year of Operation of the MKI-Cool
M.J. Barnes
Acknowledgements:
C. Bracco, W. Bartmann, O. Bjorkqvist, M. Diaz, L. Ducimetière, Y. Dutheil, G. Favia, B. Goddard,
T. Kramer, T. Maurin, V. Namora, A. Porret, D. Standen, T. Stadlbauer, P. Trubacova, L. Vega Cid,
V. Vlachodimitropoulos, W. Weterings

## Slide 2: Outline
Context
  MKI purpose and design
  Cr2O3 coating
  Damping element and MKI cool
First year of operation
  Vacuum
  Temperature
Looking forward
  RF damper
  Alumina tubes
Provisional planning for future MKI Cool installations in the LHC
Conclusions

## Slide 3: Context MKI: Injector kicker magnets for the LHC
LHC clockwise injection (4 MKI magnets)
LHC anti-clockwise injection (4 MKI magnets)
Point 8
Point 2
Typical MKI pulse:
MKI8D
MKI8B
MKI8A
MKI8C
Beam 2 direction
Point 8
Vacuum Interconnect to Quadrupole Q5

## Slide 4: Context Screen conductors inside MKI
Screen conductors carry image current of circulating beam
        ⇓
Reduce beam induced heating
Conductors are supported and electrically insulated by alumina tube (high SEY)
2017-18 YETS upgrade of MKI8D: alumina tube coated on the inside with Cr2O3:
  has a low Secondary Electron Yield (SEY)
  does not produce dust in the vacuum system
  is beneficial for high voltage issues
Alumina tube
(installed in MKI)
MKI magnet
Vacuum tank
Injected/
circulating beam
Alumina tube
24 screen conductors (one each 15 degrees, since LS1)
Slots on the tube, to insert screen conductors
Injected/
circulating beam

## Slide 5: Context Cr2O3 coating of MKI8D alumina tube, installed during YETS 2017/18
Before installation: Pressure in Q5-MKI8D vacuum interconnect was a factor of ∼3 (2012, 2015 and 2017) to ∼12 (2016) higher than that of Q5-MKI2D [first MKI2 to see beam]
After installation: The factor of 3-12 is not observed anymore in Q5-MKI8D. No other vacuum modifications were done: pressure reduction is attributed to Cr2O3 coating 👍
Alumina tube with Cr2O3 coating on the inside

## Slide 6: Context Damping element of upgraded MKI8D: the origin of MKI-Cool
Redesigned metallization and ferrite rings (damper), on the alumina tube outside of the magnet aperture
  Reduces beam induced power deposition and re-locates it from the ferrite yoke to the damper
Damper is not at pulsed high voltage
  Easier to cool !
(ΔTMKI8D)/(ΔTMKI8_Post-LS1) ≈ 0.6
Post-LS1 design
Upgraded MKI8D: lower heating of ferrite yoke
Damper
(ferrite rings exposed to beam)
Magnet
Injected/circulating beam
Screen conductors
Alumina tube
Conductive sleeve
Metallization

## Slide 7: Context MKI-Cool = damping element + water cooling
Metallization
Redesigned metallization and ferrite rings (damper) reduces beam induced power and re-locates it from ferrite yoke to damper
BUT, with HL-LHC beam, an uncooled RF damper would reach its Curie temperature, and thus would no longer re-locate losses from the ferrite yoke → yoke temperature would increase
MKI-Cool: water cooling of the RF damper to remove heat
Damper
(ferrite ring)
Magnet
Beam
Screen conductors
Alumina tube
Pipes for water cooling

## Slide 8: First MKI-Cool: installed in LHC during YETS 2022/23
MKI cool in test cage
MKI-Cool installed at location MKI8D (exchanged for, prototype, upgraded MKI8D)

## Slide 9
MKI-Cool operation in LHC during 2023 - Vacuum
Dynamic pressure:
Cr2O3 coated tube of MKI-Cool exhibited rapid conditioning with beam 👍
As per upgraded MKI8D installed during YETS 2017/18:
pressure reduction attributed to Cr2O3 coating, of alumina tube, also seen for MKI-Cool 👍
MKI-Cool
Q5-MKI2D

## Slide 10
MKI-Cool operation in LHC during 2023 - Temperature
MKI-Cool shows significant reduction in measured temperatures 👍
Magnet upstream measured temperature rise of MKI-Cool < 20% of post-LS1 designs
Tube upstream measured temperature rise of MKI-Cool < 2% of post-LS1 designs
For HL-LHC ultimate beam parameters, expected beam induced power will be a factor of <5 greater than for above: no heating issues expected for the MKI-Cool.
Post-LS1 design
Post-LS1 design
MKI Cool
MKI Cool
(ΔTMKI-Cool)/(ΔTMKI8_Post-LS1) ≈ 0.02
ΔT<7˚C
ΔT=40˚C
(ΔTMKI-Cool)/(ΔTMKI8_Post-LS1) ≈ 0.17

## Slide 11
MKI-Cool RF Damper
Good thermal contact of interface between ferrite and copper cylinder & cooling circuits is essential to:
Limit maximum temperature of ferrite
Limit mechanical stress in ferrite
Hence, ferrite and copper cylinder are vacuum brazed.
Transient thermal measurements carried out to determine Thermal Contact Conductance (TCC) of brazing [TCC required: ≥ 1000 W/(m2⋅K)]:
1st MKI-Cool RF damper: Tcc ~3000 👍
Original prototype RF damper: Tcc ~1100 (to be used in 2nd MKI-Cool) 👍
Recent production of RF dampers: Tcc ~400 👎
Studies ongoing to rectify brazing issues @ CERN. Also, discussions with industry
ANSYS: imported head load
ANSYS: predicted temperature
Thermal contact measurement

## Slide 12
MKI-Cool Alumina Tubes
One of the batch of alumina tubes, ordered during 2017, punctured during HV pulse condition of MKI, due to a thin wall 👎.
Also, an issue with slots being too wide 👎.
Puncture
Tomography of punctured tube. Courtesy: B. Bulat
1.2mm thick
Magnetic wire
Probe connected to device
Measured thickness
Technique developed to measure the wall thickness of alumina tubes
Complete batch of 2017 tubes measured, using a magnetic gauge:
  Discussions with tube manufacturer re increasing minimum wall thickness, while staying within specified geometric envelope (i.e. ensuring better concentricity of tubes)

## Slide 13
Thickness values (<2mm in red)
Interpolated profile
Electric field predictions
Goal: Maximize thickness at positions of high electric field
MKI-Cool Alumina Tubes
Python programme developed, to display the wall thickness of the alumina tubes and optimize the angular orientation of the tube in the MKI Cool (to minimize electric stress):
R&D has been carried out, by the manufacturer of the alumina tubes, to understand and overcome the previous production issues:
Three tubes successfully manufactured 👍 are being shipped to CERN
Detailed QA, including wall thickness measurements, to be performed at CERN prior to acceptance of tubes
If R&D tubes are of good quality, order for series of tubes to be placed

## Slide 14
MKI Cool #2:
Prototype MKI Cool RF damper used
Cr2O3 coated tube recovered from upgraded MKI8D (removed from LHC during YETS 22/23)
Longitudinal impedance measurements carried out:
  Very similar impedance to MKI-Cool #1 👍
MKI-Cool #2 presently undergoing oven bakeout
Installation of MKI Cool, at position MKI8C, scheduled from 24/1/2024
MKI-Cool Provisional Planning
1 MKI cool (#1)  | 1 MKI cool (#2) | 2 MKI cools | 2 MKI cools | 2 MKI Cools | 4 Spare MKI Cools
YETS 22/23 | YETS 23/24 | YETS 24/25 | Start of LS3 | During LS3 | During LS3
Point 8 | Point 8 | Point 8 | Point 2 | Point 2 | 
Note: planning could be constrained by available resources (HR and cleanroom).

## Slide 15: Conclusions
First MKI-Cool, with water cooled RF damper, installed during YETS 2022/23:
  Cr2O3 coating of alumina tube conditioned rapidly with beam 👍
  Temperature rise, due to beam induced heating of yoke, is < 20% of other MKIs 👍
  For HL-LHC ultimate beam parameters, no heating issues expected for the MKI-Cool 👍
Issues with brazing ferrite to copper cylinder (bad thermal contact), for series of RF dampers:
  Under investigation with CERN MME
  Possibilities under discussion with industry
R&D carried out, by the manufacturer of the alumina tubes, to understand and overcome the production issues:
  Three tubes successfully manufactured and are being shipped to CERN 👍
  Detailed QA, including wall thickness measurements, to be performed at CERN prior to acceptance of tubes
Based on excellent results of MKI-Cool operation 👍, MKIs to be upgraded to MKI-Cools – provisional planning shown

## Slide 16: Questions ?

## Slide 17: Spare slides

## Slide 18
Beam Induced Heating Limitations (1)
MKI limits for max number of circulating bunches are given by post-LS1 magnets installed
  Details in: V. Vlachodimitropoulos, “Hardware limitations at injection” (https://indico.cern.ch/event/663598/) and “Update on MKI impedance studies” (https://indico.cern.ch/event/734086/)
Can consider these as ‘soft’ limits: exceeding them by a small amount will not damage the MKIs nor cause a beam dump. However, cooling with existing MKIs is very poor (predicted thermal time constant for cool-down of yoke is several hours): hence, these operational limits will avoid heavy efficiency penalties.
TC of Yokes = 125°C
Curie Temp. (TC) of Rings = 250°C
Notes: Up to 7.8 us pulse length operated so far - OK for 240 bunches per train (8.2 us might be in reach, if needed, but to be evaluated in MD ﬁrst) ***check***

## Slide 19
Beam Induced Heating Limitations (2)
Steady state approach used for thermal simulations for post-LS1 MKIs and upgraded MKI8D (YETS 2017/18)
Gaussian longitudinal proﬁle with equi-populated bunches for beam
The following limits are intended for normal operation
In case of usage for speciﬁc tests, depending on the operational conditions foreseen (previous cool down, time at ﬂat top, etc.), allowed parameters (number of bunches and bunch length) to be evaluated
TC of Rings = 250°C
TC of Yokes = 125°C
1.35ns
TC of Rings = 250°C
TC of Yokes = 125°C
2160b

## Slide 20: Expected heating for post-LS1 design
Approach to modify the scaling factor for the other magnets (see Lorena’s presentation for a more detailed analysis)
  Get maximum reached temperatures (of MagnetUp sensors during 2017 operation)
  Correct for differences in initial temperatures between the different sensors (data from March 2017) and equalize with ambient temperatures (i.e. no beam/dissipated power) used in thermal simulations (22°C)
  Use P_loss-T graph to estimate the differences in total dissipated power within each magnet
  Modify the scaling factor accordingly
Example below to make things more clear (hopefully!)
Current limitation (after MKI8D upgrade) is MKI8C: ~1.32e11 p
MKI8A-C have very close intensity margins
 | MKI 8C | MKI 8D*
Measured max T (°C) | 55.5 | 62.6
Initial T (°C) | 20 | 23
“Corrected” max T (°C) | 57.5 | 61.6
Estimated dissipated power (W) | 57 | 71
Power ratio | 0.8 | 1
*Before it was upgraded in YETS 17/18
X
X
X
Margins shown for MKI8D, are the ones before the replacement with the upgraded MKI during YETS 2017/18

## Slide 21: Historical issues – now solved During 2019
Non-conformity of slots in alumina tubes purchased during 2017: slots were too wide. Thus, it was necessary to use screen conductors with a small zig-zag
[HL-NCR: https://edms.cern.ch/document/2440015/1.0]
HV pre-conditioning of MKI cool failed:
[HL-NCR: https://edms.cern.ch/document/2440015/1.0]
18 strong sparks occurred over two weeks Conditioning plateaued at ~45kV (goal=56.1kV)
Three black marks from HV breakdowns to alumina tube
Wider screen conductors
Using wider screen conductors was discarded due to influence on magnetic field (eddy currents)

## Slide 22: 2. Issues – now solved During 2019. Actions carried out
Metal supports for tube replaced by macor
RF damper end cap inside diameter enlarged (from 56mm to 60mm), to increase distance to alumina tube
Sharp edge on stainless steel short eccentric tube removed (manufacturing error)
Cooling pipes for RF damper
RF damper
Macor supports
RF damper structure was modified to mitigate HV breakdowns:
60mm & 1mm offset downwards
End-cap
1 mm radius
Sharp edge chamfered

## Slide 23: 2. Issue – now solved Inspection after conditioning (November 2020)
First observation: Still one black mark seen on the tube, at the end (3 marks in 2019)
The reason was a sharp edge due to mis-alignment of HV busbar of the magnet
HV end plate
HV busbar
1.5 mm
1.2 mm
Alumina tube
Field: ~16.3 kV/mm
Peak field ~34 kV/mm
Field: ~19.3 kV/mm
Alumina tube outside of magnet
End of magnet, without tube
Enhanced electric field (~doubled) due to dealignment of HV busbar
Solved with correct alignment

## Slide 24
MKI Beam Screens – Predictions & Measurements
Prediction: IPAC2018 (WEPMK005)
Prediction: IPAC2018 (WEPMK001) – Run 2 (1.15e11 ppb, 2808b, 1ns Gaussian bunches)
Measurement: IPAC2019 (THPRB072)
MKI8D Tube_Up
No discontinuities, but cooler than expected !
Discontinuities on some Tube_Ups during cool down
Vasilis: presentation to 21st IWG, 26/6/2018
Notes: Note: Run 2 (1.15e11 ppb, 2808b, 1ns Gaussian bunches) are taken from Vasilis’s presentation to 21st IWG, 26/6/2018