## Slide 1: Status of D1 Construction and Test
Tatsushi NAKAMOTO, KEK
On behalf of CERN-KEK Collaboration for D1 Construction for HL-LHC
13th HL-LHC Collaboration Meeting, Vancouver, Canada, Sept. 27, 2023

## Slide 2: Japanese Contribution to HL-LHC: D1 magnets
Beam separation dipole (D1) by KEK
  Design study of D1 for HL-LHC within the framework of the CERN-KEK collaboration since 2011.
  150 mm single aperture, 35 Tm (5.6 T x 6.3 m), Nb-Ti technology.
  Development 2-m long model magnets (3 units) at KEK
Deliverables for HL-LHC
  1 full-scale prototype cold mass (LMBXFP)
  6 series cold masses (LMBXF1-6)
7 units x 7-m long cold masses

## Slide 3: Design parameters
19
13
8
4
4 blocks
44 turns
Large-aperture single layer coil  Mechanical support of a coil is challenging
Shell
Collar
Nb-Ti/Cu coil
GFRP
wedge
Yoke
QPH
Insulation
Brass shoe
 | prototype, series production (7m)
Coil aperture | 150 mm
Field integral | 35 T m
Field (3D) | Nominal: 5.60 T, Ultimate: 6.04 T
Peak field (3D) | Nominal: 6.58 T, Ultimate: 7.14 T
Current | Nominal : 12.11 kA, Ultimate 13.23 kA
Operating temperature | 1.9 K
Field quality | <10-4 w.r.t B1 (Rref=50 mm)
Load line ratio (3D) | Nominal: 76.5%, Ultimate: 83.1% at 1.9 K
Differential inductance | Nominal: 4.0 mH/m
Conductor | Nb-Ti: LHC-MB outer cable
Stored energy | Nominal: 340 kJ/m
Magnetic length | 6.26 m
Coil mech. length | 6.58 m
Magnet mech. length | 6.73 m
Heat load | 135 W (Magnet total) 2 mW/cm3 (Coil peak) > 25 MGy
Radiation dose | 
Three 2 m model magnets were developed at KEK.
12 ton

## Slide 4: Powering Tests of Full-scale D1 Magnets
MBXFP1: June – Sep. 2021
  The magnet reached 106 % of Inom but training up to the ultimate current (108 % of Inom) was NOT demonstrated due to test facility limitation.
  The coil cross section was NOT fully optimized since the cable thickness was deviated from the original one for the 2-m models.
MBXF1: April – June 2023
  Upgrade of test facility allowing the powering tests up to the ultimate.
  The coil cross section for the series magnet was redesigned and the improved FQ is qualified by the MFM of MBXF1.
MBXF5: Oct. – Dec. 2023
  The cold powering test has been suspended due to the trouble of the test facility.
  The revolution indicator of the cold turbine has been repaired. Commissioning is being carried out until Oct. 6. Cooling of MBXF5 is anticipated at Oct. 9.
MBXF2: early 2024

## Slide 5: Upgrade of Test Facility

## Slide 6: Remaining Issues in KEK Test Facility after MBXFP1 Powering Test
Original energy extraction using dump resistors of 25 mW or 50 mW up to the cold powering test of MBXFP1.
  25 mW: Insufficient energy extraction resulted in incomplete helium gas recovery.
  50 mW: The maximum voltage exceeded the allowable limit of 600 V for the
  DCCB of the power converter. Training test above 106% of the nominal
  current could not be performed.
Targets of new facility
  Maximum voltage below 600 V at the ultimate current.
  Magnet dissipation energy below the safety limit of 1.5 MJ.
  Increase of helium gasbag capacity.
To satisfy these targets, new energy extraction using varistors and the additional helium gasbag were implemented before the cold test of MBXF1.
Training quench up to the ultimate current (13.2 kA) was NOT demonstrated in the powering test of MBXFP1 due to limitation of the test facility…

## Slide 7: Additional Helium Gas Storage Bag
New Helium gasbag (#40-sub, 40 m3):
  construction and system commissioning completed in March 2023.
In operation for MBXF1 powering test.

## Slide 8: New EE with Metrosil Varistors
SiC Varistors manufactured by Metrosil for overvoltage protection and effective energy extraction.
Non-linear characteristics:, C=32.01, b=0.3
Design
  5 units in parallel circuit
  Energy extraction: 2.5 MJ
  Up to 15 kA
The system was installed so that it can coexist with the original dump resistor.

## Slide 9: Validation of EE System with Varistors
Signals from Rogowski coils and temperature of SiC disks has been monitored every shutoff/quench event to check indication of imbalance.
Before powering to higher current, we performed 3kA shutoff to check reproducibility.
Run #
A typical dumped current waveforms reconstructed by Rogowski coils and integrators.
Peak current
Turn-on time
Current imbalance at peak was found to be reproducible within ± 4%
Turn-on time among the varistor units : < 0.3 msec.
Stable operation of Varistors was confirmed.
Current imbalance?
Turn-on time?

## Slide 10: Test Results of MBXF1 - Training Quench -
The detailed reports at WP3 meeting
https://indico.cern.ch/event/1290076/

## Slide 11: Quench Training of MBXF1
Nominal current (Inominal, 12.11 kA) : 2 quenches
Ultimate current (Iultmate, 13.231 kA) : 7 quenches
Furthermore NO quench was required to reach Iultmate after the thermal cycle
The last quench at Iultmate occurred during the long holding test (4 hours)
First achievement of the ultimate current rating for the full scale magnet
with an excellent training memory
Temperature: 1.9 K
Ramp rate: 12 A/s or 30 A/s
Quench detection: 0.1 V, 10 msec
Quench protection: QPH and varistor
Quench start location: quench antenna

## Slide 12: Quench Localization Analysis
Voltage taps
Quench Antenna
Vbal1 = (<VT817-1> – <VT5>) – (<VT5>-<VT818-1>)
Vbal2 = (<VT817-1’> – <VT5>) – (<VT5>-<VT818-1>)
Vbal1,2
QD trig.
0
0.2
0.4
-40
-20
-60
0
Localize either the top or bottom coil
0.1
0.3
Time (ms)
Balance voltage (V)
Skew octupole (8S)
Normal octupole (8N)
Skew sextupole (6N)
Normal sextupole (6S)
363
180
Localize both longitudinal and azimuthal position
11 antennas are distributed along the magnet axis

## Slide 13: Quench Location
#1
#2
#3
#4
#5
#6
#7
#8
Quench location changed event by event, indicating the magnet has no specific weak point
Identified
Identified
Identified
Identified
Identified

## Slide 14: Energy Curve / Helium Gas Recovery
Varistor: discrepancy observed between the simulation (design) and measured data but an amount of energy dissipated in the magnet is always below ~1.4 MJ
All evaporated helium gas was successfully recovered.
Capacity of He gas bag
Shutdown
at Iultimate

## Slide 15: Test Results of MBXF1 - Field Quality -

## Slide 16: Remarks on the MBXFP1 Test – Field Quality
MBXFP1:
  Compromised model was adopted due to the time restriction etc.
  Measured b3 and b5 are out of tolerances.
The series magnet (MBXF1-)
  We completed design study and optimized parameters are adopted.
K.Suzuki et al. IEEE TASC vol.32, no.6 Sept 2022, 9000407
 | Parameters for MBXFP | Parameters for Series
f1 | 1.1238 | 1.1680
f2 | 28.0254 | 27.8471
f3 | 50.6798 | 50.3830
f4 | 71.1408 | 70.7156
a2 | 27.3545 | 27.5527
a3 | 52.2239 | 52.5639
a4 | 68.7646 | 70.3048
Azimuthal insulation thickness (mm) | 0.1297 | 0.1297

## Slide 17: DC loop at the Z center for allowed normal (n=3-13) - MBXF1 -
Measured b3 differs from the calculation by < 4 unit at Inominal (12.11 kA).
For other allowed multipoles, measurement agrees with the calculation within 0.5 unit.

## Slide 18: Integral DC loop for allowed normal (n=3-13) - MBXF1 -

## Slide 19: FQ table of MBXF1 for Inominal (12.11kA)
RE: -3353 mm - -2853 mm
SS: -2853 mm - 2648 mm
LE: 2648 mm - 4148 mm
Central: -250 mm - 250 mm

## Slide 20: Effect of Ferromagnetic Environment on FQ of D1
w/o Cryostat | KEK pit | CERN cryostat
Horizontal bench | Vertical test stand - Off-centered by 150mm | Used for design - Centered*
(*) Actual cryostat is off-centerd by 54mm
but not taken into account for our design
~6 units
b3 vs longitudinal pos.

## Slide 21: b3 Summary
Error band defined by comparison between proto. and simulation

## Slide 22: b5 Summary

## Slide 23: Predicted FQ (Integral) in the LHC cryostat - MBXF1 -
From the obtained field quality in the KEK cryostat, we estimated the actual field quality predicted in the LHC cryostat.
  Requirements will be fulfilled in most of the harmonics.
MFM of the D1 prototype cold mass at SM18 will be crucial to confirm the effect of the LHC cryostat on FQ.
Note: difference of ferromagnetic environment between KEK test stand and LHC cryostat.

## Slide 24: Summary of Construction of D1 Cold Mass

## Slide 25
1 coil winding
2 insulation, collaring
3 yoking
4 shell & end-ring welding, end-plate, splice. Alignment target welding, cap welding for series, alignment meas.
vertical cold test
5 cap welding for prototype,
installation of tubes (BT, HXT)
final splice, instrumentation
end-cover & extremities welding
alignment & support welding
shipping to CERN
CERN HP
warm MFM
KEK
HITACHI
inspection incl. pressure test (@ 2.5 MPa)
warm MFM
KEK
SSW
Rotating coil
SSW
Rotating coil
HITACHI
Cryostating
Horizontal cold test
CERN
Flow of D1 Cold Mass Production
PV: Pressure Vessel
HP: readiness of shipping, documents.
Training Quench
MFM at cold

## Slide 26: Manufacturing of D1 Magnet
Coil size measurement system
Control of the coil size is crucial for the D1
- to attain the sufficient preload for the training performance, and
- not to exceed the mechanical limit of insulation.

## Slide 27: Summary of results of coil size measurement
Magnet | Coil | Average 20 pts (MPa) | Max value (MPa) | Min value (MPa) | Standard deviation (MPa) | Cable thickness (44 stack) wrt S2-4 cable (mm)*
MBXFP1 Tested | LPT-1 | 112 | 116 | 106 | 2.0 | 0.262
 | LPB-1 | 110 | 113 | 108 | 1.4 | 0.256
MBXF5 | LT-1 | 122 | 125 | 119 | 1.5 | 0.418
 | LB-1 | 122 | 125 | 118 | 1.8 | 0.422
MBXF1 Tested | LT-2 | 117 | 120 | 114 | 1.3 | 0.397
 | LB-2 | 125 | 128 | 112 | 1.6 | 0.403
MBXF2 | LT-3 | 123 | 127 | 119 | 1.9 | 0.321
 | LB-3 | 117 | 122 | 114 | 1.9 | 0.327
Target range of the total average: 11510 MPa.
  Ave. prestresses are within the target range.
  Excesses were observed at a few points.
Thickness of the insulated SC cables from 19 spools was determined by the “10-stack measurement” before the coil winding.
Dimension control of the wedge thickness: <30 mm
A pair of superconducting cables with similar thickness were selected for each magnet so far. This resulted in the close values of average stress between two coils in MBXFP1 and MBXF5, while the difference in total average is relatively large in MBXF1 and MBXF2.

## Slide 28: Manufacturing of D1 Magnet
QPH, ground insulation
wrapping
Top/bottom coil assembly
Brass shoe assembly
Collaring
Collared coil on bottom yoke
Yoking
Removal of collaring mandrel
Shell welding
End ring welding
Welding of alignment markers

## Slide 29: Manufacturing of D1 Magnet
Axial compression on SC coils
Splice work and bus-leads

## Slide 30
1 coil winding
2 insulation, collaring
3 yoking
4 shell & end-ring welding, end-plate, splice. Alignment target welding, cap welding for series, alignment meas.
vertical cold test
5 cap welding for prototype,
installation of tubes (BT, HXT)
final splice, instrumentation
end-cover & extremities welding
alignment & support welding
shipping to CERN
CERN HP
warm MFM
KEK
HITACHI
inspection incl. pressure test (@ 2.5 MPa)
warm MFM
KEK
SSW
Rotating coil
SSW
Rotating coil
HITACHI
Cryostating
Horizontal cold test
CERN
Flow of D1 Cold Mass Production
PV: Pressure Vessel
HP: readiness of shipping, documents.
Training Quench
MFM at cold

## Slide 31: Manufacturing of D1 Cold Mass
SC bus leads and “spider”
Insertion of CBT
Insertion of HXs
Extremities welding
Welding of end-dome, end cover
IFS assembly
Welding of saddles
Completed D1 cold mass

## Slide 32: Non-Conformities
Welding Qualification
  EDMS 2469433: Invalid Qualification Result of Fatigue Pre-cracking Requirement for 4 K Fracture Toughness Test of PQR2 HAZ Specimen for the D1 Cold Mass Manufacturing, Non-critical
MBXFP1
  EDMS 2426526: Deformation of SC cable due to over-tension, Non-critical
  EDMS 2437654: Small crack at GFRP ramp-box of LPT-1 Coil, Non-critical
  EDMS 2443118: Insulation Damage after Curing of D1 Prototype Bottom Coil, Non-critical
  EDMS 2464985: Partial Damage of Ground Insulation, Non-critical
  EDMS 2581587: Weld Defect of the D1 Cold Mass Prototype (end-cover), Non-critical
  EDMS 2595209: Crane Incident at KEK, Non-critical
  EDMS 2731453: Partial peeling of surface insulation of cryo-heater wire for MBXFP1, Non-critical
  EDMS 2753741: Partial peeling of surface insulation of QPH wire for MBXFP1, Non-critical
  EDMS 2753742: Weld Defect of Joint G-2 of MBXFP1, Non-critical
  EDMS 2753743: Weld Defects of Joints I-L2 and I-R2 of MBXFP1, Non-critical
  EDMS 2753744: Weld Defect of Joint D of MBXFP1, Non-critical
  EDMS 2753745: Out of Tolerance of the Length of the D1 Cold Mass Prototype, Non-critical
  EDMS 2753746 Out of Tolerance of the Transversal Positions of the Extremity Pipes of the D1 Cold Mass Prototype, Non-critical
MBXF5
  EDMS 2753776: Insulation damage of inner surface of MBXF5 coils, Critical
  EDMS 2913654: Weld Defect of the D1 Cold Mass (MBXF5): B-2 Joint, Non-critical
MBXF1
  EDMS 2955218: Cable deformation at coil end after cold test in MBXF1
MBXF2
  EDMS2863016: Insulation damage in the top coil for MBXF2, Non-critical
  EDMS2912993: Insulation damage of the bottom coil for MBXF2, Non-critical
Closed
In work
Coil
Welding
Welding
Wiring
Removal of collaring mandrel
Test/Coil
Coil
Welding

## Slide 33: Major NC in Manufacturing of MBXF5
LT-1 and LB-1 coils for MBXF5 were completed.
  Estimated coil pre-stress: Good.
    LB-1: L120.7 (L) & 122.9 (R), LT-1: 121.7 (L) & 122.2 (R) (unit: MPa).
    EDMS 2724784
All components for the magnet were already fabricated.
Collaring and yoking processes were successfully done in June 2022.
NC: potential coil insulation damage was found after removal of the collaring-mandrel. EDMS 2753776.
  Investigation is underway.
Spacers more than plan were removed from the RE side and the coil were exposed to the flat-rollers…
Flat rollers
Recall
EDMS 2753776

## Slide 34: Repair of MBXF5 Coils
After repair of the damaged insulation
Electrical soundness of the repaired coils was validated by electrical test (coil resistance, inductance, impulse test at 1.3 kV).
EDMS 2753776
Closed

## Slide 35: Cable deformation at coil end of MBXF1 after cold test
Height: 1~1.5mm
EDMS 2955218
Insertion of Go/No-go gage (OD: 146.2mm) was confirmed.
After the cold test of MBXF1 at KEK, the inner bore of the magnet was visually inspected. As a result, cable deformation towards the coil bore was found at both coil ends, around the innermost turn of the coil block (CB)-1B.
This cable deformation was probably caused by Lorentz force during excitation. The same issue occurred in all the 2 m-long model magnets, but no noticeable cable deformation was observed in the full-scale prototype (MBXFP1) thanks to the modification.
There is a concern that a smaller inner coil diameter can cause trouble in the insertion work of a cold bore tube (CBT).
https://indico.cern.ch/event/848426/ https://indico.cern.ch/event/897298/

## Slide 36: Repair Work
EDMS 2955218
KEK is planning to place back the deformed cable mechanically.
A proof-of-principle test was conducted using a CBT welding mandrel and MBXFS2 with the cable deformation (~1 mm) per coil.
The cable was successfully placed back and the vertical inner diameter was increased by 0.7 mm at an estimated vertical force of 22 kN.
Electrical inspection showed no detectable change.
New tooling developed for the repair work
  Max. force: 40 kN
  Stroke: 13 mm
  Longitudinal positioning wrt end plate.
Repair will start in this week.

## Slide 37: Status of Construction
MBXFP1: Delivered to CERN in April 2023. Horizontal cold test in October is planned.
MBXF5: After a major NC with coil insulation damages, the magnet was successfully recovered and completed in June 2023. The cold powering test has been suspended due to the trouble of the test facility. The powering test is anticipated in Oct. 2023.
MBXF1: The test result of the cold powering test looks good. The final cold mass assembly at Hitachi is underway. Delivery to CERN as the first series cold mass is anticipated in May 2024.
MBXF2: Coil winding was already started in February 2023 and magnet assembly (yoking) is underway.
MBXF3: Coil winding will be started in October 2023.
MBXF4: Coil winding is planned in 2024.
MBXF6: The deliverables in JFY2023 will be the whole parts needed for the coil winding and the magnet assembly, but NOT including the actual manufacturing work at Hitachi. The coil winding is foreseen in April/May 2024.

## Slide 38: Summary
Powering test of MBXF1
  Quench performance
    2 quenches to Inominal and 7 quenches to Iultimate
    No quench was needed to reach Iultimate after the thermal cycle
    No helium loss thanks to the system upgrades
  Field quality
    Comparison of the central field shows Δbn≠3 < 0.5 units and Δb3~4 units.
    The magnetic design in a series magnet was confirmed to be tuned well.
    We expect almost all the harmonics will be within the requirements.
Through the manufacturing experience of the D1 cold mass prototype (MBXFP1), the manufacturing and inspection process have been established.
  Many lessons learnt…
A good collaboration with Hitachi.
Control of the coil parts (wedges, shims, end-spacers) is very crucial for the good training performance.
  Reproducibility of coil fabrication has been confirmed.
Non-conformities
  Major NC of the insulation damages of MBXF5 was closed.
  KEK and Hitachi have a mutual concern about the coil fabrication process causing the several NCs. Preventive actions have been considered and implemented.