## Slide 1: RADWG Activities Overview
Rudy Ferraro (BE-CEM-EPR)
RadWG Workshop – 15th June, 2023

## Slide 2: Radiation Test Service
BE-CEM-EPR provides, the service of radiation testing of electronic components supporting the Radiation Working Group (RadWG)
The RadWG supports the accelerator sector equipment groups for the assessment of radiation tolerance of electronic equipment to be installed in radiation exposed areas.
It is as a forum for electronic engineers to discuss
  design practices
  radiation tests
  radiation induced failures in the accelerators.
The RadWG is one of the pillars of the CERN Radiation Hardness Assurance process
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 3: Radiation test service – BE-CEM-EPR
01
02
03
04
05
06
Test planning and structure
Each component/system is analyzed, and all the possible radiation effects are taken into account for planning the test and structure it
Board and instrumentation preparation
For each component a dedicated set of test board is prepared and the associated instrumentation is chosen to face the complexity of the radiation test
Result analysis
The results are analyzed during and after the tests for each component considering the end application and the possible operational issues
Request collection
The requests for radiation testing are collected and processed selecting the most suitable methodology and facilities
Database and Publication
The results are collected, stored and in EDMS and published in the RADWG database to allow an easy research of the best candidates for the new radiation tolerant designs
Testing
The test are carried out at CERN facilities such as CHARM or Co60 and in external facilities. The transport, personnel and instrumentation are selected considering the peculiar aspect of each facility
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 4: 2023 In Number
90 component test request for 2023 (so far)
31 components tested (so far)
5 Radiation campaigns done (3*PSI, 2*CC60)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
Compare to previous year we are in the high range of components tested per month
5 more PSI campaigns are planned, together with regular CHARM tests
We will probably test more components this year than the previous years

## Slide 5: Test Service Status: Requests per type
Total requests: 90 [not only references but also #lots]
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 6: Test Service Status: Requests per group/project
*Cryogenic Systems components are few part references but a lot of different lots
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 7: Test Service Status: Requests per lot type
Distribution of the type of lots:
Quite balanced between new test and production lot qualification
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 8: PSI 2023 Test Status: 24 devices tested so far
March 3-6 (7DUTs)
August 26-27
July 15-16
April 1-2 (9 DUTs)
May 13-14
September 8-10
October 21-22
November 25-26
FCA36N60NF x2 lots (SiC MOS – TE-CRG)
ISO7763FQDWRQ1 (Isolator – TE-CRG)
ISO124U x3 lots (Isolator – TE-CRG)
TCA9406 (I2C Transceiver – TE-CRG)
= Production Lot
= Test Lot
DS2401+ (1-Wire – SY-EPC)
CY62157EV30 (SRAM – BE-CEM)
INA146UA (Opamp – BE-CEM)
SN74LVC16T245DGG (Transceiver – BE-CEM)
PCA9615 (I2C Transceiver – BE-CEM)
( RD3P130SP (MOSFET – SY-EPC ))
CD4066 (Analog Switch BE-CEM)
SM30T12CAY (Thyristor TE-CRG)
SMP75-8 (Thyristor TE-CRG)
SP00800SDT (Thyristor TE-CRG)
SP0080SC (Thyristor TE-CRG)
SM15T12CAY (Thyristor TE-CRG)
LFSPXO018038 (Oscillator BE-CEM)
LFSPXO018041 (Oscillator BE-CEM)
LFSPXO0180xx (Oscillator BE-CEM)
IKW15N120BH6 (IGBT – SY-EPC)
ISO124U x1 lot (Isolator – TE-CRG)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
We still have available slots for this year so don’t hesitate to make requests

## Slide 9: CC60 2023 Test Status: 7 devices tested so far
September
February
June
May
Mars
April
July
August
DHC600P (HP Contactor – TE-MPE)
TC4S66F,LF (Analog Switch – BE-CEM)
CD4066BM (Analog Switch – BE-CEM)
CD4016BMG4 (Analog Switch – BE-CEM)
74LVCV2G66DC (Analog Switch – BE-CEM)
74HC4066PW (Analog Switch – BE-CEM)
74HC2G66DP (Analog Switch – BE-CEM)
No test performed.
No test performed.
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 10: Recent results: Analog Switches (DIOT / BE-CEM)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
Objective: Find a good candidate to isolate I2C devices by opening the switch placed on the digital lines, either with I2C translators or analog switches
Test Preparation
I2C level translator
PCA9306
TCA9406
Two types of devices requested:
Selection / Request
EDMS Request
© From EDMS Test request by filled by DIOT Responsible
Analog Switch
74HC4066PW
74HC2G66DP
74LVCV2G66DC
TC4S66F
CD4066BM
CD4016BMG4
DUT Information:
I2C level translators
Similar devices tested in the past had DD problems and the requested DD levels are quite high
Analog Switches
Pure MOSFET technology, but lifetime is generally low (below 200 Gy) but are immune to DD.
Test Strategy:
  Screening of Switches at CC60 to identify best candidate(s)
  Test best candidate(s) at PSI against SEEs
  Test I2C translators at PSI
Levels: 500 Gy, 7e12 neq/cm²
CC60 Test
Test Results:
Only one switch candidate survived more than 200 Gy
This one will be tested at PSI
PSI Test
I2C Level translator
PCA9306 Tested with success up to 1kGy and 1.7e12 neq.cm²
Second translator was not tested since first one was successful.
Analog Switch:
CD4066 tested with success up to 500 Gy.
From 8 candidates, two were tested with success at PSI, saving beam time for other tests.

## Slide 11: Recent results: Analog Switches (DIOT / BE-CEM)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
CC60 Results: Measurement of input-output resistance (weakest parameter) when disable (Roff)
Sudden resistance drop
Sudden resistance drop
Sudden resistance drop
Sudden resistance drop
Small resistance drop
Negligible change

## Slide 12: Recent results: Analog Switches (DIOT / BE-CEM)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
CC60 Results: Output Voltage when chips are disable and input = 3.3 V
Resistance drop induce increase of the output voltage
No visible change up to 500 Gy

## Slide 13: Recent results: Analog Switches (DIOT / BE-CEM)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
CC60 Results: Output Voltage when chips are disable and input = 3.3 V
Resistance drop induce increase of the output voltage
No visible change up to 500 Gy
No further considered

## Slide 14: Recent results: Analog Switches (DIOT / BE-CEM)
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
CC60 Results vs PSI results:
Consistent results in both facilities
No visible change up to 500 Gy
No visible change up to 500 Gy
No visible change up to 500 Gy
No visible change up to 500 Gy

## Slide 15: CHARM First 2023 test: HAS-100 (SY-EPC)
Beam Start (07.06.2023)
Beam Start (13.06.2023)
Calibration Check
(Every 12h)
Fixed Current readings
(Every 12h)
Reached Levels:
TID = 405 Gy, DDEF = 3.1 e12 neq.cm²
DUT: HAS-100 Current Transducer ( Bipolar-based integrated module)
© EPR Radiation Test Python Framework
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 16: New Test Request Template:
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )
New Test Request document: EDMS 2779784
Contains:
  Information about equipment:
    Locations, Deployment plan, lifetime, number of units in operation
  Information about radiation levels in operation: TID, DDEF, HeH, ThN
  Information about DUTs:
    Use in the system (schematic)
    Parameters of interest
    Radiation Design requirements
    Maximum tolerated failure rate (SEEs)
Will help us to track better the request and also to prepare better the tests
To be sent to: EPR-Radiation-Test-Team@cern.ch
All request are then put in the following EDMS folder: [link]

## Slide 17: Test results analysis and reporting
The website https://radwg.web.cern.ch/ embeds an User-Friendly database
  More than 558 reports from the 2011 up to 2023
225 users subscribed to the mailing list lhc-proj-radwg-members
The service produces reports in a common template for all the components tested
  Test reports template ensure a coherent reporting
databases accessible by all the equipment groups
https://radwg.web.cern.ch
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 18: Conclusions
BE-CEM-EPR provides the service of radiation testing of electronic components supporting the Radiation Working Group (RadWG)
High testing activity in 2023
CHARM Tests has restarted
3 PSI campaigns were performed and they are still some spots in the 5 next campaigns for this year
RADWG Activities Overview by R. Ferraro (BE-CEM-EPR )

## Slide 19
Thank you for your attention!