## Slide 1: MBHDP301 11T hybrid magnet Magnet overview after cooldown n°1
Mechanical Measurement Lab of EN-MME
EDMS #2711698
June 26th 2023 – Rev.1

## Slide 2: Instrumentation overview
SP301
12 instrumented collars;
8 Bullet gauges
Distributed fibers
SP302
12 instrumented collars;
8 Bullet gauges
12 Tie rods (End cage)
Distributed fibers
Instrumented SS Shell

## Slide 3: FEA estimations
EDMS 2909313 v.0.1
3D mechanical behavior of the 11T cold mass at cryogenic temperature: EDMS 2643402

## Slide 4: SP301 collars compression stress
Chart: MBHDP301 - Collars MBHSP301 - Compression Stress
| After SP301 Collaring [RT- 15-12-2022] | Before SS shell welding [RT-26-04-2023] | After SS shell welding [RT-03-05-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
CCS1 | -124.449 | -123.435 | -107.9588 | -98.0636 | -57.5137
CCS2 | -150.0623 | -147.3128 | -134.9273 | -124.8731 | -73.5918
CCS3 | -134.1892 | -133.3605 | -116.3038 | -106.4607 | -65.3499
CCS4 | -156.3607 | -154.2645 | -134.0079 | -123.5676 | -84.3579
CM1 | -118.5308 | -115.0695 | -96.7288 | -86.5547 | -35.5971
CM2 | -134.199 | -130.0358 | -122.3798 | -112.5072 | -58.0663
CM3 | -146.5132 | -149.6722 | -135.8799 | -125.9144 | -68.9048
CM4 | -135.2325 | -134.0917 | -120.0118 | -109.0888 | -66.2966
CNCS1 | -144.6959 | -134.3872 | -117.1755 | -123.7665 | -93.1156
CNCS2 | -98.5823 | -92.1472 | -78.0731 | -84.902 | -23.242
CNCS3 | -162.1328 | -150.1792 | -137.7773 | -144.1752 | -83.4044
CNCS4 | -99.0425 | -94.1199 | -87.6915 | -94.9309 | -35.9062

## Slide 5: SP302 collars compression stress
Chart: MBHDP301 - Collars MBHSP302 - Compression Stress
| After SP302 Collaring [RT-27-03-2023] | Before SS shell welding [RT-26-04-2023] | After SS shell welding [RT-03-05-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
CCS1 | -47.7068 | -48.6632 | -47.2388 | -55.0241 | -19.1365
CCS2 | -79.5337 | -77.8157 | -72.3996 | -79.7297 | -42.3205
CCS3 | -51.6458 | -50.659 | -37.0266 | -44.4756 | -6.3949
CCS4 | -83.0525 | -80.5077 | -68.5708 | -75.6454 | -22.1504
CM1 | -129.6653 | -122.772 | -103.9096 | -109.9478 | -76.6337
CM2 | -104.5171 | -96.1974 | -74.2658 | -81.5929 | -25.6666
CM3 | -145.3725 | -143.6858 | -115.128 | -121.1871 | -63.6691
CM4 | -134.6475 | -127.0425 | -110.7015 | -117.156 | -55.3228
CNCS1 | -105.7397 | -103.466 | -91.6305 | -90.3435 | -40.4561
CNCS2 | -32.915 | -39.6455 | -33.5605 | -33.5497 | -12.2469
CNCS3 | -73.0899 | -72.1451 | -66.4072 | -65.637 | -29.1249
CNCS4 | -39.8775 | -42.7245 | -47.5078 | -46.7678 | -5.8733

## Slide 6: 316 LN external shell stress
Chart: MBHDP301 - Shell - Azimuthal Stress
| Before SS shell welding [RT-26-04-2023] | After SS shell welding [RT-03-05-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
SH_CS1 | 4.8789 | 184.743 | 183.6217 | 358.1928
SH_CS2 | 4.0521 | 186.0008 | 186.2153 | 377.0298
SH_MI1 | 2.7144 | 275.7105 | 273 | 473.5332
SH_MI2 | 0.96038 | 205.3545 | 205.881 | 391.713
SH_NCS1 | 2.5769 | 239.4112 | 238.4948 | 418.0848
SH_NCS2 | 2.4784 | 175.7438 | 174.915 | 348.243
AVG Traction Stress (MPa) | 2.9435 | 211.1606 | 210.3546 | 394.4661
FEA Traction Stress (MPa) | 235 | 235 | 390

## Slide 7: End plates longitudinal stress
Chart: MBHDP301 - End Plates bullets MBHSP302 - Longitudinal Stress
| Bullet gauges loading [RT-2-05-2023] | Connection plate installation [RT-09-06-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
BCS1 | -29.99 | -31.2975 | -26.247 | -82.22
BCS2 | -31.03 | -32.1555 | 0 | 0
BCS3 | -31.6 | -36.1725 | -31.8435 | -62.54
BCS4 | -30.63 | -30.732 | -26.7345 | -43.89
BNCS1 | -33.09 | -34.6515 | -34.008 | -78.25
BNCS2 | -31.66 | -36.699 | -35.8995 | -103.9
BNCS3 | -30.02 | -32.6625 | -31.98 | -75.87
BNCS4 | -34.74 | -37.4205 | -36.738 | -92.61
Chart: MBHDP301 - End Plates bullets MBHSP301 - Longitudinal Stress
| Bullet gauges loading [RT-2-05-2023] | Connection plate installation [RT-09-06-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
BCS5 | -29.95 | -32.9745 | -29.367 | -80.2
BCS6 | -30.34 | -31.395 | -28.0215 | -37.44
BCS7 | -29.9 | -30.4395 | -25.623 | -132.3
BCS8 | -29.93 | -32.214 | -29.3475 | -39.19
BNCS5 | -33.74 | -32.7015 | -32.253 | -18.26
BNCS6 | -30.08 | -29.6595 | -29.055 | -54.63
BNCS7 | -30.68 | -33.0135 | -32.643 | -79.7
BNCS8 | -31.66 | -32.8965 | -32.487 | -84.99

## Slide 8: SP302 End cage tie rods stress
Chart: Tie rods MBHSP302 (End cage) - Connection Side Longitudinal Stress
| SP302 tie rods tightening [RT-18-04-2023] | Before SS shell welding [RT-26-04-2023] | After SS shell welding [RT-03-05-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
CS_Rods_213_U | 119.3985 | 122.4015 | 104.3055 | 103.6035 | 93.37
CS_Rods_213_M | 118.989 | 129.129 | 111.891 | 110.0385 | 125.6
CS_Rods_213_D | 116.922 | 120.2955 | 97.188 | 95.9985 | 72.94
CS_Rods_212_U | 0.10191 | 0.149 | 0 | 0 | 0
CS_Rods_212_M | 116.571 | 109.707 | 92.1375 | 90.4215 | 76.71
CS_Rods_212_D | 117.0195 | 113.1585 | 88.257 | 87.204 | 71.85
CS Average (Mpa) | 98.167 | 99.1401 | 98.7558 | 97.4532 | 88.094
3D FEA estimation (MPa) | 115 | 115 | 115 | 115

## Slide 9: SP302 End cage tie rods stress
Chart: Tie rods MBHSP302 (End cage) - Non Connection Side Longitudinal Stress
| SP302 tie rods tightening [RT-18-04-2023] | Before SS shell welding [RT-26-04-2023] | After SS shell welding [RT-03-05-2023] | Cluster-D insert checking [RT-16-06-2023] | Cooldown n°1 [1,9 K - 22-06-2023]
NCS_Rods_213_U | 114.0945 | 110.5065 | 97.11 | 43.6215 | 49.22
NCS_Rods_213_M | 113.568 | 142.6815 | 114.816 | 69.888 | 50.7
NCS_Rods_213_D | 116.0445 | 81.549 | 72.4815 | 46.215 | 8.471
NCS_Rods_212_U | 114.0165 | 109.7265 | 90.519 | 137.6505 | 44.16
NCS_Rods_212_M | 117.6045 | 115.9275 | 87.0285 | 124.8 | 99.9
NCS_Rods_212_D | 115.1475 | 111.6765 | 86.4435 | 105.4755 | 87.83
NCS Average (Mpa) | 115.0793 | 112.0113 | 91.3997 | 87.9417 | 56.7135
3D FEA estimation (MPa) | 115 | 115 | 115 | 115