## Slide 1: WP4.5 - Quench detection, protection and diagnostic methods for Nb3Sn and HTS high-field magnets - CERN
1st November 2023
Mariusz Wozniak

## Slide 2
Quench Protection – Goals and increasing complexity
Quench protection: managing the release of the stored magnetic energy in a way that prevents/mitigates any potential damage to the magnet, its circuitry, and surrounding components.
With increasing magnetic field, quench protection becomes more important and more complex:
Nb-Ti -> voltages and temperature (in most cases)
Nb3Sn -> voltages, temperatures, and conductor level stresses
HTS -> voltages, temperatures, conductor level stress and often superconductor level stress and for NI coils, a potential for a force density redistribution
Quench protection should be an integral part of the design of a superconducting magnet, affecting the design of the conductor (e.g. Cu/SC ratio, insulation) and coil, the choice of operating current, etc.
Proper quench protection analysis of high-field magnets requires advanced computer tools, and is a multidisciplinary team effort!

## Slide 3
Outline
Detection Technology
Protection Technology
Transient Simulations
Quench Detection Through Electrical Stimuli
E-CLIQ (External CLIQ) Development Progress
S-CLIQ (Secondary CLIQ) Simulations
ESC (Energy Shift with Coupling) Concept
CD (Capacitive Discharge) Protection for HTS
EE (Energy Extraction) with energy recuperation
12T VE Quench Simulation study
New tool for 2D FE quench simulations
AC loss LTS – 3D
AC loss LTS – 2D reduced order
3D FE Simulations of HTS pancakes
3D FE Simulations - High Performance Computing
2D FD Simulations of HTS pancakes stacks
3D CCT Quench Co-simulations
Material properties in Simulations

## Slide 4: Quench Detection Through Electrical Stimuli
Concept:
QD and electrical quality assurance based on magnet’s response to electrical stimuli signal.
Current Status:
Successfully measured impedance of powered superconducting magnet circuit.
Measured 5 Quenching magnet (SMC).
Upcoming Tasks
Analyze quench data and look for Quench precursors/indicators.
Upgrade measurement hardware for better low noise performance.
Perform more quench measurements – possibly on different magnets.
Courtesy of Magnus Christensen
WP4.5-T1-D5

## Slide 5: Quench Detection Through Electrical Stimuli
Key Results:
We tested the system on a D2 prototype magnet
The magnet was measured when unpowered and powered (50 A)
Impedance estimate based on 1.28 S (219 samples) of data acquisition.
Results show good correspondence between the powered, unpowered, and reference measurements.
Impedance estimates based on shorter measurement windows need additional work
Courtesy of Magnus Christensen
Publication in proceedings of MT28 under review
WP4.5-T1-D5

## Slide 6
Outline
Detection Technology
Protection Technology
Transient Simulations
Quench Detection Through Electrical Stimuli
E-CLIQ (External CLIQ) Development Progress
S-CLIQ (Secondary CLIQ) Simulations
ESC (Energy Shift with Coupling) Concept
CD (Capacitive Discharge) Protection for HTS
EE (Energy Extraction) with energy recuperation
12T VE Quench Simulation study
New tool for 2D FE quench simulations
AC loss LTS – 3D
AC loss LTS – 2D reduced order
3D FE Simulations of HTS pancakes
3D FE Simulations - High Performance Computing
2D FD Simulations of HTS pancakes stacks
3D CCT Quench Co-simulations
Material properties in Simulations

## Slide 7
External CLIQ (E-CLIQ)
New developments:
Further matured modeling tools to design and predict the behavior of the E-CLIQ coils and the expected loss in the conductor.
E-CLIQ demonstration test on a Nb3Sn cable sample preparation.
Test will be performed in GHe in cryolab.
New E-CLIQ coils designed and produced for test in combination with a SMC. Integration discussions in progress.
Setup for test in cryolab.
New E-CLIQ coils
Expected temperature increase using the calculated loss.
Courtesy of Tim Mulder
WP4.5-T4-D2
WP4.5-T5-D5

## Slide 8: Secondary CLIQ (S-CLIQ)
As fast as CLIQ or faster
Extracts part of the magnet energy
Electrically insulated from coil
Easier redundancy
auxiliary coil 1
magnet
coils
auxiliary coil 2
[1] M. Mentink and E. Ravaioli, SuST, 2020
Courtesy of Emmanuele Ravaioli
WP4.5-T4-D3

## Slide 9: ESC (Energy Shift with Coupling)
As fast as CLIQ or faster
Extracts part of the magnet energy
Sudden current drop  lower ohmic loss
Electrically insulated from coil
Easier redundancy
auxiliary coil 1
magnet
coils
auxiliary coil 2
https://indico.cern.ch/event/1321217/
Courtesy of Emmanuele Ravaioli
WP4.5-T4-D9

## Slide 10
Capacitor Discharge Quench Protection
Quench Protection Concept:
Upon quench detection, a charged capacitor bank is discharged into the NI coils.
High current pulse generates heat in the turn-to-turn resistive connections.
Fast, potentially very effective, no additional internal components required.
Reduction in hot-spot temperature
Reduction in peak radial force density
Quench
for Stacks of HTS NI Pancake Coils
Courtesy of Tim Mulder
WP4.5-T5-D6

## Slide 11: Energy extraction (EE) with energy recuperation
Courtesy of Bozhidar Panev
A new idea from the recent years proposed an implementation of energy recuperation function in energy extraction (EE) systems
Principle
  1st step: In case of quench or trip, the magnetic stored energy from SC circuit is saved in the storage unit (battery/capacitor) instead of being dumped as thermal losses in a resistor
  2nd step: The energy from the storage unit is injected in the network grid or used as a DC source
In the light of future and bigger accelerators construction involving huge amount of stored energy, such recuperation function becomes a must.
A study on the following aspects is foreseen in the coming years:
  Profitability of such functionality
  Intermediate storage and technology selection
  Reliability and circuit protection
  Design and mock-up manufacturing
WP4.5-T4-D8

## Slide 12
Outline
Detection Technology
Protection Technology
Transient Simulations
Quench Detection Through Electrical Stimuli
E-CLIQ (External CLIQ) Development Progress
S-CLIQ (Secondary CLIQ) Simulations
ESC (Energy Shift with Coupling) Concept
CD (Capacitive Discharge) Protection for HTS
EE (Energy Extraction) with energy recuperation
12T VE Quench Simulation study
New tool for 2D FE quench simulations
AC loss LTS – 3D
AC loss LTS – 2D reduced order
3D FE Simulations of HTS pancakes
3D FE Simulations - High Performance Computing
2D FD Simulations of HTS pancakes stacks
3D CCT Quench Co-simulations
Material properties in Simulations

## Slide 13: 12T VE Quench Protection studies – initial review
50 mm, 5 blocks
50 mm, 6 blocks
56 mm, 6 blocks
We have parametric quench protection software. Looking at many options is relatively low effort for us.
WP4.5-T5-D1
WP4.5-T5-D10
Magnet designs
Courtesy of
L. Fiscarelli
Thanks for great collaboration to the 12 T VE magnet team.

## Slide 14: FiQuS Multipole magnets magnetic and thermal simulations
77’380 DoFs
13’143 DoFs
10 times shorter solution time!
MQXA:
Nb-Ti / Cu cables
Cu wedges
Kapton insulations
Courtesy of E. Schnaubelt & A. Vitrano
MQY
MQXA
Robust 12 T VE
(MQXF cable with 6 blocks)
WP4.5-T5-D9
Magnet design
Courtesy of
L. Fiscarelli

## Slide 15: A 3D FEM thermo-electro-magnetic model to simulate twisted composite superconductors in transient regimes
Courtesy of Bernardo Bordini
15
Animation of the of the currents in the whole wire, 5000 T/min
Animation of the of the currents in the whole wire 5 T/min
5 T/min
An example:
Current distribution and Magnetization
in a MQXF Nb3Sn wire exposed to an increasing background field at 1.9 K
5000 T/min
WP4.5-T5-D4

## Slide 16: A 3D FEM thermo-electro-magnetic model to simulate twisted composite superconductors in transient regimes
Courtesy of Bernardo Bordini
16
5 T/min
5000 T/min
5 T/min
5000 T/min
An example:
Copper Current distribution (animations on the right) and Overall Losses (plots on the left) in a MQXF Nb3Sn wire exposed to an increasing background field at 1.9 K
5000 T/min
WP4.5-T5-D4

## Slide 17: Reduced Order Modelling of Composite Wires and Cables
Courtesy of J. Dular, F. Magnus
Objective: describe the response of composite superconductors in view of their homogenization,
  AC loss, magnetization, inductance.
We propose a 2D model:
  One problem with in-plane currents,
  One problem with out-of-plane currents,
  Coupling via circuit equations.
Example - AC loss w.r.t. field and frequency:
WP4.5-T5-D4

## Slide 18: 3D FE Simulations of HTS No-Insulation Pancake Coils
Coupled 3D magneto-thermal models resolving all turns
  Using specialized thin shell approximations
Courtesy of Sina Atalay
E. Schnaubelt et al., “Magneto-Thermal Thin Shell Approximation for 3D Finite Element Analysis of No-Insulation Coils”. In: arXiv:2310.03138
40 turns double pancake
with linear current ramp
Fully non-linear and anisotropic material relations
WP4.5-T5-D6

## Slide 19: HPC Methods for Parallel FE Simulations
Courtesy of Erik Schnaubelt
E. Schnaubelt et al., “Parallel-in-Time Integration of Transients in Superconducting Accelerator Magnets”. In: 93rd Annual Meeting of the International Association of Applied Mathematics and Mechanics (GAMM 2023). Dresden, May 30, 2023.
Parallel-in-time integration of central field of no-insulation HTS pancake coil
Parallelization in Time
  Parallelization in Space in progress
WP4.5-T5-D6

## Slide 20
New developments:
Accepts multiple pancake geometries using different conductor layouts on different circuits in one simulation.
Quench back in surround rings is possible.
Screening currents and its corresponding AC loss are fully included.
Force density can be exported for analysis in COMSOL / other software.
Used to test various quench protection strategies for stacks of NI pancake coils.
NICQS : No-Insulation HTS Coil Quench Simulator
20
Designed for the thermo-electromagnetic simulation of stacks of NI pancake coils.
40 T NI HTS Solenoid
2D-Simulation of NI-Pancake coils
Courtesy of Tim Mulder
WP4.5-T5-D6

## Slide 21: CCT magnets quench simulation in 3D
Eddy currents
Formers and Shell
Inner former
Outer former
Shell
Inner former
Outer former
Shell
Temperature
Formers and Shell
Temperature
Windings
Iteration #1
Iteration #N
Co-simulation approach used
WP4.5-T5-D13

## Slide 22: STEAM-material-library
Courtesy of Georgia Zachou
Supported Materials
Ag
AgMg
Al
BeCu
Brass
BSCCO
Cu
G10
Hastelloy
Properties
Volumetric heat capacity
thermal conductivity
Resistivity
Jc: Critical Current density
STEAM-materials python package1 used in:
PyBBQ
NICQS
BBQ
SIGMA
STEAM_MatPro MatLab-mex class2 used in:
LEDET
to .dll
He
Iron (BH)
Kapton
Nb3Sn
NbTi
Steel(Stainless Steel)
Stycast
More to come…
to .mex
One single C source
1Pypi steam-material-library
3STEAM_MatPro MatLab class
3CERNGetDP interface
Material functions used in FiQuS through CERNGetDP3
CERNGetDP
wrapper
One single source assures that the material property functions are always the same in all simulation tools.
Most common materials for superconducting magnet design are already included.
Analytical derivatives of selected material functions available.
Properties are available to everybody via the steam git repository.
https://steam-material-library.docs.cern.ch/
WP4.5-T5-D9
WP4.5-T5-D11

## Slide 23: Summary
WP4.5 focuses on quench protection, and should work together with magnet designers, builders and testers.
We already have several excellent collaborations in place between WP4.5 and other HFM work packages and other projects, like the Muon collider study.
We are ready and motivated to join up with more magnet teams/groups by:
  helping you to choose among the various quench protection technologies
  providing simulations and assessing the results (advantages and disadvantages)
  (co-)analysing the protection-related test results, to validate and further improve our models.
Let’s try to work together on an integrated conductor–magnet–quench protection design. How hard can it be?