## Slide 1: INTERNATIONAL SCHOOL ON HIGH ENERGYPHYSICS, ACCELERATOR TECHNOLOGY AND NUCLEAR MEDICINE Almaty, Kazakhstan 9-13 October 2023
PRODUCTION OF RADIOPHARMACEUTICALS AT THE INSTITUTE OF NUCLEAR PHYSICS
E. Chakrova,
e.chakrova@inp.kz

## Slide 2: What is nuclear medicine?
Nuclear medicine is a specialized area of radiology that uses very small amounts of radioactive materials, or radiopharmaceuticals, to check organ function and structure (for diagnosis) or to treat diseased organs or tissue (for treatment).

## Slide 3
Radionuclide diagnostics or imaging
SPECT, SPECT-CT, SPECT-MRI 99mТс, 123I , 67Ga, 201Tl …
PET, PET-CT, PET-MRI 18F, 68Ga, 11C, 64Cu …
Radionuclide therapy 131I, 153Sm, 177Lu, 223Ra, 225Ac …
Theranostic 68Ga-PSMA or 18F-PSMA 177Lu-PSMA or 225Ac-PSMA, 99mTc-PSMA 177Lu-PSMA, 64 Cu…
Nuclear medicine methods:

## Slide 4
18F, 57Со, 109Cd
Isotope production
С-30:
Proton: max. 30 MeV,
3 solid targets, 2 liquid targets
WWR-К, 6 МW
Max thermal neutron flux: 2.21014 n∙cm-2s-1
99Mo/99mTc, 131I, 153Sm, 177Lu, 192Ir, 60Co, 124Sb, 204Tl, 85Sr, 134Cs

## Slide 5: Radiopharmaceutical production facility
Radiochemical building:
R&D laboratories
Hot cells
Microbiological laboratory, Class A, B, C and D
Clean rooms, class C and D
Radiopharmaceutical building:
Clean rooms, Class C and D
Hot cells, Class A, B, C and D
QC laboratory, Class D
~800 м2
~ 730 м2

## Slide 6: Sodium pertechnetate 99mTc, injection from 99Mo/99mTc gel-generator
Irradiation: reactor WWR-K, 1∙1014, n∙s-1∙см2, 98Mo (n ) 99Mo (β-)99mTc,
molybdenum oxide, 15 g., 120 h.
99Мо bulk solution production- alkaline dissolution
Premises: class C
99Mo/99m gel-generator production/assembling: hot cells class C
Production: 2 times/month, 18 GBq
99mTc

## Slide 7
Na+(99mTcO4)-
x(ZrO)2+ ·y
(99MoO4)2-
(99mTcO4)-
·z(H2O)
NaCl
x(ZrO)2+ ·y
(99MoO4)2- Cl-
·z(H2O)
24 hours
x(ZrO)2+·y(99MoO4)2-·z(H2O)
+
“Gel” method concept
Direct conversion of (n, gamma) 99Mo into insoluble zirconium polymolybdate “gel” that contains 25-40 wt.% of molybdenum.
The gel is a cation exchanger with an open structure which allows free diffusion of pertechnetate anion under simple elution by saline.
Additional Al2O3 column is needed to prevent molybdenum break-through
P.W.Moore, M.E.Shying, J.M.Soeau, J.V.Evans, D.J.Maddalena and K.H.Farrington. Zirconium molybdate gel as a generator for 99mTc – II. High activity generators//Appl.Radiat.Isot. – 1987. – Vol.38, № 1. – P.25-29.
R.E.Boyd. The gel generator: a viable alternative source of 99mTc for nuclear medicine//Appl.Radiat.Isot. – 1997. – Vol.48, № 2.
99mTc

## Slide 8: Production of 99Mo/99mTc gel generators
17-21 April 2023
Speaker name: Yelena Chakrova
Slide 7/n
IAEA-CN310-329
#ISTR2023
Premises – class C Hot cell 1- for synthesis of 99Mo-Zr gel and filling of generator’s columns - class C
Hot cell 2 - for steam sterilization of cartridges and assembling of generators - class C
Design and production of hot cell equipment for 99Mo-Zr gel preparation, Pat. 27786 RK
Design of 99Mo/99mTc gel generator, Pat. 28157 RK
99mTc

## Slide 9: Sodium iodide 131I for therapy
131I
Irradiation: reactor WWR-K, 1∙1014, n∙s-1∙см2, 130Te (n )131Te (β-)131I,
tellurium oxide, 20 g., 72-120 h.
131I bulk solution production: reactor radiochemichal hot cells, dry distillation process, 700°C
Premises: class D
Production/dispensing/sterilization: hot cells class C

## Slide 10: Fluordeoxiglucouse 18F injection
18F
Irradiation: cyclotron C-30, 18 MeV, 18O(p,n)18F
2 ml enriched water, 2- 3 h.
Syntheses modules: Synthera, Neptis, dispensing - Thymotheo LT
Premises: class C
Production: hot cells class C
Dispensing/membrane sterilization: hot cells class A
Production: 3 times/day
Transportation: 1- 7 h

## Slide 11: 18F-PSMA-1007 injection
18F
Irradiation: cyclotron C-30, 18 MeV, 2 ml enriched water, 2- 3 h.
Syntheses modules: Synthera, dispensing: Thymotheo LT
Premises: class C
Production hot cells- class C
Dispensing/membrane sterilization:
hot cells class A
Production: 1 time/week

## Slide 12: Lutetium chloride 177Lu, solution for labeling
176Lu (n )177Lu
176 Yb (n )177 Yb (β-)177Lu
Irradiation: reactor WWR-K, 1∙1014, n∙s-1∙см2, 18 days
Lutetium oxide, 20 mg
177Lu
Premises: class D
Production/dispensing/sterilization: hot cells class C

## Slide 13: Status of Nuclear Medicine in Kazakhstan
9 working Centers of Nuclear Medicine
3 Centers of Nuclear Medicine is in process of building
Radiopharmaceuticals:
99Mo/99mTc gel generator, from 2001
“Sodium iodide 131I, oral solution” for therapy, from 2002
“Fludeoxyglukose 18F, injection”, from 2021
17-21 April 2023
Speaker name: Yelena Chakrova
Slide 2/n
IAEA-CN310-329
#ISTR2023
INP fully covers local demand in radiopharmaceuticals with 99mТс and 131I and 70% of local demand in radiopharmaceuticals with 18F
5
1
2
1
1
1
1