## Slide 1: Mechanical concepts for 40T Final Cooling Solenoid for the Muon Collider
C. Accettura, A. Bertarelli, B. Bordini
With several contributions from L. Bottura, A. Dudarev, A. Kolehmainen, F. Sanda
Muons Magnets Working Group
https://indico.cern.ch/e/1313020 14/12/2023, CERN

## Slide 2: Index
Introduction and motivation
Pre-compression concepts
FEA simulations for different concepts and parameters
Conclusions and perspective

## Slide 3: Introduction and Motivations
Design proposed for the Final Cooling solenoid based on single and compact coil critical stress management:
    PM=B02/2μ0~600MPa
    Hoop stress~ 1.4-2.2PM (compact coil)
Magnetic pressure vs Field
See B. Bordini, Technology options for the final cooling solenoids, IMCC Annual Meeting 2023, Orsay

## Slide 4: Introduction and Motivations
Design proposed for the Final Cooling solenoid based on single and compact coil critical stress management:
    PM=B02/2μ0~600MPa
    Hoop stress~ 1.4-2.2PM (compact coil)
Non- homogeneous and anisotropic material:
    Maximum allowable stress very weak in certain direction
    Scarce literature
    Reduced safety margin
Magnetic pressure vs Field
See B. Bordini, Technology options for the final cooling solenoids, IMCC Annual Meeting 2023, Orsay
Reference Conductor Fujikura FESC-SH12.
https://www.fujikura.co.jp/eng/products/newbusiness/superconductors/01/superconductor.pdf
REBCO conductor | 
Axial tensile stress | 700MPa
Axial tensile strain | 0.4%
Transverse compressive stress | >100MPa
Transverse tensile stress | 10-100MPa
Max shear stress | >19MPa
A pre-compression of ~200MPa is need to remain below this value

## Slide 5: Pre-compression
How to obtain the pre-compression?
Mechanical concept is based on encapsulating HTS pancake coils in an external structure, generating high radial compressive stresses. Three concepts analysed:
  Thermally-induced shrink fitting
  Adjustable shrink-discs with conical surfaces
  Hybrid solution (1+2)

## Slide 6: Shrink Fitting
Coil surrounded by a cylindrical shell with rin_shell<rext_coil
Shell is pre-heated fitting of the coil inside cool-down of the shell and thermal contraction
Simple analytical evaluation: σhoop=-500MPa200MPainterference gap ~220μm Tshell~170°C
Some practical aspects must be considered:
  Differential contraction during cooldown
  Strength of the cylinder
  Impact of the joints
  Plasticity
  Mechanical tolerances: 1MPa/μm lost
  Buckling
FEA simulations at different levels of complexity

## Slide 7: Assumptions
2D axisymmetric
Electromagnetic Forces
    Ideal Solenoid ( = 531 A/mm2)
    Real Solenoid ( = 620 A/mm2)

## Slide 8: Reference model
Ha to avoid radial tensile and shear stress after cooldown
Needed to keep the pre-compression. Soft copper was resulting in a lower pre-compression
Homogeneous tape properties

## Slide 9: Homogeneization
Radial direction springs in series
Tangential direction springs in parallel

## Slide 10: Layered model
R30
R90
12mm
R250

## Slide 11: Geometry and Materials
R30
R90
12mm
R250
4mm
1mm
Inner Connection
3mm
3mm
Outer Connection
30μm Cu
50μm Hast.
Coil

## Slide 12: Validity of homogeneous model
σTransverse,Average=-180MPa
Step 2: Cool-down
Step 3: Energization
Step 1: Shrink fitting (T external shell =250°C)
σTransverse,Average=-210MPa

## Slide 13: Validity of homogeneous model
σTransverse,Average=-180MPa
Step 2: Cool-down
Step 3: Energization
Step 1: Shrink fitting
σTransverse,Average=-210MPa
σTransverse,Average=-215MPa
750 layers: 30μm+50 μm
Step 2: Cool-down
Step 3: Energization
Step 1: Shrink fitting
σTransverse,Average=-170MPa
εz=0.18%
εz=0.17%

## Slide 14: Effect of the inner joint properties
Let the ring detach to limit radial tensile stress

## Slide 15: Effect of the tape plasticity
 | σx-radial[MPa] |  |  | εz-hoop
step | min | max | ave | max
1 | -289 | -57 | -210 | 
2 | -224 | -67 | -164 (200*) | 
3 | -416 | 77 | -213 | 0.30%
1 | -308 | -54 | -214 | 
2 | -272 | -63 | -171 (210*) | 
3 | -502 | 73 | -224 | 0.22%
Plastic
Elastic
*Average on the external edge

## Slide 16: Effect of the tape properties
 | σx-radial[MPa] |  |  | εz-hoop
step | min | max | ave | max
1 | -291 | -55 | -208 | 
2 | -264 | -60 | -171 (215*) | 
3 | -484 | 75 | -218 | 0.24%
1 | -289 | -57 | -210 | 
2 | -224 | -67 | -164 (200*) | 
3 | -416 | 77 | -213 | 0.30%
Reference
*Average on the external edge

## Slide 17: Effect of the tape properties
 | σx-radial[MPa] |  |  | εz-hoop
step | min | max | ave | max
1 | -291 | -55 | -208 | 
2 | -264 | -60 | -171(215*) | 
3 | -484 | 75 | -218 | 0.24%
1 | -289 | -57 | -210 | 
2 | -224 | -67 | -164 (200*) | 
3 | -416 | 77 | -213 | 0.30%
Reference
*Average on the external edge

## Slide 18: Effect of the tape properties
 | σx-radial[MPa] |  |  | εz-hoop
step | min | max | ave | max
1 | -291 | -55 | -208 | 
2 | -264 | -60 | -171(215) | 
3 | -484 | 75* | -218 | 0.24%
*Localized effect
εz=0.24% 
σx~10MPa 

## Slide 19: Alternative Inner Joint-1
Hastelloy orthotropic | Ey,z-hoop[GPa]
Ex-radial[GPa] | Ey,z-hoop[GPa]
100 | 200
εz=0.17% 
σx=80MPa ☒

## Slide 20: Alternative Inner Joint-2
Soft Hastelloy isotropic
E [GPa]
20
εz=0.27% 
σx=12MPa 
Model simplification, important to have a 3D design of the inner ring to take into account the real stiffness of the structure

## Slide 21: Shrink Fitting
Coil surrounded by a cylindrical shell with rin<rext_coil
Shell is pre-heated fitting of the coil inside cool-down of the shell and thermal contraction
Simple analytical evaluation: 600MPa200MPainterference gap ~300μm ~250°C
Some practical aspects must be considered:
  Differential contraction during cooldown
  Strength of the cylinder
  Impact of the joints
  Plasticity
  Mechanical tolerances: 2MPa/μm lost
  Buckling
FEM simulations at different levels of complexity

## Slide 22: Mechanical considerations - Second concept
2 Load Steps:
  Shrink Disk displacement (5 mm)
  Energization
Max. Hoop Stress (after energization): 620.4 MPa
Max. Hoop Strain (after energization): 0.344 %
Shear Stresses globally lower than 15 MPa
However, locally they can reach after energization ~ |30| MPa

## Slide 23: Mechanical considerations - Third concept
To limit shear stresses, an intermediate steel shell is added (ID 184 mm; OD 224 mm)
~ 150 µm interference with coil pack created by differential heating
3 Load Steps: 1. Shell/Coil Interference; 2. Shrink Disk Displacement (2.2 mm); 3. Energization
Min. Hoop Stress after shrinking: -426 MPa
Max. Hoop Stress after energization: 598 MPa
Max. Hoop Strain after energization: 0.332 %
Local peak shear stress ~ 10 MPa
Max Shear after energization |9.2| MPa

## Slide 24: Mechanical considerations - Third concept
To limit shear stresses, an intermediate steel shell is added (ID 184 mm; OD 224 mm)
~ 150 µm interference with coil pack created by differential heating
3 Load Steps: 1. Shell/Coil Interference; 2. Shrink Disk Displacement (2.2 mm); 3. Energization
Min. Hoop Stress after shrinking: -426 MPa
Max. Hoop Stress after energization: 598 MPa
Max. Hoop Strain after energization: 0.332 %
Local peak shear stress ~ 10 MPa
Max Shear after energization |9.2| MPa
Preliminary is ok, but limited safety margins Fundamental to have a good understanding of the material limits and failure mode

## Slide 25: Testing
σhoop~-600MPa reached on the inner radius of the coil
The required compression is achieved with 10 M16 bolts
System equipped with strain gauges and digital image correlation to characterize the coil

## Slide 26: Conclusion and next step
The final cooling solenoid requires a pre-compression to operate at 40T:
  Shrink fitting, mechanical jigs or a combined solution can provide the required pre-compressions
  Tape properties impacting the results important to benchmark them with experimental tests
  The design of the inner and outer rings is critical: 2 possible solutions identified, more modelling work is needed to finalize the design
  Different FEM models ready to investigate more options
  Extensive work of design of the tooling for the experimental characterization of the tape

## Slide 27: Validity of homogeneous model
σTransverse,Average=-180MPa
Step 2: Cool-down
Step 3: Energization
Step 1: Shrink fitting (T external shell =250°C)
σTransverse,Average=-210MPa
σTransverse,Average=-85MPa
750 layers: 30μm+50 μm

## Slide 28: Validity of homogeneous model
σTransverse,Average=-180MPa
Step 2: Cool-down
Step 3: Energization
Step 1: Shrink fitting (T external shell =250°C)
σTransverse,Average=-210MPa
σTransverse,Average=-85MPa
σTransverse,Average=-215MPa
750 layers: 30μm+50 μm
MPC CONTACT