## Slide 1: Recent Developments on the Target Magnet Design
A. Portone, J. Lorenzo, P. Testoni (F4E)
Muons Magnets Working Group
Thursday Nov 30, 2023

## Slide 2: SUMMARY
Aim: Develop an alternative solution to the hybrid US-MAP [1-3] (5 resistive coils and 19 SC coils, 2.4 m bore ) made of HTS (23 SC coils, 1.2 m bore )
Design highlights
  VIPER-like cable (HTS tapes, central cooling hole, steel jacket) with Imax61 kA
  Set of 23 coils in 3 sections (300 mm gap between sections, 20 mm gap between coils)
    Peak field on conductor 20.9 T, magnetic energy 1.1 GJ
    Cable length  8.75 km, winding mass  114 t
  Field on axis within 3.8% accuracy of Sayed-Berg formula over 16 m channel length
  Stresses in structural elements within 316 LN limits (sY 1000 MPa)
  Stresses in tapes being investigated to be minimized (txy30 MPa)
  Coils operating at 20 K, 20 bar, 15 W pumping power, 150 W heat removal
  High conductor stability (DT≥10 K!)
  Detection & dump for quenches in low field/current most challenging (long detection times) but seems compatible with hot-spot temperature limit (THS  150-200 K)
  Increasing 3-4-5 cm  HF2-3-4 coils clear bore: DL = +177 m, DE = +80 MJ, De(%)  0
  As (9)+increasing sections spacing 0.3 m0.48 m: DL = +177 m, DE = +83 MJ, De(%)  +4.9

## Slide 3
Operating current: 58 kA
Operating field: 20 T
Operating temperature: 20 K
SOLDERED HTS STACK
COPPER FORMER
COOLING CHANNEL
STAINLESS STEEL WRAP
STAINLESS STEEL JACKET
39.5
23.5
8
M. Takayasu et al., IEEE TAS, 21 (2011) 2340
Z. S. Hartwig et al., SUST, 33 (2020) 11LT01
HTS conductor design
MIT “VIPER” conductor
HTS-Based Target Solenoids: HTS Conductor

## Slide 4
HTS-Based Target Solenoids: Field Profile and Coils Geometry
Bi = 20 T
Bf = 1.5 T
Lt = 15 m
-1 m < z < 15 m
Reference field profile on axis
(H. K. Sayed and J. S. Berg, 2014)
Coil | Rc [m] | Zc [m] | DR [m] | DZ [m] | Layers | Pancakes | I [kA] | It [MAt]
1 | 0.849 | -0.185 | 0.498 | 0.830 | 12 | 20 | 58.90 | 14.137
2 | 0.870 | 0.665 | 0.540 | 0.830 | 13 | 20 | 60.71 | 15.785
3 | 0.870 | 1.515 | 0.540 | 0.830 | 13 | 20 | 60.39 | 15.702
4 | 0.808 | 2.365 | 0.415 | 0.830 | 10 | 20 | 51.65 | 10.331
5 | 0.766 | 3.215 | 0.332 | 0.830 | 8 | 20 | 47.47 | 7.595
6 | 0.704 | 4.065 | 0.208 | 0.830 | 5 | 20 | 46.50 | 4.650
7 | 0.745 | 4.708 | 0.291 | 0.415 | 7 | 10 | 46.29 | 3.240
8 | 0.704 | 5.423 | 0.208 | 0.415 | 5 | 10 | 53.17 | 2.658
9 | 0.662 | 6.065 | 0.125 | 0.830 | 3 | 20 | 43.28 | 2.597
10 | 0.662 | 6.915 | 0.125 | 0.830 | 3 | 20 | 42.15 | 2.529
11 | 0.642 | 7.765 | 0.083 | 0.830 | 2 | 20 | 49.45 | 1.978
12 | 0.642 | 8.615 | 0.083 | 0.830 | 2 | 20 | 44.18 | 1.767
13 | 0.642 | 9.465 | 0.083 | 0.830 | 2 | 20 | 39.57 | 1.583
14 | 0.642 | 10.315 | 0.083 | 0.830 | 2 | 20 | 32.71 | 1.309
15 | 0.642 | 10.958 | 0.083 | 0.415 | 2 | 10 | 46.72 | 0.934
16 | 0.642 | 11.673 | 0.083 | 0.415 | 2 | 10 | 45.90 | 0.918
17 | 0.621 | 12.315 | 0.042 | 0.830 | 1 | 20 | 52.31 | 1.046
18 | 0.621 | 13.165 | 0.042 | 0.830 | 1 | 20 | 56.06 | 1.121
19 | 0.621 | 14.015 | 0.042 | 0.830 | 1 | 20 | 51.60 | 1.032
20 | 0.621 | 14.865 | 0.042 | 0.830 | 1 | 20 | 51.38 | 1.028
21 | 0.621 | 15.715 | 0.042 | 0.830 | 1 | 20 | 50.47 | 1.009
22 | 0.621 | 16.565 | 0.042 | 0.830 | 1 | 20 | 52.86 | 1.057
23 | 0.621 | 17.415 | 0.042 | 0.830 | 1 | 20 | 57.44 | 1.149
NI=1/0100 MAt

## Slide 5
HTS-Based Target Solenoids: Coils Current and Field
Magnetic Field [T]
Peak field in coil 2

## Slide 6
HTS-Based Target Solenoids: Axial Forces
Chart: Axial force Fz (MN)
| FTZ1 | FTZ2 | FTZ3 | FTZ4 | FTZ5 | FTZ6 | FTZ7 | FTZ8 | FTZ9 | FTZ10 | FTZ11 | FTZ12 | FTZ13 | FTZ14 | FTZ15 | FTZ16 | FTZ17 | FTZ18 | FTZ19 | FTZ20 | FTZ21 | FTZ22 | FTZ23
with chicane | 251237715.71 | 59510130.85 | -101001739.63 | -101383310.92 | -58482688.43 | -17101698.03 | -16600633.34 | -2177285.98 | -5690187.15 | -2607733.33 | -1686467.77 | -914736.62 | -742835.68 | -160306.33 | -895830.13 | 375412.02 | -394118.95 | -81688.25 | -93536.75 | -34807.6 | 11369.24 | 64183.15 | -313787.55
w.o. chicane | 251236991.85 | 59509129.09 | -101002921.14 | -101384105.74 | -58483318.59 | -17102092.4 | -16600994.6 | -2177602.39 | -5690511.56 | -2608136.14 | -1686852.05 | -915191.77 | -743389.72 | -160948.03 | -896432.52 | 374581.05 | -395371.19 | -83923.59 | -97306.58 | -42716.48 | -9079.63 | -18770.95 | -987203.52
Chicane

## Slide 7
a) Hoop Stress
b) Axial Stress [Pa]
HTS-Based Target Solenoids: Jacket Stresses

## Slide 8
HTS-Based Target Solenoids Increase high field bore
.30 m
.30 m
.30 m
.30 m
+5 cm
+4 cm
+3 cm

## Slide 9
HTS-Based Target Solenoidsincrease high field bore & section spacing
.48 m
.48 m
.30 m
.30 m
+5 cm
+4 cm
+3 cm

## Slide 10
HTS-Based Target Solenoids: far field

## Slide 11: REFERENCES
R.J. Weggel, N. Souchlas, H.G. Kirk, V.B. Graves, K.T. McDonald, A TARGET MAGNET SYSTEM FOR A MUON COLLIDER AND NEUTRINO FACTORY, TUPS053 Proceedings of IPAC2011, San Sebastián, Spain
R.J. Weggel, N. Souchlas, H.K. Sayed, J.S. Berg, H.G. Kirk, X. Ding, V.B. Graves, K.T. McDonald, DESIGN OF MAGNETS FOR THE TARGET AND DECAY REGION OF A MUON COLLIDER/NEUTRINO FACTORY TARGET TUPFI073 Proceedings of IPAC2013, Shanghai, China
C. Rogers, Overview of target, capture and cooling complex, https://indico.cern.ch/event/1147941/
H.K. Sayed and J. S. Berg, Optimized capture section for a muon accelerator front end, PHYSICAL REVIEW SPECIAL TOPICS - ACCELERATORS AND BEAMS 17, 070102 (2014)
C. Accettura et al., “Conceptual design of a target and capture channel for a Muon Collider,” MT28 Conference, Sept. 2023
J. Lorenzo, A. Portone, P. Testoni, “Conceptual magnetic design for the IMCC Target Magnets (35MBYQ)” Fusion For Energy Internal Report, Nov. 2023, IDM_D_35MBYQ, v1.0

## Slide 12
THANK YOU

## Slide 13
Stress components of interest in the HTS tapes (de-bonding, degradation):
  Tensile stress across HTS tapes.
  Shear stress in HTS tapes.
The tapes are modelled as relatively stiff components (~100 GPa) due to the large amount of Hastelloy and copper.
The surrounding solder is modelled as a rather soft material (~10 GPa) due to the mix of Sn and Pb.
Parametric Analyses:
  Bonded/frictional stack.
  Number of stacks (3, 4, 6, 8).
  Width of stacks (3 mm, 4 mm, 6 mm).
SuperPower
HTS-Based Target Solenoids: Tapes Stresses

## Slide 14
Stack bonded to copper former.
Stack allowed to separate and slide in the copper former (μ = 0.2).
Tensile Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Shear Stress [Pa]
bonded stack
bonded stack
frictional contact
frictional contact
Contact Pressure [Pa]
~40 MPa
~30 MPa
Smaller tensile stress area with lower peak.
Lower shear stress in general.
HTS-Based Target Solenoids: Tapes Stresses

## Slide 15
Conductor features
  Diameter of central cooling channel = 8 mm.
  Cable diameter = 23.5 mm.
  Square steel jacket 39.5 mm x 39.5 mm (minimum thickness of 8 mm).
  1 mm thick turn insulation.
Cable features (parametric studies, 50 tapes/stack)
  Bonded/frictional stack-former contact.
  3/4/6/8 stacks of HTS tapes.
  3/4/6 mm wide HTS tapes.
HTS tape features (90 um thickness)
  44 um thick Hastelloy.
  20 um thick copper layers (x2).
  2 um thick silver layers (x2).
  1.6 um REBCO layer.
  0.4 um buffer layer.
Introduction: Conductor
Cooling Channel
Cable
Jacket
Turn Insulation
Void Filler
Copper Former
Steel Wrap
HTS Stack
Solder

## Slide 16
Introduction: Material Properties
 | Steel | Copper | Insulation | Filler | WP (smeared) | Solder | HTS Tape (smeared)
Ex [GPa] | 205 | 110 | 12 | 7 | 112 | 10 | 100
Ey [GPa] | 205 | 110 | 20 | 7 | 112 | 10 | 121
Ez [GPa] | 205 | 110 | 20 | 7 | 160 | 10 | 132
νxy [] | 0.29 | 0.33 | 0.33 | 0.3 | 0.25 | 0.33 | 0.25
νxz [] | 0.29 | 0.33 | 0.33 | 0.3 | 0.21 | 0.33 | 0.24
νyz [] | 0.29 | 0.33 | 0.17 | 0.3 | 0.21 | 0.33 | 0.30
Gxy [GPa] | 79 | 41 | 6 | 3 | 31 | 4 | 37
Gxz [GPa] | 79 | 41 | 6 | 3 | 42 | 4 | 46
Gyz [GPa] | 79 | 41 | 6 | 3 | 42 | 4 | 43
P. GAO, et al. Superconductor Science and Technology, 2020, vol. 33, no 4, p. 044015.
Properties of HTS tape obtained from smearing of isotropic properties of individual components at 77 K.

## Slide 17
Introduction: Loads
Coil | Rc [m] | Zc [m] | DR [m] | DZ [m] | NR | NZ | I [A] | It [MAt] | Fz [MN] | Fz [MN]
1 | 0.849 | -0.185 | 0.498 | 0.830 | 12 | 20 | 58905 | 14.137 | 251.2 | 251.2
2 | 0.870 | 0.665 | 0.540 | 0.830 | 13 | 20 | 60710 | 15.785 | 59.50 | 59.51
3 | 0.870 | 1.515 | 0.540 | 0.830 | 13 | 20 | 60392 | 15.702 | -101.0 | -101.0
4 | 0.808 | 2.365 | 0.415 | 0.830 | 10 | 20 | 51654 | 10.331 | -101.4 | -101.4
5 | 0.766 | 3.215 | 0.332 | 0.830 | 8 | 20 | 47469 | 7.595 | -58.48 | -58.48
6 | 0.704 | 4.065 | 0.208 | 0.830 | 5 | 20 | 46504 | 4.650 | -17.10 | -17.10
7 | 0.745 | 4.708 | 0.291 | 0.415 | 7 | 10 | 46293 | 3.240 | -16.60 | -16.60
8 | 0.704 | 5.423 | 0.208 | 0.415 | 5 | 10 | 53168 | 2.658 | -2.179 | -2.177
9 | 0.662 | 6.065 | 0.125 | 0.830 | 3 | 20 | 43280 | 2.597 | -5.691 | -5.69
10 | 0.662 | 6.915 | 0.125 | 0.830 | 3 | 20 | 42146 | 2.529 | -2.609 | -2.608
11 | 0.642 | 7.765 | 0.083 | 0.830 | 2 | 20 | 49452 | 1.978 | -1.687 | -1.686
12 | 0.642 | 8.615 | 0.083 | 0.830 | 2 | 20 | 44183 | 1.767 | -0.9150 | -0.9147
13 | 0.642 | 9.465 | 0.083 | 0.830 | 2 | 20 | 39567 | 1.583 | -0.7432 | -0.7428
14 | 0.642 | 10.315 | 0.083 | 0.830 | 2 | 20 | 32713 | 1.309 | -0.1610 | -0.1603
15 | 0.642 | 10.958 | 0.083 | 0.415 | 2 | 10 | 46717 | 0.934 | -0.8960 | -0.8958
16 | 0.642 | 11.673 | 0.083 | 0.415 | 2 | 10 | 45905 | 0.918 | 0.3742 | 0.3754
17 | 0.621 | 12.315 | 0.042 | 0.830 | 1 | 20 | 52310 | 1.046 | -0.3951 | -0.3941
18 | 0.621 | 13.165 | 0.042 | 0.830 | 1 | 20 | 56056 | 1.121 | -0.0839 | -0.08169
19 | 0.621 | 14.015 | 0.042 | 0.830 | 1 | 20 | 51602 | 1.032 | -0.0973 | -0.09354
20 | 0.621 | 14.865 | 0.042 | 0.830 | 1 | 20 | 51376 | 1.028 | -0.0427 | -0.03481
21 | 0.621 | 15.715 | 0.042 | 0.830 | 1 | 20 | 50471 | 1.009 | -0.0091 | 0.01137
22 | 0.621 | 16.565 | 0.042 | 0.830 | 1 | 20 | 52861 | 1.057 | -0.0188 | 0.06418
23 | 0.621 | 17.415 | 0.042 | 0.830 | 1 | 20 | 57438 | 1.149 | -0.9872 | -0.3138
No pre-compression needed to keep the coils together.
Gravity load is not considered.
Cool-down is not considered.
Only Lorentz forces applied.
No cyclic loading considered (fatigue).
Net Vertical Forces
(without chicane coils)
Net Vertical Forces
(with chicane coils)
Chart: Coil
| C1 | C2 | C3 | C4 | C5 | C6 | C7 | C8 | C9 | C10 | C11 | C12 | C13 | C14 | C15 | C16 | C17 | C18 | C19 | C20 | C21 | C22 | C23
w/ chicane | 251.2 | 59.51 | -101 | -101.4 | -58.48 | -17.1 | -16.6 | -2.177 | -5.69 | -2.608 | -1.686 | -0.9147 | -0.7428 | -0.1603 | -0.8958 | 0.3754 | -0.3941 | -0.08169 | -0.09354 | -0.03481 | 0.01137 | 0.06418 | -0.3138
w/o chicane | 251.2 | 59.51 | -101 | -101.4 | -58.48 | -17.1 | -16.6 | -2.178 | -5.691 | -2.608 | -1.687 | -0.9152 | -0.7434 | -0.1609 | -0.8964 | 0.3746 | -0.3954 | -0.08392 | -0.09731 | -0.04272 | -0.00908 | -0.01877 | -0.9872

## Slide 18
Analysis Strategy: Overview
2-D Axis. Global Electromagnetic Model
2-D Axis. Local Electromagnetic Model I
2-D Axis. Local Electromagnetic Model II
2-D Axis. Global Mechanical Model
2-D Axis. Local Mechanical Model I
2-D Axis. Local Mechanical Model II
3-D Homogenization Model
Nodal EM forces
Boundary conditions (Az)
Boundary conditions (Az)
Nodal EM forces
Nodal EM forces
Boundary conditions (ur, uz)
Boundary conditions (ur, uz)
Assessment Jacket and Turn Insulation
(ITER Magnet Structural Design Criteria)
Assessment HTS Tapes
(Tensile and shear stresses)
WP mechanical properties
(Ex, Ey, Ez, νxy, νxz, νyz, Gxy, Gxz, Gyz)
Fully parametric model automatized with ANSYS Parametric Design Language (APDL).
3-D Homogenization Model
Tape mechanical properties
(Ex, Ey, Ez, νxy, νxz, νyz, Gxy, Gxz, Gyz)
Magnetic Models
Mechanical Models

## Slide 19
Analysis Strategy: Global Models
Magnetic Field [T]
Displacement [m]
Homogenized WP.
Frictional contact between coils.
No pre-compression force applied.
Boundary Condition: uy = 0
Peak field in coils 2/3.
Smeared Properties
The global stiffness of the WP is modelled by means of a homogenized orthotropic material.
Nodal EM forces
Most loaded coil for detailed analysis
Global displacements

## Slide 20
Analysis Strategy: Local Models I
Magnetic Field [T] in Coil 2 cables
Tresca Stress [Pa] in Coil 2 jackets
Nodal EM forces
Frictional contact between cable and jacket
Fine distribution of magnetic field
Stresses in jackets and insulation

## Slide 21
a) Hoop Stress
b) Axial Stress [Pa]
Analysis Strategy: Local Models I

## Slide 22
Analysis Strategy: Local Models II
Magnetic Field [T] in tapes
Compressive/Tensile Stress [Pa] in tapes
Nodal EM forces
Shear Stress [Pa] in tapes

## Slide 23
Stresses in HTS Tapes
Stress components of interest in the HTS tapes (de-bonding, degradation):
  Tensile stress across HTS tapes.
  Shear stress in HTS tapes.
The tapes are modelled as relatively stiff components (~100 GPa) due to the large amount of hastelloy and copper.
The surrounding solder is modelled as a rather soft material (~10 GPa) due to the mix of Sn and Pb.
Parametric Analyses:
  Bonded/frictional stack.
  Number of stacks (3, 4, 6, 8).
  Width of stacks (3 mm, 4 mm, 6 mm).
SuperPower

## Slide 24
Bonded/Frictional Stack
Stack bonded to copper former.
Stack allowed to separate and slide in the copper former (μ = 0.2).
Tensile Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Shear Stress [Pa]
bonded stack
bonded stack
frictional contact
frictional contact
Contact Pressure [Pa]
~40 MPa
~30 MPa
Smaller tensile stress area with lower peak.
Lower shear stress in general.

## Slide 25
Stack Number (6 mm wide tape, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
~30 MPa
~30 MPa
~30 MPa
Larger tensile stress area.
81 mm2
108 mm2
162 mm2

## Slide 26
Stack Number (4 mm wide tape, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
~30 MPa
~30 MPa
~30 MPa
Larger tensile stress area.
72 mm2
108 mm2
144 mm2

## Slide 27
Stack Number (6 mm wide tape, frictional contact)
Shear Stress [Pa]
Contact Pressure [Pa]
Shear Stress [Pa]
Contact Pressure [Pa]
Shear Stress [Pa]
Contact Pressure[Pa]

## Slide 28
Stack Width (4 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Increased peak compressive stress.
Increased peak shear stress.
108 mm2
72 mm2
54 mm2

## Slide 29
Stack Width (6 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Increased peak compressive stress.
Increased peak shear stress.
162 mm2
108 mm2
81 mm2

## Slide 30
Tape Thickness (4 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
108 mm2
108 mm2
50 tapes
thickness = 90 um
75 tapes
thickness = 60 um

## Slide 31
Solder Stiffness (4 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
108 mm2
108 mm2
Esolder = 10 GPa
Esolder = 20 GPa
Larger tensile stress area.
Increased shear stress.
~30 MPa
~40 MPa

## Slide 32
Stack Number (6 mm wide tape, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]

## Slide 33
Structural Design Criteria & Assessment
ITER Magnet Structural Design Criteria:
  Part 1: Main Structural Components and Welds.
  Part 2: Magnet Windings (Radial Plates and Conductors) with High and Low Voltage Insulation and Epoxy Filler.
  Part 3: Bolts, Keys, Supports and Special Components.
  Part 4: Cryogenic Piping.
Jackets
Turn insulation
Only static stress limits are considered.
Relevance of fatigue stress to be discussed (cyclic loading?).

## Slide 34
Structural Design Criteria & Assessment: Stress Linearization
= membrane stress tensor (constant part).
= bending stress tensor (linear part).
Once membrane and bending stress tensors are known, von Mises/Tresca stresses can be computed as usual.
Von Mises/Tresca stresses do not vary linearly along the defined paths.
Source: ANSYS Theory Reference

## Slide 35
Structural Design Criteria & Assessment: Stress Classification
Primary Stress, P
  Stress developed by imposed loading.
  Necessary to satisfy laws of equilibrium.
  Not self-limiting.
  Result in failure/gross distortion if considerably exceeds yield strength.
  Thermal stress is not primary.
Secondary Stress, Q
  Stress developed by constrain of adjacent material or by self-constraint of the structure.
  Self-limiting.
  Thermal stress.
Rule of thumb:
  Thermal stresses are classified as secondary.
  Stresses induced by EM loads, inertial/gravity loads, pressure loads, etc., are classified as primary.

## Slide 36
Structural Design Criteria & Assessment: Metallic Components
ITER MSDC Part 2 for Metallic Components:
  Allowable stress:
  Primary membrane stress:
  Primary membrane + bending stress:
  Primary + secondary stress
depends on type of service conditions:

## Slide 37
Structural Design Criteria & Assessment: Metallic Components
ITER MSDC Part 2:
  Allowable stress:
  Primary membrane stress:
  Primary membrane + bending stress:
  Primary + secondary stress (not considered, no thermal load applied).
PATH

## Slide 38
Structural Design Criteria & Assessment: Metallic Components
Copper former is not intended to be a structural component in the cable but it reacts the magnetic load due to its relatively high stiffness (110 GPa vs. 205 GPa of steel).
The yield strength of copper is rather low compared to that of steel (factor ~3)), at least at room temperature (strength at cryogenic temperature needs to be investigated).
Frictional stacks
Frictional stacks
Bonded stacks

## Slide 39
Structural Design Criteria & Assessment: Non-Metallic Components
ITER MSDC Part 2 for High-Voltage Insulation:
  Allowable compressive stress normal to the reinforcing plane. The compressive static stress in the through-thickness direction of the insulating material is limited to 50% of the minimum ultimate compressive strength:
  Allowable tensile strain normal to reinforcing plane. No primary tensile strain is allowed in the direction normal to the adhesive bonds between metal and composite.
  Allowable shear stress. The allowable shear strength of an insulator depends on the applied compressive stress.
  Allowable strain in plane of reinforcing. The allowed tensile or compressive strain in the plane of the insulation material is in the range [-0.5%, 0.5%].

## Slide 40
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable compressive stress normal to the reinforcing plane.

## Slide 41
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable tensile strain normal to reinforcing plane.
Small spots in the corner regions show normal tensile strain likely due to the fact that bonded insulation layers are assumed, and no separation is allowed.

## Slide 42
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable shear stress.
A usage factor is defined as the ratio between element shear stress and allowable shear stress, which must be less than 1. Negative values correspond to tensile stresses that should be avoided, but these are likely due to the modelling of contact between adjacent insulating layers.

## Slide 43
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable strain in plane of reinforcing.

## Slide 44: COMPARE FIELD ON AXIS
Blue = US-MAP
Red = OPT. FIT

## Slide 45: Collider Choices
Hadron collisions: compound particles
  LHC collides 13.6 TeV protons
  Protons are mix of quarks, anti-quarks and gluons
  Very complex to extract physics
  But can reach high energies
Lepton collisions: elementary particles
  LEP reached 0.205 TeV with electron-positron collisions
  Clean events, easy to extract physics
  Lepton collisions  precision measurements
  Hard to reach high energies
e+e-

## Slide 46: Energy Limit
Electron-positron rings (multi-pass colliders) are limited by synchrotron radiation
Electron-positron linear colliders avoid synchrotron radiation, but are single pass
Typically cost proportional to energy and power proportional to luminosity,
Novel approach: the muon collider
Large mass suppresses synchrotron radiation => circular collider, multi-pass
Fundamental particle yields clean collisions => less beam energy than protons
But lifetime at rest only 2.2 μs (increases with energy)
Hence present energy frontier is probed by proton rings
N
S
N
S
accelerating cavities
magnets
The muon collider is part of the European Accelerator R&D Roadmap
e-: 0.511 MeV
m: 106 MeV
p+: 938 MeV

## Slide 47: Proton-driven Muon Collider Concept
Produce a low emittance muon beam…
… collide !
… accelerate muons…
Time
Beam intensity
100…200 ms
protons
muons
pions

## Slide 48: Target and capture solenoid – 1/4
Field on target 20 T, 150 mm
Beam power on target: 1…2 MW
Large stored energy o(2) GJ, mass o(300) tons, cost o(100) M
Superconducting (LTS) outsert
Rad-hard resistive insert

## Slide 49: Target and capture – 2/4
Reduce the mass (CAPEX) of the system, and increase operating temperature to improve cryogenic CoP (OPEX)
US-MAP 2010 design
LTS (14 T) + NC (6 T)
US-MAP 2011 design
LTS (14 T) + NC (6 T)
MuCol 2022 design
HTS (20 T, 20 K)
H.G. Kirk, PAC 2011

## Slide 50: Target and capture – 3/4
US-MAP
Proposal
EM = 2.9 GJ
Top = 4.2 K
Mcoils = 200 tons
Mshield = 300 tons
P = 12 MW
EM = 1 GJ
Top = 10…20 K
Mcoils = 110 tons
Mshield = 196 tons
P = 1MW
Remove resistive insert (10 MW)
Use HTS to achieve field of 20 T
Reduce shield thicknes, accepting higher heat load at 20 K
Field profile matches the requirements from beam optics

## Slide 51: Target and capture – 4/4
Operating current: 58 kA
Operating field: 20 T
Operating temperature: 20 K
SOLDERED HTS STACK
COPPER FORMER
COOLING CHANNEL
STAINLESS STEEL WRAP
STAINLESS STEEL JACKET
39.5
23.5
8
M. Takayasu et al., IEEE TAS, 21 (2011) 2340
Z. S. Hartwig et al., SUST, 33 (2020) 11LT01
HTS conductor design
MIT “VIPER” conductor
Looks much like an HTS magnet for fusion !!!

## Slide 52: Coil geometry
Coil | Rc (m) | Zc (m) | dR (m) | dZ (m) | Layers (-) | Pancakes (-) | Iconductor (A) | Turns (-) | Icoil (MA-turn) | Lpancake (m)
1 | 0.849 | -0.185 | 0.498 | 0.83 | 12 | 20 | 58905 | 240 | 14.14 | 64.0
2 | 0.87 | 0.665 | 0.54 | 0.83 | 13 | 20 | 60710 | 260 | 15.78 | 71.1
3 | 0.87 | 1.515 | 0.54 | 0.83 | 13 | 20 | 60392 | 260 | 15.70 | 71.1
4 | 0.808 | 2.365 | 0.415 | 0.83 | 10 | 20 | 51654 | 200 | 10.33 | 50.8
5 | 0.766 | 3.215 | 0.332 | 0.83 | 8 | 20 | 47469 | 160 | 7.60 | 38.5
6 | 0.704 | 4.065 | 0.208 | 0.83 | 5 | 20 | 46504 | 100 | 4.65 | 22.1
7 | 0.745 | 4.708 | 0.291 | 0.415 | 7 | 10 | 46293 | 70 | 3.24 | 32.8
8 | 0.704 | 5.423 | 0.208 | 0.415 | 5 | 10 | 53168 | 50 | 2.66 | 22.1
9 | 0.662 | 6.065 | 0.125 | 0.83 | 3 | 20 | 43280 | 60 | 2.60 | 12.5
10 | 0.662 | 6.915 | 0.125 | 0.83 | 3 | 20 | 42146 | 60 | 2.53 | 12.5
11 | 0.642 | 7.765 | 0.083 | 0.83 | 2 | 20 | 49452 | 40 | 1.98 | 8.1
12 | 0.642 | 8.615 | 0.083 | 0.83 | 2 | 20 | 44183 | 40 | 1.77 | 8.1
13 | 0.642 | 9.465 | 0.083 | 0.83 | 2 | 20 | 39567 | 40 | 1.58 | 8.1
14 | 0.642 | 10.315 | 0.083 | 0.83 | 2 | 20 | 32713 | 40 | 1.31 | 8.1
15 | 0.642 | 10.958 | 0.083 | 0.415 | 2 | 10 | 46717 | 20 | 0.93 | 8.1
16 | 0.642 | 11.673 | 0.083 | 0.415 | 2 | 10 | 45905 | 20 | 0.92 | 8.1
17 | 0.621 | 12.315 | 0.042 | 0.83 | 1 | 20 | 52310 | 20 | 1.05 | 3.9
18 | 0.621 | 13.165 | 0.042 | 0.83 | 1 | 20 | 56056 | 20 | 1.12 | 3.9
19 | 0.621 | 14.015 | 0.042 | 0.83 | 1 | 20 | 51602 | 20 | 1.03 | 3.9
20 | 0.621 | 14.865 | 0.042 | 0.83 | 1 | 20 | 51376 | 20 | 1.03 | 3.9
21 | 0.621 | 15.715 | 0.042 | 0.83 | 1 | 20 | 50471 | 20 | 1.01 | 3.9
22 | 0.621 | 16.565 | 0.042 | 0.83 | 1 | 20 | 52861 | 20 | 1.06 | 3.9
23 | 0.621 | 17.415 | 0.042 | 0.83 | 1 | 20 | 57438 | 20 | 1.15 | 3.9
Focus on coil C02 (highest current, highest field, higest energy)

## Slide 53: Conductor design
HTS tape thickness | (mm) | 62
HTS tapes | (-) | 80
HTS stack width | (mm) | 6
HTS stack thickness | (mm) | 5
HTS stack width | (mm) | 6
HTS tapes | (-) | 80
Number of HTS stacks | (-) | 4
Copper diameter | (mm) | 23
Hole diameter | (mm) | 8
Wetted perimeter | (mm) | 25
Wrap thickness | (mm) | 0.25
Jacket outer dimension | (mm) | 39.5
ASC | (mm2) | 4.2
ASubstrate | (mm2) | 77
ACu | (mm2) | 361
AHelium | (mm2) | 50
A Wrap | (mm2) | 18
AJacket | (mm2) | 1127
ACable Space | (mm2) | 511
AConductor | (mm2) | 1560
930 A/mm2
Iop = 61 kA
Bop = 20 T
Top = 20 K
Tcs = 29.7 K

## Slide 54: Heat load from recirculation
Pressure drop
Heat removed
State equation

## Slide 55: Parametric study
A = 5 mm2
Dh = 8 mm
L = 150 m
= 150 W
DT = 3K
hPump = 80%

## Slide 56: Optimal cooling conditions
Compared to typical conditions at 4.5 K, operation at 20 K implies
  High pressure, o(20) bar
  Large temperature increase, o(3) K
DT = 1 K
DT = 1 K
DT = 3 K
DT = 3 K
DT = 5 K
DT = 5 K
150 W
20 K inlet
150 W
20 bar outlet

## Slide 57: Cooling
Proton beam
D. Calzolari and A. Lechner, CERN
Double pancake length (m)
13 layers
13 layers
Innermost turns
total heat
150 W
2 W/m peak
NOTE: time stucture ignored
Double pancake length (m)
Low field
Low field
High field
3 K
target
shield
in
out
in
out
in
out
in
out
in
out
in
out
in
out
in
out
Total heat in the coil 4.1 kW
coil

## Slide 58: Nominal cooling condition
A flow dm/dt of approximately 8 g/s is required to remove a nuclear heat load of 150 W with a temperature increase DT of 3 K
With this flow the pumping loss is about 20 W (considering an adiabatic efficiency hpump of 80 %)
This is about 13 % of the nuclear heat load, and is an acceptable overhead
It would be possible to remove higher heat loads under the same temperature increase, but the pumping loss grows rapidly, approximately like (dm/dt)3
8.66 g/s
3 K
17.8 W

## Slide 59: Margin and stability – 1/3
Values of stability margin are (as expected) very high ! It is very unlikely that the cable will quench because of transient heat inputs
The stability margin is well above the enthalpy reserve of the cable, also including helium. The reason is that the transient is slow, and there is time to conduct and convect heat away even for very large INZ lengths
This effect is even more marked at low field (high temperature margin)
INZ = 0.1 m
INZ = 1 m
Operating current 61 kA
Operating temperature 20 K
Cable+He enthalpy
Cable enthalpy

## Slide 60: Margin and stability – 2/3
The temperature margin DT is about 10 K at nominal conditions of current, field and temperature
  Iop = 61 kA
  Bop = 20 T
  Top = 20 K
In the low field regions of the coil (e.g. 4 T) the temperature margin is above 40 K
The large stability in the low field region may make protection difficult ?
Operating current 61 kA
Operating temperature 20 K
20 T
16 T
12 T
8 T
4 T
Cable+He enthalpy
Cable enthalpy

## Slide 61: Margin and stability – 3/3
Operating at higher temperature than 20 K (e.g. 25 K) may still be an option, the energy margin is substantial
Operating at lower temperature than 20 K (e.g. 15 K) does not bring a substantial benefit in energy margin
  Recall that the heat capacity drops dramatically at low temperature
Operating current 61 kA
Operating field 20 T
Cable+He enthalpy
Cable enthalpy

## Slide 62: Detection and protection – 1/3
Coil Module 2 (high field and current)
Single coil stored energy: 165 MJ
Coulped stored energy: 299.7 MJ
Dump voltage: 5 kV
Detect at 100 mV
2.2 s
0.15 m/s
Two sided
INZ in the center of the double pancake
10 cm length quenched
Exponential dump following trigger
trigger
130 K

## Slide 63: Detection and protection – 2/3
Wilson’s Gamma function
Detection with “reasonable” voltage values appears to work !

## Slide 64: Detection and protection – 3/3
Study the detection and dump for quenches in the low field region or at low current/field
  The low field region at nomnal current seems to be most dangerous
  Low current/low field (e.g. during ramp) implies long detection times, but this appears compatible with modest hot-spot limits
Iop (kA) | Bop (T) | tDetection (s) | Tmax (K)
61 | 20 | 2.2 | 130
61 | 4 | 2.8 | 172
30 | 9.84 | 14.8 | 140

## Slide 65: HTS cable mechanics
63 MPa
45 MPa
stensile //c
t //ab
40 MPa
< 10 MPa
bonded
not bonded
stensile //c
t //ab
B
I
F
May this be the reason why soldered and twisted high field and high current cables are also subject to degradation ?

## Slide 66: Opportunities and perspective
We are looking for a solution to the design of the target and capture channel of the Muon Collider, which needs a peak field of 20 T on axis, based on an HTS force-flow cooled cable operating at 20 K
  Lower footprint, mass, stored energy and cost than a LTS/NC hybrid
  Better energy efficiency than a 4.5 K system
Though there is much work to do, the design selected seems not too far from being feasible !
This is also interesting because of implications for
    Compact fusion machines
    Hybrid UHF magnets for science
Notes: The reason for this talk is that we have received a strong recommendation from the group that proposes priority for particle physics in Europe. The recommendation, received in March 2020 and approved at the Council session of June 2020, contains a very strong statement on the need to ramp-up R&D effort on high-field accelerator magnets

## Slide 67: Proton-driven Muon Collider Concept
Produce a low emittance muon beam…
… collide !
… accelerate muons…
Steady state
Steady state
Pulsed
Steady state
Pulsed
Time
Beam intensity
100…200 ms
protons
muons
pions

## Slide 68: The need for high field
Beam energy
Dipole field
Bending radius
This is the reason for the steady call for higher fields in accelerator magnets
Upper limit of LTS (Nb3Sn)
HTS is the only path beyond 16 T

## Slide 69: The need for energy
CERN uses today 1.3 TWh per year of operation, with peak power consumption of 200 MW (running accelerators and experiments), dropping to 80 MW in winter (technical stop period)
Electric power is drawn directly from the French 400 kV distribution, and presently supplied under agreed conditions and cost
Supply cost, chain and risk are obvious concerns for the present and future of the laboratory

## Slide 70: Energy efficient cryogenics
The 60…80 K range would be a dream…
LHC
(FCC)
ESS
Need efficient cryo-plant and heat removal scheme in the range of 10…20 K (see work at ESS)
This could be the best range of operating temperature of a future HEP collider
RHIC
Tevatron
HERA
LHC
HTS may be the only path towards a future collider
Nb-Ti
8T
5T
Nb3Sn
16T
12…14T
HTS
40…60T
20…40T
a few T
1.9
4.2
77
Credits to P. De Sousa and R. Van Weelderen, CERN
W/Q = (Th-Tc)/Tc

## Slide 71
Future helium supply is limited and entails a substantial economical and availability risk
Courtesy of F. Ferrand, CERN

## Slide 72: The need for economics
A large component in the magnet cost is the amount of superconductor (coil cross section)
High-field superconductors are (significantly) more expensive than good-old Nb-Ti
Need to work in two directions:
  Reduce the coil cross section (increase J !)
  Reduce unit conductor cost
HTS may offer both
j
w
Rin

## Slide 73: Conductor cost
Grateful thanks to fusion !
Impressive cost reduction in HTS !
Based on CERN orders and requests for quotations 2010-2022
Normalised costs are not aligned to currency, nor corrected for inflation