## Slide 1
Superconducting Splices
for the Rope 6+1
Project HITRIplus – WP8 meeting 22
R.U. Valente, E. De Matteis, D. Pedrini, G. Crespi
INFN LASA
Superconducting Magnet Group
Milan Italy

## Slide 2
Outline
NbTi rope characteristics
Experimental test
Data analysis
Results

## Slide 3
HITRIplus Rope
The rope consists in 6 NbTi strands twisted around 1 Cu strand
The insulation is a double braid in polyester
Not insulated rope | 
Strand number | 6 (NbTi) + 1 (Cu)
Diameter [mm] | 2.46
Cu/non-Cu | 1.75
Twist pitch [mm] | 40
Copper
NbTi
Twist pitch 40 mm

## Slide 4
Experimental Test - Motivation
Measurement of the splice resistance as a function of splice length.
Measurement of the splice resistance with and without soldering (Sn96.5Ag3Cu0.5).
  Super-stabilized splice (crimping + soldering)
    Pro: thermal and mechanical stability
    Cons: low resistance means higher loop currents during current ramps
  Not stabilized splice (crimping)
    Pro: lower loop currents
    Cons: lower thermal stability
Comparison between 'prayer hands' and 'shaking hands' junctions.
Shacking hands
Prayer hands

## Slide 5
Experimental Test - Setup
The measurement is performed in the MAGIX cryostat (480 mm diameter):
Temperature 4.2 K (LHe)
Max current 500 A
No background field
We are quite limited in current  we lost in sensitivity

## Slide 6
Experimental Test - Scheme
Splice ID | Length [mm] | Type | Soldering (Sn96.5Ag3Cu0.5)
PH30S | 30 | Prayer Hands | Yes
PH40S | 40 | Prayer Hands | Yes
PH60S | 60 | Prayer Hands | Yes
PH40 | 40 | Prayer Hands | No
SH40S | 40 | Shaking Hands | Yes
SH60S | 60 | Shaking Hands | Yes
D. Pedrini

## Slide 7
Experimental Test – Splice Detail
Vtap
Crimp
Crimp
Vtap
Prayer hands
Shacking hands

## Slide 8
Experimental Test – Measurement
We measure the voltage drop of the splices injecting the current at step or with a ramp rate (5 A/s or 10 A/s)
We use different methods to identify the inductive voltages and recover a stable signal before the bus-bar overheating
Inductive peak
Resistive plateau

## Slide 9
Data Analysis
The resistance is obtained from the measurement with a weighted linear regression
The error of the measured resistance is the Standard Error computed on the slope coefficient of the fit
95%
Data with low weight

## Slide 10
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | 3,4E-09 | 9,9E-10
10 A/s | 3,1E-09 | 1,1E-10
5 A/s | 2,8E-09 | 3,5E-11
Data Analysis – Example PH40s
step
Ramp-rate 10 A/s
Ramp-rate 5 A/s
The resistance is computed as the average
The error is the root of the sum squared errors

## Slide 11
Results
Resistance vs Length
SpliceID | Splice Length [mm] | Resistance [nΩ] | Standard Error[nΩ] | Type | Soldering (Sn96.5Ag3Cu0.5)
PH30S | 30 | 4,48 | 0,33 | Prayer Hands | Yes
PH40S | 40 | 3,10 | 0,99 | Prayer Hands | Yes
PH60S | 60 | 1,57 | 0,43 | Prayer Hands | Yes
PH40 | 40 | 440,63 | 0,81 | Prayer Hands | No
SH40S | 40 | -0,16 | 0,93 | Shaking Hands | Yes
SH60S | 60 | -0,45 | 1,77 | Shaking Hands | Yes
The resistance of the ‘prayer hands’ splices is well-fitted by the Wilson model
M. N. Wilson, Superconducting Magnets. Oxford, U.K.: Clarendon, 1983, p. 314.

## Slide 12
Results
Soldering contribution
SpliceID | Splice Length [mm] | Resistance [nΩ] | Standard Error[nΩ] | Type | Soldering (Sn96.5Ag3Cu0.5)
PH30S | 30 | 4,48 | 0,33 | Prayer Hands | Yes
PH40S | 40 | 3,10 | 0,99 | Prayer Hands | Yes
PH60S | 60 | 1,57 | 0,43 | Prayer Hands | Yes
PH40 | 40 | 440,63 | 0,81 | Prayer Hands | No
SH40S | 40 | -0,16 | 0,93 | Shaking Hands | Yes
SH60S | 60 | -0,45 | 1,77 | Shaking Hands | Yes
The soldering is crucial to have resistance of the order of nano ohms
(verified only for prayer hands junctions, but general result)

## Slide 13
Results
Prayer vs. Shaking hands
SpliceID | Splice Length [mm] | Resistance [nΩ] | Standard Error[nΩ] | Type | Soldering (Sn96.5Ag3Cu0.5)
PH30S | 30 | 4,48 | 0,33 | Prayer Hands | Yes
PH40S | 40 | 3,10 | 0,99 | Prayer Hands | Yes
PH60S | 60 | 1,57 | 0,43 | Prayer Hands | Yes
PH40 | 40 | 440,63 | 0,81 | Prayer Hands | No
SH40S | 40 | -0,16 | 0,93 | Shaking Hands | Yes
SH60S | 60 | -0,45 | 1,77 | Shaking Hands | Yes
The ‘shaking hands’ splice resistance is compatible with zero (anomalous), and the motivation is under investigation.
We are studying a dedicated setup to measure a single shaking hands splice at nominal current (1500 A) to have better resolution.

## Slide 14
Conclusions
The experimental setup allowed us to perform satisfactory measurements. To improve the current threshold and the voltage sensitivity
The results show the rope splices made with crimping+soldering can be of few nano ohms  low power dissipation at operation
We found a scaling law for the splice length
There is an anomaly in shaking hands measurements, maybe due to the apparatus

## Slide 15
Backup slides summary
Data analysis of all the measurements
Critical current measurements recap
Wilson’s model

## Slide 16
Results – Prayer Hands 30 mm Soldered
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | 4,2E-09 | 1,4E-10
10 A/s | 4,8E-09 | 3,0E-10

## Slide 17
Results – Prayer Hands 40 mm Soldered
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | 3,4E-09 | 9,9E-10
10 A/s | 3,1E-09 | 1,1E-10
5 A/s | 2,8E-09 | 3,5E-11

## Slide 18
Results – Prayer Hands 60 mm Soldered
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | 1,7E-09 | 4,0E-10
10 A/s | 1,4E-09 | 1,6E-10

## Slide 19
Results – Prayer Hands 40 mm
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | 4,4E-07 | 8,1E-10

## Slide 20
Results – Shacking Hands 40 mm Soldered
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | 2,9E-10 | 9,2E-10
10 A/s | -7,2E-10 | 9,7E-11
5 A/s | -5,2E-11 | 0,0E+00

## Slide 21
Results – Shacking Hands 60 mm Soldered
Ramp rate | Resistance [Ω] | Standard Error [Ω]
step | -4,9E-10 | 1,8E-09
10 A/s | -4,1E-10 | 9,3E-11

## Slide 22
Critical Current Density - Rope
The Ic of the 6+1 rope is compatible with the Ic of 6 wires
High repeatability
Ic10 Rope 6+1 [A] |  |  |  | 
B [T] | Virgin x 6 | 1° rope | 2° rope | Discrepancy between ropes
9 | 477 | 499 | 498 | 0.24%
8.4 |  |  | 800 | 
8.2 |  |  | 998 | 
8 | 1088 | 1136 | 1132 | 0.35%
7.8 |  |  | 1271 | 
7.5 |  | 1482 | 1477 | 0.34%
7.4 |  |  | 1549 | 
7 | 1780 | 1834 |  | 
6.5 |  | 2181 |  | 
Wires from the same batch
1° rope and 2° rope are different lengths mounted on different sample holders
The data are already temperature-corrected
No self-field correction
The Bottura fit is used to fit the critical current data of the Discorap 3° generation

## Slide 23
Rope Splice Resistance – Wilson’s Model
The rope is assumed to be an equivalent cylinder in the center of which the nominal current (1500 A) flows
From M. Wilson, Superconducting Magnets, paragraph 13.1.3
Rope
Soldering
2b
2a
L

## Slide 24
Rope Splice Resistance – Wilson’s Model
The typical resistivity of the soldering (40% lead, 60% tin) is at cold
The typical value for f is 0.1
Therefore the splice resistance vs splice length is
For example: if L = 40 mm (1 rope twist pitch), Rj = 15 nΩ
Chart: f = b/a