## Slide 1: PUR Jack Taskforce Meeting #2 27/09/2023
P. Bestmann

## Slide 2: Agenda
Minutes approval
  The minutes will be send out by mail to the taskforce members for comments
  After approval, attached to the INDICO page and send to the distribution list
  Any comments or remarks for the minutes of the Meeting No. 2?
Latest News
Jack Test Stand Presentation
PU chemical compatibility test plans
Chemical Analysis

## Slide 3: Updated list of Members
E-group: SPS-Jack-Taskforce@cern.ch
Distribution List: SPS-Jack-Taskforce-Distribution@cern.ch
Zoom Room:PU Jack Taskforce
https://cern.zoom.us/j/66439161311?pwd=VDZXcDNhL3UySW5NVHpJVzgyYUJnZz09
Scientific Secretary: Philip Schwarz
Members | Alternates | Group
Philip Schwarz | Jeremie Bauche | TE-MSC
Roland Piccin | Sebastien Clement | TE-MSC
Patrick Bestmann | J-F. Fuchs | BE-GM
Michel Noir | Mateusz Sosin | BE-GM
Miguel Lino Diogo Dos Santos | Sylvain Girod | BE-EA
Stefano Sgobba | Mickael Denis Crouvizier | EN-MME
Colette Charvet | Benoit Teissandier | TE-VSC

## Slide 4: Latest news
Taskfore presented to LMC last wednesday
Storage conditions for Pads
  In closed box with Logger for Temp. & Rel. Humidity
  With Silicagel to keep humidity <30%
Mechanical Tests
  Comparable results apart from yellow pads
Mechanical Dimensions
  75ShA with 20% NonConformities on height >0.5mm
  90ShA with 40% NonConformities on height >0.5mm
  Problems with air inclusions and unsuficciant scraping

## Slide 5: Ongoing actions
  Mechanical Models ongoing with MME by Luca Piacentini & Federico Carra
  Discussions with INSA concerning new materials
  Naming defined for Tracability
    Using CERN general Scheme
        H (Handling & Supports)
        HJPU (Jack Polyurethan)
          HJPUH (Jack Polyurethan Heavy)
          HJPUL (Jack Polyurethan Light)
          HJPUHP (Jack Polyurethan Heavy Pad (90ShA))
          HJPULP (Jack Polyurethan Light Pad (75ShA))
    Creation of Assets and custom fields in INFOR EAM
  Full Property matrix for Samples in preparation