## Slide 1: HL-LHC MCBRD CCT Magnets: Review and Latest Progress in China
Qingjin XU
IHEP-CAS
For the CCT Magnet Team
20 Sep 2023

## Slide 2
LHC 2008-2022
HL-LHC 2026-2035
MCBRD: the HL-LHC D2 orbit correctors, 12+1 units, providing a 5 Tm integrated field in two apertures, vertical in one and horizontal in the other.
E. Todesco

## Slide 3
Items | Values
CCT skew angle | 30°
No. of turns per layer | 365
Slot size in former (mm) | 2×5
Spacing per turn | 5.222
Inside/Outside diameter of the former (mm) | Inner former:105.35/119.35 Inner former:120.80/134.85
Inside diameter of the groove/slot(mm) | 1st layer: 109.15/119.15 2nd layer: 124.65/134.65
Reference radius (mm) | 35
Diameter of aperture (mm) | 105
Current (A) | 395
Ø 614 mm
Aperture
Cooling hole
Hole for tie rod
Hole for fixing pin
Yoke alignment
CCT Coils
Items | Values
Diameter of yoke (mm) | 614
Thickness of yoke lamination (mm) | 5.8
Diameter of aperture (mm) | 167
Position of aperture (mm) | 94.19
Yoke key slot(mm) | 8(3.01) ×6
Diameter of cooling hole (mm) | 110
Position of cooling hole (mm) | 205
Main design parameters of the magnet

## Slide 4: Progress of series production
 | Coil name | Winding method | Location | Coil stand-alone performance (4.2 K) | Magnet performance at 4.2 K
Magnet 1 | MCBRD_CB01 | Wet wind | CERN | 530 A | Both apertures reached ultimate current 422 A, and passed 4-hour stability test
 | MCBRD_CB03 | Direct wind |  | 410 A (training stopped due to the availability of the test station) | 
 | MCBRD_CB02 | Direct wind | CERN | Failed to reach the design current | 
Magnet 2 | MCBRD_CB04 | Wet wind | CERN | 422 A(training stopped due to the availability of the test station) | Both apertures reached ultimate current 422 A, and passed 4*1 hour stability test
 | MCBRD_CB06 | Wet wind |  | 530 A | 
Magnet 3 | MCBRD_CB09 | Direct wind with new channel size | Shipped to CERN | 530 A | Both apertures reached ultimate current 422 A, and passed stability test
 | MCBRD_CB12 | Direct wind with new channel size |  | 526 A (25 quenches) | 
Magnet 4 | MCBRD_CB13 | Direct wind with new channel size | IMP | 530 A (20+33 quenches) | -
 | MCBRD_CB14 | Direct wind with new channel size | BAMA | 530 A (30+34 quenches), put in quarantine | -
 | MCBRD_CB17 | Direct wind with new channel size | IMP | 524 A (47 quenches) | -
MCBRD_CB18-19 |  | Direct wind with new channel size | IHEP | Waiting for stand-alone test | -
MCBRD_CB20 |  | Direct wind with new channel size | BAMA | Under fabricaiton | 
MCBRD_CB10, 11, 15, 16 |  | Shipped to CERN for fabrication |  |  | 

## Slide 5
Stand-alone training of the CCT coils

## Slide 6
Stand-alone training of CB17
Chart: Training history of CB017
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48
Current | 336.06 | 370.8 | 387.89 | 414 | 417.8 | 414.23 | 421.67 | 433.2 | 442.95 | 441.08 | 443.37 | 445.57 | 451.48 | 458.02 | 456.7 | 474.03 | 458.54 | 470.85 | 463.62 | 475.55 | 457.66 | 479.59 | 475.5 | 494.49 | 481.18 | 490 | 486.8 | 494.94 | 499.99 | 473.49 | 506.7 | 504.71 | 512.32 | 512.78 | 503.9 | 518.13 | 513.04 | 518.61 | 489.42 | 513.04 | 518.07 | 512.15 | 524.03 | 494.35 | 515.3 | 520.61 | 523.28 | 514.71
524A

## Slide 7
Manufacture of CB14

## Slide 8
Manufacture of CB14

## Slide 9
Stand-alone test of CB14 at IHEP

## Slide 10
Stand-alone test of CB14
Detraining
Changes:
Changes of the operators.
The inlet pipeline between mix tank and impregnation furnace (exposed in the air ~10℃) didn’t use any thermal insulation.
It takes a longer time (6~7h) of injection compared with CB09 ~ CB13 (3~4h).

## Slide 11
Corrective action of the VPI station
Inlet pipeline
Heating belt
T controller for the inletpipeline:52-58
Thermal insulation
Ultrasonic flow meter
60.1 - 58.0 - 58.6 - 58.5
T controller for the mold

## Slide 12
Qualification of the VPI system
Thermal insulation for the inlet pipeline
We use a 0.5m quadrupole CCT magnet as a qualification of the VPI system after applying the corrective actions.
This magnet will be tested this week.

## Slide 13
Training history of MCBRD03 (1st test)
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.

## Slide 14
Training history of MCBRD03 (2nd test)
Nominal current : 394 A
Ultimate current : 422 A
Nominal current : -394 A
Ultimate current : -422 A
Both Apertures reached the nominal current without any quenches after thermal cycle.
Training history and quench location of the 2nd test
4.1 K

## Slide 15
Integral Field and Transfer Function
Stair steps & magnet filed measurement of Aperture 2 (MCBRD_CB09)
Field Quality of MCBRD03

## Slide 16
Field Quality of MCBRD03
Multipoles (individual powering)

## Slide 17
Field Quality of MCBRD03
Crosstalk- Multipoles (combined powering)
Crosstalk-transfer function (combined powering)

## Slide 18
Chart: The training history of MCBRD04
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36
Aperture 1_quench | 345 | 340 | 367 | 387 | 392 | 394 | 391 | 391 | 394 | 406 | 412 | 412 | 413 | 415 | 418 | 421 | 404 | 416 | 404 | 420 | 423 | -394 | -423
Aperture 2_quench | 380 | 394 | 404 | 380 | 404 | 405 | 410 | 418 | 409 | 395 | 422 | 423 | -394 | -423
AP1(CB17，47 quenches 524A) reached ±422A after 15 quenches.
AP2(CB13, 53 quenches 530A) reached ±422A with 10 quenches.

## Slide 19
Performance of SCQ-CCT coils
SCQ-1
Well impregnated magnet SCQ-1 experienced long training
With the modified channel size, the training performance of SCQ-2 significantly improved.

## Slide 20
4 sets of series CCT magnets have been fabricated. All of them reached the ultimate current at 4 K. The 5th magnet is under fabrication
The 4th magnet to be delivered in late Oct or early Nov. The 5th magnet to be assembled in Nov, tested and delivered in late Dec 2023 or early Jan 2024
Production rate for the rest of series magnets: every 3 month per magnet
Components for 2 CCT magnets have been shipped to CERN from IHEP, to verify the performance with components from China and CERN fabrication process.
Summary

## Slide 21
Thanks for your attention