## Slide 1: Field model for MCBXF magnets
A. Chmielińska
P. Rogacki
L. Fiscarelli
WP3 meeting 08.11.2023

## Slide 2: MCBXFB / A
Parameter | Value (B / A)
Aperture (mm) | 150
Magnetic length (m) | 1.2 / 2.2
Int. field (Tm) | 2.5 / 4.5
Current inner (A) | 1740 / 1593
Current outer (A) | 1430 / 1340
  Inner coils produce a vertical field (main field B1, normal).
  Outer coils provide horizontal field (main field A1, skew).

## Slide 3: TF from magnetic measurements
2.4 %
2.2 %

## Slide 4: b3 and a3 from magnetic measurements
bn and an normalized to 2.5 Tm
(nominal field)

## Slide 5: Coupling of saturation
The MCBXF magnets show a saturation that depends on the field level of both planes (coupling).
The coupling impacts the field up to:
  2.2 % for the B1, 28 units for the b3
  1.2 % for the A1, 12 units for the a3
A model able to predict such effect is required.

## Slide 6: FiDeL field model - static components
FiDeL website, https://lhc-div-mms.web.cern.ch/tests/MAG/Fidel/
Geometric
Saturation where
DC magnetization and residual magnetization are not considered

## Slide 7: New model for the saturation of MCBXF
where
A multiplication factor G, function of the two currents, is added to modulates the saturation effect.

## Slide 8: The coupling factor “G(I1,I2)”
The saturation parameters and are fitted for the “intermediate cycle” (main diagonal) by setting
Keeping the same parameters and , the values of are found at different angles.
The values of at different angles are fitted by using the equation:

## Slide 9: The coupling factor “G(I1,I2)”
If one wants to keep the same definition for the angle
then must have a different definition depending on the field component (order, normal or skew)
In addition, a ∆ (~0.001) is added to avoid that the saturation goes to ∞ when the current of the planes is zero.

## Slide 10: Prediction of B1

## Slide 11: Prediction of A1

## Slide 12: Evaluation of the model error
The new model has been already evaluated on individual magnets
  https://indico.cern.ch/event/1192527/
  https://indico.cern.ch/event/1296834/
At present we have measured
  4 MCBXFB
  1 MCBXFA
We can check if one set of parameters can be used for all magnets of the same type
  First comparison
    Same saturation parameters for all magnets
    Magnet-specific versus family-average geometric component
 | MCBXFB | MCBXFA
Multipole | Error [units] | Error [units]
b1 | ±30 | ±15
a1 | ±28 | ±17
b3 | ±4 | ±3
a3 | ±4 | ±3

## Slide 13: Fit of B1 and A1
B1 |  | 
Component | Parameter | Average value
Geometric | γ | 1.4648 E-3
Saturation | 𝜎 | 0.0485 E-3
Saturation | I0 | 1445
Saturation | S | 4.7
 | a | 0.728
 | b | 0.091
A1 |  | 
Component | Parameter | Average value
Geometric | γ | 1.8052 E-3
Saturation | 𝜎 | 0.0665 E-3
Saturation | I0 | 1200
Saturation | S | 3.9
 | a | 0.368
 | b | 0.540
Multipole | MCBXF01 | MCBXF02b | MCBXF03 | MCBXFBP2c | AVERAGE
B1 | 1.4647 E-3 | 1.4660 E-3 | 1.4642 E-3 | 1.4644 E-3 | 1.4648 E-3
A1 | 1.8030 E-3 | 1.8037 E-3 | 1.8008 E-3 | 1.8133 E-3 | 1.8052 E-3
Magnet-specific geometric component γ
Family-average parameters

## Slide 14: Fit of B3 and A3
B3 |  | 
Component | Parameter | Average value
Geometric | γ | -1.2 E-6
Saturation | 𝜎 | -4.5 E-6
Saturation | I0 | 1445
Saturation | S | 4.7
 | a | 0.737
 | b | 0.089
A3 |  | 
Component | Parameter | Average value
Geometric | γ | 1.8 E-6
Saturation | 𝜎 | 5.2 E-6
Saturation | I0 | 1023
Saturation | S | 3.7
 | a | 0.430
 | b | 0.380
Multipole | MCBXF01 | MCBXF02b | MCBXF03 | MCBXFBP2c | AVERAGE
B3 | -1.5 E-6 | -1.0 E-6 | -1.1 E-6 | -1.1 E-6 | -1.2 E-6
A3 | 1.6 E-6 | 1.6 E-6 | 1.9 E-6 | 2.1 E-6 | 1.8 E-6
Magnet-specific geometric component γ
Family-average parameters

## Slide 15: Modeling errors
Multipole | MCBXF01 |  | MCBXF02b |  | MCBXF03 |  | MCBXFBP2c | 
b1 | 27 | 27 | 29 | 37 | 30 | 33 | 28 | 29
a1 | 23 | 36 | 15 | 24 | 15 | 40 | 27 | 70*
b3 | 2.9 | 4.9 | 3 | 3.8 | 2.6 | 2.6 | 2.6 | 4.0
a3 | 3.0 | 3.0 | 1.9 | 2.5 | 2.4 | 3.0 | 2.7 | 4.4
Max normalized errors for |I| > 500A (units normalized to 2.5 Tm)
Magnet-specific geometric component / Family-average geometric component
* MCBXFBP2c has a different coil length

## Slide 16: Conclusions
The MCBXF magnets show a non-negligible coupling of the two planes that affects the saturation.
This effect can be modelled by using a modified “FiDeL” saturation model.
The model works for both MCBXFB and MCBXFA magnet types.
By analysing the measurements taken so far on 3 MCBXFB series magnets, we see that:
  Family-average parameters can be used for both geometric and saturation components;
  The residual errors are:
    <40 units for b1/a1;
    <5 units for b3/a3.
Discussion on-going on how to use the model for beam simulations and operations.

## Slide 17: Annex

## Slide 18: B1 with average geometric component

## Slide 19: B1 with magnet-specific geometric component

## Slide 20: A1 with average geometric component

## Slide 21: A1 with average geometric component
Based only on series magnets

## Slide 22: A1 with magnet-specific geometric component

## Slide 23: B3 with average geometric component

## Slide 24: B3 with magnet-specific geometric component

## Slide 25: A3 with average geometric component

## Slide 26: A3 with magnet-specific geometric component