## Slide 1: Field quality of MBXF2 / Power test results of MBXF5 in the 1st TC
Kento Suzuki
WP3meeting 2023.11.08

## Slide 2: Japanese Contribution to HL-LHC: D1 magnets
Beam separation dipole (D1) by KEK
  Design study of D1 for HL-LHC within the framework of the CERN-KEK collaboration since 2011.
  150 mm single aperture, 35 Tm (5.6 T x 6.3 m), Nb-Ti technology.
  Development 2-m long model magnets (3 units) at KEK
Deliverables for HL-LHC
  1 full-scale prototype cold mass (LMBXFP)
  6 series cold masses (LMBXF1-6)
7 units x 7-m long cold masses

## Slide 3: Brief review of production status
MBXF5
  Under the power test at KEK (This talk)
MBXF1
  Cold mass assembly is ongoing at Hitachi
  Final reception test (SSW) at the KEK is planned in Mar.-Apr. 2024
MBXF2
  Warm magnetic measurement of Yoked magnet was completed (This talk)
  Arrival at KEK for the power test is foreseen in Feb. 2024
MBXF3
  Coil winding is ongoing

## Slide 4: Contents of the talk
MBXF2:
  Magnetic measurement at the Hitachi premise (5th - 6th Oct)
MBXF5:
  The power test results from the 1st thermal cycle (9th Oct-2nd Nov.)

## Slide 5: Magnetic measurement of MBXF2
EDMS:1966491

## Slide 6: MM after yoking, at Hitachi
NOTE: This was taken during
the prototype measurement
Radial coil (L=80)
Encoder disk
Place: The Hitachi Rinkai Factory
Yoked magnet

## Slide 7: Measurement / data coverage
Measured b1 profile is fitted to the 3D calculation “OPERA”
Probe coverage : Zmagnet= 1940 – 3620 mm, where Zmagnet=0 corresponds to the longitudinal magnet center
Field quality is evaluated by averaging the data over the straight section (z=1940-2260 mm)
LE
RE
Used for
field quality evaluation
Coverage by portable system
End section (LE)
SS
Lamination yoke
Rotating coil

## Slide 8: Example) Measured field profile of MBXF2
→LE
→LE
Warm, Yoked magnet

## Slide 9: SS-averaged field quality of MBXF2 – comparison with calc.

## Slide 10: Summary of the field quality (portable) so far
Warm, Yoked mag. Hitachi premise
Warm, Yoked mag. Hitachi premise
＊) MBXFP’s cross-section design differs from the series
For the series magnet, variation in b3 and a2 is ~3 units
＊
Series
Prototype

## Slide 11: Power test of MBXF5 - Quench training

## Slide 12: Test summary of MBXF5
22nd Aug. : Cryostat installation
  Warm magnetic measurement by the vertical MM system
  Test had been suspended due to a malfunction of the cold-box turbine monitoring system
9th Oct. – 2nd Nov. : The 1st thermal cycle
  13th : Hipot test at 1.9 K
  16th - 18th : System check / magnetic measurement at 3 kA
  19th - 25th : Quench training up to the ultimate current
  26th : 4-hours current holding at 12.31 kA (=Nominal + 200A)
  27th - 31st : Magnetic / joint-resistance measurement
Current holding test at the ultimate current, 13.23kA,
is postponed until the 2nd thermal cycle (13th Nov.-)

## Slide 13: Quench protection
Quench protection heater
  2 strips x 4 circuits
5-units varistor (Metrosil®)
  Validated in the MBXF1 test
  Healthiness is monitored by the Rogowski coils
Once the magnet current is shut off at the current above 3 kA, we perform a ‘3kA-check’ run to inspect healthiness of the varistors

## Slide 14: Run history
Chart: MBXF5 1stTC - Run history
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39
Iq PLC (A) | 0 | 0 | 0 | 0 | 974 | 2977 | 985 | 986 | 985 | 50 | 2974 | 4975 | 2975 | 6977 | 2976 | 8983 | 2977 | 9980 | 2973 | 10638 | 2975 | 11213 | 2975 | 11434 | 2975 | 11964 | 2975 | 12485 | 2973 | 12582 | 2977 | 12746 | 2977 | 12994 | 2975 | 13215 | 2974 | 13231 | 12310
Reach the ultimate
4-hours holding at 12.31 kA
Training
System check
(current shutoff)

## Slide 15: Training summary
Quench# | Iq (A) | Top or Bottom | LE or RE
1 | 10673.4 | Bottom | LE
2 | 11246.0 | Bottom | LE
3 | 11460.5 | Top | LE
4 | 11978.1 | Top | RE
5 | 12513.8 | Top | RE
6 | 12610.5 | Bottom | RE
7 | 12778.3 | Bottom | RE
8 | 13004.3 | Top | N.A.
9 | 13231 | Bottom | LE

## Slide 16: Quench antenna results
No quench concentration is observed
#2,#3
#1,#7,#9
#5
#4,#6
No signal
Quench#1
#2
#3
#4
#5
#6
#7
#8
#9

## Slide 17: Power test of MBXF5 - Vertical magnetic measurement

## Slide 18: Measurement system
Field quality of MBXF5 at room temperature / 1.9 K using the KEK’s vertical measurement system
  Rotating coil (PCB):
    3 sets of radial coils
    Long coils (500) for integral measurement
    Short coils (50) for fine search
  Scanning capability
    Stepping motor and Magnescale®
    10-m-shaft to cover the full-length of the magnet
50
500
50
10-m shaft

## Slide 19: Measured items
Z-scan
  Warm, before cooling
  I =3 kA, before training
  I = [687, 3k, 7k, 10k, 11k, 12.11k, 11k, 10k, 7k, 3k, 687] A, after training and machine cycle (see below)
DC loop at 1.9 K
  Rotating coil position is fixed at the magnet center (z=0)

## Slide 20: DC loop – comparison with calc.
due to current
monitoring issue
Central field quality was evaluated by the long coil (L=500) brought to the longitudinal magnet center (z=0)
Measured curves are reproducible by the calc. (Roxie2D)

## Slide 21: Integral measurement – comparison with calc.
Warm <-> Cold : good reproducibility
Good agreement with the calculation

## Slide 22: Integral measurement – comparison with MBXF1
Very good reproducibility
Other harmonics data are also plotted in the backup slides

## Slide 23: Summary of the field quality (integral) so far
I=12.11 kA, KEK cryostat
I=12.11 kA, KEK cryostat
＊) MBXFP’s cross-section design is different from the series
＊
Series
Prototype

## Slide 24: Ref) Summary table : SS averaged & Integral
Warm
T=1.9 K, I=12.11kA

## Slide 25: Summary
Warm magnetic measurement of MBXF2 at the Hitachi premise
  Measured field quality agrees with the design value to within ~1 units.
  Series statistics so far : 3
    Good reproducibility
    Variation in b3 and a2 : ~3 units
Power test of MBXF5 (1st TC) in the KEK cryostat
  Reached the nominal current after 4 quenches
  Reached the ultimate current after 9 quenches
  No quench concentration
  4-hours holding at the nominal+200A was successful
  4-hours holding at the ultimate current is pending until the 2nd TC
  Field quality
    Good reproducibility and well reproduced by calculation
  The 2nd TC will be started from 13th Nov.

## Slide 26: Thank you !

## Slide 27: Supplement

## Slide 28: MIITs

## Slide 29: Integral – comparison with MBXF1

## Slide 30: Integral – comparison with MBXF1

## Slide 31: Integral – comparison with MBXF1
a2：MBXF1の時ほどの顕著な大きさはみられない。
ヒステリシスにも違いが現れている