## Slide 1: SRF beyond Niobium: Thinner is better How multilayer might break through the barrier
Marc Wenskat - on behalf of the SRF R&D Team

## Slide 2
Let’s look beyond Niobium?

## Slide 3
Leave no one behind
→ Q0,max ~ 1 x 1011
→ Eacc,max = 42 MV/m
critical magnetic field Hc,1: 180 mT → phase transition
Quality factor Q0 as figure of merit for the loss
Non-vanishing RF resistance
RBCS ~ 8 nΩ at 2K and 1.3 GHz, Nb
Rres ~ 4-6 nΩ

## Slide 4
The real world
EXFEL Spec
[Reschke et al., Phys. Rev. Accel. Beams, 20, 042004 (2017)]
[Grassellino et al., SUST, 26, 102001 (2013) ]
[Grassellino et al., SUST, 30, 094004 (2017) ]
[Posen et al., Phys. Rev. Applied 13, 014024]
[Gurevich, APL, 88, 012511 (2006)]
Standard Cavity
Doped Cavity
Infused Cavity
Mid-T Bake
SIS Coating
LCLS-II CW
@2K
Theory
Curves are exemplary representations
Cavities limited by quench
Q0 and Eacc (seperately) approach the thermodynamic limit of Nb
→ We need to look beyond
?

## Slide 5
Why thinner should be better?

## Slide 6
Why thin and not thick?
Take a cavity and coat it with a “higher” Tc superconductor
- Fewer rf losses & higher Q0 compared to Nb at 2K since RBCS ~ exp(-Tc)
How do we increase Eacc?
Such superconductors usually have a lower Hc,1 compared to Nb (although Hsh is higher)
H / mT
Hc,1
Hsh
Chart: 
| Nb | NbN | Nb3Sn | NbTiN
 | 180 | 20 | 50 | 30
 | 50 | 240 | 490 | 409

## Slide 7
Taka finished what Alex started
Energetically suppressed vortices in thin films cause enhancement of “field of first flux entry” a.k.a. Hc1
Alex’ idea: Coat a cavity with a thin superconducting film with insulating layer, acting as vortex barrier
Controversy around effectiveness
Taka’s new argument: Bean-Livingston Barrier increase through “counter current”
[G. Stejic et al., PRB 49.2 (1994)]
Co-Autor: Gurevich
[N. Schäfer et al., J. Appl. Phys. 128, 133902 (2020)]
Hc,1 of Nb3Sn is 50mT
[A. Gurevich, APL 88 (2006)]
[D. Liarte, SUST 30 (2017) 033002]
[T. Kubo, SUST 30 (2017)]
[Asaduzzaman, arXiv: 2304.09360]
[Keckert, S. PhD Thesis, Siegen 2019]

## Slide 8
Summarizing the theory
Top superconductor should see majority of rf field → this way Q0 improves most
Field should not decay completely in the top layer → layer should be thinner as λL,Top
Insulating layer creates more interfaces, prevents flux avalanches / free movement, pancake vortices
λL=185nm
λL=40nm
Taken from [T. Kubo, SUST 30 (2017)]

## Slide 9
How to maximize the field enhancement?
Depends on Hc,1 and λL of both SC and “defectiveness” η
  Assume NbTiN – I – Nb
    Hc,1 Nb 180 mT
    Hc,1 NbTiN 213 mT
    For η = 1
  Isolator 15nm, NbTiN 100nm
  → Hffp = 270mT oder 63 MV/m
    For η = 0.7
  Isolator 10nm, NbTiN 60nm,
  → Hffp = 224mT oder 52 MV/m
[T. Kubo, SUST 30 (2017)]

## Slide 10
Who is coating SIS?
SIS-Network is now larger
INFN / HZB / CNRS / USI / UKRI / UVic / STFC / RTU / IEE / U Lancaster … + Theory
Surely I‘m missing someone!
Thomas Proslier
Method of choice: ALD
First steps @ ANL 2009 (coated cavity w. Al2O3)
Anne-Marie Valente-Feliciano
Method of choice: HiPIMS
First steps @ TJNAF 2011 (flat samples)

## Slide 11
What are we doing?
(since 2019)

## Slide 12
Method of choice: Atomic Layer Deposition
Thermal ALD
PEALD
Taken from: L. Mai, (2020), DOI:10.13154/294-7658.
Material candidates for SIS
S: NbN, NbTiN
I: AlN, Al2O3
Deposition choice at UHH: Thermal ALD/PEALD

## Slide 13
SIS multilayers (PE)-ALD investigation at UHH
Thermal ALD: Al2O3
Capability for coating
single-cell cavities
Capability for coating
planar samples
PEALD: AlN, NbTiN, NbN
Thermal ALD: Al2O3
Capability for coating
single-cell cavities

## Slide 14
Successful Al2O3 coating of high-gradient cavities by thermal ALD
[M. Wenskat et al., 2023 SUST 36 01501]
Thermal ALD setup
Process optimization
Cavity performance
Successfully coated three cavities so far
„Oxide-layer manipulation“ studies as spin-off

## Slide 15
SIS multilayers (PE)-ALD investigation at UHH
Thermal ALD: Al2O3
Capability for coating
single-cell cavities
Capability for coating
planar samples
PEALD: AlN, NbTiN, NbN
Capability for coating
planar samples
PEALD: AlN, NbTiN, NbN

## Slide 16
Tailored AlN-NbTiN multilayers on Nb and Si
DEPOSITION PARAMETERS
Temperature: 250 °C
Plasma power: 300 W
Base pressure: 1E-1 mbar
Developed recipe leads to a Tc of 15.4 K on coated samples
[I. González Díaz-Palacio et al., Journal of Applied Physics 134(3), 035301 (2023)]

## Slide 17
Annealing the layer improves Tc – but why?
Identified optimal temperature on Si
Crystallinity improves – nanocrystalline / polymorphous at the beginning
XPS studies show significant changes during annealing
Current hypothesis: pollution by metallo-organic precursor is reduced
  Fits to literature results in better vacuum
  Fits to KEK studies
10 nm
TEM

## Slide 18
Hc1 measurements
VSM measurements
  Filmthickness identical 75nm – on Si
  Magnetic dipolemoment m as function of B and T
Hc1 of Bulk NbTiN on the order of 30mT (depends on stochiometry)
Significant increase of Hc1 observed
Consistent with publications from ODU
  75nm NbTiN auf Nb
  DC „punchthrough“ measurement H ≈ 250mT
Best explanation: pancake effect since NbTiN on Si
[I. H. Senevirathne, SUSPB025, SRF2023]

## Slide 19
Related ongoing studies
Thermal conductivity studies at UHH/DESY
Commissioning of the UHH Quadrupole Resonator (QPR) at DESY
Flux expulsion studies at
CERN
forming a hollow cavity

## Slide 20
PEALD AlN-NbTiN cavity coating
Upgraded system
High versatility in one system:
PEALD and thermal ALD
Capable depositing:
  NbTiN / NbN
  AlN
  Al2O3
In-situ annealing
  dissolve oxide layers before coating
  after coating
EXTEND SINGLE-CELL FURNACE TO PEALD-SINGLE-CELL COATING SYSTEM
Status:
Design
Fabrication ongoing
Commissioning

## Slide 21
SRF R&D Roadmap of UHH
Now-ish

## Slide 22
Summary
We have to start looking for alternatives beyond Nb…
… and SIS is one (awesome and fun) candidate
SIS / thin film community already large and keeps growing
UHH pushes deep into the topic and tries to catch up fast…
…already at eye-level on some points

## Slide 23
Thank you
Thanks to
Robert Blick (UHH), Frederic Braun (U. Wuppertal), Maik Butterling (HZDR), Jakub Cizek (U Prague), Getnet Deyu (UHH), Alexey Ermakov (DESY), Jürgen Eschke (DESY), Erik Hirschmann (HZDR), Wolfgang Hillert (UHH), Arno Jeromin (DESY), Thomas Keller (UHH), Nicolay Krupka (DESY), Anton Lorf (UHH), Kay Jensch (DESY), Thomas Keller (DESY), Oskar Liedke (HZDR), Lutz Lilje (DESY), Dirk Lützenkirchen-Hecht (U. Wuppertal), Cornelius Martens (UHH), Giso Marquardt (DESY), Trupen Parik (DESY), Lea Preece (UHH), Detlef Reschke (DESY), Cem Saribal (UHH), Nils Schäfer (TUDA), Lea Steder (DESY), Andreas Stierle (DESY), Vedran Vonk (DESY), Birte van der Horst (DESY), Andreas Wagner (HZDR), Nick Walker (DESY), Hans Weise (DESY), Mateusz Wiencek (DESY), Artem Zaidman (UHH), Robert Zierold (UHH) and many more
Questions?

## Slide 25
ALD cavity coating PEALD SIS studies Thermal conductivity
8
How we grow AlN-NbTiN multilayers by PEALD
TBTDEN: (t-Butylimido)tris(diethylamino)niobium(V)
TDMAT: tetrakis(dimethylamino)titanium(IV)
TMA: Trimethylaluminum
Precursors: Al, Ti, and Nb
NbN
TiN
AlN
H2/N2 PLASMA
Plasma reactive species
GEMStar XT-P from Arradiance
DEPOSITION PARAMETERS
Temperature: 250 °C
Plasma power: 300 W
Base pressure: 1E-1 mbar
NbxTi1-xN
SIS motivation ALD principle ALD coating cavities PEALD SIS studies Outlook
SRF2023, Isabel González Díaz-Palacio, UHH

## Slide 26
Nb3Sn/Nb (Cornell - FNAL) – PCT
Quench field vs Average Gap
Bulk Δ for Nb3Sn is 3.4 to 3.5 meV
Max expected quench field is ~ 91 mT ≈ 21 MV/m
World Record FNAL Nb3Sn Cavity mit 22 MV/m ≈ 93mT
Comment: Could be a property of the specific coating procedure!