## Slide 1: AC loss calculation for RCS 1.8 T magnet (ReBCO-HTS option)
Simon Otten, Anna Kario, Herman ten Kate
With contributions of: H. Piekarz, M. Breschi and F. Boattini
Muon Collider Collaboration Meeting, CERN, 13th of March 2024

## Slide 2: Outline
Hysteresis loss calculations, 2 case studies:
  ReBCO-HTS magnet design by FNAL (H. Piekarz et al.)
  Modified magnet design by Unibo/CERN (M. Breschi, F. Boattini et al.)
Outlook: possible methods for AC loss reduction

## Slide 3: Conceptual magnet design by H. Piekarz et al. (Fermilab)
Image by H. Piekarz
Magnet cross-section
Warm core with H-shaped hole
30 mm pole gap for beam pipe
Target gap field ± 2 T
ReBCO coils 72 kA-turns
water-cooled iron core
HTS coils
72 kA-turns
Sub-cable
2-mm-wire REBCO tapes (12x)
Two layers, six tapes per layer
HTS coil
2x6 sub-cables
6 kA per sub-cable
stainless steel cooling pipe
3.5 mm inner radius
4.0 mm outer radius
ReBCO tapes

## Slide 4: AC hysteresis loss calculation approach
Two steps:
Magnetostatic FEM:
  calculate core magnetic field as function of current
Network model:
  calculate AC loss for six parallel REBCO cables with applied magnetic field and current
  https://doi.org/10.1109/TASC.2024.3364120
Network model assumptions
2D geometry based on cross-section
each sub-cable has 12 strands in 2 layers
layer radii are 4.05 and 4.15 mm
tape width 2 mm
0.5 mm gaps between tapes within a layer
gaps in successive layers are never aligned
zero tape thickness
40 elements per tape
angle dependent Jc(B) for SuperPower tape (Robinson database)
power law E(J) relation with n = 30
each tape carries the same current
no coupling loss
no current redistribution
no eddy current loss
no core loss

## Slide 5: Core - magnetic field calculation
Core magnetic field calculated by subtraction of the cable’s magnetic field
Calculation done at I = 1, 2, 3, …, 40 kA to generate interpolation data
I = 36 kA

## Slide 6: Some magnetic field plots
Magnetic field expelled at low amplitudes
Magnetic field penetrates at high amplitudes
sub-cable 1
|B| = 0.43 T
sub-cable 2
|B| = 0.27 T
sub-cable 3
|B| = 0.17 T
sub-cable 4
|B| = 0.08 T
sub-cable 5
|B| = 0.07 T
sub-cable 6
|B| = 0.19 T

## Slide 7: AC loss for a ramp from -36 to +36 kA
1 kT/s ramp
-36 kA
+36 kA
+1.70 T
-1.70 T
12.3 J/m per quarter magnet
--> 49 J/m for the full magnet
--> ~ 0.5 kW/m with 5 Hz repetition rate!
Negligible dependence on ramp rate
(hysteresis only!)
Used Jc(B) data of SuperPower AP tape measured at 20 K.
tramp = 6 ms
integration window for Q
Chart: AC loss for ramp from -36 kA to + 36 kA for different ramp rates at 20 K
| 100 | 200 | 300 | 400 | 500 | 1000 | 2000 | 3000 | 4000
AC loss for ramp from -36 kA to + 36 kA for different ramp rates at 20 K | 12.0866 | 12.1603 | 12.2027 | 12.2325 | 12.2575 | 12.3271 | 12.3967 | 12.437 | 12.4623

## Slide 8: AC loss as a function of temperature
Total AC loss decreases with temperature because saturated tapes dominate AC loss
Note: critical current is defined as at 36 kA applied current (so not the load line intersection)
Chart: temperature [K]
| 15 | 20 | 25 | 30 | 35 | 40
sub-cable 1 | 10773.6369 | 9373.6223 | 7863.346 | 6394.6781 | 5094.3588 | 4040.1302
sub-cable 2 | 11033.1497 | 9703.1489 | 8234.7455 | 6790.2841 | 5474.1053 | 4385.7726
sub-cable 3 | 11200.4298 | 9912.4789 | 8488.4957 | 7082.5011 | 5777.4568 | 4671.6976
sub-cable 4 | 11312.7311 | 10051.1196 | 8660.8033 | 7289.3811 | 6015.7709 | 4907.8576
sub-cable 5 | 11369.6328 | 10117.3977 | 8742.7436 | 7393.5475 | 6136.86 | 5033.3984
sub-cable 6 | 11328.878 | 10064.3123 | 8675.2457 | 7307.5814 | 6036.8462 | 4931.9481
applied current | 6000 | 6000
Chart: temperature [K]
| 15 | 20 | 25 | 30 | 35 | 40
sub-cable 1 | 5.4864 | 5.1445 | 4.758 | 4.3656 | 3.9969 | 34.7142
sub-cable 2 | 3.5095 | 3.3248 | 3.0959 | 2.8659 | 2.6847 | 5.3476
sub-cable 3 | 2.064 | 2.017 | 1.9407 | 1.8394 | 1.7727 | 2.1962
sub-cable 4 | 0.9383 | 0.9835 | 1.0147 | 1.0331 | 1.0795 | 1.253
sub-cable 5 | 0.1139 | 0.1986 | 0.3237 | 0.5148 | 0.7018 | 0.91167
sub-cable 6 | 0.5551 | 0.6597 | 0.7636 | 0.8638 | 1.0087 | 1.1756
total | 12.6672 | 12.3281 | 11.8966 | 11.4826 | 11.2443 | 45.5983
Sub-cable critical current as function of temperature
Hysteresis AC loss as function of temperature
6 kA sub-cable current

## Slide 9: Comparison with simple analytical loss estimate
Simple and easy calculation yielding similar loss with some 20-30 % possible deviation
Reasons for discrepancy:
  Formula assumes saturated tapes, not true at low amplitudes
  Formula does not take into account transport current, and thus underestimates the loss for high
Chart: temperature [K]
| 15 | 20 | 25 | 30 | 35 | 40
matlab | 12.6672 | 12.3281 | 11.8966 | 11.4826 | 11.2443 | 45.5983
Tiemo and Fedor | 14.4279 | 12.6917 | 10.7932 | 8.9321 | 7.2404 | 5.8256
Formula by F. Gömöry et al. for saturated twisted tapes in perpendicular B-field:
is critical current per tape, so is critical current per sub-cable
is lay angle ( straight tape)
is effective tape width.
See Solovyov et al. https://doi.org/10.1088/1361-6668/acb08e
Hysteresis AC for the quarter magnet (6 sub-cables)

## Slide 10: Hysteresis loss reduction by changing conductor position
Cable position optimized for minimum perpendicular magnetic field in COMSOL:
reduced from 0.43 T to 0.19 T (~ 50% effect)
1 kT/s ramp
-36 kA
+36 kA
+1.71 T
-1.71 T
AC loss per half cycle reduced from 12.3 to 7.6 J/m
(-38% !)

## Slide 11: Outline
Hysteresis loss calculations, 2 case studies:
  ReBCO-HTS magnet design by FNAL (H. Piekarz et al.)
  Modified magnet design by Unibo/CERN (M. Breschi, F. Boattini et al.)
Outlook: possible methods for AC loss reduction

## Slide 12: Modification of 1.8 T resistive magnet
H-type resistive magnet by Breschi et al.
Modified magnet:
Same core geometry and material
Cu conductor replaced by ReBCO-HTS conductor
4x cooling pipe with ReBCO conductor (12x2 mm)
5.44 kA
Conductor loss estimation 2 kW/m
(F. Boattini et al., “Recent progress on the models of power converters and resistive magnets”, https://indico.cern.ch/event/1374333/ )

## Slide 13: Comparison of AC hysteresis loss
ascf
Chart: full magnet hysteresis loss for 5 Hz repetition
| 15 | 20 | 25 | 30 | 35 | 40 | 45
Unibo/CERN | 434.6442 | 384.0525 | 329.5245 | 277.1093 | 229.9529 | 189.8835 | 156.7027
FNAL | 410.8108 | 363.5189 | 312.524 | 263.5368 | 219.494 | 182.019 | 150.9378
Similar loss level for both designs (within 10%)
(critical state estimation)
Chart: power consumption with ideal Carnot cooling
| 15 | 20 | 25 | 30 | 35 | 40 | 45
min. refrigerator power | 8258.2394 | 5376.7347 | 3624.7691 | 2493.9838 | 1741.0717 | 1234.2426 | 887.9819
COP | 0.052632 | 0.071429 | 0.090909 | 0.11111 | 0.13208 | 0.15385 | 0.17647
Minimum refrigeration power exceeds loss of resistive option for Tc < 30 K

## Slide 14: Conclusion
Hysteresis loss estimate of considered designs is 0.2 – 0.5 kW/m in the cold
ReBCO conductor loss is below resistive Cu option (2 kW/m), however, refrigerator power is excessive for T < 30 K and needs to be included
Outlook: possible ways to reduce loss of the ReBCO-HTS option
  Adapt magnet layout to reduce perpendicular field on coated conductor
  Adaptation of the conductor layout, e.g. filamentization
  Increasing operation temperature for lower refrigerator power.