## Slide 1: Non – ferrous metals for particle accelerators
Ignacio Avilés Santillana
CERN EN / MME – MM
Email: iaviles@cern.ch
Mechanical & Materials Engineering
for Particle Accelerators and Detectors

## Slide 2: The most important slide of this presentation
Materials are your friends.
Get to know them as good as you can.
Do not ask them for things they cannot do.
"Close friends are truly life's treasures. Sometimes they know us better than we know ourselves.” Vincent Van Gogh
CAN I BE YOUR FRIEND?

## Slide 3: Outline
Environmental conditions of particle accelerators
General rules for selection of materials in particle accelerators
Families of non – ferrous materials:
    Aluminum
    Copper
    Titanium
    Niobium
Conclusions

## Slide 4: Environmental conditions of particle accelerators
Cryogenic temperatures.
Ultra – high and extreme vacuum.
Electro – magnetic fields.
Radiation.
High temperatures and high strain rate.

## Slide 5: Environmental conditions of particle accelerators
Cryogenic temperatures  down to 1.9 K (superfluid helium).
Ultra – high and extreme vacuum  down to 10 -11 mbar.
Electro – magnetic fields.
Radiation.
High temperatures and high strain rate  beam intercepting devices (dumps, collimators, targets).

## Slide 6: Environmental conditions of particle accelerators
Cryogenic temperatures  down to 1.9 K (superfluid helium).
Ultra – high and extreme vacuum  down to 10 -11 mbar.
Electro – magnetic fields.
Radiation.
High temperatures and high strain rate  beam intercepting devices (dumps, collimators, targets).
From: Herring, Daniel H., Vacuum Heat Treatment, BNP Custom Media Group, 2012.

## Slide 7: Environmental conditions of particle accelerators
Ultra – high and extreme vacuum  down to 10 -11 mbar.
Cryogenic temperatures  down to 1.9 K (superfluid helium).
Electro – magnetic fields.
Radiation.
High temperatures and high strain rate  beam intercepting devices (dumps, collimators, targets).
Courtesy of
B. Bordini

## Slide 8: Environmental conditions of particle accelerators
Cryogenic temperatures  down to 1.9 K (superfluid helium).
Ultra – high and extreme vacuum  down to 10 -11 mbar.
Electro – magnetic fields.
Radiation.
High temperatures and high strain rate  beam intercepting devices (dumps, collimators, targets).

## Slide 9: Environmental conditions of particle accelerators
Ultra – high and extreme vacuum  down to 10 -11 mbar.
Cryogenic temperatures  down to 1.9 K (superfluid helium).
Electro – magnetic fields.
Radiation.
High temperatures and high strain rate  beam intercepting devices (dumps, collimators, targets).
Courtesy of
E. Lopez Sola

## Slide 10: General rules for materials’ selection in particle accelerators
The golden rule to be remembered (from S. Sgobba in stainless steel, can be extended to any material):
    “A material for an accelerator part is not a mere chemical composition or designation”
    Low / high temperature, magnetism, ultrahigh vacuum, radiation, require special care.
Material designation
Strain rate
sensitivity
Notch
sensitivity
Physical properties
Temper state
Inclusion content
Weldability
Controlability
Transformations

## Slide 11: Non – ferrous materials
Aluminium
  Second-most abundant metallic element in Earth's crust after silicon.
  The name comes from its compound form, a mineral rock called ‘alumen’ (meaning binding) used as dyeing fixative.
  Silver from clay
The legend sais that Tiberius beheaded a goldsmith who first crafted aluminium since it could devaluate the price of gold.

## Slide 12: Non – ferrous materials
Aluminium
  Two millennia after, the extraction of Al from bauxite was very scarce. Al was more precious than gold (as Tiberius feared).
Napoleon III had, for his most distinguished guests, Al cutlery. The rest had to settle for gold.

## Slide 13: Non – ferrous materials
Aluminium
  Electrolysis (Hall – Héroult process) of alumina (Bayer process).
  Victim of its own success: it is produced in similar quantities than all other non-ferrous metals combined
~ 70M tons in 2023

## Slide 14: Aluminium for particle accelerators
  Low modulus of elasticity
  High thermal contraction coefficient
  Paramagnetic
Al shrinking cylinders for
MQXF
quadrupoles
Øext = 614 mm
H = 1366 mm
H
Source: DUTHIL, Patxi. Material properties at low temperature. arXiv preprint arXiv:1501.07100, 2015.

## Slide 15: Aluminium for particle accelerators
  Very low thermal emissivity
  High thermal and electrical conductivity
Al coil for CERN’s first particle accelerator:
The Synchrocyclotron
MLI (Al coated Mylar) HL – LHC’s cold box

## Slide 16: Aluminium for particle accelerators
  Feeble interaction with particle beams
    Low density
    Low atomic number
Developments of Al vacuum chambers and bellows

## Slide 17: Wrought aluminum alloys
Designation AA | Major alloying elements | Alloy group | Heat treatable? | Examples
1xxx | - | Pure Al | No | 
2xxx | Cu | Al – Cu | Yes | 2219
3xxx | Mn | Al – Mn | No | 3003
4xxx | Si | Al – Si | No | Filler
5xxx | Mg | Al – Mg | No | 5061
6xxx | Mg, Si | Al – Mg - Si | Yes | 6082
7xxx | Zn, Mg | Al – Zn | Yes | 7050
8xxx | any |  | (yes) | 8090
Can be strengthened by a suitable thermal treatment (heat treatable)
Can only be strengthened by hot or cold working (non – heat treatable)

## Slide 18: Wrought aluminum alloys designations
1xxx series (pure Al)
Example: CMS conductor
4N (99.99 %) Al stabilizer
Excellent workability & ↑ conductivity

## Slide 19: Wrought aluminum alloys designations
2xxx series (Al – Cu)
    Example: EN AW 2219 T6
Example: vacuum chamber bodies. (NEG coated).
↑ Mechanical properties
↓ corrosion resistance

## Slide 20: Wrought aluminum alloys designations
3xxx series (Al – Mn)
    Example: EN AW 3003 H22
Example: CMS Solenoid thermal shield
Moderate mechanical properties, workability,
Corrosion resistance and th. conductivity

## Slide 21: Wrought aluminum alloys designations
    Al - Si alloys are used in welding wire and as brazing alloys.
4xxx series (Al – Si)
    Major alloying element of this group is silicon, added in sufficient quantities (around 12%), cause substantial lowering of the melting point without producing brittleness (eutectic point).

## Slide 22: Wrought aluminum alloys designations
5xxx series (Al – Mg)
    EN AW 5083 H321, H116 and H111
Example: Mandrels for CMS coil
moderately ↑ mechanical properties
↑ ductility, weldability
Example: hydroformed bellows

## Slide 23: Wrought aluminum alloys designations
6xxx series (Al – Mg – Si)
    Example: EN AW 6082 T6
Example: ICARUS neutrino detector
Combination of formability, mechanical strength, weldability and weight

## Slide 24: Wrought aluminum alloys designations
7xxx series (Al – Zn – Mg)
    Example: EN AW 7075 T6
Example: Al shells MQXFBP1 magnet
Al shell
↑ Mechanical properties

## Slide 25: Wrought aluminum alloys designations
8xxx series
    Reserved for miscellaneous compositions. Alloying elements include: iron, lithium, copper, zinc, magnesium, silicon, manganese, vanadium, zirconium, titanium, chromium & bismuth.
    Al – Li alloys, for weight reduction. Al - Li alloys possess increased Modulus of Elasticity, high specific stiffness, increased fatigue strength and cryogenic strength.

## Slide 26: Wrought aluminum alloys: temper states
Alphanumeric designations that contain information about the thermomechanical history of the material to achieve the desired properties.
AA 7075
AA 7075

## Slide 27: Wrought aluminum alloys: temper states
“Men are like steel: if they loose their temper, they loose their worth”
materials

## Slide 28: Wrought aluminum alloys: temper states
A capital letter indicating the major class of fabrication treatment(s) used + one (or more) numbers providing more speciﬁc information about how the processing was carried out.

## Slide 29: Wrought aluminum alloys: temper states
O, annealed: given a high – temperature treatment, sufficient to remove the effects of prior working, usually resulting in complete recrystallization of the material. Lowest strength and maximum ductility and toughness.
Source: ASM aluminium and
aluminium alloys handbook
Portion of Al – Cu
phase diagram

## Slide 30: Wrought aluminum alloys: temper states
H, strain hardened: non-heat-treatable wrought alloys that have had their strength increased by strain hardening. H is always followed by two or more digits:
    The ﬁrst number after the H tells whether the strain-hardened alloy has been thermally treated
    The second number indicates the approximate amount of cold work
HX1
HX8
% cold work
Source: Aluminium in Commercial Vehicle – European Aluminium Association – 2011

## Slide 31: Wrought aluminum alloys: temper states
H, strain hardened: non-heat-treatable wrought alloys that have had their strength increased by strain hardening. H is always followed by two or more digits:
    The ﬁrst number after the H tells whether the strain-hardened alloy has been thermally treated
    The second number indicates the approximate amount of cold work
    Any subsequent numbers deﬁne special practices, variations of the normal indicated by the ﬁrst two numbers.
Example:
AA 5083 H116 (marine grade)

## Slide 32: Wrought aluminum alloys: temper states
T, thermally treated to produce stable tempers: heat-treatable wrought alloys that have followed a solution heat treatment followed by a quench and either natural or artiﬁcial aging.
Heat treatment to increase the strength of Al alloys is a three step process:
  Solution heat treatment: dissolution of soluble phases
  Quenching: development of supersaturation
  Age hardening: precipitation of finely dispersed precipitates

## Slide 33: Wrought aluminum alloys: temper states
T, thermally treated to produce stable tempers: heat-treatable wrought alloys that have followed a solution heat treatment followed by a quench and either natural or artiﬁcial aging. T is always followed by one or more digits:
    The ﬁrst digit after the T can be any from 1 to 10. It is a combination of:
      Cooled from elevated temperature or solution heat treatment
      Cold worked or not cold worked
      Naturally aging or artificial ageing
From EN 515:
Al and Al alloys
- Wrought products -
Temper designations

## Slide 34: Wrought aluminum alloys: temper states
Iso – yield – strength curves for EN AW 7075
Source: ASM aluminium and
aluminium alloys handbook

## Slide 35: Wrought aluminum alloys: temper states
T, thermally treated to produce stable tempers: heat-treatable wrought alloys that have followed a solution heat treatment followed by a quench and either natural or artiﬁcial aging. T is always followed by one or more digits:
    The ﬁrst digit after the T can be any from 1 to 10. It is a combination of:
      Cooled from elevated temperature or solution heat treatment
      Cold worked or not cold worked
      Naturally aging or artificial ageing
    Additional numbers indicate a variation in treatment that signiﬁcantly alters the product characteristics that are or would be obtained using the basic treatment. There is not a full list of all such possible variations.

## Slide 36: Wrought aluminum alloys: weldability
Most non – heat treatable alloys plus series 6xxx can be fusion welded, and precaution should be taken with heat treatable high strength alloys.
    When non – heat treatable alloys are welded, they loose the effect of an eventual work hardening  softening of HAZ.
Source: ASM aluminium and
aluminium alloys handbook

## Slide 37: Wrought aluminum alloys: weldability
Most non – heat treatable alloys plus series 6xxx can be fusion welded, and precaution should be taken with heat treatable high strength alloys.
    When welding heat – treatable alloys  redistribution of hardening constituents  softening of HAZ. Attention to liquation cracking.
EN AW 6061
Source: ASM aluminium and
aluminium alloys handbook

## Slide 38: Wrought aluminum alloys: failure analysis
Catastrophic failure of MQXFAP2
Al shell. Failure analysis:
EDMS 2088319

## Slide 39: Wrought aluminum alloys: failure analysis
Mechanical testing at cryogenic temperature shows the material choice is correct
However, EN AW 7075 T651 is sensitive to the presence of sharp notches at 4 K.
Aluminium alloy shell: failure analysis and material properties at cryogenic temperature. EDMS 2088319

## Slide 40: Non – ferrous materials
Copper
  Its name comes from ‘cuprum’, meaning “from the island of Cyprus”.

## Slide 41: Non – ferrous materials
Copper
  One of the oldest materials known, and one of the most produced.
~ 21.5M tons in 2023

## Slide 42: Copper for particle accelerators
  Elastic modulus close to Nb3Sn
  Diamagnetic
Courtesy: M. Crouvizier

## Slide 43: Copper for particle accelerators
  Extremely high thermal and electrical conductivity
18 kA HL-LHC current leads
HIE ISOLDE quarter wave resonator substrate
Courtesy:
P. Moyret

## Slide 44: Copper for particle accelerators
  Ductile and tough down to 4 K
Stress vs strain curve OFE – copper. ¼ hard (H01) temper state.
Face centered
cubic (FCC)
crystal structure
See also 
CAS course on “Mechanical & Materials engineering”, K-P. Weiss, Mechanical testing

## Slide 45: Copper for particle accelerators
  High availability, moderate price, formability, machinability.
RF fingers of
a collimator
RFQ
Cu gasket Conflat flange UHV

## Slide 46: Wrought copper alloys: temper states
Annealed tempers
Cold worked tempers
Notes: The annealing temperature of Cu depends on the amount of cold work introduced in it.For OFE copper, it can go up to 650 C if you want a dead soft annealed state, but it can also be as low as 300 C

## Slide 47: Copper and copper alloys
“electrical coppers”
Cu OFE, C10100
Cu OF, C10200
Cu OFS, C10700
99.8Cu-0.15Al2O3, C15715
CERN Phase II collimator.
Glidcop© sectorized jaw
Source: ASM copper and
copper alloys handbook

## Slide 48: Copper and copper alloys
High strength copper alloys
Cu-2%Be, C17200
Cu-0.3%Be-0.5%Co, C17410
Cu-1%Cr-0.15%Zr,C18150
C17410 RF fingers of a
secondary LHC collimator
C18150 for TIDVG dump’s core & cooling plates

## Slide 49: Copper and copper alloys
70Cu-30Ni, C71500
90Cu-10Ni, C70600
C70600 for the cooling circuit of phase II collimators

## Slide 50: OFE Copper
Weldability / brazeability
Ease of machining

## Slide 51: OFE Copper
CLIC accelerating structure.
Diamond turning / milling
Øo = 83 mm
18 kA HL-LHC current lead during machining.
Ra = 5 nm
Courtesy: S. Atieh
See also 
CAS course on “Mechanical & Materials engineering”, J. Tschoepel, Machining
Courtesy:
P. Moyret

## Slide 52: Non – ferrous materials
Titanium
    The name comes from Titan, son of Gaea.
    High corrosion resistance, low density, high mechanical resistance.
If price is not a problem,
Ti overwhelms Al in many
aspects
Titanium
    Everyone knows it from the song of David Guetta
    High corrosion resistance, low density, high mechanical resistance.

## Slide 53: Titanium in particle accelerators
  High specific strength.
  Paramagnetic
  Lower thermal expansion / contraction than stainless steel
Courtesy: C. Loffler
Cross section MQXF. Ti pole

## Slide 54: Titanium in particle accelerators
  Certain grades are ductile and moderately tough at cryogenic temperature.
  Thermal contraction closer to Nb than stainless steel.
  Weldable with Nb (total solubility)
Titanium (II) He tanks of the crab cavities for HL - LHC

## Slide 55: Titanium grades
Microstructures of Ti
α Ti – hexagonal closed packed (HCP)
β Ti – body centred cubic (BCC)
We privilege compact structures (α – Ti) for cryogenic application

## Slide 56: Titanium grades
Extra – low interstitials (ELI)
We privilege ELI grades for cryogenic application

## Slide 57: Titanium grades
Pure Ti
He tanks surrounding
Crab cavities. Ti grade 2

## Slide 58: Titanium grades
Grade 5
& Grade 5 ELI
(grade 23)
RF feedthrough flanges of the crab cavities.
Ti grade 23

## Slide 59: Titanium grades
Grade 6
& Grade 6 ELI
Axial force tie rods of the ATLAS
barrel toroid magnet
CMS longitudinal tie rods
Source: S. Sgobba et al. (2003, July). Manufacturing, quality control and assessment of the cryogenic properties of a titanium alloy for application to the coil suspension system of the Compact Muon Solenoid (CMS). In Proc. 10th World Conference on Titanium (pp. 13-18).
Source: P. Jenni (CERN), ATLAS overview, status and plans. Workshop on cooperation in HEP between CERN and China. Beijing, 14 – 15 May 2005.

## Slide 60: Non – ferrous materials
Niobium
  Element of the periodic system with the highest critical temperature.
  The name comes from Niobe, the daughter of Tantalus:

## Slide 61: Non – ferrous materials
Niobium
  Element of the periodic system with the highest critical temperature.
  The name comes from Niobe, the daughter of Tantalus:
    Nb is found in combination with Ta (Coltan)
    You can still find it in old texts by Cb (columbium)
Mineral Coltan, a combination of columbite and tantalite
Source: Bauer, W. (1980). Fabrication of niobium cavities. In Proc. 1st Workshop RF Supercond., M. Kuntze, ed., Karlsruhe (p. 271).

## Slide 62: Families of non – ferrous materials
Niobium
  90 % of its production is used to alloy stabilized steel grades or high temperature superalloys.
Nb, Ti carbides and nitrides in dark grey and yellow respectively. Inconel 718 for ITER magnet supports.
Inconel 718 for ITER magnet supports.

## Slide 63: Non – ferrous materials
Niobium
  90 % of its production is used to alloy stabilized steel grades or high temperature superalloys.
  Superconducting wires for high field magnets (NbTi, Nb3Sn).
LHC dipole
NbTi wire
11T dipole
11T dipole’s coil section
Nb3Sn wires
See also 
CAS course on “Mechanical & Materials engineering”, S. Sanfilippo, Superconducting Magnets

## Slide 64: Non – ferrous materials
Niobium
  90 % of its production is used to alloy stabilized steel grades or high temperature superalloys.
  Superconducting wires for high field magnets (NbTi, Nb3Sn)
  Ultrahigh purity Nb
DQW crab cavity
RFD crab cavity
5 cell elliptical cavity

## Slide 65: Niobium for SCRF cavities
  High critical temperature (9.2 K)
  High critical magnetic field
  High formability, ‘easy’ to machine and weldable.
  Available in practically any size
Buffered
chemical
polishing
(BCP)
Electron beam
melting
Spoke cavity
Øo = 440 mm
Source: Shepard, K. W et al, (1999). Prototype 350 MHz niobium spoke-loaded cavities.
High order mode (HOM) antenna
Øo = 440 mm
Courtesy: S. Atieh
Øi = 74 mm
Notes: Apart from the elliptical and crab cavities I showed before, the hagh formability, machinability and availability allows to fabricate more exotic cavities like this spoke cavity and other RF equipment such as this antenna to dump high order modes in the crab cavities. Everything which is in green is made of niobium

## Slide 66: Niobium grades
ASTM B392 & B393
RRR = residual resistivity ratio
An accurate measurement of the
purity above 99.999%

## Slide 67: Niobium grades & SCRF
CERN technical specification
  Equilibrium between:
    RF performance
    Mechanical robustness
    Material soundness
See also 
CAS course on “Mechanical & Materials engineering”, T. Lucas, RF applications
RF performance DQW cavities
Displacements (in mm) of RFD cavity. 1 bar external pressure
NDT of Nb technical specification
Courtesy: E. Cano Pleite
Notes: CERN technical specification, inspired from DESY, is an equilibrium of RF performance, mechanical robustness and material soundness

## Slide 68: SCRF Nb: failure analysis
Same material specification
Same material supplier
2 different material lots
Same tooling
Same operators
Same forming procedure
Same press machine
Material that shows bad formability complies with CERN Nb spec. & DESY Nb Spec.!
Strain hardening coefficient ‘n’ value seems to be significantly different, as well as the ratio Rp0.2/Rm
Material | n 0.02 – 0.20 | Rp0.2/Rm
Lot OK | 0.35 – 0.38 | 0.31 – 0.33
Lot NOK | 0.28 – 0.30 | 0.42 – 0.50
Courtesy: A. Gallifa
RFD Pole forming trials held at CERN Main Workshop (May 2022).
See also 
CAS course on “Mechanical & Materials engineering”, F. Carra, Computational tools
A. Gallifa Terricabras, et al Optimizing the Manufacture of High-Purity Niobium SRF Cavities Using the Forming Limit Diagram: A Case Study of the HL-LHC Crab Cavities RFD Pole.

## Slide 69: Conclusions
Key takeaways:
    Materials are your friends, get to know them as good as you can.
    “A material for an accelerator part is not a mere chemical composition or designation”:
        Specification. Fabrication route. Temper state
        Controls
        Price
    Attention to “the hidden iceberg properties” (e.g. notch sensitivity, strain hardening) and to the butterfly effect.
The very particular environment of particle accelerators limits the choice.
Time (and problems) are saved if material selection is integrated from the beginning of the conceptions.
    Advanced non conventional materials require extensive prior R&D

## Slide 70
Thank you for your attention.
Questions?
Mechanical & Materials Engineering
for Particle Accelerators and Detectors

## Slide 71: Additional slides

## Slide 72
Dislocations are the carriers of plastic deformation
Precipitates hinder dislocation motion. There are 2 types: coherent and incoherent
Dislocation bows out between
incoherent precipitates
A loop is left around
each particle
From R. E. Smallman and A. H. W. Ngan. Physical Metallurgy and Advanced Materials. Elsevier, 2007
A dislocation cuts through a
coherent particle, i.e. it passes
through the precipitate on the same
slip plane as in the matrix
Precipitation strengthening

## Slide 73: Wrought aluminum alloys: temper states
H, strain hardened: non-heat-treatable wrought alloys that have had their strength increased by strain hardening. H is always followed by two or more digits:
    The ﬁrst number after the H tells whether the strain-hardened alloy has been thermally treated:
H2
H1
H3
H4
Cold worked

## Slide 74: Wrought aluminum alloys: temper states
T, thermally treated to produce stable tempers:
Cooled from elevated temperature
No
Yes
Cold
worked
Aging
Natural
Artificial
Natural
Artificial
T1
T5
T2
T10

## Slide 75: Wrought aluminum alloys: temper states
T, thermally treated to produce stable tempers:
Solution heat treatment
No
Yes
Cold
worked
Aging
Natural
Artificial
Natural
Artificial
T4
T6
T3
T8
Overaged
T7
T9

## Slide 76: Prices
  Al and Al alloys general purpose  5 EUR / Kg
  EN AW 2219 forged blanks  80 EUR / Kg
  Special forgings, EN AW 6061  15 EUR / Kg
  OFE Cu  25 - 40 EUR / Kg (3D forged)
  OF Cu 10 EUR / Kg (basis)
  CuBe, high (low) Be  40 - 90 EUR / Kg (strips)
  Glidcop  55 EUR / Kg
  Grade 2 50 EUR / Kg (plates)
  Ti6Al4V (ELI)  50 (140) EUR / Kg
  Nb (RRR 300)  600 EUR / Kg
Aluminium and alloys
Coppers
Titanium
Niobium

## Slide 77: Books