## Slide 1
CAS
Mechanical & Materials Engineering for Particle Accelerators and Detectors
June 2024, Sint-Michielsgestel, Netherlands
Vacuum Brazing
S. Mathot
EN/MME

## Slide 2
Outline:
Introduction
Brazing / Soldering
Wetting
Vacuum Brazing
Vacuum Furnace
Vacuum Brazing assembly
Metal/Metal Vacuum Brazing Examples
Case of Glidcop
Brazing and partial Diffusion Bonding
Vacuum Soldering Examples
Case of the RFQ
Vacuum Brazing of Alumina (Ceramic)
With Metallisation
With Active Alloys
Vacuum Brazing by Diffusion Brazing
Vacuum Brazing of large quantities

## Slide 3
Brazing – a “old” story
Achéménide pendant - 4° s. B.C. (Louvre)
PIXE analysis – LARN

## Slide 4
Brazing & Soldering
° Brazing & Soldering: Assembly with a filler metal having a melting point lower than for the assembled materials
° Soldering: Melting point of the filler metal < 450 °C, Brazing: > 450 °C.
° Allow the assembly of different metals and no-metals (ceramics).
° Allow high precision assembly.
° Mechanical resistance generally less than for welding.
° Wetting of the filler metal obtained using a flux or with vacuum / reductive atmosphere (and coating if needed).
Time
Temperature
Vacuum brazing & soldering
Air brazing & soldering

## Slide 5
The Wetting
ϒSL + ϒLV cos (Θ) = ϒSV (Young’s relation)
- Interaction - cos(Θ) ↑
ϒSL ↓ Θ↓
(Ex.: Cu-Ag on Cu)
- Pas d’interaction - cos(Θ) ↓
ϒSL ↑ Θ ↑ , cos(Θ) > 90°
(Ex.: Cu-Ag on Alumina)
Brazing / Soldering: θ < 30° …. Ideally 0° for good brazing by capillarity.
What prevents good wetting (a good interaction) on a metal is oxidation!
Two solutions: the flux or the vacuum

## Slide 6
Vacuum Brazing
Main objective of the vacuum brazing: Oxide reduction at high temperature / low O2 partial pressure
Example with Copper (Cu):
Gibbs energy of metal oxide formations:
→
G = H – TS H = U + PV
For the reaction:
At equilibrium, for the production of one mole of O2:
If :
→
→
The oxide is stable
The oxide decompose
For CuO2, A= -169881 and B= 74.43 [Source: CRC Handbook]
At 800°C, DG = -90 kJ  DG = -180 kJ for 1 mole of O2.
With DG = -180 kJ,
With P = 760 Torr,

## Slide 8
For CuO2, A= -169881 and B= 74.43 [Source: CRC Handbook]
At 800°C, DG = -90 kJ  DG = -180 kJ for 1 mole of O2.
With DG = -180 kJ,
With P = 760 Torr,
Vacuum Brazing – The Ellingham diagram
For Al2O3, A= -1689572 and B= 328.66 [Source: CRC Handbook]
At 800°C, DG = -1337 kJ  DG = -891 kJ for 1 mole of O2.
With DG = -893 kJ,
With P = 760 Torr,
Ellingham diagram
Reduction of the Copper Oxyde possible at 800 °C in a vacuum furnace.
Reduction of the Alumiun Oxyde (Alumina) impossible in a vacuum furnace.

## Slide 9
Vacuum Furnace
Vertical(1) or Horizontal(2) configuration, made of a high-speed vacuum pump (diffusion pump)(3), vacuum chamber with double walls water cooled(4), stainless steel / molybdenum screens(5), molybdenum heaters(6), molyddenum support(7), electrical cabinet(8).
(case for a all-metal vacuum furnace)
Visit 112-R-A10
1
2
3
4
5
6
7
8

## Slide 10
Vacuum Brazing assembly
° Wetting is generally excellent.
° Brazing on large surfaces possible.
° Allow very good thermal and electrical contacts.
° Assembly clean and UHV compatible.
(Filler metal and material with low vapor pressures!)
° Dissimilar materials can be join.
° Allow high precision assembly with little or no
distortion of the components
But:
° Heat treatment can affect the properties of
the base materials.
° Mechanical tolerances are tight
Filler metal seen on the vacuum side

## Slide 11
Metal/Metal Vacuum Brazing Examples
Joint configuration:
- Groove, no gap (Ra  0.8 µm)
- Groove on a diameter
- Chamfer
- Foil
- Paste
Copper (OFE) / Stainless Steel (316LN)

## Slide 12
Metal/Metal Vacuum Brazing examples
Stainless Steel / Stainless Steel (316LN)

## Slide 13
Nb – Stainless steel
Cu – Stainless steel - Ti
Mo – Stainless steel
Glidcop - CuNi
Metal/Metal Vacuum Brazing examples

## Slide 14
Metal/Metal Vacuum Brazing examples
Case of Glidcop

## Slide 15
Brazing & Partial Diffusion Bonding
a
b
c
a
b
c
Metal/Metal Vacuum Brazing examples

## Slide 16
° High purity SnAg or SnPb solders can be used in vacuum …
- Typical solders:
SnAg (eutectic): m.p. 221°C
SnPb (eutectic): m.p. 183°C
- Wetting acceptable on:
Cu and Ag
Metal/Metal Vacuum Soldering examples
Zn
Cd
Pb
Ag
Sn
Al
Cu
Au
Pd
Fe
Ni

## Slide 17
Vacuum soldering of High Temperature Superconductor (HTS) tapes for the LHC current leads.
HTS tapes soldering – SnAg
HTS stacks soldering – SnPb
Metal/Metal Vacuum Soldering examples
Kovar “boxes” – SnAg

## Slide 18
Metal/Metal Vacuum brazing examples
Case of the RFQ
The RFQ (Radio Frequency Quadrupole)
Perturbation (Modulation) of the Electrodes (Vanes) produces a longitudinal electric field for the acceleration of the ions.
T. P. Wangler (2011)
RFQ Performances:
- The RF field allows the Focusing, Bunching and Acceleration
- Is the only linear accelerator accepting a low energy continuous beam
- Acceleration up to 5 - 10 MeV for protons
4-Vanes
4-Rods

## Slide 19
Metal/Metal Vacuum brazing examples
Case of the RFQ
Synchronism between the modulation and the velocity of the particle in an RFQ
2.6 cm
4.1 cm
PIXE-RFQ (2MeV)
(750 MHz)
HF-RFQ (5MeV)
(750 MHz)
Views of the high energy side (last cells) of the vane for two RFQ’s at same frequency, same ion but different end-energy.

## Slide 20
Metal/Metal Vacuum brazing examples
Case of the RFQ
RFQ are generally used as an injector (LINAC4), but (recently) can be used as well as stand alone accelerator (ELISA)

## Slide 21
Metal/Metal Vacuum brazing examples
Case of the RFQ
Mechanical Tolerances
Brazing surface L
Brazing surface R
Braz. surf. L
Braz. surf. R
Flatness of the Left and Right brazing surfaces: After machining and after heat treatment at 800 °C
Tolerances are very tight for an RFQ … but good machining and good alignment are not enough. Deformations during brazing must be anticipate!
Recipe:
1. Discuss a cavity design which reduce the machining time and constraints and limit the risks during brazing.
2. Alternate machining and heat treatment steps, last machining before brazing must be very “light”.
3. Have a good alignment strategy (and good metrology).
4. Have a good tooling reducing possible movement during brazing.
5. Use a thermal cycle adapted to the size of the piece.

## Slide 22
Metal/Metal Vacuum brazing examples
Case of the RFQ
4-Vanes design
Machining with shape tools

## Slide 23
Metal/Metal Vacuum brazing examples
Case of the RFQ
Metrology – Alignment –Machining of reference surfaces

## Slide 24
Metal/Metal Vacuum brazing examples
Case of the RFQ
First brazing : alignment and assembly

## Slide 25
Metal/Metal Vacuum brazing examples
Case of the RFQ
First brazing : Fixture and brazing

## Slide 26
Metal/Metal Vacuum brazing examples
Case of the RFQ
Second brazing : Fixture and brazing

## Slide 27
Metal/Metal Vacuum brazing examples
Case of the RFQ
Good job …. One module finished ….

## Slide 28
Vacuum brazing of Alumina (Ceramic)
First process = Mo-Mn metallization
Mo + MnO (Mn) powder on alumina (Al2O3) @ T > 1200 °C and PH2O / PH2 > 10-4 induce:
- Mo reduction and MnO/Al2O3/SiO2… vitreous phase formation. - Interaction with the Alumina base material and the binder.
- Sintering of the Mo powder in the vitreous phase during cooling.
- Formation of Mo-Mn layer strongly adhering the support.
- Ni layer added to improve the brazing.

## Slide 29
Metal thermal expansion AND metal yield strength should be taken into account for Metal / Alumina brazing.
Métal | TCF
Niobium Platine Tantale Cuivre Titane Kovar Nickel CuNi Fe-42Ni Monel Invar Molybdène Inox 304 Inconel 600 Tungstène | 88 33 28 20 8.8 7.7 6.7 4.8 4.5 4.0 3.7 3.5 2.9 2.1 2.0
Vacuum brazing of Alumina (Ceramic)
TCF = Thermomechanical Compatibility Factor
With
Max. TCF => Min. Stress

## Slide 30
Vacuum brazing of Alumina with Metallization - Examples
Cu – Alumina (up to diameter 400 mm!)
Ti – Alumina – Cu
Kovar (Dilver) – Alumina

## Slide 31
Vacuum Brazing of Ceramic
Second process = Active Brazing
- Brazing alloy containing reductive metal: Ti, Zr, Be, …
- At brazing temperature, under high vacuum, strong interaction with oxides (alumina), carbide, nitrite, ….
- Complex chemical reactions formed at the ceramic / brazing metal interface. Ex.: SiC/Ti > Ti3SiC2, Ti5Si3C, Ti5Si3Cx,….
- ↑ Interaction (wetting) possible with several types of ceramics.
- ↓ Possible formation of brittle phases.
- Example of Active Brazing Alloys:
CuSil ABA (Ag 63, Cu 35.25, Ti 1.75)
Silver ABA (Ag 92.75, Cu 5, Al 1, Ti 1.25)
Gold ABA (Au 96.4, Ni 3, Ti 0.6)
Ellingham diagram
TiO2
ZrO2
2 BeO
Al2O3

## Slide 32
Vacuum Brazing of Ceramics with Active Alloy - Examples
AlN – Dilver
Sapphire
(F 115 mm)
Dilver
Alumina
Nb
Diamond (F 5 mm) – Ti
Carbon – CuSil ABA – CuNi

## Slide 33
° Active brazing on ceramics
ZrO2 – Ti
Alumina – Monel
Alumina – Ti
Alumina – Ti
Alumina – Cu
Vacuum Brazing of Ceramics with Active Alloy - Examples

## Slide 34
Vacuum Brazing of Metals with Active Alloy - Examples
Ta tube /316LN with CuSil ABA
(A. Gerardin)
Cu – W
(CuSil ABA)

## Slide 35
Vacuum Brazing by Diffusion brazing
Diffusion brazing: The filler metal is form by diffusion during the heat treatment.
Example: Alumina/Cu, Metallized ceramic with a Silver layer, Cu with Silver layer
Porosities

## Slide 36
Vacuum Brazing of large quantities
Vacuum brazing (and vacuum furnaces) are adapted to produce large quantities of similar pieces. Not common at CERN, but why not when needed ….
23 km of HTS tapes vacuum soldered in stacks
Hundreds of Cu/Stainless steel junctions
18000 brazing for the thermal links

## Slide 37
Final remarks - comments
Vacuum brazing is a technique that allows highly precision assemblies,
which allows different materials, including ceramics, to be assembled.
The preparation of parts and machining is always high precision. But success begins with the discussion of the design and the follow-up of a very precise procedure, including for surface treatments.
High temperature brazing always modifies the properties or even the dimensions of the parts... this must always be taken into account.