## Slide 1: Thin Films for Accelerator Components
G. Rosaz – CERN – TE/VSC-SCC
On behalf of the SCC section

## Slide 2: Outline
Methods / Materials
Main applications
NEG films
a-C films
SC thin films
Challenges

## Slide 3: Methods / Materials

## Slide 4: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition

## Slide 5: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-1 mbar)

## Slide 6: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-1 mbar)

## Slide 7: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-1 mbar)

## Slide 8: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-1 mbar)
Diode Sputtering
Simple set-up
High working pressure
higher contamination
low energy
~20cm
Courtesy P. Costa-Pinto

## Slide 9: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))

## Slide 10: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-

## Slide 11: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-
Magnetron Sputtering

## Slide 12: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-
Low working pressure
High coating rate
More complex set-up

## Slide 13: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-
Low working pressure
High coating rate
More complex set-up

## Slide 14: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-
Low working pressure
High coating rate
More complex set-up

## Slide 15: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-
Low working pressure
High coating rate
More complex set-up

## Slide 16: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Ar (10-4/-3 mbar))
e-
Low working pressure
High coating rate
More complex set-up
Courtesy P. Costa-Pinto
Courtesy S. Leith

## Slide 17: Needs and technological solutions
Main requirements:
metallic thin films
Ultra-pure (UHV compatibility)
Technological choice: Physical Vapor Deposition
Direct Current Magnetron Sputtering
DC power supply
Power regulated
High coating rate
Poor conformality, porosities
Pulsed DCMS
Pulsed DC power supply
Arc mitigation
Dielectrics
Reactive sputtering
High Power Impulse Magnetron Sputtering
Pulsed power supply
Low duty cycle (~2%)
Metallic vapor ionization (~70%)
Dense layers (using biasing voltage)
Bombardment energy control
Low substrate heating
Low coating rate
Ar (10-4/-3 mbar))
e-
Low working pressure
High coating rate
More complex set-up

## Slide 18: Main Applications

## Slide 19: Thin films for accelerator complex

## Slide 20: Thin films for accelerator complex
Non Evaporable Getters Ti-Zr-V

## Slide 21: Thin films for accelerator complex
Accelerating Cavities (Nb/Cu)
Non Evaporable Getters Ti-Zr-V

## Slide 22: Thin films for accelerator complex
Accelerating Cavities (Nb/Cu)
Non Evaporable Getters Ti-Zr-V
Cu coating on graphite blocks (collimation)

## Slide 23: Thin films for accelerator complex
Accelerating Cavities (Nb/Cu)
Non Evaporable Getters Ti-Zr-V
Cu coating on graphite blocks (collimation)
High resistivity coatings on ceramics

## Slide 24: Thin films for accelerator complex
Accelerating Cavities (Nb/Cu)
Non Evaporable Getters Ti-Zr-V
Cu coating on graphite blocks (collimation)
High resistivity coatings on ceramics
Low Secondary Electron Yield coatings

## Slide 25: Non Evaporable Getters

## Slide 26: NEG coatings
NEG
Temperature
Time
RT
Activation temperature
Oxide layer
Oxygen in the film
Active surface for pumping
Chemically adsorbing gas molecules (CO, O2, H2O, CO2, N2, H2).
Not pumped: noble gases and CH4 (at room temperature)
Principle

## Slide 27: NEG coatings
NEG
Temperature
Time
RT
Activation temperature
Oxide layer
Oxygen in the film
Active surface for pumping
Chemically adsorbing gas molecules (CO, O2, H2O, CO2, N2, H2).
Not pumped: noble gases and CH4 (at room temperature)
Principle
Why is it interesting?
…
…
PUMP

## Slide 28: NEG coatings
NEG
Temperature
Time
RT
Activation temperature
Oxide layer
Oxygen in the film
Active surface for pumping
Chemically adsorbing gas molecules (CO, O2, H2O, CO2, N2, H2).
Not pumped: noble gases and CH4 (at room temperature)
Principle
Why is it interesting?
…
…
PUMP
P(x)
x
Pmax (no NEG)

## Slide 29: NEG coatings
NEG
Temperature
Time
RT
Activation temperature
Oxide layer
Oxygen in the film
Active surface for pumping
Chemically adsorbing gas molecules (CO, O2, H2O, CO2, N2, H2).
Not pumped: noble gases and CH4 (at room temperature)
Principle
Why is it interesting?
…
…
PUMP
P(x)
x
Pmax (no NEG)
Pmax (NEG)

## Slide 30: NEG production at CERN
3mm wires of Ti, Zr and V

## Slide 31: NEG production at CERN
3mm wires of Ti, Zr and V

## Slide 32: NEG production at CERN
3mm wires of Ti, Zr and V
>3km of beam pipes in the LHC
Courtesy P. Costa-Pinto

## Slide 33: NEG production beyond CERN

## Slide 34: NEG production beyond CERN
Courtesy P. Costa-Pinto

## Slide 35: a-C coatings

## Slide 36: e- Cloud Problematic
p+
p+
p+
p+
hν
Sec. e-
Electron Stimulated Desorption
Prim. e-
Thermal load
Courtesy P. Costa-Pinto

## Slide 37: e- Cloud Problematic
Mitigation
Reduce Secondary Electron Yield of the surfaces
p+
p+
p+
p+
hν
Sec. e-
Electron Stimulated Desorption
Prim. e-
Thermal load
Courtesy P. Costa-Pinto

## Slide 38: e- Cloud Problematic
Mitigation
Reduce Secondary Electron Yield of the surfaces
p+
p+
p+
p+
hν
Sec. e-
Electron Stimulated Desorption
Prim. e-
Thermal load
Courtesy P. Costa-Pinto

## Slide 39: e- Cloud Problematic
Mitigation
Reduce Secondary Electron Yield of the surfaces
p+
p+
p+
p+
hν
Sec. e-
Electron Stimulated Desorption
Prim. e-
Thermal load
Courtesy P. Costa-Pinto

## Slide 40: Coatings for our machines (in-situ)
> 200 components coated in the SPS tunnel
Courtesy P. Costa-Pinto

## Slide 41: Coatings for our machines (in-situ)
> 200 components coated in the SPS tunnel
doi:10.18429/JACoW-IPAC2021-WEPAB338
Courtesy P. Costa-Pinto

## Slide 42: Coatings for our machines (ex-situ)
doi:10.18429/JACoW-IPAC2021-WEPAB338
Courtesy W. Vollenberg

## Slide 43: Superconducting thin films

## Slide 44: Accelerating cavities

## Slide 45: Needs
Superconducting thin film (Nb)
Low surface resistance (nOhms)
Low power consumption (high quality factor)
High accelerating fields
PURITY AND CLEANLINESS ARE CRITICAL

## Slide 46: Activities overview
LEP
216 elliptical cavities (352 MHz) coated in industry
LHC
21 elliptical cavities (400MHz) coated in industry
8 new spares to be manufactured
SOLEIL
2 elliptical cavities (352 MHz) coated at CERN
HIE-ISOLDE
23 quarter wave cavities (101 MHz) coated at CERN
R&D Programs
1.3 / 1.5 GHz / low beta 704MHz Cu cavities
Others
Cornell Cavity (200MHz), Super-3HC cavities (double cell 1.5 GHz)
FCC
400/800 MHz elliptical cavities
WOW (Nb/Cu crabbing cavities)

## Slide 47: Methods

## Slide 48: Methods

## Slide 49: Methods

## Slide 50: Challenges / Opportunities

## Slide 51: NEG coatings
ELETTRA Chambers
927 mm
6.5o
17
mm
110 mm
Electrons
chamber
photons
chamber
Defining
coating method
Coating recipe
Transfer to industry for production (72 chambers)
Courtesy S. Saroglia

## Slide 52: a-C coatings: Beam Screens Treatment project
LHC in-situ coating of the cryomagnets
Goal: reduce overall e-cloud induced heat load
In total: 10.6 km of beam screen to be coated (2026-2028)
Coating by sections of 53m
Full mock-up to be built
Coating robots to be designed and built
Limited space < 250 mm
Courtesy V. Petit

## Slide 53: a-C coatings: Beam Screens Treatment project
LHC in-situ coating of the cryomagnets
Goal: reduce overall e-cloud induced heat load
In total: 10.6 km of beam screen to be coated (2026-2028)
Coating by sections of 53m
Full mock-up to be built
Coating robots to be designed and built
Modular sputtering source displaced by cables
Courtesy V. Petit

## Slide 54: SC coatings
Reduce surface resistance
Increase maximum reachable field

## Slide 55: SC coatings
Reduce surface resistance
Increase maximum reachable field
LHC
FCC-ee
2-cell
1-cell
4.5 K
2 K
1.7 K
4.5 K
Courtesy F. Peauger

## Slide 56: SC coatings
Reduce surface resistance
Increase maximum reachable field
LHC
FCC-ee
2-cell
1-cell
4.5 K
2 K
1.7 K
4.5 K
Courtesy F. Peauger

## Slide 57: SC coatings
Reduce surface resistance
Increase maximum reachable field
Mobile and compact sputtering source

## Slide 58: SC coatings
Trending up field
New investments
Courtesy D. Smekens

## Slide 59: Conclusion
Wide use of surface modification by thin film coating
Broad range of applications / materials / substrates
Short term future of CERN strongly relies on that expertise
Worldwide demand for coatings for accelerators
CUSTOM COATING SETUPS : industry support needed
- Setup manufacturing
- Targets procurement
- Large productions (outsourcing)

## Slide 60: Thank you for your attention