Timing Characterization of LGADs for Space Based Applications
A. Bisht, M. Boscardin, F. Caso, L. Cavazzini, M. Centis Vignali,
F. Ficorella, O. Hammad Ali, G. Paternoster
lcavazzini@fbk.eu

---
Energy
Advantages of Timing
Identification of back-scattered hits from calorimeters
Time of Flight (ToF) measurements
Improved e/p
Requirements in Space
Power consumption
Timing O(100 ps)
Large Channel size ← (Small Particle Flux)
But are produced with channels of few mm2
Shower
Incoming direction
The Scientific Reason
LGADs are good candidates: Time resolution O(10 ps)...

---
Layout Types
Type 1: Open Frame
Type 2: Fully Metallized, Contacts at the edge of the active area
Type 3: Fully Metallized, Contact points spread in the active area
Active Thickness
50 um
100 um
150 um
Active Area
6.25 mm2
25 mm2
100 mm2
Type 3
Type 1
Type 2
2
3
Space LGAD production

---
Setup: Scanning TCT, Particulars
Infra-Red (1060 nm) and Red (600 nm) pulsed laser
X/Y translation stage (0.8 um precision)
Beam Monitor
1 MIP calibration with radioactive source
[A. Bisht, Development of Low Gain Avalanche Detectors for Astroparticle Physics Experiments in Space, Trento 2023]
PCB: FNAL 16 channels
The Setup

---
LGAD
PIN
Gain

---
Two Acquisitions:
Single Waveform → Noise Estimation
Average Waveform → Slew Rate Estimation via Fitting the leading edge
Jitter

---
@200 V
1 cm2 → 80 ps
6.25 mm2 → 30 ps
Sensitive area plays a major role in the jitter
LGADs
Performance vs Area

---
Type 1: Open Frame
Type 2: Fully Metallized, Contacts at the edge of the active area
Type 3: Fully Metallized, Contact points spread in the active area
Gain smaller than expected (100)
1 cm2 LGADs
Performance

---
Type 1: Open Frame
Type 2: Fully Metallized, Contacts at the edge of the active area
Type 3: Fully Metallized, Contact points spread in the active area
☺ Jitter ~ 30 ps
1 cm2 LGADs
Performance

---
X
X
Reference point is the signal bond
“Standard” Hit position
X = Uniformity Check points
1 cm = 30 ps @ light speed
X
X
X
Signal formation and transmission variability
1 cm2 LGADs
Uniformity

---
Signal propagation within the sensor is comparable with jitter
Example with two different sensors
1 cm2 LGADs
Uniformity

---
We produced 1 cm2 devices which achieve:
100 um @ 300 V→35 ps
150 um @ 400 V→30 ps
Must be considered the Time of Arrival (< 50 ps) of the signal for the Resolution, for every layout
Conclusions
With the current technology, LGADs have time resolution capabilities O(10 ps), in case of a mm2 device.

---
A. Bisht, M. Boscardin, F. Caso,
L. Cavazzini, M Centis Vignali, F. Ficorella, O. Hammad Ali, G. Paternoster
lcavazzini@fbk.eu

---
Silicon detector with charge multiplication
Gain layer provides high-field region
Improved SNR: 5-10 times better than current PIN detectors
Excellent radiation hardness > 1015 neq/cm2
Time resolution O(10 ps)
Typical channel area 1-2 mm2
[G. Kramberger et al. NIMA 2018,
DOI: https://doi.org/ 10.1016/j.nima.2018.02.018]
LGADs in Brief

---
Preliminary: Capacitance

---
PCB channel Internal gain:
Beam Monitor Fluctuation
→Normalized Charge
Charge Sistematic Error ~ 8%
Preliminary: Charge vs Thickness

---
Calibration

---
Noise

---
LT-Spice Simulation
M = Gain
F = Excess Noise Factor
Jitter vs Thickness Simulations

---
The non-uniform energy deposition generated by an impinging MIP, amplified by the gain, creates variations of the signal shape on an event-to-event basis
https://doi.org/10.1016/j.nima.2022.166739
Landau Noise

---
SLAPP Production