## Slide 1
The numerous configurations of „interstitial boron“ and their involvement in ARP of LGADs 30.11.2023
Competence in Silicon
Kevin Lauer, Aaron Flötotto, Katharina Peh, Robin Müller, Wichard Beenken, Erich Runge, Dirk Schulze, Stefan Krischok, Thomas Ortlepp

## Slide 2
Existing ASi-Sii-defect model
Configurations of “interstitial boron” obtained by DFT calculations
Defect energy landscape
Explanation of ARP in LGADs by the BSi-Sii-defect mode
Summary
Acknowledgement
Overview

## Slide 3
Existing ASi-Sii-defect model

## Slide 4
ASi: acceptor atom is close to its substitutional position
Silicon interstitial is moving around (tetrahedral, hexagonal and split interstitial position assumed so far)
Model and experimental evidence recently reviewed [1]
ASi-Sii defect model
[1] K. Lauer et al. In: Phys. Status Solidi A (Aug. 2022), 2200099

## Slide 5
Configuration coordinate total (electronic + elastic) energy diagram [1] deduced from simulation results of the silicon interstitial [2]
Three charge states (+, 0, -) and three configurations (S1, S2 and S3) of ASi-Sii exist within the model
Energy barriers between configurations (e.g. E34, E46)
Negative charge state: S3 energetically favored
Neutral charge state: S2 and S1 energetically favored
ASi-Sii defect model
[1] K. Lauer et al., Physica Status Solidi (c) 14, 1600033 (2017).
[2] R. Jones et al., Materials Science and Engineering: B 159–160, 112 (2009).

## Slide 6
LID: light-induced degradation in silicon solar cells [1]
Transition 1 to 3: defect captures electrons under illumination
Transition 3 to 4: thermally stimulated, fast component of LID (FRC)
Transition 4 to 6: thermally stimulated, slow component of LID (SRC)
Transition 7 to 1: thermally stimulated, recovery of defect, without illumination
Explanation of LID by ASi-Sii defect model
[1] C. Möller et al., phys. stat. sol. RRL 7, 461 (2013)

## Slide 7
Configurations of “interstitial boron” obtained by DFT calculations

## Slide 8
DFT calculation of stable defect configurations
BSi Sii
Bi
BiSiiV
Six different stable configurations found
unstable
To be published A. Flötotto et al. 2024

## Slide 9
BSiSii defect in C3v configuration is shallow donor
DFT calculation of density of states (DOS)
Shallow donor
BsiSii defect (C3v)
Si bulk
Deep donor
BiSiiV defect (C1h)
To be published A. Flötotto et al. 2024

## Slide 10
Calculated electronic defect states
To be published A. Flötotto et al. 2024
shallow
deep
4 deep and 3 shallow centers found

## Slide 11
Defect energy landscape

## Slide 12
Calculated defect energy landscape
Calculation of all Minimal Energy Paths (NEB method) between defect configurations for each charge state
Ground state in positive charge state (p-type silicon) is C3v configuration
From DFT calculations: no energetical reason for the substitutional boron to follow the Watkins replacement reaction!
To be published A. Flötotto et al. 2024

## Slide 13
Explanation of ARP in LGADs by the BSi-Sii-defect mode

## Slide 14
Irradiation removes silicon atoms from lattice positions
At low temperatures (~20K) the removed silicon atom moves due to the energy gained by the collision event and is eventually captured by substitutional boron. [1]
At about room temperature the removed silicon atom might additionally diffuse thermally due to its weak mobility. [2]
Shallow donor mode of the BSi-Sii-defect (C3v) forms
Explanation of ARP in LGADs by BSi-Sii-defect mode
[1] K. Lauer et al., https://arxiv.org/abs/2311.07280
[2] A.N. Buzynin et al., NIMB, 186(1), 366–370 (2002).

## Slide 15
Summary
Comprehensive DFT calculations made for “interstitial boron”
Six different stable configurations found
Configuration with lowest energy in p-type silicon is C3v with boron residing very close to regular lattice position
C3v configuration is found to be a shallow donor
Explanation of acceptor removal phenomenon (ARP) in low-gain avalanche detectors (LGAD):
  Substitutional boron acceptor captures silicon atom, which was removed from a lattice position by irradiation.
  The resulting defect is a shallow donor.
  Amplification property of the boron gain layer in LGADs gets lost by irradiation.

## Slide 16
Thank you for your kind attention!
DFG Project SimASiSii:
DFG KR 2228/11-1, LA 4623/1-1, RU 1383/6-1
BMWI Project eLGAD (49MF220095)
Titular Saint
Franz of Assisi

## Slide 17
Thanks to RD50 for possibility to present crazy ideas!

## Slide 18
Back-up

## Slide 19
1 MeV electron irradiation of silicon generates silicon recoils exhibiting kinetic energy
~10% of these recoils have more than 80eV
~50% of these 10% travel more than 1nm (SRIM)
For 1016cm-3 boron density every 23th of these left recoils is able to reach a boron atom
If 10% of the silicon recoils reaching boron to form the BSi-Sii-defect, a BSi-Sii-defect density of about 1015cm-3 is under typical conditions (electron current and duration) possible.
=> Sufficient to explain EPR signals [1] without assumption of fast defect diffusion [2]
[1] G.D. Watkins, Physical Review B 12(12), 5824 (1975).
[2] K. Lauer et al., https://arxiv.org/abs/2311.07280
Possibility for silicon recoils to reach B atoms