## Slide 1: PU jacks mechanical simulations and tests proposals
Luca Piacentini (RTU)
29/09/2023

## Slide 2: Outline
Material model proposal for static studies
Material model validation by simulating the compression test
Compression simulation with 4 piston, no jack (SPS).
Additional discussion topics
Future tasks and proposals

## Slide 3: Material model proposal for static studies: hyperelastic model
Hyperelastic behaviour noted
Viscoelastic behaviour from previous load-unload tests
Chart: Stress - Strain
Stress-strain calculated curves from https://edms.cern.ch/document/2922835/1
Built in hyperelastic models on Ansys

## Slide 4: Material model proposal for static studies: hyperelastic model
Hyperelastic behaviour noted
Different proposed models from Ansys library
Ansys material definition workflow
  Import test data (true stress – true strain)
  Chose the fit model
  Fit the curve(s)
1
2
3

## Slide 5: Material model proposal for static studies: hyperelastic model
Hyperelastic behaviour noted
Different proposed models from Ansys library
Ansys material definition workflow
  Import test data (true stress – true strain)
  Chose the fit model
  Fit the curve(s)
Chart: Force - displacement
https://edms.cern.ch/document/2922835/1
Stress-strain curve calculation
  Assumed incompressibility (volume=constant)
  Assumed cylindric shape constant (no barreling)
V0
V0
Chart: Stress - Strain

## Slide 6: Material model proposal for static studies: hyperelastic model
Hyperelastic behaviour noted
Different proposed models from Ansys library
Ansys material definition workflow
  Import test data (true stress – true strain)
  Chose the fit model
  Fit the curve(s)
Mooney Rivlin 9par
Yeoh 3rd order
MR 9 better fit to uniaxial test data, but grows exponentially on biaxial and shear
Yeoh 3rd worse fit to uniaxial, does not explode for low strain

## Slide 7: Material model validation by simulating the compression test
Mooney Rivlin 9par fails to converge when refining mesh, different measures tried, no results + high element distortion
Yeoh 3rd order: solution converges with finer mesh, the elements seem to behave better
Simulate the compression test (hard barreling hypothesis)
Check the force displacement curve against the real tests

## Slide 8: Material model validation by simulating the compression test
Simulate the compression test (hard barreling hypothesis)
Check the force displacement curve against the real tests
Chart: Compression test VS compression FEA

## Slide 9: Material model validation by simulating the compression test
Simulate the compression test (hard barreling hypothesis)
Check the force displacement curve against the real tests
Chart: Force-displacement
Max vertical displacement 10 mm (2 pads, ±5 mm each)

## Slide 10: Compression simulation ShA 90 with 4 piston, no jack (SPS)

## Slide 11: Compression simulation ShA 90 with 4 piston, no jack (SPS)
No jack influence, ShA 90 PU pad, 1/8 symmetry.
Max vertical displacement on upper face 6.5 mm (Average: 5.16 mm ½ of real case ± 10 mm)
Max Von-Mises stress 41.8 MPa, average: 8.3 MPa, SIF: 5 (lower bound due to mesh quality)

## Slide 12: Compression simulation ShA 75 with 4 piston, no jack (SPS)
No jack influence, ShA 75 PU pad, 1/8 symmetry.
Max vertical displacement on upper face 6.7 mm (Average: 5.17 mm ½ of real case ± 10 mm)
Max Von-Mises stress 15.2 MPa, average: 3.2 MPa, SIF: 5 (lower bound due to mesh quality)

## Slide 13: Additional discussion topics
Phases of PU jack alignment:
  Pre-squeeze/load/V alignment/H alignment
  Pre-squeeze/load/H alignment/V alignment
  Load/V alignment/H alignment
  Load/H alignment/V alignemnt
Stress requirement:
  Average & peak VM
  Average & ,

## Slide 14: Future tasks and proposals
Tasks:
Increase the imposed deformation to meet application range
Add the effect of a loaded flat piston in SPS (WIP)
Add the effect of a loaded inclined piston in SPS
Analyse the LHC study case
Proposals to further tune the material model:
Tension test on subsize specimens with extensometer, (cut from pads, 10/15 axial & orthogonal) possibility of DIC. M. Crouvizier
New compression test on pads with DIC (10?)
Shear (long term)
Bi-axial (long term)

## Slide 15: Test samples geometry
https://doi.org/10.28991/cej-030966