## Slide 1: Limitations from LHC RF Fingers
Presenters: Chiara Antuono and Patrick Krkotić
G. Bregliozzi, S. Calatroni, E. De La Fuente, A. Galloro, B. Salvant, L. Sito, C. Zannini
Joint Accelerator Performance Workshop, 6 December 2023

## Slide 2: Contents
01
RF Finger Module Failure Beam and X-rays revelations
02
Understanding of the Failure Material and Production Analysis
03
Impedance Assessment Experiments and Simulations
04
Possible Mitigation Strategies Ongoing Impedance and Vacuum Studies

## Slide 3
May 25-26, 2023: Pressure spikes within the vacuum sector A4L1 during the fill ID 8828 (1.63 1011 p/b – 2358 bunches) lead to a beam dump due to losses.
Fault recording in 2023

## Slide 4
ID212.7 RF Finger Module
Type of module :
Circular
Standard RF Finger
Aperture 212.7 mm
Installation length 400 mm
Spring ensures the electrical contact between fingers/transition tube
Transition Tube
Cu OFE
RF finger CuBe + Ag plating
Contact point
Tension spring AISI 301
Fault recording in 2023

## Slide 5
Visual inspection:
  annealed/plasticised spring  localized temperature increase to more than 500°C
  localised extremely high temperature producing debris, sputtering and sublimation of austenitic stainless-steel spring
  cascade of failure with consequent loss of electrical contact of RF fingers on the transition tube perimeter
Fault recording in 2023

## Slide 6
Inspection of all 71 modules present in the LHC machine
  1 failed, 8 degraded
Higher opening (≈2-3 mm) between consecutive RF fingers
Nominal gap 1.5 mm
LSS1
VMBGA.C4L1.X – A4L1.X – failed module
VMBGA.B4R1.X – A4R1.X – spring degradation
LSS5
VMBGA.C4R5.X – A4R5.X – spring degradation
VMBGA.B4R5.X – A4R5.X – spring degradation
LSS8
VMBGG.A4L8.X – A4L8.X – spring degradation
VMBGC.A4R8.X – A4R8.X – spring & finger degradation
VMBGD.A4R8.X – D4R8.X – finger degradation
LSS4
VMBGA.A5R4.B – D5R4.B – finger & spring degradation
2 Beams
1 Beam
Horizontal beam offset
X-ray investigation

## Slide 7
02
Understanding of the Failure Material and Production Analysis

## Slide 8
Stainless Steel 1.4310 AISI 301 (X10CrNi18-8)
Good mechanical properties and corrosion resistance
  The material can theoretically be used up to +250°C
Effects of the bake-out cycle: elasticity of the spring versus different elongations (EDMS)
  As received: compatible with specifications
  8 days 250°C bake out: no degradation
  8 days 330°C bake out: removal of pre-load and length increase
Chart: Traction Tests Before and After Bake-Out
| 0 | 0.98100000000000009 | 1.9620000000000002 | 2.9430000000000001 | 3.9240000000000004 | 4.9050000000000002 | 5.8860000000000001
Spring 4 As Received | 0 | 0.011828 | 0.097503 | 0.18318 | 0.26885 | 0.35184 | 0.43483
Spring 4 After BO at 15% Extension | 0 | 0.041398 | 0.12439 | 0.21006 | 0.29305 | 0.37604 | 0.46171
Spring 4 After BO 330 at 15% Extension | 0.0080645 | 0.092473 | 0.17546 | 0.25845 | 0.34143 | 0.42442 | 0.50741
Specification Limits | 0 | 0 | 0.28632
Specification Limits | 0 | 0 | 0.41453
Chart: Traction Tests Before and After Bake-Out
| 0 | 0.98100000000000009 | 1.9620000000000002 | 2.9430000000000001 | 3.9240000000000004 | 4.9050000000000002 | 5.8860000000000001
Spring 4 As Received | 0 | 0.011828 | 0.097503 | 0.18318 | 0.26885 | 0.35184 | 0.43483
Spring 4 After BO at 15% Extension | 0 | 0.041398 | 0.12439 | 0.21006 | 0.29305 | 0.37604 | 0.46171
Spring 4 After BO 330 at 15% Extension | 0.0080645 | 0.092473 | 0.17546 | 0.25845 | 0.34143 | 0.42442 | 0.50741
Specification Limits | 0 | 0 | 0.28632
Specification Limits | 0 | 0 | 0.41453
Chart: Traction Tests Before and After Bake-Out
| 0 | 0.98100000000000009 | 1.9620000000000002 | 2.9430000000000001 | 3.9240000000000004 | 4.9050000000000002 | 5.8860000000000001
Spring 4 As Received | 0 | 0.011828 | 0.097503 | 0.18318 | 0.26885 | 0.35184 | 0.43483
Spring 4 After BO at 15% Extension | 0 | 0.041398 | 0.12439 | 0.21006 | 0.29305 | 0.37604 | 0.46171
Spring 4 After BO 330 at 15% Extension | 0.0080645 | 0.092473 | 0.17546 | 0.25845 | 0.34143 | 0.42442 | 0.50741
Specification Limits | 0 | 0 | 0.28632
Specification Limits | 0 | 0 | 0.41453
Chart: Traction Tests Before and After Bake-Out
| 0 | 0.98100000000000009 | 1.9620000000000002 | 2.9430000000000001 | 3.9240000000000004 | 4.9050000000000002 | 5.8860000000000001
Spring 4 As Received | 0 | 0.011828 | 0.097503 | 0.18318 | 0.26885 | 0.35184 | 0.43483
Spring 4 After BO at 15% Extension | 0 | 0.041398 | 0.12439 | 0.21006 | 0.29305 | 0.37604 | 0.46171
Spring 4 After BO 330 at 15% Extension | 0.0080645 | 0.092473 | 0.17546 | 0.25845 | 0.34143 | 0.42442 | 0.50741
Specification Limits | 0 | 0 | 0.28632
Specification Limits | 0 | 0 | 0.41453
Tension spring properties

## Slide 9
Visual inspection and radiography indicate that heating of the spring is the triggering mechanism of the first module failure
Finite Element Method simulations via COMSOL were conducted to determine the power deposition necessary to heat the spring in a steady state (EDMS)
uniform power distribution
localised power
Thermal simulations

## Slide 10
Visual inspection and radiography indicate that heating of the spring is the triggering mechanism of the first module failure
Finite Element Method simulations via COMSOL were conducted to determine the power deposition necessary to heat the spring in a steady state (EDMS)
uniform power distribution
localised power
Annealing condition of the spring: annealing/plasticisation of the spring at a temperature of 500°C
130 mW
500 °C
~ 27 W
Thermal simulations

## Slide 11
In 2004, BINP initiated the production using a single sheet of CuBe
  RF Finger width 3.6 mm
  Distance between fingers 1.47 mm
The RF finger was cut into 3 identically segments
  44 fingers each
  Welded individually on the bottom flange of the RF insert
smaller spacing
RF finger production

## Slide 12
03
Impedance Assessment Experiments and Simulations

## Slide 13
Impedance measurements - field leakage
Beam-like excitation on axis
Port 2
leakage
leakage
Port 3
Port 1
It is the mechanism that allows some of the beam induced power to be dissipated on the spring
spring
spring
Low frequency resonances (below vacuum pipe cut-off frequency)
  Field leakage through RF fingers / transition tube
Transmission between Port 1 and Port 3

## Slide 14
EM fields leak through the pipe slots
The simulations confirmed the presence of field leakage from the fingers and the transition tube
Even higher field leakage due to RF finger spacing
Electromagnetic simulation - field leakage

## Slide 15
Very similar frequency response between simulation and measurements
  First resonance below 400 MHz
  Several resonances below pipe cut-off frequency
The simulation model is used for impedance assessment
Simulations vs Measurements : validation of the model
Virtual measurement setup reproduced in e.m. simulation

## Slide 16
07/12/23
* Power loss calculation in separated and common beam chambers of the LHC, C. Zannini, G. Rumolo, G. Iadarola, 5th International Particle Accelerator Conference, Dresden, Germany, June 2014
: beam spectrum
: angular revolution frequency
: offset of beam 1 from center
: offset of beam 2 from center
longitudinal impedances of orders 0 and 1
delay between arrival times of the two beams
Two beam power loss
Two beam power loss
Beam induced power assessment

## Slide 17
Lost contact case
Non symmetric RF fingers distribution
Lost contact fingers-transition tube
Degraded contact case
Non symmetric RF fingers distribution
Degraded contact fingers-transition tube
Ideal contact case
Non symmetric RF fingers distribution
Perfect contact fingers-transition tube
Loss of contact
larger gap
Impedance is more affected by production defects especially in presence of beam offset
Perfect contact
Design case
Symmetric RF fingers distribution
Perfect contact fingers-transition tube
Contact degradation between fingers-transition tube largely increases the beam induced power on the spring
Different scenarios studied
Notes: Δ𝑊 could be higher (inclusion of the 𝑍_(||)^1, first order impedance) or dominated by the 𝑍_(||)^1
Metti foto del contatto fingers/tube

## Slide 18
degraded contact
Lost contact
~200 W
~0.13 W
Annealing condition
  Temperature above 500° C
  ~0.13 W for localized power
  ~27 W for distributed power
0.07 W
~2 W
Worsening the quality of contact
ideal contact
EM simulations show localized heating
gap
beam
~27 W
Beam induced power loss on the spring

## Slide 19
In IP4,IP8 the degradation mechanism is somewhat different
  Due to the restriction of the beam pipe cavity-like structures
    Forest of quite strong resonances
      power could be dissipated on the fingers
      From thermal studies : it could explain fingers degradation
BSRT
VMBGA.A5R4.B
Identified Issue
VMBGC.A4R8.X
Identified Issues
TDIS
    Beam pipe restrictions in both IP4,IP8
Pipe restrictions
VMBGC.D4R8.X
Disclaimer : preliminary results
Pipe restrictions
IP4, IP8: observed finger degradation

## Slide 20
04
Possible Mitigation Strategies Ongoing Impedance and Vacuum Studies

## Slide 21
Replace and transform the current 71 modules in the ID212.7 RF contact with newly designed modules wherever it is possible to implement such a substitution . Anchor ‘unnecessary’ ID212.7 modules (EDMS)
WM
WM
WM
VC 5500 mm
VC 5500 mm
Could be suppressed
Deformable RF Finger (flexible)
Optimised Bellows (flexible and anchored)
Transformed ID 212.7 (anchored)
Essence of the mitigation strategy
Notes: Length of ID212 vacuum chambers in (304L SS) was defined by the height of the vacuum furnace -> Max 5.5 m
The layout was defined based on this length -> WM every 5.5m
During the bakeout (230C) the elongation of 11m of SS chambers is ≈32 mm that could be absorbed by the WM (Free length 380mm, Axial stroke of ± 20mm, Installation length of 400m)
Roughly half of the WM could be removed

## Slide 22
Fixed extremities
No spring and no possibility to lose electric contact
CuBe RF fingers
3 mm width
0.1 mm thickness
A Nominal height of 2.7 mm (11° angle) is considered for the nominal operation position.
Evaluation of the cumulative impact of 25 Modules on the LHC:
  The additional impedance contribution is compatible with beam stability requirements (EDMS)
Deformable RF Fingers – DRF

## Slide 23
Fixed Positioning
  Reallocate the thermal expansion during bake-out cycles to designated bellows
Robust thermal endurance
  10 mm solid copper material, engineered to withstand substantial heat loads should they manifest
Flange tube
Transition ring
Re-use part of the RF insert
New transition
Impedance
  Expected to behave as a straight vacuum chamber
Transformed ID212.7 Module in straight vacuum chamber

## Slide 24
13 Convolutions Bellow Ø 212.7 mm Stainless Steel
Secure choice concerning mechanical and thermal considerations
Rapid and cost-effective production
Higher impedance compared to the ID212.7 RF contact fingers
  Longitudinal and transverse impedance will be affected
    to be studied in detail
Optimised Bellows

## Slide 25
Replace and transform the current 71 modules in the ID212.7 RF contact with newly designed modules wherever it is possible to implement such a substitution. Anchor ‘unnecessary’ ID212.7 modules (EDMS)
Deformable RF Fingers
25 Modules
10 x IP1, 10 x IP 5, 5 x IP 8
Transformed ID 212.7 Modules
21 Modules
8 x IP 1, 8 x IP 5, 2 x IP 4, 3 x IP 8
Optimised Bellows
Production could start in Q2 2024
To be seen during 2024
Total
EYETS 23/24
YETS 24/25
Modules 71
Replaced modules 47
Replaced modules 24
Two-stages approach
Full consolidation in YETS 24/25
Essence of the mitigation strategy

## Slide 26
Conclusion and Outlook

## Slide 27
  1 Failure observed only in 2023 with a maximum total intensity of ~3.8e14 p. (with 1.63e11 ppb)
    Localized heating on spring enhanced by the beam offset and production defects
    24 module will keep the original spring+finger design
      No failure expected with ideal contact
      Failure can occur due to degraded contact quality
        An intensity threshold cannot be identified due to the strong
        dependence on contact quality
    Other possible failure mechanism (preliminary results)
        Damage of RF fingers in IP4,8
          heating of the RF fingers due to the machine layout
Do we expect additional failure in 2024 run?

## Slide 28
EN-MME
Thibaut Coiffet
Alessandro Dallocchio
Florent Fesquet
Ana Teresa P. Fontenla
Damien Jerome Foresy
Gonzalo A. Izquierdo
Jean-Marc Malzacker
Alexandre Porret
Laurent Prever-Loiri
TE-VSC
Giuseppe Bregliozzi
Sergio Calatroni
Paolo Chiggiato
Isabel Cuevaz
Thomas Da Silva
Florent Fesquet
Alessio Galloro
Jan Hansen
Patrick Krkotic
Fabrice Santangelo
Orlando Santos
Josef Sestak
Benoit Teissandier
Marc Thiebert
BE-ABP
Chiara Antuono
Elena De La Fuente Riccardo De Maria Stéphane Fartoukh
Lorenzo Giacomel
Nicolas Mounet
Yannis Papaphilippou
Giovanni Rumolo
Benoit Salvant
Leonardo Sito
Carlo Zannini
TE-MSC
Mariano Pentella
SY-RF
Ivan Karpov
Christine Vollinger
On behalf of…

## Slide 29
Thank you for your attention!
Any questions?

## Slide 30
01
WHAT IS BEAM IMPEDANCE?
Wakefields and Impedances
Backup

## Slide 31
Simulations Vs measurements : validation of the model

## Slide 32
Smaller diameter modules are expected to be less critical
    higher frequency modes
    Only 1 beam
    smaller beam offset
    less production defects
    lower impact of the machine layout
Do we expect failure of the smaller modules?
DN100
DN130
Smaller transition in terms of diameter
1 gap or 2
Easier production
Less prone to defect
How many modules built from 3 segments do we have in the LHC machine?
    ID212.7 & ID196 -> 71 units in total
    DN130 & DN100 have 2 segments: Less prone to gap problems (Max aperture <2-3 mm)
    DN80 & DN63 one single segments: Respected the tolerances of the drawings.
Can this problem happen to the other RF inserts?
    If the problem with the increased spacing is confirmed there is no reason to have the same failure module with warm modules inserts DN80 and DN63. DN130 and DN100 need further studies.
From G. Bregliozzi, LMC

## Slide 33: Spring Properties
Stainless Steel 1.4310 – AISI 301
(X10CrNi18-8)
Good mechanical properties and corrosion resistance
Capable of high tensile strength following cold work
Tensile strength: 2239-2254 N/mm2
Magnetic following cold work
Spring of module 5
…but most of it is totally amagnetic
Bregliozzi Giuseppe – TE-TM – 12th June 2023
33
The material 1.4310 can theoretically be used up to +250°C.
After production, the spring is heat treated. At least 30min at 250°. Then cool at room temperature.

## Slide 34: X rays – A4L1
VGI.628.4L1.X
TAN
Module 9
Module 8
Module 7
Module 6
VMBGA.C4L1.X
≈114 m from IP1
B2
B1
MBWX
Module 4
Module 3
Module 2
Module 1
Module 5
FAULTY

## Slide 35: X Rays – VMBGA.B4R5.X – Module 3

## Slide 36
X rays – A4L8
Double Beams
36
TCLIA
B2
B1
VMBGC.A4L8.X
Identified Issue
Bregliozzi Giuseppe – LMC – 18/10/2023
TCTPH & TCTPV

## Slide 37
X rays – A4R8 (E4R8.X8)
Double Beams
37
B2
B1
VMBGC.A4R8.X
Identified Issue
Bregliozzi Giuseppe – LMC – 18/10/2023
TDIS

## Slide 38: B4R8.X - VMBGC.E5R8.X
38
No spring coil degradation detected
Bregliozzi Giuseppe – LMC – 18/10/2023

## Slide 39
X rays – D5R4
Single Beam
39
BSRT
B2
B1
VMBGA.A5R4.B
Identified Issue
Bregliozzi Giuseppe – LMC – 18/10/2023
D3R4

## Slide 40: Pictures of VMBGA.A5R4.B

## Slide 41: Pictures of VMBGA.A5R4.B

## Slide 42: Module 5 RF & Insert with new and old spring
Bregliozzi Giuseppe – TE-TM – 12th June 2023
42
The OLD spring compared to a new one is about 3-4 cm longer.