## Slide 1: Some bulk Cu and aC coating preliminary results obtained with the Vacuum Pilot Sector during 2023 run
Quentin DUONG
TE – VSC – VSM
quentin.duong@cern.ch
06/12/2023

## Slide 2: Outline
Description
72b and hybrid fills at 450 GeV
Hybrid physics fill at 6.8 TeV
Electron energy distribution for bulk Copper
TE – VSC – VSM

## Slide 3: Disclaimer
I present the observations performed on some of the 2023 fills
Results are therefore preliminary
TE – VSC – VSM

## Slide 4: Description
TE – VSC – VSM

## Slide 5: Layout
TE – VSC – VSM
  Vacuum Pilot Sector (VPS)
  Location: between Q4L8 and Q5L8
  2 beamlines :
    External: B1 (Blue beamline)
    Internal: B2 (Red beamline)
  Installed in 2015:
    1.4m-long thick a-C coating ~500nm
    1.4m-long bulk Cu
  a-C
  Cu

## Slide 6: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by bunch ionising the residual gas
  Secondary electrons: induced by primary electrons, accelerated by successive bunches, hitting the surface
TE – VSC – VSM
Electron
cloud
Image current
Beam pipe
p+
p+
primary e-
photoelectron
e-
secondary e-
ionised gas i+
accelerated e-
free electron e-
PEY
SEY
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)
  Secondary Electron Yield (SEY)

## Slide 7: Electron current and energy detection
TE – VSC – VSM
A
A
p+
p+
Electron
cloud
Image current
Beam pipe
[0 ; 350] V
[-1.5 ; 1.5] kV
+9V
  Electron pickups
  Energy Analyser
  Electron pickups
    Electromagnetic shield: 7%-transparency
    Geometrical surface:
    Bulk copper collector
    Positively biased:
    Measurement: « electron cloud current »
  Energy Analyser (only copper station)
    « Retarding Field Analyser (RFA) »
    Electron pickup: with bias
    Biased filtering grid:
    Biased filtering grid:
    Measurement:
    « electron cloud current below »
Cu
Cu
Cu
Cu
Cu

## Slide 8: Total pressure detection
TE – VSC – VSM
p+
p+
Image current
Beam pipe
  Total pressure gauges
    Bayard-Alpert gauges « VGI »
    Measurement: « desorbed gas pressure »
  Total pressure gauges
  Two main material properties for gas increase:
  Photodesorption
  Electrodesorption
ionised gas i+
free electron e-
Electron
cloud
electrodesorbed gas
photodesorbed gas
PSD
ESD
  Pressure elevation during LHC functionning
  Photodesorbed gas: induced by photons hitting the surface
  Electrodesorbed gas: induced by electrons hitting the surface

## Slide 9: 72b and hybrid fills at 450 GeV
TE – VSC – VSM
72b: fills 8673
Hybrid (7*8b4e+3*36b): fill 8736

## Slide 10: Electron cloud comparisons for 72b and hybrid fills
TE – VSC – VSM
  72b
  Hybrid
a-C B1
Cu B1
Cu B1
  Detection limit:
  (Corresponds to the mean baseline plus of its gaussian distribution.)
Electron flux [A.cm-2]
  Copper is 4 orders of magnitude above carbon.
  Carbon below detection limit for 8b4e.
  For copper:
B1 intensity
B1 intensity
Total beam intensity [p+]
a-C B1

## Slide 11: Pressure comparisons for 72b and hybrid fills
  Hybrid
TE – VSC – VSM
  72b
a-C B1
Cu B1
a-C B1
Cu B1
  At equal beam intensity for copper:
  Pressure in carbon station possibly induced by RF bridge.
  Thus, pressure rise cannot always be considered as equivalent to electron presence.
B1 intensity
B1 intensity
Pressure [mbar]
Total beam intensity [p+]

## Slide 12: Electron cloud response of copper during injection
TE – VSC – VSM
Electron flux 72b
[A.cm-2]
Hybrid
72b
  More bunches needed for hybrid fill to reach linear behaviour
  For high number of bunches:
Electron flux hybrid
[A.cm-2]
:72b trains
  Hybrid train:
Hybrid trains:
4
6
8
10
12
14
28
21
15
13
10
8
5
0
400
800
1200
1600
2000
Number of bunches

## Slide 13: Cu ESD for 72b and hybrid fills
TE – VSC – VSM
  Pressure rise assumed to be induced only by
  Electrostimulated desorption computation for copper station
  Measured ESD correspond to a copper surface at a dose of a few
M. Haubner et al. Vacuum 207 (2023) 111656
Filling scheme |  | 
72b | 8 | 
Hybrid |  | 
Filling scheme |  | 
72b |  | 
Hybrid |  | 

## Slide 14: Hybrid physics fill at 6.8 TeV
TE – VSC – VSM
Hybrid (7*8b4e+5*36b): 8741

## Slide 15: Photoelectrons during energy ramp-up
TE – VSC – VSM
a-C B1
Cu B1
Electron flux [A.cm-2]
a-C Cu
  Photoelectrons detected by electron pickup at which corresponds to a synchrotron radiation critical energy of 2 eV, matching the work function of copper or carbon (~ 4-5 eV)
Energy
B1 intensity
Total beam intensity [p+]
Beam energy [GeV]

## Slide 16: Electron cloud current evolution during a fill
  Provided the knowledge of the number of photons absorbed in the stations, one can compute their Photo Electron Yield
TE – VSC – VSM
a-C B1
Cu B1
Electron flux [A.cm-2]
B1 intensity
Energy
  Multipacting occuring only for copper
  Bumbed curve for copper
  Flat curve for carbon
  Only photoelectrons at the end of the fill
  Both signals scale with beam intensity

## Slide 17: Electron energy distribution for bulk Copper
TE – VSC – VSM
Hybrid (7*8b4e+5*36b): 9072

## Slide 18: During energy ramp-up
TE – VSC – VSM
  No significant impact of the beam energy ramp-up on the electron energy distribution.
 |  |  |  | *
620 | 1.60 | 6.0 | 203 | 269
2674 | 1.60 | 5.8 | 202 | 266
6799 | 1.59 | 5.9 | 203 | 263
620 | 1.60 | 6.0 | 203 | 269
2674 | 1.60 | 5.8 | 202 | 266
6799 | 1.59 | 5.9 | 203 | 263
  Double lognormal fit
  Assess the energy peaks of secondary and accelerated electrons
    Measurement step around : 3-5 eV
    Measurement step around : 30 eV
  Cannot describe measurements in-between peaks and above accelerated one
*J. Scott Berg. CERN LHC Project Note 97, July 1997.
Electron energy spectrum: Fill 9072
Normalised signal
Secondary
electrons
Beam kicked
electrons

## Slide 19: At Stable Beam: t = 0h
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Bunch intensity:
  Fit results
  Low energy:
  High energy:

## Slide 20: At Stable Beam: t = 6h
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Bunch intensity:
  Fit results
  Low energy:
  High energy:

## Slide 21: At Stable Beam: t = 11h
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Bunch intensity:
  Fit results
  Low energy:
  High energy:

## Slide 22: Impact of the beam intensity at 6800GeV
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Stable Beam |  |  |  | *
0H | 1.59 | 6 | 203 | 263
6H | 1.23 | 6 | 120 | 166
11H | 0.99 | 6 | 89 | 114
0H | 1.59 | 6 | 203 | 263
6H | 1.23 | 6 | 120 | 166
11H | 0.99 | 6 | 89 | 114
  No impact of the bunch intensity on the energy of the secondary electrons.
  Decrease of the energy gained by accelerated electrons with bunch intensity.
  Kick energy formulae gives a reasonable energy assessment at 30%
*J. Scott Berg. CERN LHC Project Note 97, July 1997.

## Slide 23: Summary
TE – VSC – VSM
  At 450GeV:
  Electron cloud responses for copper orders of magnitude above carbon ones
  For copper,
  At a certain number of bunches,
  Pressure rise is not equivalent to local electron cloud presence
  During a hybrid physics fill lifetime:
  Photoelectrons detected for
  Multipacting only in copper
  Electron energy distribution:
  No significant impact of the energy ramp-up on the electron energy distribution
  Decrease of the accelerated energy peak with ppb
  Kick energy formula is a reasonable first approximation

## Slide 24: Perspectives
TE – VSC – VSM
  Electrostimulated and Photostimulated Desorption (ESD, PSD) computations with Residual Gas Analyser
  Photoelectron Yield (PY) estimations
  Secondary Electrons Yield (SEY) evaluation with RFA by refining measurements around electron peaks
  Measurements of the electron cloud bunch by bunch with a scope
  Heat load evaluation with calorimeters
  Confrontation of measurements and parameter evaluations against simulations (PyEcloud, Vasco, Molflow, Synrad…)
  Fill parameters which may help electron cloud parameters assessment:
  Long fill (> 10h) at of hybrid scheme with beam intensity > with long injection time (> 2h) to disentangle electrons from photons contributions
  Long fill (> 5h) at of spaced trains and 50ns inter-bunch scheme with and to evaluate photons contribution
  Use of a “calibration” fill to assess evolution of the parameters along the year

## Slide 25: Backups
TE – VSC – VSM

## Slide 26: Station 2 – Amorphous carbon
TE – VSC – VSM
St 1
St 3
z
Ext
Int
7%
7%
7%
7%
K4
K5
Canon 1-12
K6
Sc3a
K16
K18
K17
Canon 1-12
Sc3b
Liner B23
Liner R25
129
110
124
122
121
120
119
118
116
Dash line : Downer side
Red line : Scope
NU : Unused
cal : calorimeter
xx % : pickup with a xx%-transparent grid
Trig : trigger
ph : photodetector
Blue line : Keithley with variable bias
Position :
X
X
X
X
VGI : Bayard-Alpert Gauge (BAG)
VGRB : Pirani gauge​
VQM : Vacuum Quality Monitor
RGA : Residual Gas Analyser
VGPB : Penning Gauge
N : NEG cartridge
X
VPIA : Vacuum Pump
Unused
VF : Vacuum Flange
.5L8.
B
R
RFA : Retarding Field Analyser
kick : kicker (Electron Kicker Detector)

## Slide 27: Station 3 – New unbaked copper
TE – VSC – VSM
St 2
St 4
z
Ext
Int
7%
7%
7%
50%
15%
50%
7%
15%
Sc1a
K7
Canon 1-12
K8
Sc2a
K26
K9
K27
Canon 1-12
Sc2b
K21
Sc1b
Liner B26
Liner R27
92
73
87
85
84
83
82
81
79
Dash line : Downer side
Red line : Scope
Int
NU : Unused
cal : calorimeter
xx % : pickup with a xx%-transparent grid
Trig : trigger
ph : photodetector
Blue line : Keithley with variable bias
Position :
X
X
X
X
VGI : Bayard-Alpert Gauge (BAG)
VGRB : Pirani gauge​
VQM : Vacuum Quality Monitor
RGA : Residual Gas Analyser
VGPB : Penning Gauge
N : NEG cartridge
X
VPIA : Vacuum Pump
Unused
VF : Vacuum Flange
.5L8.
B
R
RFA : Retarding Field Analyser
kick : kicker (Electron Kicker Detector)

## Slide 28: Station 4 – Old unbaked copper
TE – VSC – VSM
St 3
LHCb
z
Ext
Int
Liner 7
Liner 8
55
36
50
48
46
44
42
7%
0,2%
K23
K24
Canon 1-12
Canon 1-12
SHV3
SHV1
K12 + SHV2
K22 + SHV4
K11
HV BIAS 28
0,2%
7%
Dash line : Downer side
Red line : Scope
Blue line : Keithley with variable bias
NU : Unused
cal : calorimeter
xx % : pickup with a xx%-transparent grid
Trig : trigger
ph : photodetector
4
Position :
X
X
X
X
VGI : Bayard-Alpert Gauge (BAG)
VGRB : Pirani gauge​
VQM : Vacuum Quality Monitor
RGA : Residual Gas Analyser
VGPB : Penning Gauge
N : NEG cartridge
X
VPIA : Vacuum Pump
Unused
VF : Vacuum Flange
.5L8.
B
R
RFA : Retarding Field Analyser
kick : kicker (Electron Kicker Detector)
Pt100 air B
Pt100 air R

## Slide 29: Hybrid and 72b filling schemes
TE – VSC – VSM
Ppb vs Bunch site number for hybrid (top) and 72b (bottom) filling scheme
1 turn of the LHC
« hybrid»
7*(8b4e) + 3*(36b)
  Fill 8673
  Fill 8736
2*(72b)
 | Filling scheme |  |  | 
8736 | Hybrid | 1818 | 1.43 | 2.60
8673 | 72b | 1020 | 1.42 | 1.45
 | Filling scheme |  |  | 
8736 | Hybrid | 1818 | 1.43 | 2.60
8673 | 72b | 1020 | 1.42 | 1.45

## Slide 30: ESD formula and plots
TE – VSC – VSM
a-C B1
Cu B1
a-C B1
Cu B1
Pressure / Electron flux [mbar/(A.cm-2)]
B1 intensity
B1 intensity
a-C Cu
Pressure / Electron flux [mbar/(A.cm-2)]
a-C Cu
  Fill 8673 – 72b
  Fill 8736 – hybrid

## Slide 31: Ecloud as a function of beam mean ppb
TE – VSC – VSM
  Multipacting presence
  Barely present for carbon: ecloud mainly dominated by photoelectrons
  Huge contribution for copper
  Assymptotic root method
  Root of linear asymptotic behaviour for high ppb
  Method to assess the variations of multipacting with time
linear
multipacting
regime
primary electrons
regime
a-C B1
new-Cu B1
Electron flux [A.cm-2]
Mean ppb
Mean ppb
  Assymptotic root method is NOT aimed at giving a multipacting threshold as ecloud effect has been identified for lower ppb.
Electron flux vs Mean ppb: Fill 9072

## Slide 32: Electron flux scaling with beam intensity at end of fill
TE – VSC – VSM
Electron flux normalised by beam intensity vs Time: Fill 8741
Normalised electron flux [A.cm-2]
a-C B1
Cu B1

## Slide 33: RFA raw data
TE – VSC – VSM
  RFA scan
  Scanning time:
  Filtering voltage:
  Current at a set voltage :
    current of electrons with an energy under
RFA scan: Fill 9072
Electron current vs Filtering voltage: Fill 9072
Electron current
  The energy spectrum of the electrons can be obtained by derivating this curve.

## Slide 34: Energy spectrum double lognormal fit
TE – VSC – VSM
Electron energy spectrum: Fill 9072
Normalised signal
  Spectrum properties
  Peak at:
  Low peak: Energy of secondary electrons
  High peak: Energy of accelerated electrons
  Limit of the fit: within [20eV ; 100eV] and above 600eV

## Slide 35: Kick approximation principle
TE – VSC – VSM
  Two different types of motions during the passage of a bunch:
  Autonomous approximation: The electrons are strongly pulled by the bunch and begin to oscillate around it.
  Kick approximation: The electrons haven’t started to move very much before.
  Deciding which approximation to use:
    consists of comparing the oscillation period with respect to the time for the bunch to pass
    is equivalent to introducing a transition radius to delimit the domains of validity of both approximations
  Introduction of the critical radius above which the kick approximation is used, and below which the autonomous approximation is used.
  Mean energy kick within these regions:
  Energy kick for an electron on the wall:
  Total mean energy gain:
Ref: “ Energy Gain in an Electron Cloud During the Passage of a Bunch ” – J. Scott Berg

## Slide 36: Kick approximation formulae
TE – VSC – VSM
  Transverse and longitudinal bunch distributions assumed Gaussian
Beam parameters
  Relativistic beta:
  RMS bunch length:
  RMS beam radius:
  Electron properties
  Radius:
  Rest mass:
Ref: “ Energy Gain in an Electron Cloud During the Passage of a Bunch ” – J. Scott Berg

## Slide 37: Energy ramp-up at 620GeV
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Intensity:
  Fit results
  Low energy:
  High energy:

## Slide 38: Energy ramp-up at 2074GeV
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Intensity:
  Fit results
  Low energy:
  High energy:

## Slide 39: Energy ramp-up at 6799GeV
TE – VSC – VSM
TE – VSC – VSM
06/12/2023
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Intensity:
  Fit results
  Low energy:
  High energy: