## Slide 1: Damage Mechanisms in High-Temperature Superconducting (HTS) Tapes
Delphine Domange, Marco Bonura, David Gancarcik, Cedric Hernalsteens, Carmine Senatore, Daniel Wollmann
With contributions from Andreas Oslandsbotn, Andreas Will, William Martin Sorensen, Jannik Lassen, Anne Kirstine Herskind
MPE-CB Section meeting – 26/10/2023
Results from beam-induced and current-discharge heating experiments

## Slide 2: Outline
Overview and motivations
The HiRadMat-37 experiment: beam-induced heating on HTS tapes
Capacitive current discharge heating experiment
Conclusions and next steps

## Slide 3: Outline
Overview and motivations
The HiRadMat-37 experiment: beam-induced heating on HTS tapes
Capacitive current discharge heating experiment
Conclusions and next steps

## Slide 4: Overview and motivations
Superconductivity
Operation below the critical surface → No resistance
Typically implies cryogenic temperature operation
Used in accelerator magnets to provide high magnetic fields
  NbTi used on LHC magnets
  Nb3Sn used for the new HL-LHC triplet quadrupoles
Newly developed materials provide
  High-Temperature Superconductors (HTS) (if Tc ≥ 77K)
  Room temperature superconductors [1]
HTS REBCO Tape
Operation at 77K or at 4K with higher external magnetic field
0.2mm thick multilayer tape
Considered for future colliders
[1] S. Lee and al., The First Room-Temperature Ambient-Pressure Superconductor, 2023 https://doi.org/10.48550/arXiv.2307.12008

## Slide 5: Overview and motivations
Courtesy V. Raginel
Accelerator failure scenarios
Beam losses: quenches → Availability issue
Failure scenarios: possible long-term degradation of magnet coils? → Machine protection issue
A large experimental campaign was started to assess the damage mechanisms and to quantify the damage limits of the different superconductors: LTS and HTS

## Slide 6: Outline
Overview and motivations
The HiRadMat-37 experiment: beam-induced heating on HTS tapes
Capacitive current discharge heating experiment
Conclusions and next steps

## Slide 7: The HiRadMat-37 experiment
P+
Experimental table setup in the
HiRadMat tunnel

## Slide 8: The HiRadMat-37 experiment
Cryostat
Sample holders placed on the cryostat
HTS
LTS
Second layer removed

## Slide 9: The HiRadMat-37 experiment
HTS samples holder
6 batches of 7 samples
HTS samples holder after beam impact
Horizontal tape: Batch 1 - 4
Vertical tape: Batch 5 - 6
HTS tape
Dimensions:
  Length: 60mm
  Width: 4mm
  Thickness: 0.2mm
B1
B2
B3
B4
B5
B6
S1
S2
S3
S4
S5
S6
S7

## Slide 10: HiRadMat-37: Post-beam-impact analysis
HiRadMat-37
Tapes impacted
Tapes removed from the sample holder
First visual inspection
Study physical characteristics during the experiment
Beam position
Beam size
Beam intensity
Temperature inside the cryostat
Determination of thermal conditions reached in the tapes
Monte Carlo simulation
Energy → Temperature
Hotspot and gradient
Study superconducting characteristics degradation
Measurement of critical current at the University of Geneva
Comparison and analysis
Assessment of damage mechanisms and quantitative analysis of damage limits

## Slide 11: HiRadMat-37: Monte Carlo simulation

## Slide 12: HiRadMat-37: Monte Carlo simulation
From specific energy to temperature
with Cp specific heat capacity

## Slide 13: HiRadMat-37: Monte Carlo simulation
Sample | Hotspot Temperature | Relative error | 
Sample ID | [K] | - | +
B1S1 | 352 | 1.99% | 1.99%
B1S2 | 522 | 1.34% | 1.34%
B1S3 | 694 | 1.01% | 1.01%
B1S4 | 888 | 0.68% | 0.56%
B1S5 | 1006 | 0.89% | 0.80%
B1S6 | 1131 | 0.62% | 0.62%
B1S7 | 1218 | 0.49% | 0.49%
B2S1 | 328 | 5.79% | 5.79%
B2S2 | 486 | 1.65% | 1.44%
B2S3 | 646 | 2.48% | 2.48%
B2S4 | 815 | 0.98% | 0.86%
B2S5 | 954 | 1.05% | 0.94%
B2S6 | 1046 | 0.86% | 0.76%
B2S7 | 1148 | 0.96% | 0.87%
Hotspot values for Batch 1 and Batch 2

## Slide 14: HiRadMat-37: Post-beam-impact analysis
HiRadMat-37
Tapes impacted
Tapes removed from the sample holder
First visual inspection
Study physical characteristics during the experiment
Beam position
Beam size
Beam intensity
Temperature inside the cryostat
Determination of thermal conditions reached in the tapes
Monte Carlo simulation
Energy → Temperature
Hotspot and gradient
Study superconducting characteristics degradation
Measurement of critical current at the University of Geneva
Comparison and analysis
Assessment of damage mechanisms and quantitative analysis of damage limits

## Slide 15: Critical current measurement
Current supply
Cryostat with liquid helium:
Measure at 4K or 77K
Electro-magnet
for the external magnetic field
Removable tube on which the sample is fixed
Setup of the University of Geneva Lab

## Slide 16: Critical current measurement
Removable tube on which the sample is fixed via the sample holder
Sample holder
HTS tape
Voltage tap for the measurement

## Slide 17: Critical current measurement
Critical current determination
Electric field criteria
Qualification samples | Batch 1 | Batch 2
R1 | B1S1 | B2S1
R2 | B1S2 | B2S2
R3 | B1S3 | B2S3
R4 | B1S4 | B2S4
 | B1S5 | B2S5
 | B1S6 | B2S6
 | B1S7 | B2S7
Measured samples
Measured
Not measured
Stuck in samples holder

## Slide 18: Critical current measurement

## Slide 19: Critical current measurement

## Slide 20: Critical current measurement
> 700-800 K
> 900-1000 K

## Slide 21: Critical current measurement
Critical current density values of the qualification samples
Larger deviation value
± 2 kA/mm2

## Slide 22: Critical current measurement
Bad quality? Other damage mechanisms?
No degradation
Minor degradation
Two steps of degradation
B1 ≠ B2 → Mechanical damage ?
Broken

## Slide 23: HiRadMat-37: next steps
Mechanical analysis
Critical current measurement
  Batch 3 and 4: increase size of available dataset
  Batch 5 and 6: to allow comparison with “horizontal tapes”

## Slide 24: Outline
Overview and motivations
The HiRadMat-37 experiment: beam-induced heating on HTS tapes
Capacitive current discharge heating experiment
Conclusions and next steps

## Slide 25: Capacitive current discharge heating experiment
Hundreds of milliseconds heating damage on HTS tape
No significant mechanical effect on the tape
Courtesy W. Sorensen
Experimental setup

## Slide 26
Capacitive current discharge heating experiment
Samples | Target | CLIQ Parameters |  | Simulated maximum values |  | 
 | Temperature (K) | VC (V) | C (mF) | Temperature (K) | Current (A) | Short current(A)
R1 | 420 | 200 | 30 | 415.7 | 549.5 | 552.6
B1S1 | 500 | 300 | 20 | 494.4 | 706.9 | 710.3
B1S2 | 600 | 500 | 10 | 603.1 | 890.9 | 894.1
B2S1 | 640 | 300 | 30 | 638.8 | 824.2 | 828.9
B2S2 | 740 | 400 | 20 | 732.7 | 942.4 | 947
R4 | 820 | 300 | 40 | 816.5 | 914.4 | 920.3
R2 | 1040 | 300 | 50 | 1037.1 | 988 | 995
Determination of the variable circuit parameters based on target temperatures
Constant parameters
Courtesy W. Sorensen
Equivalent electric circuit

## Slide 27
Discharge experiment
Results of the design-stage simulations
Current and voltage measurements during the experiment
Validation of modelling hypotheses
Tape resistance
Thermal mechanisms modelling
Evaluation of uncertainties
Determination of thermal conditions reached by the tapes
Heat generated inside the tape
Heat → Temperature
Study of critical current degradation
Measurements of critical current at the University of Geneva
Comparison and analysis
Capacitive current discharge heating experiment
Assessment of damage mechanisms and quantitative analysis of damage limits

## Slide 28: Modelling hypotheses
Heat flow during the experiment
Thermal diffusivity at 20°C:
Copper :
Hastelloy :
Thermal effusivity at 20°C:
Copper :
Hastelloy :
Thermal diffusivity = Speed of the heat transfer on a material
→ Heat produced in the tape remains in the tape due to the low Hastelloy thermal diffusivity
Thermal effusivity = Speed of the heat absorption of a material
→ Copper clamps absorb the heat produced in the contact region
Q

## Slide 29: Modelling hypotheses
Resistance of the tape and contacts
I
I
is 50% of the total measured resistance
→ 50% of the total generated heat is used to calculate the temperature on the tape body

## Slide 30: Measurement analysis

## Slide 31: Measurement analysis
Samples | Target | CLIQ Parameters |  | Simulated maximum values |  |  | Measured maximum value |  |  | 
 | Temperature (K) | VC (V) | C (mF) | Temperature (K) | Current (A) | Short current(A) | Temperature (K) | CLIQ current(A) | Rog current (A) | Tape voltage (V)
R1 | 420 | 200 | 30 | 415.7 | 549.5 | 552.6 | 363 | 553.7 | 585 | 1.2
B1S1 | 500 | 300 | 20 | 494.4 | 706.9 | 710.3 | 412 | 713.9 | 725.6 | 1.8
B1S2 | 600 | 500 | 10 | 603.1 | 890.9 | 894.1 | 481 | 930.2 | 964.4 | 2.3
B2S1 | 640 | 300 | 30 | 638.8 | 824.2 | 828.9 | 540 | 832.5 | 886.2 | 2.9
B2S2 | 740 | 400 | 20 | 732.7 | 942.4 | 947 | 602 | 959.5 | 1013 | 3.4
R4 | 820 | 300 | 40 | 816.5 | 914.4 | 920.3 | 681 | 910.6 | 983.9 | 3.8
R2 | 1040 | 300 | 50 | 1037.1 | 988 | 995 | 1079 | 974.1 | 1072 | 10
Results of the experiment
Hotspot values lower than the target values but still relevant to analyse the degradation of the HTS tapes critical current

## Slide 32
Discharge experiment
Results of the design-stage simulations
Current and voltage measurements during the experiment
Validation of modelling hypotheses
Tape resistance
Thermal mechanisms modelling
Evaluation of uncertainties
Determination of thermal conditions reached by the tapes
Heat generated inside the tape
Heat → Temperature
Study of critical current degradation
Measurements of critical current at the University of Geneva
Comparison and analysis
Capacitive current discharge heating experiment
Assessment of damage mechanisms and quantitative analysis of damage limits

## Slide 33: Critical current analysis
Completely degraded → transport issue
No degradation
Minor degradation
Issue during measurement ?
No degradation
Broken

## Slide 34: Critical current analysis

## Slide 35: Outline
Overview and motivations
The HiRadMat-37 experiment: beam-induced heating on HTS tapes
Capacitive current discharge heating experiment
Conclusions and next steps

## Slide 36: Conclusion and next steps
The HiRadMat-37 experiment
  Two approximate threshold temperatures for critical current degradation → Performing IC measurements on the remaining batches is required to draw definitive conclusions
  Possible mechanical effect to explain the observed degradation → Analysis to be done using ANSYS simulation
Capacitive current discharge heating experiment
  Interesting experiment to allow a comparison of time scale and with less mechanical effect
  Lots of external factors lead to big uncertainties on the values of critical current after the experiment → Good learning for further experiments: Minimize the dependency factors
Results based on detailed analysis of IC variations (pre-irradiation, post-irradiation, post-discharge)

## Slide 37: Thanks for your attention

## Slide 38: HiRadMat-37: Post-beam-impact analysis
Batch | Beam intensity | x offset position | y offset position
B1 | 3.15e+12 | -1.12 mm | -0.11 mm
B2 | 3.06e+12 | -1.17 mm | -0.08 mm
B3 | 3.08e+12 | -1.26 mm | -0.08 mm
B4 | 3.10e+12 | -1.16 mm | -0.02 mm
B5 | 3.16e+12 | -1.27 mm | -0.07 mm
B6 | 3.05e+12 | -1.36 mm | -0.01 mm
Beam intensity slightly different for the different batches
Offset along axis x due to misalignment of the sample holder
Offset along axis y can be due to different reasons*
* More details in Internal note: Beam Impact on Superconductor short samples of Nb3Sn, Nb-Ti and YBCO, https://edms.cern.ch/document/2068064/1
B1
B2
B3
B4
B5
B6
S1
S2
S3
S4
S5
S6
S7
y
x
z

## Slide 39: HiRadMat-37: Monte Carlo simulation
Temperature gradient along x axis

## Slide 40: HiRadMat-37: Monte Carlo simulation
Sample | Hotspot Temperature | Temperature gradient | 
Sample ID | Hotspot Temperature | Negative x | Positive x
 | [K] | [K/mm] | [K/mm]
B1S1 | 352 | 89.15 | 88.32
B1S2 | 522 | 135.02 | 134.83
B1S3 | 694 | 182.76 | 179.36
B1S4 | 888 | 231.68 | 227.65
B1S5 | 1006 | 259.01 | 255.55
B1S6 | 1131 | 279.76 | 278.48
B1S7 | 1218 | 295.88 | 296.38
B2S1 | 328 | 83.3 | 83.83
B2S2 | 486 | 124.96 | 125.25
B2S3 | 646 | 166.5 | 167.77
B2S4 | 815 | 182.92 | 183.78
B2S5 | 954 | 241.89 | 241.55
B2S6 | 1046 | 263.52 | 263.02
B2S7 | 1148 | 277.86 | 279.68