## Slide 1
Non-Evaporable Getter (NEG) materials
NEG thin films for particle accelerators
Production of Ti-Zr-V NEG thin films
Visit of Zanon R&I
P.Costa Pinto, M.Taborelli

## Slide 2
Working principle
NEG
Temperature
Time
RT
Activation temperature
Oxide layer
Oxygen in the film
Active surface for pumping
Molecules pumped on the surface: CO, O2, H2O, CO2, N2.
H2 is dissociated on the surface and diffuses into the bulk.
1- Non-Evaporable Getter materials (NEG)
Not pumped: noble gases and CH4 (at room temperature)

## Slide 3
2- NEG thin films for particle accelerators: motivation
Vacuum pumping in long narrow pipes (typical in accelerators) is limited by conductance
P(0)
S
P(x)
x
x
L
Distributed outgassing
P(0)
S
Pmax
pump
pump
2R

## Slide 4
P(0)
S
P(x)
x
x
L
Distributed outgassing and pumping
P(0)
S
Pmax
Non Evaporable Getters can provide distributed pumping along the vacuum chamber
2- NEG thin films for particle accelerators: motivation
Vacuum pumping in long narrow pipes (typical in accelerators) is limited by conductance

## Slide 5
2- NEG thin films for particle accelerators: history
The LEP (Large Electron Positron collider, 27 km) was pumped by NEG strips (SAES st101) (1985 – 2001)
Beam pipe
NEG strip (SAES)
Non Evaporable Getters can provide distributed pumping along the vacuum chamber: “bulk” NEG on resistive heated strips as first accelerator application
Vacuum pumping in long narrow pipes (typical in accelerators) is limited by conductance

## Slide 6
Before coating
after coating
2- NEG thin films for particle accelerators: history
Beam pipe
NEG strip (SAES)
Idea: from the strip to a thin film covering the entire chamber surface
However, strips activated at 740C (later another composition at 400C)….

## Slide 7
Before coating
after coating
2- NEG thin films for particle accelerators: history
Cristoforo Benvenutti
Idea: from the strip to a thin film covering the entire chamber surface
However, strips activated at 740C (later another composition at 400C)….

## Slide 8
after coating
2- NEG thin films for particle accelerators: more than just pumping
Advantages:
Global distributed pumping speed;
Low particle induced desorption
Low secondary electron emission

## Slide 9
Sticking probability for distributed pumping: some structure effect
coated at 100oC
coated at 300oC
Surface capacity (CO) ~8x1014 molecules/cm2
Surface capacity (CO) ~7x1015 molecules/cm2
activation | Sticking coefficient H2 min ~max | Sticking coefficient CO min ~max | Surface capacity for CO [molecules/cm2]
24 h@180o C | 2x10-3 ~ 9x10-3 | 0.5 ~ 1 | 3x1014 ~ 8x1014 («standard») > 5x1015 for rough films
2 h@230o C | 8x10-3 | 0.45 | 3x1014 ~ 6x1015
24 h@230o C | 5x10-3 ~ 2x10-2 | 0.6 ~ 1 | 
24 h@250o C | 6x10-3 ~ 3x10-2 | 0.6 ~ 1 | 
2- NEG thin films for particle accelerators: sticking probability
LHC

## Slide 10
as received
after 2h @ 120oC
after 2h @ 160oC
after 2h @ 200oC
Threshold for electron multipacting in the LHC ~1.3
2- NEG thin films for particle accelerators: Secondary Electron Yield
Low Secondary Electron Yield (SEY) for anti-multipacting (or anti e-cloud)

## Slide 11
Courtesy from Yasunori Tanimoto, KEK
2- NEG thin films for particle accelerators: PSD
Low Photon Stimulation Desorption yield (PSD)
To limit dynamic outgassing

## Slide 12
Courtesy from Yasunori Tanimoto, KEK
Low Photon Stimulation Desorption yield (PSD)
To limit dynamic outgassing
2- NEG thin films for particle accelerators: PSD

## Slide 13
Courtesy from Yasunori Tanimoto, KEK
Low Photon Stimulation Desorption yield (PSD)
To limit dynamic outgassing
2- NEG thin films for particle accelerators: PSD

## Slide 14
Temperature
Time
RT
Activation temperature
3- NEG thin films for particle accelerators: activation
Activation time and temperature must be compatible with the application.
For vacuum chambers it must be compatible with the material of the chamber (change of mechanical properties with temperature)

## Slide 15
3- The Ti-Zr-V NEG thin film: composition & activation
Ti-Zr-V with activation temperature 180 oC.
Composition diagram (at.%)
Good activation
30
40
50
60
Ti-Zr-V
Substrate
 (degrees)
Large crystals
grain size ≥ ~100 nm
XRD intensity (a.u.)
Ti-Zr-V
30
40
50
60
 (degrees)
Substrate
XRD intensity (a.u.)
Nanocrystalline
grain size < 5 nm
~Ti33-Zr33-V33 +/-20% acceptable

## Slide 16
Ti-Zr-V with activation temperature 180 oC: can be applied on copper and aluminium alloy chambers.
Composition diagram (at.%)
Good activation
Large crystals
grain size ≥ ~100 nm
Nanocrystalline
grain size < 5 nm
~Ti33-Zr33-V33 +/-20% acceptable
Malyshev et al. reported lower activation temperature for the quaternary alloy Ti-Zr-V-Hf,
J. Vac. Sci. Technol. A 2014, 32, 061601
3- The Ti-Zr-V NEG thin film: composition & activation

## Slide 17
Produced by sputtering
Planar magnetron
(TiZrV alloy targets available)
Cylindrical magnetron sputtering
(multiwire targets; alloy targets not available)
intertwisted wires of Ti, Zr and V
Glow discharge
Vacuum chamber
3- Production of Ti-Zr-V NEG thin films

## Slide 18
Large scale production: more than 3 km of beam pipes in the LHC
3mm wires of Ti, Zr and V
3- Production of Ti-Zr-V NEG thin films

## Slide 19
ESRF (France)
FMB Berlin (Germany)
LNLS (Brazil)
PSI
(Switzerland)
GSI (Germany)
KEK (Japan)
Widely
used in synchrotron light sources
Produced world wide
SAES getters
(Italy)
Thai Synchrotron
DESY
3- Production of Ti-Zr-V NEG thin films

## Slide 20
Synchrotron light sources
Source: “8th Low Emittance Rings Workshop”, Oct. 26-30, 2020, Frascati (held remotely), R. Bartolini, DESY
https://agenda.infn.it/event/20813/timetable/#all.detailed
3- Production of Ti-Zr-V NEG thin films

## Slide 21
Key challenges
Narrow
&
Complex
Beam pipes
Adhesion
Thickness uniformity
3- Production of Ti-Zr-V NEG thin films

## Slide 22
Key challenges
Adhesion: requires surface treatment adapted to each substrate (copper, stainless steel, aluminium).
Peel-off can occur in thermally affected areas
3- Production of Ti-Zr-V NEG thin films

## Slide 23
Key challenges
Adhesion: requires surface treatment adapted to each substrate (copper, Stainless steel, aluminium).
Peel-off can occur in thermally affected areas
Peel off can occur on surfaces milled with specific parameters
Coating and thermal cycle can reveal surface defects
(copper incrustations due to defective extruding tool)
3- Production of Ti-Zr-V NEG thin films

## Slide 24
Key challenges
Adhesion: requires surface treatment adapted to each substrate (copper, Stainless steel, aluminium).
Peel-off can occur in thermally affected areas
Peel off can occur on surfaces milled with specific parameters
Coating and thermal cycle can reveal surface defects
(copper incrustations due to defective extruding tool)
Surface preparation is crucial
(etching by wet chemistry or ion bombardment, sometimes followed by thermal treatments)
3- Production of Ti-Zr-V NEG thin films

## Slide 25
Key challenges
Adhesion: requires surface treatment adapted to each substrate (copper, stainless steel, aluminium).
Beam pipes for synchrotron light sources becoming narrower and complex.
MAXIV
3- Production of Ti-Zr-V NEG thin films

## Slide 26
Key challenges
Adhesion: requires surface treatment adapted to each substrate (copper, Stainless steel, aluminium).
Beam pipes for synchrotron light sources becoming narrower and complex.
Increasing demand on the uniformity of the thickness.
MAXIV
Minimal thickness for functionality: 150 nm
Maximal thicknesses (beam impedance):
LHC: > 1.5 mm
ELETTRA2: 500 nm
SLS2: 400 nm
FCC –ee: 200 nm
3- Production of Ti-Zr-V NEG thin films

## Slide 27
3- Production of Ti-Zr-V NEG thin films: quality control
Decrease of O on the surface
Reduction of the oxides of all the metals: the surface is metallic and reactive
Ti
Zr
V
O decrease
monitoring activation process by X-ray Photoemission Spectroscopy:

## Slide 28
Summary
NEG thin films can provide distributed pumping, reduced electron multiplication and low particle induced outgassing.
These thin films are produced by sputtering from alloy targets (planar magnetron) or intertwisted wire targets.
Surface preparation is crucial.
Many of the 4th generation synchrotron light sources require extensive use of NEG thin films.
Key challenges include adhesion, narrow and complex chambers, restriction on maximal thicknesses accepted in some accelerators.

## Slide 29
THANK YOU FOR YOUR ATTENTION
QUESTIONS?

## Slide 30
Thickness effect
4 activation cycles at 250C

## Slide 31
Y.Tanimoto, M.Ady, P.Costa Pinto
Measured at KEK photon factory
Thickness effect

## Slide 32: Aging of TiZrV: role of the coating thickness
Equivalent to 1 ion pump of 100 l/s every meter!
From P.Chiggiato