## Slide 1: Environmental Stress Cracking of Thermoplastic Polyimide Wires

## Slide 2: High voltage wires in superconducting magnets
Polyimide is often the first choice for the HV insulation of wires operating under demanding environmental and operating conditions in HEP and Fusion machines
HV wires are a fundamental part of superconducting magnet systems:
  Voltage taps for quench detection
  Magnet wires and leads
Magnet wires connection box
Quench detection wires in ITER TF coil terminal

## Slide 3: Failure mechanisms of HV wires
ESC is the premature initiation of cracking of a plastic due to the simultaneous action of stress/strain and the contact with a fluid
Externally applied
Residual from manufacturing process
Moisture
Chemicals
  Pinching / Handling at installation
  Thermomechanical stresses at operation
  High Voltage
  Environmental Stress Cracking (ESC)

## Slide 4: ESC on TPI wires for quench detection
ESC may arise at the extraction point of high voltage wires from the coil insulation
Among other studies, it is worthy to mention:
ESC of TPI wires exposed to epoxy & cyanate-ester blend (D. Evans, unpublished)
ESC of Kapton wires in water at elevated temperatures (C.J. Wolf & D.L. Fanter)
Amorphous plastic - Thermoplastic Polyimide (TPI)
Exposure to Chemical / Fluid (epoxy/hardener system) + Temperature (epoxy curing stage)
Strain/stress (residual, wire routing, operational loads)

## Slide 5: Wires and Epoxy Systems
Thermoplastic polyimide (TPI) wire
Resin systems (RT curing systems)
Mix | Epoxy | Hardener | Accelerator
A | jER 807 | Jeffamine D230 | -
B | jER 807 | Baxxodur EC 302 | Acc 400
C | Araldite GY 282 | Jeffamine D 400 | Acc 400
D | Araldite DBF | HY 951 | -
E | EpoPro 275 A | EpoPro 275 B | -
F | EE 4215 | HD 3561 | -
G | Stycast 2850 FT | 24 LV | -
TPI thickness: 0.9 ± 0.1 mm
Processing: continuous extrusion
Two layouts:
W1
Single Layer TPI
W2
Double Layer TPI
This study investigates the compatibility of thermoplastic polyimide (TPI) wires with a range of epoxy systems commonly utilized in superconducting magnet systems

## Slide 6: I ) Immersed mandrel test
Assess the effect of amine-based hardeners (strong bases > 10 pH)
Compare time-to-crack-onset (TTCO)
Determine the ESC accelerating factors (strain, temperature, time)
Four strain levels:
0%, 2.5%, 5%, 10%
Two temperatures:
Room Temperature and 60 ℃
Six hardener types:
D230, D400, HY951, EpoProB, HD3561, LV24

## Slide 7: Time-to-crack-onset (TTCO)
 | T [°C] | Strain [%] | D 230 | D 400 | HY 951 | Epo ProB | HD 3561 | 24 LV
W1 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 | 96h |  |  |  |  | 
 |  | 5 | 2h |  |  |  |  | 
 |  | 10 | 2h |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 4h |  |  | 9h
 |  | 5 | 2h | 2h | 4h | 2h | 24h | 2h
 |  | 10 | 2h | 2h | 4h | 2h | 96h | 9h
W2 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 |  |  |  |  |  | 
 |  | 5 | 48h |  |  |  |  | 
 |  | 10 |  |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 96h |  |  | 
 |  | 5 | 2h |  | 96h | 96h |  | 
 |  | 10 | 2h |  |  | 36h |  | 
HARDENERS
WIRE TYPE

## Slide 8: Time-to-crack-onset (TTCO)
 | T [°C] | Strain [%] | D 230 | D 400 | HY 951 | Epo ProB | HD 3561 | 24 LV
W1 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 | 96h |  |  |  |  | 
 |  | 5 | 2h |  |  |  |  | 
 |  | 10 | 2h |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 4h |  |  | 9h
 |  | 5 | 2h | 2h | 4h | 2h | 24h | 2h
 |  | 10 | 2h | 2h | 4h | 2h | 96h | 9h
W2 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 |  |  |  |  |  | 
 |  | 5 | 48h |  |  |  |  | 
 |  | 10 |  |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 96h |  |  | 
 |  | 5 | 2h |  | 96h | 96h |  | 
 |  | 10 | 2h |  |  | 36h |  | 
HARDENERS
WIRE TYPE
1)
Crack onset can be very rapid

## Slide 9: Time-to-crack-onset (TTCO)
 | T [°C] | Strain [%] | D 230 | D 400 | HY 951 | Epo ProB | HD 3561 | 24 LV
W1 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 | 96h |  |  |  |  | 
 |  | 5 | 2h |  |  |  |  | 
 |  | 10 | 2h |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 4h |  |  | 9h
 |  | 5 | 2h | 2h | 4h | 2h | 24h | 2h
 |  | 10 | 2h | 2h | 4h | 2h | 96h | 9h
W2 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 |  |  |  |  |  | 
 |  | 5 | 48h |  |  |  |  | 
 |  | 10 |  |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 96h |  |  | 
 |  | 5 | 2h |  | 96h | 96h |  | 
 |  | 10 | 2h |  |  | 36h |  | 
HARDENERS
WIRE TYPE
1)
Crack onset can be very rapid
2)
Temperature and strain are accelerating factors

## Slide 10: Time-to-crack-onset (TTCO)
 | T [°C] | Strain [%] | D 230 | D 400 | HY 951 | Epo ProB | HD 3561 | 24 LV
W1 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 | 96h |  |  |  |  | 
 |  | 5 | 2h |  |  |  |  | 
 |  | 10 | 2h |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 4h |  |  | 9h
 |  | 5 | 2h | 2h | 4h | 2h | 24h | 2h
 |  | 10 | 2h | 2h | 4h | 2h | 96h | 9h
W2 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 |  |  |  |  |  | 
 |  | 5 | 48h |  |  |  |  | 
 |  | 10 |  |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 96h |  |  | 
 |  | 5 | 2h |  | 96h | 96h |  | 
 |  | 10 | 2h |  |  | 36h |  | 
HARDENERS
WIRE TYPE
3)
D230 vs Stycast (HD3561 and 24LV)
1)
Crack onset can be very rapid
2)
Temperature and strain are accelerating factors

## Slide 11: Time-to-crack-onset (TTCO)
 | T [°C] | Strain [%] | D 230 | D 400 | HY 951 | Epo ProB | HD 3561 | 24 LV
W1 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 | 96h |  |  |  |  | 
 |  | 5 | 2h |  |  |  |  | 
 |  | 10 | 2h |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 4h |  |  | 9h
 |  | 5 | 2h | 2h | 4h | 2h | 24h | 2h
 |  | 10 | 2h | 2h | 4h | 2h | 96h | 9h
W2 | RT | 0 |  |  |  |  |  | 
 |  | 2.5 |  |  |  |  |  | 
 |  | 5 | 48h |  |  |  |  | 
 |  | 10 |  |  |  |  |  | 
 | 60 | 0 |  |  |  |  |  | 
 |  | 2.5 | 2h |  | 96h |  |  | 
 |  | 5 | 2h |  | 96h | 96h |  | 
 |  | 10 | 2h |  |  | 36h |  | 
HARDENERS
WIRE TYPE
4)
Insulation layout counts
1)
Crack onset can be very rapid
3)
D230 vs Stycast (HD3561 and 24LV)
2)
Temperature and strain are accelerating factors

## Slide 12: Crack appearance
I) Azimuthal sub-superficial crazes appeared in the bulk of the TPI under tensile stress
II) Often the fracture surface covered the entire cross-section of the wire

## Slide 13: Comparative analysis of “aged ” and “virgin” samples
Very similar thermal phenomena for all virgin and aged samples
Typical behavior of amorphous TPI
No major morphological changes
Peaks corresponding to amide groups at 1639 cm−1 (symmetric stretching of C=O in the amide group) and 1534 cm−1 (stretching of C–N and bending of N–H in the amide group)
Indication of the imide-ring opening
Possible alkaline hydrolysis
Differential Scanning Calorimetry (DSC)
Fourier Transform Infrared Spectroscopy (FTIR)
T glass 249 ℃
Cold crystallization 304 ℃
T melting 389 ℃

## Slide 14: II ) Encapsulated wire bending test
The test aimed to compare the failure rate at bending of wires encapsulated in the epoxy mix
The encapsulated wire samples were prepared to reproduce the recommended proportion of chemicals and curing times
Samples were tested in a dedicated jig in four orthogonal directions
Bending was repeated once per week till rupture

## Slide 15: Failure rates at bending
 | A | B | C | D | E | F | G
W1 | 6/6 | 1/6 | 1/3 | 2/3 | 0/3 | 1/3 | 0/3
W2 | 6/6 | 0/6 | 0/3 | 1/3 | 0/3 | 0/3 | 0/3
D230
Stycast
Results pretty aligned with the outcome of the immersed mandrel test:
Lower failure rate for the wires W2 (two-layer insulation)
High failure rate of mix A (D230)
Failure rates at bending
Hardness (nanoindentation)
Increase of hardness with respect to the reference value measured on a virgin sample:
+ 18% for mix A (D230)
+ 7% for other mixes

## Slide 16: Fracture surface of encapsulated wire
crack initiation
Crack propagates from the wire / epoxy interface
More aggressive hardeners may etch the TPI surface causing micro-defects

## Slide 17: Conclusions
ESC appears in TPI wires exposed to amine-hardeners. Rapid crack onset (few hours), aggravated at temperatures of 60 ℃
Even in low concentration, the hardeners causes physical changes in TPI that may promote cracking
To mitigate the risk of ESC great caution must be given to the selection of materials (wire insulation, epoxy systems, etc.) and the wire insulation layouts

## Slide 18
Thank you