## Slide 1
UNIVERSITY OF TWENTE.
Measurement and FE modelling critical transverse loading limits of REBCO round cables for fusion
A. Nijhuis1,3 ,G. Anniballi1, J. Rietberg1, N. van Dusschoten1, A. Kario1,7, V.J. Ellenbroek1,2,
R. Lübkemann3, J. Leferink3, C. Soyarslan2, A.H. van den Boogaard2, J.D. Weiss4, K. Radcliff 4, D.C. van der Laan4, H. Jin5, C. Zhou1,5, W. Yu5, J.G. Qin5, E. Garibaldi6, M. Breschi6
1 University of Twente, Faculty of Science & Technology, Enschede, The Netherlands
2 University of Twente, Faculty of Engineering Technology, Enschede, The Netherlands
3 Foundation SuperACT, Hengelo, The Netherlands
4 Advanced Conductor Technologies, Boulder, CO & University of Colorado, Boulder, CO, USA
5 Institute of Plasma Physics, Chinese Academy of Sciences, China
6 University of Bologna, Bologna, Italy
7 CERN, Geneva, Switzerland
ASIPP
CCA Workshop 2025, CERN, 12 Mar 2025

## Slide 2: Conductor design optimization
UNIVERSITY OF TWENTE.
Single tape Ic – mech. load testing
Axial tensile stress, Ic & mech. props.
Axial tensile & compressive strain, Ic & eirr
TransverseStress sirr
Winding angle, Ic & min. diam.
Cable cyclic load testing Twente Press
Critical current/loadIc(F)
Transverse stiffness d(F)
Inter tape contact resistance Rc
FE cable model
Materials
Design

## Slide 3: Single tape: Ic – mechanical testing
UNIVERSITY OF TWENTE.
U-Spring axial tensile & compressive strain Ic(B,T,e)
Axial tensile stress, mechanical properties, Ic & eirr
Transverse stress, Ic & sirr (77 K)
Winding angle Ic & min core diam. (77 K)

## Slide 4
Axial tensile strain: setup
Goal:
Stress-strain properties, Ic & irreversibility limit for tensile axial strain
Tape | tSubstrate [𝜇m] | tCopper [𝜇m] | Ic [A]
SSTC | 52 | 22 | 186
Fujikura | 49 | 25 | 204
Faraday | 39 | 13 | 162
Substrate : Hastelloy, width = 4 mm
UNIVERSITY OF TWENTE.
5 MPa
Comparison data manufacturer

## Slide 5
Axial tensile Stress-Strain curves
UNIVERSITY OF TWENTE.
Tape | E [GPa] | 𝜎ys [MPa]
SSTC | 125 | 600
Fujikura | 135 | 621
Faraday | 150 | 875
Tape | 𝜖irr[%] | 𝜎irr [MPa]
SSTC | 0.48 | 709
Fujikura | 0.43 | 626
Faraday | 0.58 | 900
Axial tensile Stress-Strain curves & Ic(𝜖)

## Slide 6
Winding performance
SSTC retains 100% Ic, wound at 45° on 4 mm former.
Fujikura shows Ic-reversible reduction (7%).
UNIVERSITY OF TWENTE.
Ic wound is normalized with Ic0 of initial straight configuration.
Critical core diameter >3 mm, critical angle < 60° for standard tape dimensions.
3 winding diameters (3, 4 and 5 mm)
3 winding angles (30°, 45° and 60°)
REBCO layer faces core
  Wound
  Straight
  Relaxed
Minimum winding radius (irreversibility limits)
Verification of current retention/reduction

## Slide 7
Transverse load (10 x 4 mm2)
UNIVERSITY OF TWENTE.
Ic/Ic0 and n/n0 at zero load after applied stress.
Tape | 𝜎irr [MPa]
S-Innovation | > 900
Fujikura, 22-0012-09 | 400
SSCT, ST2903-105 | 750

## Slide 8: Conductor design optimization
UNIVERSITY OF TWENTE.
Single tape Ic – mech. load testing
Axial tensile stress, Ic & mech. props.
Axial tensile & compressive strain, Ic & eirr
Transverse
Stress sirr
Winding angle Ic & min. diam.
Cable cyclic load testing Twente Press
Critical current/loadIc(F)
Transverse stiffness d(F)
Inter tape contact resistance Rc
FE cable model
Materials
Design

## Slide 9
Transverse load: Twente Cable Press
UNIVERSITY OF TWENTE.
9
Hydraulic press based on principle of lever mechanism and wedge
Sample length: 400 mm
Measuring: Ic, Rc, force, displacement and AC loss (only at 4.2 K).
T-operating temperatures: 4.2 and 77 K

## Slide 10
ACT CORC©-CICC Twente Press test sample
7 mm
OD
Extruded C101 Cu Keystones
Machined C110 Cu support
Central cooling tube
Selected tapes (8) for critical current and inter-tape contact resistance measurements.
Cu keystone
SS support
UNIVERSITY OF TWENTE.
10
CORC© cable used in ACT Sultan sample with 36 tapes, OD of 7.04 mm (including thin plastic tube) in groove with 7.54 mm.

## Slide 11
CORC© Twente Press ACT samples #1 & 2
9,000 cycles successive F-increases
(Ec=10 mV/m), n-value (22-21)
Irreversible degradation = critical load (CL):
Both ACT samples CL~ 100 kN/m.
UNIVERSITY OF TWENTE.
11
ACT sample #1
ACT sample #2
Sub-cable parameters both samples | 
Tape Manufacturer | SuperPower
SC Tapes | 36
Tape width | 4 mm
Tape thickness | 63 m
Substrate thickness | 50 m
Copper thickness | 5 m
Spacing | 0.5 mm
Core | Cu Rod
Core OD | 5.34mm
Strain window | [-1.3%, 0.45%]

## Slide 12
Twente Press ASIPP sample #1 & #3
ASIPP sample #3, degradation for spiral at 210 kN/m (x6 = 1260 kN/m). Solid core 450 kN/m (x6=2700 kN/m).
Degradation ACT samples ~ 90 kN/m < (x6 = 540 kN/m).
Main difference with ATC samples:
radius Cu profile matches to cable.
No plastic tube around cable.
UNIVERSITY OF TWENTE.
12
ASIPP sample #3
Main parameters ASIPP |  | 
ASIPP Sultan # | #3 | #1
tape supplier | SSTC | SSTC
Cu Core OD | 4.0 mm | 4.6 mm
SC tape layer | 16 | 22
tape No. layer | 2x3 Cu+ SC(2x4+3x8+4x4)+4x2 Cu | SC(2x4+3x7+ 4x11)+4x1 Cu
tape No. | 48 | 73
winding angle | 33.5-49° | 36.5-56°
gap | ~0.6 mm | 0.4 mm
OD | ~8.6 mm | 9.6 mm
width | 4 mm | 4 mm
thickness | 0.1 mm | 0.1 mm
Ic @ 77K,SF | 160 -210 A | 160-190 A
ASIPP sample #1
Solid Cu core

## Slide 13
ACT #1 & 2, ASIPP #1 & 3 (spiral), Press F(d)
UNIVERSITY OF TWENTE.
13
Two stiffness regimes:
ACT #1
ACT #2
ASIPP #1
22 layers
16 layers (SS spiral)
12 layers
12 layers
ASIPP #3
“The greater the winding pre-tension force, the smaller the helical curvature radius”
space/layer - sample | ACT #1 | ACT #2 | ASIPP #3 | ASIPP #1
(Dcab – Dcore)/(2N)-t [mm] | 11.6 | 11.6 | 48 | 9.5
dmeas/(2N)-t [mm] | 5.0 | 6.3 | 31 | 17.0
K. Wang, Y. Gao, W. Luo, Y. Zhou, A. Nijhuis, Nonlinear contact behavior of HTS tapes during pancake coiling and CORC cabling, Supercond. Sci. Technol. 34 (2021) 075003 https://doi.org/10.1088/1361-6668/abf710

## Slide 14
Outer layer damage Press test
UNIVERSITY OF TWENTE.
14
ACT cables: tightly wound, less layers then ASIPP, Cu groove and key-stone have larger radius than cable (stress concentration). Thin plastic tube around cable.
ASIPP cables: Inner layers withstands 800 kN/m, homogeneous contact.
More loosely wound (groove radius matches cable’s), early degradation outer squeezed tape layers (→ bending).
r-cable
r-Cu-groove
Tapes are squeezed towards open space at sides.
Tapes are squeezed towards open space at sides.
Space needed for cable to “breath” due to voids from anticlastic winding effect.
Remedies:
Tighter winding of tapes to reduce voids.
Outer Cu (ASIPP) or plastic tube (ACT) for tape containment.

## Slide 15
Contact resistance results: Rc(F)
Contact resistance: initial Rc and after 3,000 cycles, 2 to 10 𝜇𝛺m in all conductors (under load).
Rc evolution with cycling in qualitative agreement (peak).
UNIVERSITY OF TWENTE.
15

## Slide 16: Conductor design optimization
UNIVERSITY OF TWENTE.
Single tape Ic – mech. load testing
Axial tensile stress, Ic & mech. props.
Axial tensile & compressive strain, Ic & eirr
Transverse
Stress sirr
Winding angle Ic & min. diam.
Cable cyclic load testing Twente Press
Critical current/loadIc(F)
Transverse stiffness d(F)
Inter tape contact resistance Rc
FE cable model
Materials
Design

## Slide 17: Model validation – experimental data
ACT single CORC© experiment with transverse anvil loading.
Parameters | 
Tapes | 12
Layers | 6
Tape width | 3 mm
d-Tape | 44 m
d- Substrate | 30 m
d-Copper | 5 m
Gap spacing | 0.5 mm
Core | Cu/SS rod
Strain window | [-1.3 %, 0.45 %]
D.C. van der Laan et al, 2018 Supercond Sci Technol 32, DOI:10.1088/1361-6668/aae8bf
D.C. van der Laan et al 2019 Supercond. Sci. Technol. 32 015002
D.C. van der Laan, private communication.
UNIVERSITY OF TWENTE.
Good match irreversibility limits:
model versus experiment
NCR = no current sharing between tapes.
PCR = perfect current sharing between tapes.
Cu core
SS core

## Slide 18: ASIPP CICC MD; Gap 1 and 0.5 mm
Reducing gap reduces voids and bending - significantly improving performance.
Gap spacing = 1 mm
Gap spacing = 0.5 mm
UNIVERSITY OF TWENTE.
F
F

## Slide 19: Model results – ASIPP MC single cable
ACT cable model validation results compared with 0.5 and 1.0 mm Cu tube.
Strain distribution with 0.5 mm Cu-wall thickness.
Outer copper tube around cable & solid Cu core: 500 kN/m.
UNIVERSITY OF TWENTE.

## Slide 20
Mechanical & EM Load (BL)
UNIVERSITY OF TWENTE.
20
Difference between body load (EM) and mechanical load (flat anvil) for different tape thicknesses and gap sizes.
Critical transverse EM load < mechanical load (30%).
Displacement (mm) for Mech Load and Electromagnetic Load at 200 kN/m.

## Slide 21: Model – ASIPP MC samples
Original gap 1.3 mm
Cu-keystones
SS spiral
Critical force:
MC Sultan #1: 400 kN/m
MC 1.3 mm gap, Cu-keystones: 600 kN/m
MC 0.6 mm gap, Cu-keystones: 1,000 kN/m
MC 0.6 mm gap, solid core: 1,300 kN/m
UNIVERSITY OF TWENTE.
21
0.6 mm gap
Modest improvement
SS spiral
0.6 mm gap
Cu-keystones
SS spiral
0.6 mm gap
Cu-keystones
Solid Cu core
IxB CS | I [kA] | B [T] | F(IxB) [kN/m]
ASIPP | 42 | 20 | 840
EU-DEMO | 60 | 18 | 1080

## Slide 22: Summary
UNIVERSITY OF TWENTE.
(New) setups for characterizing mechanical and electrical properties of REBCO tapes.
Round cable FE model validated.
Critical transverse load CORC®-like cables after cycling (4 samples) varies from 90 to 450 kN/m.
Observations to be further optimized for CICC with round cable:
  void fraction - winding tension – winding angle - # tape layers
  space for tape bending (breathing) and cable containment

## Slide 23: Short term plans
UNIVERSITY OF TWENTE.
Testing mechanical and electrical properties of REBCO tapes different manufacturers.
Design optimization (number of layers, void fraction, tape bending etc).
Cable tests (Ic, Rc, d) under cyclic loading in Twente Press:
  ACT-cable with matching cable and Cu-groove radii.
  ASIPP-cable within Cu-tube.
  Stacked tape conductors (+ modeling).

## Slide 24
UNIVERSITY OF TWENTE.
Thank you!

## Slide 25: Model results – ASIPP MC sample #1
Prediction & SULTAN Tcs reduction coincide.
Irreversibility:
MD: 200 kN/m.
MC with copper tube: 500 kN/m.
UNIVERSITY OF TWENTE.
25
Sub-cable Parameters | 
Tape Manufact. | Fujikura
SC Tapes | 36
Simulated Tapes | 9
Tape width | 4 mm
d-tape | 110 m
d-substrate | 50 m
d-copper | 23 m
Gap spacing | 1.3/1.6 mm
Core | SS Spiral
Strain window | [-1.3, 0.29 %]
Cu tube

## Slide 26: Model prediction - SULTAN results (ASIPP)
80 kA
Tcs@40kA, 10.85T
Test in April 2023
26

## Slide 27: Inter-tape friction
Axial strain at 1000 kN/m EM load.
UNIVERSITY OF TWENTE.
27
friction factor =zero
friction factor 0.2
Tapes slide due to EM load. Gap is reduced and near tape edges irreversibility limit 0.3% is exceeded.
For ff=0.2, tapes do not move due to contact friction with tapes underneath and above.

## Slide 28
Critical load REBCO tape for different Cu layer thickness: 1 mm anvil width.
K. Ilin, K.A . Yagotintsev, C. Zhou, P. Gao, J. Kosse, S.J . Otten, W.A.J. Wessel, T.J . Haugan, D.C . van der Laan and A. Nijhuis 2015 Experiments and FE modeling of stress–strain state in RECO tape under tensile, torsional and transverse load, Supercond Sci Technol 28 055006 [10.1088/0953-2048/28/5/055006]
Local transverse load and tape Cu-layer thickness
1 mm width pushing heads were used.
UNIVERSITY OF TWENTE.

## Slide 29
Press testing profile
UNIVERSITY OF TWENTE.
29