## Slide 1: iFast task 7.5 status
Objective
Build and test two prototypes of the X-band (12 GHz) accelerating structure designed for the CompactLight project.
Courtesy Pedro Morales sanchez
Mockup of the first prototype:
Three trials were carried out under different conditions to check:
- Machinability
- Alignment
- Brazing materials
- Leak tightness
- Weight

## Slide 2: iFast task 7.5
Courtesy Pedro Morales sanchez
Performed
- UT analysis,
- microscopy and
- Brazing Filler Material (BFM) inspection.
The alignment and flatness of the structure were kept as expected after the cycle

## Slide 3: iFast task 7.5
The first structure
will be brazed in January 2024
with low power RF tests
beginning of February 2024.
First prototype production