## Slide 1: Mechanical properties for FalconD 12T program
Date: December 5th, 2023
Authors: N. Sala on behalf of FalconD collaboration
RD Line 4 fourth Forum meeting, - Modelling Tools, Materials Protection and Cryogenics

## Slide 2
ANSYS Mechanical model: mesh
30 000 Plane183 (8-node quadrilateral elements)
w/ Plane stress
Esize = 2.5 mm
Intel(R) Core(TM) i5-10400 CPU @ 2.90Ghz (6 cores)
Solution time 7 min

## Slide 3
Coils physical properties*
Conductors & Insulation
Copper wedges
mm/m
«Characterization of the thermal contraction of superconducting magnet coils for the High-Luminosity upgrade of the Large Hadron Collider (HL-LHC)» by S. Hoell (2022)
https://cds.cern.ch/record/2845427?ln=en

## Slide 4
Coils mechanical properties*
*«11T Cable Stacks Compression Tests at RT and 77K» by. O Sacristan (2019)
https://indico.cern.ch/event/850550/contributions/3574865/attachments/1914741/3165117/EDMS_2208499_11T_Cablestacks_Tests2019v2.pdf

## Slide 5
Coils mechanical properties*
*«Mechanical structures for superconducting dipoles. Different configurations for different applications» by. D. Perini (2022)
Conductors & Insulation
MPa *
MPa *
https://indico.cern.ch/event/1192313/attachments/2549170/4390531/Seminar.pdf
MPa *

## Slide 6
ANSYS Mechanical model: contacts
Standard contact (sliding & detachment permitted) contact
No separation (sliding permitted) contact
Standard rigid-deformable
(sliding & detachment permitted contact)

## Slide 7
ANSYS Mechanical model: BCs

## Slide 8
ANSYS Mechanical model: Lorentz forces
Magnetic force [N/m]

## Slide 9
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | [mm/m]
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
ODS Copper | ductile | 110 (110) | 270 | 340 | 3.37
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | 
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
ODS Copper | ductile | 110 (110) | 270 | 340 | 3.37
wedges properties
* «A Review of the Mechanical Properties of Materials Used in Nb3Sn Magnets for Particle Accelerators» by G. Vallone (2023) DOI: 10.1109/TASC.2023.3248544

## Slide 10
Keys properties
* «A Review of the Mechanical Properties of Materials Used in Nb3Sn Magnets for Particle Accelerators» by G. Vallone (2023) DOI: 10.1109/TASC.2023.3248544
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | [mm/m]
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
SS316LN* | ductile | 193 (210) | 238 | 610 | 2.80
Kawa SS* | ductile | 186 (204) | 320 | (?) | 1.80
Nitronic 40* | ductile | 225 (210) | 682 | 1427 | 2.60
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | 
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
SS316LN* | ductile | 193 (210) | 238 | 610 | 2.80
Kawa SS* | ductile | 186 (204) | 320 | (?) | 1.80
Nitronic 40* | ductile | 225 (210) | 682 | 1427 | 2.60

## Slide 11
Pad properties
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | [mm/m]
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
SS316LN* | ductile | 193 (210) | 238 | 610 | 2.80
Nitronic 40* | ductile | 225 (210) | 682 | 1427 | 2.60
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | 
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
SS316LN* | ductile | 193 (210) | 238 | 610 | 2.80
Nitronic 40* | ductile | 225 (210) | 682 | 1427 | 2.60
* «A Review of the Mechanical Properties of Materials Used in Nb3Sn Magnets for Particle Accelerators» by G. Vallone (2023) DOI: 10.1109/TASC.2023.3248544

## Slide 12
Iron properties
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | [mm/m]
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
ARMCO* | fragile | 224 (213) | 286 | 975 | 2.00
Magnetil* | fragile | 200 (200) | 249 | 723 | 2.00
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | 
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
ARMCO* | fragile | 224 (213) | 286 | 975 | 2.00
Magnetil* | fragile | 200 (200) | 249 | 723 | 2.00
Fragile:
** «Review of Key-and-Bladder structures» by P. Ferracin (2016)
* «A Review of the Mechanical Properties of Materials Used in Nb3Sn Magnets for Particle Accelerators» by G. Vallone (2023) DOI: 10.1109/TASC.2023.3248544

## Slide 13
Shell properties
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | [mm/m]
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
A7075* | fragile | 72 (79) | 480 | 490 | 4.20
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | 
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
A7075* | fragile | 72 (79) | 480 | 490 | 4.20
* «A Review of the Mechanical Properties of Materials Used in Nb3Sn Magnets for Particle Accelerators» by G. Vallone (2023) DOI: 10.1109/TASC.2023.3248544

## Slide 14
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | [mm/m]
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
Conductors | fragile | 31 (39) | 100 | 120 | 3.80
Glidcop wedges | ductile | 110 (110) | 270 | 340 | 3.37
Fiberglass | - | - | - | - | -
SS316LN* pad | ductile | 193 (210) | 238 | 610 | 2.80
Kawa SS keys | ductile | 186 (204) | 320 | (?) | 1.80
Iron yoke* | fragile | 204 (225) | 250 | 720 | 2.00
Al7075* shell | fragile | 72 (79) | 480 | 490 | 4.20
Material | Behaviour | E [GPa] | Stress limit [MPa] | Stress limit [MPa] | 
 |  | @ R.T. (1.9K) | @R.T. | @1.9K | R.T. → 1.9K
Conductors | fragile | 31 (39) | 100 | 120 | 3.80
Glidcop wedges | ductile | 110 (110) | 270 | 340 | 3.37
Fiberglass | - | - | - | - | -
SS316LN* pad | ductile | 193 (210) | 238 | 610 | 2.80
Kawa SS keys | ductile | 186 (204) | 320 | (?) | 1.80
Iron yoke* | fragile | 204 (225) | 250 | 720 | 2.00
Al7075* shell | fragile | 72 (79) | 480 | 490 | 4.20
ANSYS Mechanical model: properties*
* «A Review of the Mechanical Properties of Materials Used in Nb3Sn Magnets for Particle Accelerators» by G. Vallone (2023) DOI: 10.1109/TASC.2023.3248544

## Slide 15
Thanks for the attention