## Slide 1
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program (www.chart.ch).
Modelization of Impregnated Nb3Sn Cable Composite at PSI B. Auchmann (PSI/CERN), D. M. Araujo, A. Brem, M. Daly, A. Milanese (CERN) X. Kong, P. Studer, T. Tervoort (ETHZ/D-MAT/SMG)
05.12.23 – RDL4 Mtg

## Slide 2: CHART / SMACC / Materials
CHART is a research network. LTS ASC competences are distributed
  Conductor, Cable: UniGE, CERN
  Insulation materials (resins, 10-stack characterization): ETHZ SMG, PSI
  Powered samples: PSI, UTwente
  Magnet design and construction: PSI
PSI is working on stress-managed solutions  special requirements for coil composite:
  Training in CCTs and possible all SM solutions scales with length of magnet.
  Minimal-training impregnation material required.
  No RT preload  relatively soft materials are eligible.
The BOX program has identified candidates:
  Paraffin wax
  Filled paraffin wax
  Filled epoxy
No 10-stack data or Walther-spring measurements exists with these materials.

## Slide 3: Multi-scale 1/5 WireChar
UniGE: WASP measurement and simulations.
[C. Senatore, M. Bonura, et al., CHART annual meeting, indico link, Oct. 2023.]

## Slide 4: Multi-scale 2/5 MagComp
ETHZ: 10-stack measurements with image analysis (particle-tracking method).
  Epoxy vs. paraffin, vs. filled epoxy and paraffin.
Extraction of homogenized material description for ANSYS (or other) pending.
[X. Kong, T. Tervoort, et al., CHART annual meeting, indico link, Oct. 2023.]

## Slide 5: Multi-scale 3/5 MagDev
PSI/UTwente: transverse pressure characterization of Rutherford cable in background field.
Courtesy S. Otten et al.
Courtesy M. Daly
[M. Daly, S. Otten, et al., CHART annual meeting, indico link, Oct. 2023.]

## Slide 6: Multi-scale 4/5 2D and 3D Approaches
Comparison of 10-stack to strand-based 2D models.
CEA CoCaSCOPE ANSYS model of 11-T cable for analysis of ETHZ 10-stack measurements.
Generation of
  10-stack model: 3D constitutive law
  U-shaped UTwente sample: validation of Ic()
[G. Lenoir et al.]
[J. Ferradas, TE-MSC Seminar,
indico link, June 2023.]

## Slide 7: Multi-scale 5/5: Impact on Magnet Design MagNum2
Include missing mechanical and performance data into conceptual design of SMACC (Stress Managed Common Coil).
Provide fully consistent, traceable, and repeatable CDR, including measurement data, multi-scale FEA model validation, design, and expectations for strain-gauge data, all via Model-Based Systems Engineering (MBSE).
Versioned CDR as a living document.
PhD at PSI with ETHZ D-ITET-IEF to start in ‘24.
[D. M. Araujo, HFM Annual Mtg,
indico link, Oct 2023.]
[http://cern.ch/auchmann/chart/magnum http://cern.ch/auchmann/hts4.]

## Slide 8: Future Multi-scale Topics
Multi-physics multi-scale:
  Mechanical models, discussed in this meeting,
  Electromagnetic models (coupling currents, etc),
  Thermal behavior.
Up- (homogenization) and down- (return to reference volume) scaling.
LTS and HTS models.
ML homogenization experiments.