## Slide 1: Radiochemistry Developments on 224Radium(224Ra)
MUHAMMAD INZAMAM
(PINSTECH, Pakistan Atomic Energy Commission)

## Slide 2: Layout
Introduction
Production of 224Radium (224Ra)
224Ra/212Pb Generator Production
Labelling of 212Pb with DOTA
Conclusion

## Slide 3: Introduction
224Radium is a pure alpha emitter
Favorable half life 3.6 day
Short lived daughter product
Notes: Radium is very situabile candidate for the
The demand of these radionuclides is significantly high than the available resources but international efforts are under way to increase the number and production capacity of such radionuclides.Ra is not very much popular in nuclear medicine for direct use as in case of 223Ra simple salt of radium is an only EMA and FDA approved alpha emitting drug used for treatment of metastatic prostate cancer

## Slide 4: Production of 224Radium
Several method for the production
  Radiochemical separation from the Th/U
  Spallation reaction of thorium by proton irradiation
  228Th/224Ra Generator

## Slide 5: 224Radium/212 Lead Generator Production
There are two methods of 224Ra/212Pb generator production
  Collection of emanated radon from radium source
  Radiochemical separation of using cation exchange resin.

## Slide 6: 224Ra/212Pb Generator by Radon Collection
224Radium is used as source in the generator
Glass bottle with plastic lid as generator body
Source adsorbed on the glass wool
Collection chamber for radon
Decays into 212Pb

## Slide 7: Elution of Generator
Elution of generator after the establishment of secular equilibrium
Elution of 212Pb with 0.1M HCl

## Slide 8: Efficiency and Stability
Generator from few kBq to 80MBq are produced
Elution are taken every two days for several weeks
Generators are eluted with average efficiency of 33%
High activity did not damage the generator structure

## Slide 9: 224Ra/212Pb Generator by Cation exchange resin
Generator consist of a glass column
Cation exchange resin for adsorption of radium source
Preconditioning of column
224Ra loading on the column followed by washing
Elution of generator with few ml of HCl

## Slide 10: Efficiency of the Generator
Generator eluted for three time after every two day
Average 56% of the 212Pb recovered from the generator
Ra breakthrough was observed in the elution up to 9%
Some issues identified during experiment which will lead to improvement
Chart: No.of Elution
| 1 | 2 | 3
212Pb | 0.62 | 0.5 | 0.55208
Radium breakthrough | 0.09 | 0.05 | 0.09

## Slide 11: Radiation Safety
All the following steps for generators carried out in Gloves box
  224Ra foil retrieval for target holder
  Dissolution of the 224Ra
  Generator production
  Elution
  No release of radon or any contamination

## Slide 12: Quality of 212Pb from Generator
Gamma spec. analysis of elution
In first generator, no radium was detected (<224Ra MDA) in elution
Generator of activity ~80MBq dispatch to one of partner institute for further evaluation/labelling studies
In cation exchange resin, up to 9% radium was detected used internally only on experimental work

## Slide 13: Labelling and Further Studies
Radon collection type generator of 80MBq dispatch to partner institute for further studies
  Labelling of the 212Pb with DOTATATE
  Stability of Pb-DOTA Complex in mouse serum
Request trough PRISMAP for clinical translation studies in Dresden University Hospital

## Slide 14: Conclusion
Production of 224Ra/212Pb generator of two different types
With generator efficiencies up to 33% and 56%.
High quality product with safe operation
Good labelling result and stability results