## Slide 1
A
x
0
t
0
τ
Pa
Pa
1D heat equation:
Boundary conditions:
x=0
The general heat equation solutions are the so called «error functions»
(A is a homogeneous semi-infinite metal)
(k and α are assumed here to be temperature independent)
Temperature increase at a metal (superconducting) surface
in the presence of a pulsed rf electromagnetic field

## Slide 2
In the case of Neuman boundary conditions, for 0 ≤t ≤τ, the solution is :
ierfc +
x=0
+
The x dependence for t=τ is :
Chart: 
| 0 | 0.1 | 0.2 | 0.30000000000000004 | 0.4 | 0.5 | 0.6 | 0.7 | 0.79999999999999993 | 0.89999999999999991 | 0.99999999999999989 | 1.0999999999999999 | 1.2 | 1.3 | 1.4000000000000001 | 1.5000000000000002 | 1.6000000000000003 | 1.7000000000000004 | 1.8000000000000005 | 1.9000000000000006 | 2.0000000000000004 | 2.1000000000000005 | 2.2000000000000006 | 2.3000000000000007 | 2.4000000000000008 | 2.5000000000000009 | 2.600000000000001 | 2.7000000000000011 | 2.8000000000000012 | 2.9000000000000012 | 3.0000000000000013 | 3.1000000000000014 | 3.2000000000000015 | 3.3000000000000016 | 3.4000000000000017 | 3.5000000000000018 | 3.6000000000000019 | 3.700000000000002 | 3.800000000000002 | 3.9000000000000021 | 4.0000000000000018 | 4.1000000000000014 | 4.2000000000000011 | 4.3000000000000007 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.6999999999999993 | 4.7999999999999989 | 4.8999999999999986 | 4.9999999999999982
 | 1 | 0.91388 | 0.83274 | 0.75655 | 0.68525 | 0.61875 | 0.55694 | 0.49971 | 0.44689 | 0.39833 | 0.35386 | 0.31328 | 0.27639 | 0.243 | 0.21287 | 0.18582 | 0.16161 | 0.14003 | 0.12089 | 0.10397 | 0.089078 | 0.076027 | 0.064637 | 0.054738 | 0.046173 | 0.038794 | 0.032464 | 0.027057 | 0.022459 | 0.018566 | 0.015285 | 0.012532 | 0.010231 | 0.0083186 | 0.0067348 | 0.0054295 | 0.0043586 | 0.0034839 | 0.0027728 | 0.0021973 | 0.0017337 | 0.001362 | 0.0010653 | 0.00082959 | 0.00064318 | 0.00049646 | 0.00038151 | 0.00029187 | 0.00022229 | 0.00016855 | 0.00012722
x/xD
T0
TMax
The espression is the same reported
by I.Wilson , CLIC Note 52 (15.10.87)

## Slide 3
It is easy to show that the overall t dependence, at x=0, is :
+
Chart: 
Chart: 
t/τ
t/τ
+
TMax
T0
(Note that even for t=100τ the temperature is higher that T0 . This would be true
for any t, and repeeating the pulses would cause a continuous increase of TMax.
This is simply due to the fact that the model does non include a bath at T0 .

## Slide 4
A
B
x
0
t
0
τ
Pa
L
Pa
Let’s consider the case of an A/B interface, where A is a metal
of thickness L and B is a homogeneous semi-infinite metal.
We need to solve two coupled 1D heat equations:
x=0
with the boundary conditions:
x=L
x=L
(neglecting Kapitza resistance)

## Slide 5
is the power crossing the A/B interface
The two coupled A/B equations, with the given boundary conditions, cannot (?)
be exactly solved analytically. An approximate solution can be obtained
considering for the solutions the same form of the homogeneous case :
+
+
The boundary conditions imply :
)
C1B and C2A are (mild) functions of t so that TA and TB are not exact solution of the heat equation.

## Slide 6
0
2
4
3
x
L
TMax
>
A
T0
B
A tipycall x dependence of the temperature is reported below :
(the ratio of the temperature vs x dependence slopes at the A/B interface is kA/ kB)
xDB

## Slide 7
If the surface power is supplied via a r.f. electromagnetic field we can write :
Rs is the A material surface resistance
Eacc is here the maximum surface electric field
In the model discussed so far, Pa is assumed to be deposited as a delta function at x=0
Here the power is adsorbed in a layer of thickness δ (λ if the material is a superconductor), so the model approximation is satisfied only if δ (λ ) << L.
If Rs = Rs(T) (rapidly increasing with T, as is the case of a superconducting material) and if
the power systems keeps the accelerating field Eacc = constant , the adsorbed power Pa increases with temperature and, depending on the materials parameters and the initial conditions, can cause a large increase of the surface temperaure, up to thermal runaway.
The temperature dependence of Rs can be described, for a superconductor, by the two-fluid formula :
where is the surface resistance of the superconductor at the initial temperature
and α=4 , β =3/2 for a BCS superconductor and α=2 , β =0.3 for a HTCS superconductor.

## Slide 8
Chart: 
Chart: 
Eacc = 51.06MV/m
This iterative calculation has been implemented using excell for N=100.
Input parameters are T0 , kA/B , αA/B (or Cp and ρ), τ , LA, Rs0 , Tc and Eacc .
TMax (K)
The reported examples show the time evolution of the surface temperature for a
Nb/Cu interface (Nb, RRR=30, Cu, RRR=300) with LA= 10μm from the liquid helium
starting temperature. In figure on the left the calculation for Pa=cost is also reported.
Thermal runaway occurs for Eacc = 51.06MV/m.
The calculation could be further improved including the temperature dependences of kA/B , αA/B , if known in analytical form or tabulated data.
TMax (K)
Eacc = 49 MV/m
Pa =cost
τ
t (μs)
t (μs)
τ

## Slide 9
+
To estimate the error of the approximate solutions, we can set A=B in the solution for TMax :
We already know that , for a uniform material (A), it is :
+
So that the difference between the approximate solution and the exact in this case is :
Chart: 
| 0 | 0.2 | 0.4 | 0.60000000000000009 | 0.8 | 1 | 1.2 | 1.4 | 1.5999999999999999 | 1.7999999999999998 | 1.9999999999999998 | 2.1999999999999997 | 2.4 | 2.6 | 2.8000000000000003 | 3.0000000000000004 | 3.2000000000000006 | 3.4000000000000008 | 3.600000000000001 | 3.8000000000000012 | 4.0000000000000009 | 4.2000000000000011 | 4.4000000000000012 | 4.6000000000000014 | 4.8000000000000016 | 5.0000000000000018 | 5.200000000000002 | 5.4000000000000021 | 5.6000000000000023 | 5.8000000000000025 | 6.0000000000000027 | 6.2000000000000028 | 6.400000000000003 | 6.6000000000000032 | 6.8000000000000034 | 7.0000000000000036 | 7.2000000000000037 | 7.4000000000000039 | 7.6000000000000041 | 7.8000000000000043 | 8.0000000000000036 | 8.2000000000000028 | 8.4000000000000021 | 8.6000000000000014 | 8.8000000000000007 | 9 | 9.1999999999999993 | 9.3999999999999986 | 9.5999999999999979 | 9.7999999999999972 | 9.9999999999999964



 | 0 | 0.054797 | 0.092049 | 0.11443 | 0.12472 | 0.12564 | 0.11975 | 0.10932 | 0.096293 | 0.082203 | 0.068221 | 0.055158 | 0.043513 | 0.033529 | 0.025256 | 0.01861 | 0.01342 | 0.0094747 | 0.0065509 | 0.0044368 | 0.002944 | 0.0019142 | 0.0012197 | 0.00076167 | 0.00046622 | 0.00027973 | 0.00016453 | 9.4861e-05 | 5.3619e-05 | 2.9713e-05 | 1.6142e-05 | 8.5977e-06 | 4.4896e-06 | 2.2985e-06 | 1.1537e-06 | 5.6779e-07 | 2.7396e-07 | 1.296e-07 | 6.0108e-08 | 2.7333e-08 | 1.2186e-08 | 5.3266e-09 | 2.2828e-09 | 9.5916e-10 | 3.9512e-10 | 1.5958e-10 | 6.3191e-11 | 2.4532e-11 | 9.3372e-12 | 3.4842e-12 | 1.2747e-12
error
L/xAD
The approximation made over estimates the maximum surface
temperature up to a maximum of about 12% when L=xAD

## Slide 10
Finally we have :
+
+
+
and :

## Slide 11
The problem can be easily faced dividing the pulse time lenght τ into N small intervals Δτ
(so that τ= NΔτ) sufficiently small that Rs can be considered constant in that interval.
The solution can than be found by a simple iteration procedure :
+
with :
T2
with :
( )
+
, and :
x=0
+
, and :
x=0