## Slide 1: MuSR study on the quantum magnetism of 2D frustrated compounds
Shanghai Jiao Tong University
Jie Ma
2024.04.21.
Workshop on Muon Physics at the Intensity and Precision Frontiers (MIP 2024)

## Slide 2: Outline
Geometrically Frustrated Magnet
2. Quantum effect in triangular lattice
3. Disorder state of Honeycomb lattice
2
4. Conclusion and outlook

## Slide 3: Geometrically Frustrated Magnet
Competing or contradictory constraints on a large fraction of the magnetic sites ─ geometric magnetic frustration
?
?
?
Fig. 2D frustrated model.
Fig. 3D model.
RuCl3
J < 0
J > 0

## Slide 4: Geometrically Frustrated Magnet
Examples of frustrated lattice
Fig. Kagome lattice.
Fig. Spinel lattice AB2O4.
Fig. Pyrochlore lattice A2B2O7.
?
?
?
Fig. Frustrated model of 2D and 3D system.
Fig. Triangular lattice.
─ Edge/corner sharing triangles
triangular/kagome lattices (2D)
─ Corner sharing tetrahedra
Spinel/Pyrochlore lattices (3D)
Competing or contradictory constraints on a large fraction of the magnetic sites ─ geometric magnetic frustration
4

## Slide 5: Geometrically Frustrated Magnet
Examples of frustrated lattice
?
?
?
Fig. Frustrated model of 2D and 3D system.
─ Edge/corner sharing triangles
triangular/kagome lattices (2D)
─ Corner sharing tetrahedra
Spinel/Pyrochlore lattices (3D)
Competing or contradictory constraints on a large fraction of the magnetic sites ─ geometric magnetic frustration
5
Superconductor
P.W. Anderson 1973、1987
Physics Today 69, 30 (2016).

## Slide 6
Competing or contradictory constraints on a large fraction of the magnetic sites ─ geometric magnetic frustration
Examples of quantum-spin-liquid
PRL 91, 107001 (2003); PRL 100, 087202 (2008); PRL 95, 177001 (2005); JACS 130, 2922 (2008); Nature Phys. 6, 865 (2010); Nature 464, 199 (2010); npj Quant. Mater. 4, 12 (2019); npj Comp. Mater. 8, 10 (2022).
Material | Lattice | Θcw (K) | J (K)
κ-(BEDT-TTF)2Cu2(CN)3 | anisotropic triangular | -375 | 250
EtMe3Sb[Pd(dmit)2]2 | anisotropic triangular | -375~-325 | 220-250
YbMgGaO4 | Triangular | -4 | 1.5
Na4Ir3O8 | Hyperkagome | -650 | 430
PbCuTe2O6 |  | -22 | 15
ZnCu3(OH)6Cl2 (herbertsmithite) | Kagome | -314 | 170
Cu2Zn(OH)6FBr (barlowite) | Kagome | -200 | 170
Rb2Cu3SnF12 | Kagome | -100 | 154.4
Ca3Cr7O28 | Distorted Kagome |  | -9
6
Quantum Spin Liquid
─ No magnetic long-range ordering
─ No symmetry broken
─ Fractional excitation: spinon
─ Strong fluctuation at low energy
Quantum Spin Liquid

## Slide 7
Competing or contradictory constraints on a large fraction of the magnetic sites ─ geometric magnetic frustration
7
Quantum Spin Liquid
─ No magnetic long-range ordering
─ No symmetry broken
─ Fractional excitation: spinon
─ Strong fluctuation at low energy
Quantum Spin Liquid
Identification of quantum-spin-liquid
Specific heat measurements: the low-energy density of states;
Thermal transport measurements: localized or itinerant excitations;
Neutron scattering/Nuclear-magnetic resonance: excitations and correlations;
Reflectance measurements: power-law optical conductivity
Spin-orbital (Wilson Ratio)
R = [4π2kB2χ0] / [3(gμB)2γ]
Frustration

## Slide 8: Geometrically Frustrated Magnet
Examples of frustrated lattice
Competing or contradictory constraints on a large fraction of the magnetic sites ─ geometric magnetic frustration
Nature 540 22 (2016); Nat. Phys. 17, 726 (2021); Nat. Commn. 13, 5796 (2022)

## Slide 9
Is there a pure QSL?
Adv. Quant. Technol., 1900089 (2019); The Innov. 4, 100484, (2023); Nat. Phys. 19, 922 (2023).
PRB 108, 174424 (2023); arxiv 2402.07730 (2024)
Ba3MnSb2O9
Na2BaCo(PO4)2
9

## Slide 10
NaYbSe2
10
P. Dai, et al., PRX 11, 021044 (2021); Z. Zhu et al., The Innov. 4, 100459 (2023).
(a) QSL’s evidences:
Cm/T (<0.5 K) is almost a constant, indicating the spinon Fermi surface spin liquid;
the 𝜇SR spectra show no spin freezing with robust dynamics and strong quantum fluctuations;
Continuous spin excitations by INS.
NMR indicates the coexistence of short-range magnetic order and QSL

## Slide 11
μSR study of NaYbSe2
11
Z. Zhang, et al., PRB 106, 085115 (2022
No oscillation is seen in the ZF-μSR spectra down to 50mK;
No spin-glass-like freezing
Both λ and β go up to a plateau below 0.3 K, indicating the emergence of a stable magnetically disordered QSL ground state.

## Slide 12: Outline
Geometrically Frustrated Magnet
2. Quantum effect in triangular lattice
3. Disorder state of Honeycomb lattice
12
4. Conclusion and outlook

## Slide 13
Kitaev model
arXiv: cond-mat/0506438v3
  Anyons in an exactly solved model
  Energy gaps: local excitations
  Topological Quantum Numbers: excitations stable
  Topological Order

## Slide 14
Honeycomb-Kitaev
  H3LiIr2O6
R. Yadav, et. al., PRL 121, 197203 (2018); S. Nishimoto, et. al., Nat. Comm. 7, 10273 (2016); S. Hwan Chun, et al., Nat. Phys. 11, 462 (2015).
4d/5d transition mental
The Kitaev model extended to a Heisenberg-Kitaev model:
Kitaev term K,
off-diagonal symmetric exchange term  and Γ′,
J (JNN), and the third NN coupling J3
  α-Li2IrO3
  α-Na2IrO3
14

## Slide 15
  α-RuCl3
A. Banerjee et al. Nat. Mater. 15, 733 (2016)
Dominant Kitaev term K
Magnetic ordered at 0 T while disordered at 7 T (potential QSL)
Quantum spin liquid behavior
α-RuCl3
15

## Slide 16
  Co2+ 3d7
A. K. Bera, et al. Phys. Rev. B 95, 094424 (2017); C. Kim et al., arXiv:2012.06167 (2020).
Splitting of the degenerate d7 states
Octahedral and Trigonal crystal field in a single-electron picture
Spin-orbit coupling in a multi-electron picture
3d transition metal
16

## Slide 17
M. Songvilay et al., PRB 102, 224429 (2020); A. K. Bera, et al., PRB 95, 094424 (2017); J. Yan, et al., PRM 3, 074405 (2019)
Na3Co2SbO6 and Na2Co2TeO6 have the similar structure
Distortions of Na2Co2TeO6 and Na3Co2SbO6 are different
Na2Co2TeO6 and Na3Co2SbO6
  Na2Co2TeO6
  Na3Co2SbO6

## Slide 18
Heat capacity & Magnetic susceptibility
CV
CV
CV
  With the field,
  1) Long-range ordering disappeared;
  2) Anisotropy between ab-plane and c-axis;
  3) All susceptibilities crossed at around 11.5 T.
18

## Slide 19
High-field electron spin resonance
  Four modes are observed: 1) A and B modes almost overplot on each other, gab~4.13;
  2) C mode is gapped with gc~2.25;
  3) D mode is broad and weak, between A/B and C lines.
A. Ponomaryov, et. al., PRL 125, 037202 (2020)
19

## Slide 20
20
Magnetic torque measurements
  Differential magnetic susceptibility and ,
  - reflects the off-diagonal magnetic susceptibility；
  - three transition: BC1 ~ 6 T, BC2 ~ 7.5 T and BC3 ~ 10 T for B // a*.
  - the region between BC2 and BC3 is a phase distinct from the trivial polarized phase.

## Slide 21
Temperature- and field-dependence of torque
Between BC2 and BC3, perfect 6-fold symmetry and the amplitude of the torque is larger than the polarized phase above BC3, indicating a disordered ground state with obvious quantum fluctuations ;
21

## Slide 22
H vs T phase diagram, B // a*-axis
  Phases are complicated
  1) QSL-like phase is observed
  2) No plateau is observed, only spin flip
npj Quantum Materials 3, 8 (2018)
22

## Slide 23
Spin-dynamics
23

## Slide 24
24
PRB 103, L180404 (2021); PRB 102, 224429 (2020); JPCM 34, 045802(2021); PRL 129, 147202 (2022); PRB 106, 014413 (2022).
Comparisons
Low-energy dynamics can be dictated by the J3-Δ model, indicating the J3 is important.

## Slide 25
25
μSR by M20D at TRIUMF
  ZF-μSR : very fast depolarization and superimposed oscillations within 50 ns below TN, strong quasistatic internal field;
  λT reflects the width of static magnetic field distribution.
  TF and T* present anomalies.
LF=0.1T

## Slide 26
26
μSR by GPS at PSI
arXiv:2307.16451v1 (2023)
  Vmag(0K) = 60 % suggests the bond-dependent anisotropic frustrations (Kitaev interactions) and quantum fluctuations；
  Strong spin dynamics at low temperature.

## Slide 27
27
Inelastic Neutron Scattering
QSL mean-field K-J1-Γ-Γ′-J3 model
Background field to enforce the symmetry-breaking

## Slide 28
28
Inelastic Neutron Scattering
J1 = −1.54 meV, J3 = 1.32 meV, K = 1.408 meV, Γ = −1.32 meV, and Γ′ = 0.88 meV,
J1 = 0.066 meV, J3 = 1.32 meV, K = −3.399 meV, Γ = 0.286 meV, and Γ′ = 0.077 meV.

## Slide 29: Conclusions
  Quantum effect in 2D triangular/honeycomb lattices could very strong
  New physical properties could be introduced with the complicated interactions of the quantum fluctuation and spin/orbital
  Spinons of RVB? or Vortex fermion excitations?
  muSR has a strong contribution to the proof of QSL
29

## Slide 30: Quantum Spin Liquid Candidate
REChX (RE = rare earth; Ch = O, S, Se, Te; X = F, Cl, Br, I)
Chin. Phys. Lett. 38， 047502 (2021)

## Slide 31
Yb3+
Jeff=1/2
3.51 Å
3.72 Å
Triangular lattice in a single layer and the neighbor layers form a stacked honeycomb lattice.
An AFM transition was detected at about 1.3 K.
Strong anisotropy in M-H curves.
YbOCl

## Slide 32
Thermodynamic measurements of YbOCl
The AFM transition moves toward high temperature with increasing field.
A spin disordered state was detected.
The anisotropic spin Hamiltonian was constructed.
Notes: From the magnetic dependent heat capacities and magnetic susceptibilities, the phase transition peak shows exotic behavior. Firstly, the peak should move to lower temperature with increasing magnetic field for a traditional AFM phase, because the magnetic field could suppress the magnetic fluctuation, while in this material, the peak shows a distinct magnetic-field dependence. Secondly, the sharp peak that represents phase transition becomes broad and smooth when magnetic field is up to 0.2 T, suggesting the system enters a disordered region with strong fluctuation. This character is also captured by alternating current magnetic susceptibility measurements. AC susceptibility measures the ability of a spin to respond or flip with a change in the external magnetic field, allowing it to be related to the magnetization or spin fluctuations in the system. In the magnetic field from 0.1-3.5 T range, the AC magnetic susceptibility is nearly constant at a plateau, this is a fascinating finding closely related to the spin disorder. This magnetic field driving spin disorder state is related to the special magnetic structure confined in ab-plane, thus the magnetic field along the c-axis is a transverse field, which can enhance the quantum fluctuation. Additionally, we executed single crystal inelastic neutron scattering experiment at TASP, and the extra magnetic peaks separated from nuclear peaks those can be indexed by propagation vector (0 0 1.5) were detected below 1.3 K. This is consistent with the heat capacity and magnetic susceptibility measurements and verify the AFM transition. Interestingly, from the magnetic field dependence of the magnetic peak (001.5), we find the magnetic Bragg peak is almost undetectable under 0.3 T, suggesting that a relatively small magnetic field can suppress the magnetic phase transition and push the spin system into a disordered state.
In order to reveal the abundant physics in YbOCl, we and our theoretical collaborators construct the Hamiltonian and the full diagonalization method was applied to simulate the magnetization and heat capacity data to derive various parameters in the Hamiltonian. Considering the strong SOC of Yb3+ and the distorted octahedral
structure, the off-diagonal terms of the anisotropic spin interaction will play an important role. Therefore, the anisotropic spin Hamiltonian is represented as follows: where HHoneycomb is the NN spin Hamiltonian, Htriangular is the NNN spin Hamiltonian, and HZeeman is the splitting term. For the NN spin Hamiltonian

## Slide 33
FD simulation results of YbOCl
Jzz=1.05K, J=-0.6K
Jzz=0.26K, J=-0.42K
J=0.39K, Jz=0
J =0.13K, Jz=0
J1=-0.71K, K1=0.78K
1=1.27K, 1=0.49K
J2=-0.11K, K2=-0.26K
2=0.05K, 2=0.07K
Derived parameters
NPD and INS results
Notes: In order to obtain the diagonal terms firstly, we choose to simulate the data at high temperature and high field, where the spins are essentially aligned with the direction of the external magnetic field and the off-diagonal terms can be ignored. Through the fitting and simulation calculations of the M/H-T data, we found an optimal set of parameters, namely Jzz = 1.05 K, J′zz = 0.26 K, J± = -0.6K, and J′± = -0.42 K. This set of parameters can well reproduce both the MH and MT experimental results. Then the off-diagonal terms can be derived by fitting heat-capacity data at polarization region. And J±±=0.39K, J±±’=0.13K, Jz±=0, Jz±’=0 were obtained. It should be pointed out that the spin Hamiltonian in YbOCl is strictly equivalent to the J-K-Γ-Γ’ model, which allows a mutual conversion of spin-exchange interactions between the two models, resulting in J1 ∼ -0.71 K, K1 ∼ 0.78K, Γ1 ∼ 1.27 K, and Γ′1 ∼ 0.49 K for the honeycomb lattice, and J2 ∼ -0.11 K, K2 ∼ -0.26 K, Γ2 ∼ 0.05 K, and Γ′2 ∼ 0.07 K for the triangular lattice. Apparently, the NNN spin interactions are smaller than the NN spin interactions in the representation of J −K −Γ−Γ′ model, which suggests that the spin interactions in the honeycomb lattice play a major role in the magnetism of YbOCl. We also performed powder inelastic neutron scattering on Pelican, ANSTO and the data of elastic part were extracted to analyze the magnetic structure at ground state of YbOCl. Three distinct magnetic peaks indexed by (001.5) (007.5) (102.5) were observed with a propagation vector (001.5). Although the resolution is not good enough to do the Rietveld refinement, we can use the relative intensity of these different magnetic peaks and nuclear peaks combined with the thermodynamics data to rule out some spin configurations. Firstly, the magnetic moments should lie in ab plane mainly. Secondly, the magnetic structure is more likely to be a collinear one because the spin system can be polarized so easily when the magnetic field is applied in ab-plane. The magnetic structure is determined by iterating through the possible magnetic space group (MSG) solutions, which were derived from the k-SUBGROUPSMAG program of the Bilbao Crystallographic server. Through total 14 possibilities, the magnetic structure of magnetic moments align parallel in ab-plane and antiparallel along c-axis coincides with our experimental data best. This ground state is also verified by DMRG calculation based on the spin Hamiltonian above. The in-plane ferromagnetic and interlayer AFM ordered state in YbOCl is distinct from the observations in some other Kitaev compounds. For instance, the ground-state magnetic structure in α-RuCl3 and Na2IrO3 is a zigzag ordered state, and the ground state of YbCl3 is a Neel state. This may be closely related to the fact that J± and J′± are ferromagnetic interactions while Jzz and J′zz are antiferromagnetic interactions. Then this magnetic structure and the spin Hamiltonian were used to simulate the powder averaged INS data by SPINW package, and the calculated results highly reproduce the experimental measurements.

## Slide 34
Acknowledgements
Sample synthesis and characterization:
H. D. Zhou, Q. Zhang
Theoretical calculation:
Y. Wan, C. Batista, Y. Kamiya, M. Mourigal, J. Wu,
R. Yu, Z. Liu, J. Park
Neutron Beamline Scientists:
ORNL: M. Matsuda, S. Chi, H. Cao, T. Hong, G. Ehlers,
Feng Ye, D. Abernathy, M. Stone, O. Garlea
NCNR: N. Butch, Yiming Qiu
HZB: Z. L. Lu, J. Q. Xu, M. Russina, G. Günther
FRM-II, J-Parc, PSI, ANSTO, etc
μSR Beamline Scientists:
PSI: T. Shiroka, T. Shang; TRIUMF：X. Li, S. Dunsiger
34
NMR and ESR:
W. Yu, Z. Qu, W. Tong, X. Luo

## Slide 35
Thanks!