## Slide 1
Task 8.6 Superconducting ReBCO cable
T. Winkler (GSI) on behalf of task 8.6 members
I.FAST 3rd annual meeting, 18.04.24

## Slide 2: WP/Task structure and objectives
Design Parameters for a round, high current, low AC loss HTS ReBCO cable
Application: fast ramped, high field accelerator magnets
Milestone: M24 (https://doi.org/10.5281/zenodo.7995185)
Deliverable: M32 (https://doi.org/10.5281/zenodo.10697495)
Members:
  Institute of Electrical Engineering (IEE), Slovak Academy of Sciences, Slovakia
  ILK Dresden, Germany
  GSI, Germany
  EMS Chair, University of Twente (UT), Netherlands

## Slide 3: Cable layout
Starting point:
SIS100 cable (GSI/JINR) (LTS)
CORC/CORT type cable (ACT/IEE) (HTS)
Idea: use good direct cooling properties, and windability of SIS100 cable and apply it to HTS
CORC by ACT, advancedconductor.com

## Slide 4
AC loss and the cooling capacity are the main focus of year 2
HTS Cable
Mechanics
AC loss
Cooling
Magnet Design

## Slide 5: HTS tape mechanics

## Slide 6: HTS tape bending - results

## Slide 7: AC loss and cooling - striation
From last years meeting:
AC loss for a ramp from 1.9 T to 7.5 T:
373 W/m
Extending the ramp from 1 sec to 10 sec and introducing 0.5 mm wide filaments:
4.6 W/m
factor of 80 reduction

## Slide 8: AC loss – tape striation
https://doi.org/10.1109/TASC.2024.3364133
Sample:
230 mm length, 10 mm former diameter,
12 mm wide tape with 19 filaments
wf = 0.5 mm wide, gaps of wg = 0.1 mm
lay angle ⍺ = 67 degrees
Additional coupling loss for the Cu stabilized sample

## Slide 9: Cooling
Radial temperature for a short cable piece
Heat load 27 W/m
Simulation accounts for:
heat transfer coefficient He to pipe wall,
”effective” thermal conductivity of tape stack