## Slide 1
WP 9.3 progress at INFN-LNL
Nb3Sn magnetron sputtering
Dorothea Fonnesu – INFN Legnaro National Labs
I.FAST 11th WP 9 meeting
UKRI/STFC Daresbury Laboratory – 18.01.2024

## Slide 2: Outline
brief recap (since last meeting on 14.09.2023)
ongoing for Nb3Sn/Cu R&D at LNL and within I.FAST
new characterization results from LOT / Uni Siegen
plan for next characterizations

## Slide 3: Where we left
Tc trends on deposition parameters
cathode power ↘ critical temperature ↗
deposition pressure ↗ critical temperature ↗
observed on sapphire, not on Cu or Nb(1um)/Cu substrate
Sapphire + 1 μm Nb3Sn
Cu + 1 μm Nb3Sn
Cu + 1 μm Nb + 1 μm Nb3Sn
↑↓↗↘

## Slide 4: Where we left
Tc trends on deposition parameters
cathode power ↘ critical temperature ↗
deposition pressure ↗ critical temperature ↗
observed on sapphire, not on Cu or Nb(1um)/Cu substrate
Tc further improves by:
increasing thickness of Nb buffer layer (1um  ...  50 um)
decreasing annealing time (24h  5h  0h)
Cu + 1 μm Nb + 1 μm Nb3Sn
Cu + 30 μm Nb + 1 μm Nb3Sn

## Slide 5: Where we left
Tc trends on deposition parameters
cathode power ↘ critical temperature ↗
deposition pressure ↗ critical temperature ↗
observed on sapphire, not on Cu or Nb(1um)/Cu substrate
Tc further improves by:
increasing thickness of Nb buffer layer (1um  ...  50 um)
decreasing annealing time (24h  5h  0h)
Ongoing:
INFN-LNL: Tc, EDS, XRD, data analysis
LOT/Uni Siegen: SEM, EDS of FIB milled cross sections, SIMS (planned)
HZDR: magnetometry, RBS (planned), FLA tests
Uni Bratislava: magnetometry (samples @Uni Siegen)

## Slide 6: New characterisations
Sample/(buffer layer)/substrate [Tdeposition] | Tc (K) | Sn (At%)
Nb3Sn / Cu [600°C] | 12.8 ± 0.3 | 21.7
Nb3Sn / Nb(50µm) / Cu [600°C] | 17.3 ± 0.3 | 23.1
Nb3Sn / Cu [500°C] | 9.4 ± 0.3 | 24.7
Nb3Sn / Nb(50µm) / Cu [500°C] | 12.6 ± 0.2 | 26.3
Nb3Sn / Cu [600°C] annealed | 13.0 ± 0.1 | 20.9
Nb3Sn / Nb(1µm) / Cu [600°C] annealed | 14.1 ± 0.2 | 25.4
Nb3Sn / Nb(30µm) / Cu [600°C] annealed | 16.5 ± 0.1 | 23.1
(discussed in backup)
5h ANNEALING
NO ANNEALING
Samples sent to LOT (Uni Siegen)
Tc, composition (and more) measured at INFN-LNL
SEM surface images, EDS maps of FIB cross sections measured at LOT, Uni-Siegen by A. Zubtsovskii, T. Staedler
Lehrstuhl für
Oberflächen- und
Werkstofftechnologie

## Slide 7
Samples without buffer layer
Grain pattern of Cu substrate is visible
Cu_600
Cu_500
Grain size increases with deposition temperature
Sn content decreases
Tc = 9.4 K Sn = 24.7 At%
Tc = 12.8 K Sn = 21.7 At%

## Slide 8
Pt
Cu
Nb
Sn
Film/copper interface appears smeared and Sn-depleted
Rare voids at the top
Not enough to infer about Sn-Cu interdiffusion
Cu_500
Tc = 9.4 K Sn = 24.7 At%

## Slide 9
Pt
Cu
Nb
Sn
Film/copper interface appears porous and Sn-depleted
Voids at the film bottom (Pt contamination)
Cu diffusion visible
Cu_600
Tc = 12.8 K Sn = 21.7 At%

## Slide 10
Samples with 50 µm Nb buffer layer
Nb50_Cu_600
Nb50_Cu_500
Change in morphology and tin cluster density
Tc = 12.6 K Sn = 26.3 At%
Tc = 17.3 K Sn = 23.1 At%

## Slide 11
Nb50_Cu_500
Pt
Nb3Sn
Nb
FIB:
20 µm x 3 µm cut
Large wedge-like islands on top
Voids between islands
Nb
Pt
Sn
Tc = 12.6 K Sn = 26.3 At%

## Slide 12
Nb50_Cu_500
Tc = 12.6 K Sn = 26.3 At%

## Slide 13
Nb50_Cu_600
Pt
Nb3Sn
Nb
FIB:
20 µm x 3 µm cut
Voids in the top part of film
Visible interface between porous and non-porous region
Nb
Pt
Sn
Tc = 17.3 K Sn = 23.1 At%

## Slide 14: Next characterisations
LOT:
  Nb3Sn/Cu and Nb3Sn/Nb(1um)/Cu at 500 °C and 600 °C for SIMS (investigate weight of Nb buffer layer into Sn-Cu interdiffusion, if any)
HZDR:
  is RBS and magnetometry possible on samples sent for FLA tests? (Nb3Sn/Cu (2x), Nb3Sn/Nb(1um)/Cu, Nb3Sn/Nb(15um)/Cu, Nb3Sn/Nb(30um)/Cu (2x), deposited at 650 °C, not annealed)
Uni Bratislava:
  Nb3Sn/Nb(50um)/Cu at 500 °C and 600 °C from LOT for magnetometry
  Nb3Sn/Nb(9um)/Cu, Nb3Sn/Nb(40um)/Cu, Nb3Sn/Nb(50um)/Cu at 600 °C (*) with Nb3Sn film 0.6 um thick (standard is 1 um)
  is magnetometry of samples on sapphire substrate possible? we could ship those corresponding to the runs analysed by LOT and HZDR
10 mm x 10 mm x 1 mm sapphire substrate
10 mm x 20 mm x 0.5 mm copper substrate
FIB milling location

## Slide 15
Thank you!
Giovanni Marconato
Davide Ford
Eduard Chyhyrynets
Cristian Pira
Dorothea Fonnesu
Roberta Caforio
Alessandro Salmaso

## Slide 16: Backup

## Slide 17: Annealed samples
Sample/(buffer layer)/substrate [Tdeposition] | Tc (K) | Sn (At%)
Nb3Sn / Cu [600°C] annealed | 12.97 ± 0.13 | 20.9
Nb3Sn / Nb(1µm) / Cu [600°C] annealed | 14.09 ± 0.16 | 23.1
Nb3Sn / Nb(30µm) / Cu [600°C] annealed | 16.46 ± 0.14 | 25.4

## Slide 18
Cu_600
Cu_600_annealed(5h)
Tc = 12.97 K Sn = 20.9 At%
Tc = 12.8 K Sn = 21.7 At%

## Slide 19
Nb50_Cu_600
Nb30_Cu_600_annealed(5h)
Tc = 16.46 K Sn = 25.4 At%
Tc = 17.3 K Sn = 23.1 At%

## Slide 20
Nb3Sn/Nb[50µm]/Cu at 500°C
Nb3Sn/Nb[30µm]/Cu at 600°C