## Slide 1: Exploiting Cherenkov in Calorimetry
Nural Akchurin
TTU

## Slide 2: Start with an Example : BSO
Six distinct features distinguish Cherenkov radiation from scintillation:
  Directionality (Cherenkov cone, qc=cos-1 (1/bn(l), vs isotropic emission)
  Emission/wavelength spectrum (1/l2 vs scintillator specific)
  Cherenkov threshold (T=(g-1)mc2, for n=2 electrons:~80 keV, protons: ~140 MeV)
  Timing (Prompt vs ~several ns)
  Polarization (linearly polarized vs unpolarized)
  Cherenkov light is feeble (scintillation is often not)

## Slide 3: How (EM) Many Cherenkov Photons? (I)
We need realistic light yield estimates in order to set the scale for the calorimeter performance:
Critical values are the following:
  500 eV/cm in the form of Cherenkov photons
  Consider photon energy range from 1.7 eV to 3.0 eV
  160 to 250 Cherenkov photons are produced per cm
  Minimally ionizing particle loses 4.5 MeV/cm in quartz

## Slide 4: How (EM) Many Cherenkov Photons? (II)
Take 1 GeV electron/gamma shower in a block of quartz:
  Assume tracks as a collection of MIPs
  (1,000 MeV/4.5 MeV/cm) = 222 cm total track length
  (222 cm)(~200 photons/cm) = 44,000 Cherenkov photons per GeV
  Not all charged particles are above the Cherenkov threshold (T=190 keV)
  Cuts down to ~70%, i.e. 31,000 photons
There are three other major factors if quartz fiber calorimeter is considered:
  Packing fraction: ~1% by volume
  Fiber trapping efficiency: typically ~1% (depending on fiber 0.5 to 3%)
  Detection of these photons by a bi-alkaline PMT results in ~20% signal
  Therefore, we are left with ~0.62 p.e. per GeV
  Examples: CMS HF (copper) = 0.53 p.e./GeV; CMS HF (steel) = 0.25 p.e./GeV

## Slide 5: QQ, QP, Plastic, and Air-clad Fibers
 | QQ | QP | Plastic | Air-clad
NA | 0.22 | 0.37 | 0.55 | ~0.9
ncore | 1.46 | 1.46 | 1.5 | 1.46
ftrap | 0.57% | 1.61% | 3.36% | 9.5%
Optical fiber is an electromagnetic waveguide and light propagation through this waveguide is complex but can be solved for exactly. Depending on the refractive indices of the core and clad material and the geometry, the relevant features for calorimetry can be optimized. CMS HF hosts QP fibers.
If the radiation damage were not an issue, the choice of fiber
would be easy.
Plastic (PS) NA = 0.72 but suffers from short attenuation length (latt ~ 3 m)

## Slide 6: QQ, QP and Plastic Fibers and EM Energy Resolution - I
EM energy resolution is essentially scales with 1/sqrt{E}, thus it is dominated by Poisson photoelectron statistics in quartz fiber calorimeters
The constant term arises from non-uniformities in packing fractions (see CMS HF(steel), when summed linearly, it is ~4%)
At 100 GeV, practically achievable energy resolutions range 10% to 23% with quartz fibers alone

## Slide 7: QQ, QP and Plastic Fibers and EM Energy Resolution - II
Calorimeter | Fiber | Packing | Fiber-to-fiber dist (mm) | Fiber core dia (um) | Light yield (p.e./GeV)
CMS HF(copper) | QQ | 1.5% | 2.3 | 300 | 0.53
CMS HF(steel-L) | QP | 0.57% | ~7.1 | 600 | 0.25
DREAM | QP | 12.6% | ~4 | 600 | 8
 | P | 12.6% | ~4 | 600 | 18
Scaling approximately holds (ignore other contributions for now). For example,
  CMS HF(copper) to DREAM QP: (12.6/1.5)(1.61/0.57)(0.53)=12 vs 8
  CMS HF(steel-L) to DREAM QP: (12.6/0.57)(0.25)=6 vs 8

## Slide 8: QQ, QP and Plastic Fibers and EM Energy Resolution - III
40%/sqrt{E} EM resolution is clearly achievable with Cherenkov photons and can be further improved (perhaps 15-20%/sqrt{E}) in several ways:
  Improve NA or ftrap (~2x) [new optical structures…]
  Improve QE (~2x) [SiPMs vs PMTs …]
  Increase packing fraction (see RD52 prototypes)
  Improve sampling frequency

## Slide 9: Quartz Fiber/Cherenkov Hadronic Energy Resolution
Hadronic energy resolution of highly non-compensating calorimeters behaves significantly differently than typical scintillation-based calorimeters
At high energies (~1 TeV), most quartz Cherenkov calorimeters will perform similarly but at low energies, the situation is more complicated
For illustration purposes, assume c = -0.18-19 and Eo= 0.7 GeV

## Slide 10: Cherenkov Radiation and Polarization - I

## Slide 11: Cherenkov Radiation and Polarization - II

## Slide 12: Measuring Cherenkov Polarization in Three Steps
Setup 0 : No polarizer
Setup 1 : Favorable
Setup 2 : Unfavorable
Setup 0 : No polarizer
Setup 1 : Favorable
Setup 2 : Favorable

## Slide 13: BSO (Bi4Si3O12) Crystal - I
 | BSO | BGO | PWO
Density (g/cm3) | 6.80 | 7.13 | 8.28
Radiation length (mm) | 11.5 | 11.2 | 8.9
Decay time (ns) | ~100 | ~300 | ~10
Peak emission (nm) | 480 | 480 | 410-500
Relative light output | 0.04 | 0.1 | 0.01
Refractive index | 2.06 | 2.15 | 2.20
Cherenkov angle (o) | 61 | 62 | 63
Any transparent medium with a refractive index will generate Cherenkov light when a relativistic charged particle traverses it. BSO crystal is used as an example because the spectral characteristics proved convenient.

## Slide 14: BSO (Bi4Si3O12) Crystal - II

## Slide 15: Setup 0 : No Polarizers
Open symbols = muon
Filled symbols = pion
--------- = 1/cos(q)
C/S

## Slide 16: Setup 1 : Favorable Polarization Selection
The polarizers at both Cherenkov and scintillation side are oriented such that the horizontal components are transmitted as shown on the right.
The vertical components are
blocked.

## Slide 17: Setup 1 : C (Favorable) & S (Favorable)
Open symbols = muon
Filled symbols = pion
--------- = 1/cos(q)
C/S

## Slide 18: Setup 2 : Unfavorable Polarization Selection
The polarizer at Cherenkov side is oriented such that the vertical components are transmitted which on average add to zero as shown on the right.
The horizontal components are blocked.

## Slide 19: Setup 2 : C (Unfavorable) & S (Favorable)
Open symbols = muon
Filled symbols = pion
--------- = 1/cos(q)
C/S

## Slide 20: Polarization Profile in EM Showers

## Slide 21: Unfavorable Polarizer Orientation
C/S

## Slide 22: Favorable Polarizer Orientation
C/S

## Slide 23: Longitudinal Cherenkov Polarization Profile
Polarization of Cherenkov light in the earlier stages of the em shower development (<7 Xo) is preserved and the effect is relatively large
After the shower maximum, as expected Cherenkov polarization has no unique orientation
This aspect of Cherenkov radiation maybe useful in different applications in calorimetry if polarization can be measured per event, etc.
 | a | b
Favorable (Sci) | 5.11 ± 0.28 | 0.568 ± 0.029
Favorable (Che) | 4.08 ± 0.25 | 0.465 ± 0.028
Unfavorable (Sci) | 5.18 ± 0.28 | 0.579 ± 0.030
Unfavorable (Che) | 4.94 ± 0.27 | 0.549 ± 0.029

## Slide 24: A Possible Application – Air Calorimeter Example ?
It may be possible to perform this measurement in fully sampling large media (e.g. air, ice, big crystals). The polarization component of Cherenkov light adds another (independent) feature that is worth exploring. This approach will enable us to measure the early part of the shower and effectively longitudinally segment the early part of the shower (by polarization).

## Slide 26: Flipped Cherenkov Radiation - I
“Normal” Cherenkov
“Flipped” Cherenkov
In normal Cherenkov radiation, the real part of the refractive index is positive (n=2 above, q~60o, e.g. BSO) and the group and phase velocities of the wave coincide
If the refractive index is negative (LHM), the Cherenkov angle (q~115o above) is large and the photons and charged particles go in opposite directions. In such dispersive media, the phase and group velocities are different (n=c/(w/k)= -sqrt(mrer) ~ -2.38) and ng=c/(dw/dk)~6.57 and the energy flows with the group velocity
j satisfies the condition tan(180-j)=[(n/ng)sinq cosq]/[1-(n/ng)cos2q]

## Slide 27: Flipped Cherenkov Radiation - II
The effect is demonstrated in microwaves (~8-12 GHz) with metamaterials where the feature size is measured in mm (much smaller than the wavelength). In the optical region where Cherenkov photons are more abundant and potentially useful in HEP, the feature size needs to be in nm
If such metamaterials are realized, flipped Cherenkov effect might prove useful for calorimetry (readout upstream)
S. Xi et al PRL 103 194801 (2009)
H. Chen et al Materials Today 14 1-2 (2011)

## Slide 28: Cherenkov Light in Gas
Index of refraction for gasses is in general small n=1+d (d~10-3). Example: dC4H8=0.00258. This has the following consequences:
  Cherenkov angle is small: sin qc ~ sqrt(2d) ~ 0.05 which means particles and light come out of the detector at the ~same time and time spread is small
  The Cherenkov threshold is high: Eth ~ me/sqrt{2d} ~ 11.2 MeV which means decay products from radioactivation do not generate signal/noise
If high quality (>95%?) reflective surfaces can be made (a few meters long) for UV+VIS, a calorimeter based on gas Cherenkov would be very radiation hard (indestructible?)
O. Atramentov et al ALCW (2003)

## Slide 29: Longitudinal Segmentation with Timing
Fibers generate and efficiently transport fast Cherenkov radiation. With appropriate timing (sampling), it may be possible to effectively segment the calorimeter in depth
Signal time = L1/c + L2/(c/n),
(c/n) = velocity of light in fiber (n~1.45)
~20 cm/ns or ~1 cm/50 ps
L1
L2
Fibers
There is significant savings in channel count (and calibration) as one fiber represents many channels along the depth of calorimeter.

## Slide 30: Simulations/Estimates with Cherenkov Photons
Average Space Profile
Average Time Profile
50 GeV p+ in 1.2 cm x 1.2 cm tower
1 ns
(20 cm)
0.2 ns
(4 cm)
0.05 ns
(1 cm)

## Slide 31: Deconvolution of Cherenkov Pulse Train with CNN
It seems possible to deconvolve overlapping SiPM (Cherenkov) pulses to reveal the true distribution of shower components using CNN:
  Green: Convoluted SiPM pulse train
  Blue: Deconvoluted SiPM pulse train
  Orange: True pulse train
Single Cherenkov photon SiPM pulse obtained in 2023 beam test
Readout Box
Amplifiers
7 SiPMs
Fibers
Fast Output
Standard Output

## Slide 32: Conclusions
Cherenkov radiation is rich in interesting features, and many can be exploited for calorimetry
  Polarization adds another interesting one but need to figure out how to take advantage of it for HEP calorimetry
  Fast signals lend themselves for effective longitudinal segmentation, and better energy and timing resolution
  Metamaterials might open new possibilities in calorimetry