## Slide 1: Some bulk Cu and aC coating preliminary results obtained with the Vacuum Pilot Sector during 2023 run
Quentin DUONG
TE – VSC – VSM
quentin.duong@cern.ch
20/02/2024
Dr. Vincent BAGLIN (CERN) CERN supervisor
Dr. Gaël SATTONNAY (IJCLab-Paris Saclay University) Doctoral supervisor

## Slide 2: Outline
Description & Physics principles
LHC physics fill’s lifetime
72b and hybrid fills at 450 GeV
Hybrid physics fill at 6.8 TeV
Electron energy distribution for bulk Copper
TE – VSC – VSM

## Slide 3: Disclaimer
I present the observations performed on some of the 2023 fills
Results are therefore preliminary
TE – VSC – VSM

## Slide 4: Description & Physics principles
TE – VSC – VSM

## Slide 5: Layout
TE – VSC – VSM
  Vacuum Pilot Sector (VPS)
  Location: close to LHCb
  2 beamlines
  Installed in 2015:
    1.4m-long thick a-C coating ~500nm
    1.4m-long bulk Cu
  a-C
  Cu
  CMS
  ATLAS
  ALICE
  LHCb
  B1
  B2
  VPS
  LHC

## Slide 6: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by bunch ionising the residual gas
  Secondary electrons: induced by primary electrons, accelerated by successive bunches, hitting the surface
TE – VSC – VSM
Electron
cloud
Image current
Beam pipe
p+
p+
primary e-
photoelectron
e-
secondary e-
ionised gas i+
accelerated e-
free electron e-
PEY
SEY
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)
  Secondary Electron Yield (SEY)

## Slide 7: Electron current and energy detection
TE – VSC – VSM
A
A
p+
p+
Electron
cloud
Image current
Beam pipe
[0 ; 350] V
[-1.5 ; 1.5] kV
+9V
  Electron pickups
  Energy Analyser
  Electron pickups
    Electromagnetic shield: 7%-transparency
    Geometrical surface:
    Bulk copper collector
    Positively biased:
    Measurement: « electron cloud current »
  Energy Analyser (only copper station)
    « Retarding Field Analyser (RFA) »
    Electron pickup: with bias
    Biased filtering grid:
    Biased filtering grid:
    Measurement:
    « electron cloud current below »
Cu
Cu
Cu
Cu
Cu

## Slide 8: Total pressure detection
TE – VSC – VSM
p+
p+
Image current
Beam pipe
  Total pressure gauges
    Bayard-Alpert gauges « VGI »
    Measurement: « desorbed gas pressure »
  Total pressure gauges
  Two main material properties for gas increase:
  Photodesorption
  Electrodesorption
ionised gas i+
free electron e-
Electron
cloud
electrodesorbed gas
photodesorbed gas
PSD
ESD
  Pressure elevation during LHC functionning
  Photodesorbed gas: induced by photons hitting the surface
  Electrodesorbed gas: induced by electrons hitting the surface

## Slide 9: LHC physics fill’s lifetime
TE – VSC – VSM

## Slide 10: Hybrid scheme injection
TE – VSC – VSM
  Time
  Injection phase
1 turn of the LHC: ~89µs
ppb
« hybrid »
7*(8b4e) + 3*(36b)
Beam energy
450
6800
B1 intensity
B2 intensity
Beam energy

## Slide 11: Fill lifetime overview
TE – VSC – VSM
  Time
  A
  B
  C
  D
Beam energy
450
6800
B1 intensity
B2 intensity
Beam energy
2000 | 1.5 | 3 | 0.5
2000 | 1.5 | 3 | 0.5
Orders of magnitude of typical beam parameters
  Phases
  Injection (A): batch injections at 450GeV
  Energy ramp-up (B): beam accelerated until 6800GeV
  Stable beam (C): bunch collisions for the experiments
  Ramp-down (D): beam dumped and RF ramp-down
ppb: proton per bunch

## Slide 12: 72b and hybrid fills at 450 GeV
TE – VSC – VSM
72b: fills 8673
Hybrid (7*8b4e+3*36b): fill 8736

## Slide 13: Electron cloud comparisons for 72b and hybrid fills
TE – VSC – VSM
  72b
  Hybrid
a-C B1
Cu B1
Cu B1
  Detection limit:
  (Corresponds to the mean baseline plus of its gaussian distribution.)
Electron flux [A.cm-2]
  Copper is 4 orders of magnitude above carbon.
  Carbon below detection limit for 8b4e.
  For copper:
B1 intensity
B1 intensity
Total beam intensity [p+]
a-C B1

## Slide 14: Pressure comparisons for 72b and hybrid fills
  Hybrid
TE – VSC – VSM
  72b
a-C B1
Cu B1
a-C B1
Cu B1
  At equal beam intensity for copper:
  Pressure in carbon station possibly induced by RF bridge.
  Thus, pressure rise cannot always be considered as equivalent to electron presence.
B1 intensity
B1 intensity
Pressure [mbar]
Total beam intensity [p+]

## Slide 15: Electron cloud response of copper during injection
TE – VSC – VSM
Electron flux 72b
[A.cm-2]
Hybrid
72b
  More bunches needed for hybrid fill to reach linear behaviour
  For high number of bunches:
Electron flux hybrid
[A.cm-2]
:72b trains
  Hybrid train:
Hybrid trains:
4
6
8
10
12
14
28
21
15
13
10
8
5
0
400
800
1200
1600
2000
Number of bunches

## Slide 16: Hybrid physics fill at 6.8 TeV
TE – VSC – VSM
Hybrid (7*8b4e+5*36b): 8741

## Slide 17: Photoelectrons during energy ramp-up
TE – VSC – VSM
a-C B1
Cu B1
Electron flux [A.cm-2]
a-C Cu
  Photoelectrons detected by electron pickup at which corresponds to a synchrotron radiation critical energy of 2 eV, matching the work function of copper or carbon (~ 4-5 eV)
Energy
B1 intensity
Total beam intensity [p+]
Beam energy [GeV]

## Slide 18: Electron cloud current evolution during a fill
  Provided the knowledge of the number of photons absorbed in the stations, one can compute their Photo Electron Yield
TE – VSC – VSM
a-C B1
Cu B1
Electron flux [A.cm-2]
B1 intensity
Energy
  Multipacting occuring only for copper
  Bumbed curve for copper
  Flat curve for carbon
  Only photoelectrons at the end of the fill
  Both signals scale with beam intensity

## Slide 19: Electron energy distribution for bulk Copper
TE – VSC – VSM
Hybrid (7*8b4e+5*36b): 9072

## Slide 20: During energy ramp-up
TE – VSC – VSM
  No significant impact of the beam energy ramp-up on the electron energy distribution.
 |  |  |  | *
620 | 1.60 | 6.0 | 203 | 269
2674 | 1.60 | 5.8 | 202 | 266
6799 | 1.59 | 5.9 | 203 | 263
620 | 1.60 | 6.0 | 203 | 269
2674 | 1.60 | 5.8 | 202 | 266
6799 | 1.59 | 5.9 | 203 | 263
  Double lognormal fit
  Assess the energy peaks of secondary and accelerated electrons
    Measurement step around : 3-5 eV
    Measurement step around : 30 eV
  Cannot describe measurements in-between peaks and above accelerated one
*J. Scott Berg. CERN LHC Project Note 97, July 1997.
Electron energy spectrum: Fill 9072
Normalised signal
Secondary
electrons
Beam kicked
electrons

## Slide 21: At Stable Beam: t = 0h
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Bunch intensity:
  Fit results
  Low energy:
  High energy:

## Slide 22: At Stable Beam: t = 6h
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Bunch intensity:
  Fit results
  Low energy:
  High energy:

## Slide 23: At Stable Beam: t = 11h
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Bunch intensity:
  Fit results
  Low energy:
  High energy:

## Slide 24: Impact of the beam intensity at 6800GeV
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Stable Beam |  |  |  | *
0H | 1.59 | 6 | 203 | 263
6H | 1.23 | 6 | 120 | 166
11H | 0.99 | 6 | 89 | 114
0H | 1.59 | 6 | 203 | 263
6H | 1.23 | 6 | 120 | 166
11H | 0.99 | 6 | 89 | 114
  No impact of the bunch intensity on the energy of the secondary electrons.
  Decrease of the energy gained by accelerated electrons with bunch intensity.
  Kick energy formulae gives a reasonable energy assessment at 30%
*J. Scott Berg. CERN LHC Project Note 97, July 1997.

## Slide 25: Summary
TE – VSC – VSM
  At 450GeV:
  Electron cloud responses for copper are orders of magnitude above carbon ones
  For copper,
  At a certain number of bunches,
  Pressure rise is not equivalent to local electron cloud presence
  During a hybrid physics fill lifetime:
  Photoelectrons detected for
  Multipacting only in copper
  Electron energy distribution:
  No significant impact of the energy ramp-up on the electron energy distribution
  Decrease of the accelerated energy peak with ppb
  Kick energy formula is a reasonable first approximation

## Slide 26: Perspectives for run 2024
TE – VSC – VSM
  Electrostimulated and Photostimulated Desorption (ESD, PSD) computations with Residual Gas Analyser
  Photoelectron Yield (PY) estimations
  Secondary Electrons Yield (SEY) evaluation with RFA by refining measurements around electron peaks
  Measurements of the electron cloud bunch by bunch with a scope
  Heat load evaluation with calorimeters
  Confrontation of measurements and parameter evaluations against simulations (PyEcloud, Vasco, Molflow, Synrad…)

## Slide 27: Backups
TE – VSC – VSM

## Slide 28: Station 2 – Amorphous carbon
TE – VSC – VSM
St 1
St 3
z
Ext
Int
7%
7%
7%
7%
K4
K5
Canon 1-12
K6
Sc3a
K16
K18
K17
Canon 1-12
Sc3b
Liner B23
Liner R25
129
110
124
122
121
120
119
118
116
Dash line : Downer side
Red line : Scope
NU : Unused
cal : calorimeter
xx % : pickup with a xx%-transparent grid
Trig : trigger
ph : photodetector
Blue line : Keithley with variable bias
Position :
X
X
X
X
VGI : Bayard-Alpert Gauge (BAG)
VGRB : Pirani gauge​
VQM : Vacuum Quality Monitor
RGA : Residual Gas Analyser
VGPB : Penning Gauge
N : NEG cartridge
X
VPIA : Vacuum Pump
Unused
VF : Vacuum Flange
.5L8.
B
R
RFA : Retarding Field Analyser
kick : kicker (Electron Kicker Detector)

## Slide 29: Station 3 – New unbaked copper
TE – VSC – VSM
St 2
St 4
z
Ext
Int
7%
7%
7%
50%
15%
50%
7%
15%
Sc1a
K7
Canon 1-12
K8
Sc2a
K26
K9
K27
Canon 1-12
Sc2b
K21
Sc1b
Liner B26
Liner R27
92
73
87
85
84
83
82
81
79
Dash line : Downer side
Red line : Scope
Int
NU : Unused
cal : calorimeter
xx % : pickup with a xx%-transparent grid
Trig : trigger
ph : photodetector
Blue line : Keithley with variable bias
Position :
X
X
X
X
VGI : Bayard-Alpert Gauge (BAG)
VGRB : Pirani gauge​
VQM : Vacuum Quality Monitor
RGA : Residual Gas Analyser
VGPB : Penning Gauge
N : NEG cartridge
X
VPIA : Vacuum Pump
Unused
VF : Vacuum Flange
.5L8.
B
R
RFA : Retarding Field Analyser
kick : kicker (Electron Kicker Detector)

## Slide 30: Station 4 – Old unbaked copper
TE – VSC – VSM
St 3
LHCb
z
Ext
Int
Liner 7
Liner 8
55
36
50
48
46
44
42
7%
0,2%
K23
K24
Canon 1-12
Canon 1-12
SHV3
SHV1
K12 + SHV2
K22 + SHV4
K11
HV BIAS 28
0,2%
7%
Dash line : Downer side
Red line : Scope
Blue line : Keithley with variable bias
NU : Unused
cal : calorimeter
xx % : pickup with a xx%-transparent grid
Trig : trigger
ph : photodetector
4
Position :
X
X
X
X
VGI : Bayard-Alpert Gauge (BAG)
VGRB : Pirani gauge​
VQM : Vacuum Quality Monitor
RGA : Residual Gas Analyser
VGPB : Penning Gauge
N : NEG cartridge
X
VPIA : Vacuum Pump
Unused
VF : Vacuum Flange
.5L8.
B
R
RFA : Retarding Field Analyser
kick : kicker (Electron Kicker Detector)
Pt100 air B
Pt100 air R

## Slide 31: Electron cloud for hybrid fills
TE – VSC – VSM
a-C B1
Cu B1
  Detection limit:
  (Corresponds to the mean baseline plus of its gaussian distribution.)
Electron flux [A.cm-2]
  Copper is 4 orders of magnitude above carbon.
  Carbon below detection limit for 8b4e.
  For copper:
B1 intensity
Total beam intensity [p+]
Notes: As a first result, you’ve here plots of the electron flux in ampere per cm² versus time for both filling schemes and for copper in orange and carbon in grey. Plotted in purple you have the detection limit of my measurements, which is about 10pA and corresponds to the mean baseline of the station plus 1 sigma of its gaussian distribution. Finally you’ll find the beam intensity in blue, withh it scale on the right side.
Two points can be noticed:
One is that copper gives responses orders of magnitude above carbon, which is even under the detection limit for the hybrid fill.
The other is that for copper signals are 20 times higher for 72b than hybrid scheme at same beam intensity.

## Slide 32: Ecloud as a function of beam mean ppb
TE – VSC – VSM
  Multipacting presence
  Barely present for carbon: ecloud mainly dominated by photoelectrons
  Huge contribution for copper
  Assymptotic root method
  Root of linear asymptotic behaviour for high ppb
  Method to assess the variations of multipacting with time
linear
multipacting
regime
primary electrons
regime
a-C B1
new-Cu B1
Electron flux [A.cm-2]
Mean ppb
Mean ppb
  Assymptotic root method is NOT aimed at giving a multipacting threshold as ecloud effect has been identified for lower ppb.
Electron flux vs Mean ppb: Fill 9072

## Slide 33: Electron flux scaling with beam intensity at end of fill
TE – VSC – VSM
Electron flux normalised by beam intensity vs Time: Fill 8741
Normalised electron flux [A.cm-2]
a-C B1
Cu B1

## Slide 34: Cu ESD for 72b and hybrid fills
TE – VSC – VSM
  Pressure rise assumed to be induced only by
  Electrostimulated desorption computation for copper station
  Measured ESD correspond to a copper surface at a dose of a few
M. Haubner et al. Vacuum 207 (2023) 111656
Filling scheme |  | 
72b | 8 | 
Hybrid |  | 
Filling scheme |  | 
72b |  | 
Hybrid |  | 
Notes: To end this section on fills at 450GeV, here are given the ESD for both schemes and considering only dihydrogen.
They’re are very similar results and are consistent very the measurement made in the lab and published by Michal Haubner that you can see on the right.
This plot giving the ESD as a function the electron dose indicates that for an ESD of 10^-3 molecule per electrons is reached for an electron dose of a few 10^18 e/cm²

## Slide 35: RFA raw data
TE – VSC – VSM
  RFA scan
  Scanning time:
  Filtering voltage:
  Current at a set voltage :
    current of electrons with an energy under
RFA scan: Fill 9072
Electron current vs Filtering voltage: Fill 9072
Electron current
  The energy spectrum of the electrons can be obtained by derivating this curve.

## Slide 36: During energy ramp-up
TE – VSC – VSM
  No significant impact of the beam energy ramp-up on the electron energy distribution.
 |  |  |  | *
620 | 1.60 | 6.0 | 203 | 269
2674 | 1.60 | 5.8 | 202 | 266
6799 | 1.59 | 5.9 | 203 | 263
620 | 1.60 | 6.0 | 203 | 269
2674 | 1.60 | 5.8 | 202 | 266
6799 | 1.59 | 5.9 | 203 | 263
  Double lognormal fit
  Assess the energy peaks of secondary and accelerated electrons
    Measurement step around : 3-5 eV
    Measurement step around : 30 eV
  Cannot describe measurements in-between peaks and above accelerated one
*J. Scott Berg. CERN LHC Project Note 97, July 1997.
Electron energy spectrum: Fill 9072
Normalised signal
Secondary
electrons
Beam kicked
electrons
Notes: The plot you see on the right gives the energy distribution of the electrons, in blue, and presents two peaks, one around 200eV related to the electons kicked by the beam, and one around 6eV related to secondary electrons.
In order to find the energies related to each peak a double lognormal fit as been used locally around those. However, this fit cannot explains the measurements in-between the peaks and above the second one.
These electron peak energies have been identified at different beam energies and gave similar results, just as for Delta Etot, which is the approximation of the energy gained by electrons in presence of beam established by Scott Berg in its paper. Thus, one can observe no significant impact of the beam energy ramp-up on the electron energy distribution.

## Slide 37: Energy spectrum double lognormal fit
TE – VSC – VSM
Electron energy spectrum: Fill 9072
Normalised signal
  Spectrum properties
  Peak at:
  Low peak: Energy of secondary electrons
  High peak: Energy of accelerated electrons
  Limit of the fit: within [20eV ; 100eV] and above 600eV

## Slide 38: Kick approximation principle
TE – VSC – VSM
  Two different types of motions during the passage of a bunch:
  Autonomous approximation: The electrons are strongly pulled by the bunch and begin to oscillate around it.
  Kick approximation: The electrons haven’t started to move very much before.
  Deciding which approximation to use:
    consists of comparing the oscillation period with respect to the time for the bunch to pass
    is equivalent to introducing a transition radius to delimit the domains of validity of both approximations
  Introduction of the critical radius above which the kick approximation is used, and below which the autonomous approximation is used.
  Mean energy kick within these regions:
  Energy kick for an electron on the wall:
  Total mean energy gain:
Ref: “ Energy Gain in an Electron Cloud During the Passage of a Bunch ” – J. Scott Berg

## Slide 39: Kick approximation formulae
TE – VSC – VSM
  Transverse and longitudinal bunch distributions assumed Gaussian
Beam parameters
  Relativistic beta:
  RMS bunch length:
  RMS beam radius:
  Electron properties
  Radius:
  Rest mass:
Ref: “ Energy Gain in an Electron Cloud During the Passage of a Bunch ” – J. Scott Berg

## Slide 40: Energy ramp-up at 620GeV
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Intensity:
  Fit results
  Low energy:
  High energy:

## Slide 41: Energy ramp-up at 2074GeV
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Intensity:
  Fit results
  Low energy:
  High energy:

## Slide 42: Energy ramp-up at 6799GeV
TE – VSC – VSM
TE – VSC – VSM
19/02/2024
Electron energy spectrum: Fill 9072
Normalised signal
  Beam parameters
  Energy:
  Intensity:
  Fit results
  Low energy:
  High energy: